	Table 1. Composition of water solution (ad 50g) for spray-drying

	Sample name
	PHCl [mg]
	Mannitol [mg]
	Na-HA [mg]
	PEG [mg]

	PHCl-spd
	2000
	-
	-
	-

	PHCl+M-spd
	2000
	2000
	-
	-

	PHCl-mcomp
	500
	500
	300
	500


	Table 2. The particle size distribution of the dried samples

	Samples
	D 0.1 (µm)
	D 0.5 (µm)
	D 0.9 (µm)

	PHCl
	8.5
	38.4
	137.9

	PHCl-spd
	4.1
	18.9
	145.4

	PHCl+M-spd
	10.0
	67.3
	275.2

	PHCl-mcomp
	3.1
	5.7
	10.0


	Table 3. Thermoanalytical values of the samples

	Samples
	Integral (mJ)
	Normalized (Jg-1)
	Peak (oC)

	PHCl
	-542.28
	-123.24
	163.58

	PHCl-spd
	-479.92
	-113.72
	162.72

	PHCl+M-spd
	-264.34
	-55.77
	159.77

	PHCl-mcomp
	-64.76
	-14.76
	153.47


