Melamine polyphosphate –

the reactive and additive flame retardant for polyurethane foams

Jacek Lubczak, Renata Lubczak

Faculty of Chemistry, University of Technology, Al. Powstańców Warszawy 6, 35-959 Rzeszów, Poland

Corresponding author: e-mail: jml@prz.edu.pl

Supplementary section

Table S1. TG analysis of foams

| # Foams obtained from oligoetherols | # No Comp # as Table 3 | T5% | T10% | T25% | T50% |
| --- | --- | --- | --- | --- | --- |
| mMPP:EC = 1:22 | 14 | 197 | 250 | 305 | 373 |
| mMPP:EC:PC = 1:10:6 | 19 | 225 | 251 | 305 | 370 |