Supplementary Data
Synthesis, characterization and biological studies of new linear thermally stable Schiff base polymers with flexible spacers

Farah Qureshi*, M.Y. Khuhawar, T.M. Jahangir, A.H. Channar

Institute of Advanced Research Studies in Chemical Sciences, University of Sindh, Jamshoro, Sindh, Pakistan.

*Corresponding author, Tel: +92-229213213, +92-3313534844

E-mail: farahqureshi94@yahoo.com

Table of Contents
	S. No.
	Description


	Page

	1.
	E.I Mass Spectrum of monomer (HOB)

	2

	2.
	FT-IR spectrum of (a) HOB (monomer) and 
(b) PHOBen (Polymer)
	2


	3.
3.1
3.2
	1HNMR spectrum of monomer and polymer
1HNMR spectrum of HOB (monomer)

1HNMR spectrum of PHOBTSc (Polymer)
	3
3
3

	4.
	  Combined UV/Vis spectra of monomer HOB and polymers
	4

	5.
5.1
5.2
	TG/ DTA Spectrum of monomer and polymer

TG/DTA spectrum of HOB (monomer)
      TG/DTA spectrum of PHOBTSc (polymer)
	4
4

5

	6.

6.1

6.2
	Spectrofluorometric of monomer and polymer
 Spectrofluorometric spectrum of HOB (momomer)
 Spectrofluorometric spectrum of PHOBPh (polymer)
	5
5
6

	


1. E.I mass spectrum of monomer (HOB)
[image: image1.jpg]Fiotane Smamcnoris
|G | TS
Lo

81

m





2. FT-IR spectrum of (a) HOB (monomer) and (b) PHOBen (Polymer)

[image: image2.emf]700.38


730.47


831.06


922.19


1005.16


1067.23


1110.73


1151.88


1215.82


1250.29


1307.94


1396.83


1474.70


1507.11


1593.19


1682.29


2013.10


2851.64


2942.83


M1 15-7-14


 20


 40


 60


 80


 100


%T


681.12


733.87


834.15


1021.61


1109.47


1166.55


1239.51


1306.72


1392.40


1423.55


1466.01


1510.88


1574.90


1602.91


1640.13


1687.12


2863.02


2940.59


F-P1


 10


 20


 30


 40


 50


 60


 70


 80


 90


 100


%T


 500   


 1000  


 1500  


 2000  


 2500  


 3000  


 3500  


 4000  


Wavenumbers (cm-1)




700.38

730.47

831.06

922.19

1005.16

1067.23

1110.73

1151.88

1215.82

1250.29

1307.94

1396.83

1474.70

1507.11

1593.19

1682.29

2013.10 2851.64

2942.83

M1 15-7-14

 20

 40

 60

 80

 100

%T

681.12

733.87

834.15

1021.61

1109.47

1166.55

1239.51

1306.72

1392.40

1423.55

1466.01

1510.88

1574.90

1602.91 1640.13

1687.12

2863.02

2940.59

F-P1

 10

 20

 30

 40

 50

 60

 70

 80

 90

 100

%T

 500     1000    1500    2000    2500    3000    3500    4000  

Wavenumbers (cm-1)


3. 1HNMR spectrum of monomer and polymer

3.1. 1HNMR spectrum of HOB (monomer)
[image: image3.png]VoW

R

H

H





3.2. 1HNMR spectrum of PHOBTSc (Polymer)
[image: image4.png]



4. Combined UV/Vis spectra of monomer HOB and polymers

[image: image5.png]SEREREREREREISERERE

N

N

§58





5. TG/ DTA Spectrum of monomer and polymer

5.1 TG/DTA spectrum of HOB (monomer)
[image: image6.png]



5.2. TG/DTA spectrum of PHOBTSc (polymer)
[image: image7.png]



6. Spectrofluorometric of monomer and polymer
6.1. Spectroflourometric spectrum of HOB λex 313nm, λem 362nm
[image: image8.png]



6.2. Spectroflourometric spectrum of PHOBPh λex 280nm, λem 388nm.
[image: image9.png]



6

