Space Charge Layer Effect in Solid State Ion Conductors and Lithium Batteries: Principle and Perspective
Xiangxin Guo
  State Key Laboratory of High Performance Ceramics and Superfine Microstructure, Shanghai Institute of Ceramics, Chinese Academy of Sciences, 1295 Ding Xi Road, Shanghai 200050, China
This paper is dedicated to Prof. Janko Jamnik, who was my enthusiastic and helpful MPI colleague as well as with high academic level and reputation in science community.
Abstract

The space charge layer (SCL) effects were initially developed to explain the anomalous conductivity enhancement in composite ionic conductors. They were further extended to qualitatively as well as quantitatively understand the interfacial phenomena in many other solid state conductors. Especially in nanometre-scale systems, the SCL effects could be used to manipulate the conductivity and construct artificial conductors. Recently, existence of such effect either at the electrolyte/cathode interface or at the interfaces inside the composite electrode in all solid state lithium batteries (ASSLB) has attracted attention. Therefore, in this article, the principle of SCL on basis of defect chemistry is first presented. The SCL effects on the carrier transport and storage in typical conducting systems are reviewed. For ASSLB, the relevant effects reported so far are also reviewed. Finally, the perspective of interface engineer related to SCL in ASSLB is addressed.
Keywords: Space charge layer, Defect chemistry, Interfacial resistance, All solid state lithium battery, 

1. Introduction

Space charge layer (SCL) effects correspond to carrier redistribution at space charge regions near a two-phase contact. This concept was first used by Carl Wagner to explain conductivity effects at the interface of two semiconductors.1 It was tentatively developed to explain the interfacial phenomena in ionic conductor systems by T. Jow and J.B. Wagner.2 Later on, J. Maier made fruitful achievement on understanding of SCL effects at various boundary problems, based on quantitatively derived profiles of defect concentrations through consideration of local thermodynamic and electrostatic relationships.3 From then on, SCL effects proved to be of great importance for ion conduction in solids, especially if the interfacial spacing is on the nanometre scale. In the last decades, a large number of instances for space charge effects on the ionic transport in solids has been provided. Variation of not only the magnitude but also the type of conductivity were verified in composites, grain boundaries in polycrystalline materials and epitaxial heterostructures.4-20 Conductivities of various functional materials might be manipulated for fundamental research as well as application. Introduction of interfaces not only led to strong variations in conductivity, but also induced qualitatively change of the type of conductivity. 
In recent years, all solid state lithium batteries (ASSLB) have attracted a great deal of attention, since they may provide solution to the safety issue as well as enhancement of energy density compared to the currently commercial rechargeable lithium batteries. The key materials for ASSLB are the solid-state electrolytes and the critical problems are the relevant solid-solid interfaces between the electrolyte and the cathode or inside the composited electrolytes. Though there have already been some discussions on SCL at the sulphide-electrolyte-based batteries,21 understanding of such effect is still in its infancy. In particular for oxide-electrolyte-based batteries, clarification as well as manipulation of SCL at the interfaces of composited electrolytes or electrolyte/cathode is highly demanded. 
Therefore, in Section 2, we will address basic knowledge of the SCL effect according to defect redistribution near a two-phase contact. In Section 3, we will present typical examples of SCL effects occurred at various boundaries of functional materials. In Section 4, we will focus on the SCL effects in solid state batteries. The conclusion and outlook will be given finally. 
2. Defect chemistry at space charge layers near the two-phase boundary
At the boundary between the two materials, carrier redistribution in the space charge region is required from the thermodynamical point of view (uniformity of electrochemical potential).22 The following discussion seems more closely related to a lateral two-phase contact, the basic knowledge is also applied to the interface in the systems including polycrystalline or composited materials. 

In the core-space charge model,23, 24 it is generally assumed that the dilute defects on a continuum level, no structural changes up to the interface (
[image: image62.png]Oxide Sulphide Oxide  Sulphide

Oxide IL Sulphide Oxide IL Sulphide



), and the same mobility of defects in SCL as in the bulk (
[image: image2.wmf]¥

=

x

). In the case of mobile carrier 
[image: image3.wmf]j

, its concentration enrichment 
[image: image4.wmf]z

 in equilibrium is


[image: image5.wmf](

)

(

)

(

)

[

]

T

k

x

e

c

x

c

x

B

z

j

j

z

j

j

j

¥

¥

-

-

=

ú

ú

û

ù

ê

ê

ë

é

=

f

f

z

exp

1

,

1

                                                                          (1),
where 
[image: image6.wmf]c

 is the carrier concentration of the defect, and 
[image: image7.wmf]f

 the electrical potential which is determined by the Poisson equation


[image: image8.wmf]0

2

e

e

r

f

-

=

Ñ

                                                                                                                   (2).

[image: image9.wmf]r

represents the charge density equal to 
[image: image10.wmf]å

k

k

k

ec

z

. In the above expressions, 
[image: image11.wmf]e

 and 
[image: image12.wmf]0

e

 are the relative permittivity and the dielectric constant of free space, 
[image: image13.wmf]B

k

 and 
[image: image14.wmf]T

 are the Boltzmann’s constant and the temperature, 
[image: image15.wmf]e

 is the absolute value of the electronic charge, 
[image: image16.wmf]k

z

is the charge number of the defect 
[image: image17.wmf]k

. 

If all the carriers are mobile in equilibrium, their electrochemical potentials are constant. Then combination of Eq. (1) and (2) leads to the Poisson-Bolzmann relationship in the direction perpendicular to the interface

 
[image: image18.wmf][

]

(

)

ú

û

ù

ê

ë

é

-

-

-

=

-

¶

¶

¥

¥

¥

å

T

k

x

e

z

z

c

e

x

x

B

k

k

k

k

f

f

ee

f

f

exp

)

(

,

0

2

2

                                                     (3).
Note that in this case the excess charge is directly given by the species that determine the conductivity. The solution of Eq. (3) for semi-infinite boundary conditions comes to the Gouy-Chapman profile,23, 25, 26 which can be written as  


[image: image19.wmf](

)

(

)

(

)

(

)

2

exp

1

exp

1

÷

÷

ø

ö

ç

ç

è

æ

-

-

-

+

=

=

±

±

¥

±

±

±

l

J

l

J

z

x

x

c

x

c

x

                                                                                 (4),
where 
[image: image20.wmf]¥

¥

-

¥

+

º

=

c

c

c

 because of the electroneutrality in bulk and 
[image: image21.wmf]x

 being the distance from the interface. As a result, 
[image: image22.wmf]0

=

x

 and 
[image: image23.wmf]¥

=

x

 refer to the interface and the bulk, respectively. 
[image: image24.wmf]l

 is the Debye length,


[image: image25.wmf]2

1

2

2

0

2

÷

÷

ø

ö

ç

ç

è

æ

=

¥

c

e

z

T

k

B

ee

l

               
[image: image26.wmf]                                                                                              (5).
The parameter 
[image: image27.wmf]J

 (dependent on 
[image: image28.wmf]0

z

 and hence on 
[image: image29.wmf]0

c

) is defined as follows 


[image: image30.wmf]m

J

z

z

J

-

=

+

-

=

±

±

±

1

1

2

1

0

2

1

0

                                                                                                             (6)

and represents the degree of influence. For 
[image: image31.wmf]0

=

±

J

, i.e. 
[image: image32.wmf]1

0

=

±

z

, the defect chemistry in the space charge region is the same as in the bulk. It approaches +1 for maximum enrichment (
[image: image33.wmf]1

0

>>

±

z

) and –1 for maximum depletion (
[image: image34.wmf]1

0

<<

±

z

). Such profiles are shown in Fig. 1(a).  

[image: image35.png]bulk)

In(c/c

(a) Gouy-Chapman profiles

bulk)

6

In(c/c

A

[ (b) Mott-Schottky profiles

Immobile impurities

v

5
x/A




Fig.1 Typical defect profiles in the case of (a) Gouy-Chapman and (b) Mott-Schottky.
While Gouy-Chapman profiles serve as a natural picture for accumulation layers, enrichment effects can also be found in Mott-Schottky situations. Then the conductivity determining carrier has to be a minority carrier with a high mobility in order to surpass the bulk value of the majority carrier significantly. Now, we refer to an extrinsic situation in which the mobile majority species are impurity compensated in the bulk but depleted close to the interfaces. Ideally the impurity profile is assumed to be flat everywhere as shown in Fig. 2(b). The impurity then is considered to be incorporated during preparation but frozen under operation. In such cases, Eq. (1) is only valid for the mobile carriers. As to Eq. (2), the invariant quantity 
[image: image36.wmf]¥

,

imp

c

 dominates the space charge density and hence Poisson’s equation reads approximately
[image: image1.wmf]0

=

x

[image: image60.wmf]*

³

l

x

      
[image: image37.wmf]ï

î

ï

í

ì

=

-

=

¶

¶

¥

0

)

(

0

,

2

2

const

ec

z

x

x

imp

imp

ee

f

                                                                                       (7).
Eq. (7) can be easily integrated with the boundary conditions: 
[image: image38.wmf]0

=

¶

¶

*

=

l

f

x

x

 and 
[image: image39.wmf]0

)

0

(

f

f

=

=

x

 denoting the define value from the potential in the electroneutral bulk by 
[image: image40.wmf]¥

f

, resulting in a quadratic potential profile,27, 28
       
[image: image41.wmf](

)

¥

*

¥

+

-

-

=

f

l

ee

f

2

0

,

2

)

(

x

ec

z

x

imp

imp

                                                                             (8),
where
[image: image42.wmf]*

l

is the effective space charge thickness:


[image: image43.wmf](

)

0

,

0

2

f

f

ee

l

-

=

¥

¥

*

imp

imp

ec

z

                                                                                                  (9)

that exceeds 
[image: image44.wmf]l

 by the factor 
[image: image45.wmf](

)

0

4

f

f

-

¥

T

k

e

z

B

imp

. 

Since the typical potential difference is on the order of several 100 mV, this equation indicates that the space charge region in the Mott-Schottky case can be significantly more extended than in the Gouy-Chapman case. 

At the point 
[image: image46.wmf]*

=

l

x

, 
[image: image47.wmf]j

z

 becomes unity, i.e. the concentration of the mobile carrier reaches the bulk value. When 
[image: image48.wmf]*

£

l

x

, according to Eq. (1), the defect concentration can be expressed as

 
[image: image49.wmf](

)

(

)

2

1

,

1

2

exp

÷

÷

ø

ö

ç

ç

è

æ

-

=

ú

ú

û

ù

ê

ê

ë

é

=

*

¥

l

l

z

x

c

x

c

x

j

j

z

j

j

z

j

                                                                             (10).
In the overlap situation (i.e. 
[image: image50.wmf]*

<

l

2

l

),  the electro-neutral bulk does not exist and thus 
[image: image51.wmf]¥

¹

f

f

)

2

(

l

. Rather in this case, the preferred boundary conditions are 
[image: image52.wmf]0

2

=

¶

¶

=

l

x

x

f

 and 
[image: image53.wmf]0

)

0

(

f

f

=

. Hence, the integration of Eq. (7) yields a potential profile


[image: image54.wmf]0

2

2

0

,

2

2

2

)

(

f

ee

f

+

ú

ú

û

ù

ê

ê

ë

é

÷

ø

ö

ç

è

æ

-

÷

ø

ö

ç

è

æ

-

-

=

¥

l

l

x

ec

z

x

imp

imp

                                                                      (11)

and the defect concentration profile becomes

  
[image: image55.wmf](

)

(

)

(

)

ï

þ

ï

ý

ü

ï

î

ï

í

ì

-

-

ú

ú

û

ù

ê

ê

ë

é

÷

ø

ö

ç

è

æ

-

÷

ø

ö

ç

è

æ

-

=

ú

ú

û

ù

ê

ê

ë

é

=

¥

¥

f

f

l

z

0

2

2

2

1

,

1

2

2

4

exp

T

k

e

x

z

c

x

c

x

B

imp

z

j

j

z

j

j

j

l

l

                           (12).
As the mobile majority carrier is depleted, Mott-Schottky analysis mainly applies to resistive boundaries. If however a minority carriers of the same sign as the impurity has a very high mobility, it can well be conceived that its accumulation leads to a conductance increase even though the impurity level is not exceeded. As already pointed out, this demands a high ratio of 
[image: image56.wmf]majority

ority

u

u

min

(
[image: image57.wmf]u

, carrier mobility).

3. Space charge layer effects on conductivities at various boundaries
Based on the above discussed carrier redistribution at SCL, conductivity anomaly at various boundaries has been quantitatively studies. Briefly speaking, the SCL concept has quantitatively accounted for the composites (Figure 2a), polycrystallines (Figure 2b) and heterostructural multilayers (Figure 2c), the typical examples of which are respectively addressed in the following. 
[image: image58.png]Composites Polycrystallines Heterostructural Multilayers




Fig.2 Typical space charge layer situations of (a) composites; (b) polycrystallines; (c) heterostructural multilayers.
The earliest attractive composite known as “composite electrolytes” or “heterogeneous electrolytes” was the two-phase system LiI-Al2O3, reported by Liang et al. with the ionic conductivity 50 times greater than that of the pure LiI.29 Concerning that the Al2O3 particles are insulating, the conductivity enhancement is attributed to the boundary layer phenomena, which can be perfectly explained by the SCL effects. Besides Al2O3 similar oxides including SiO2, CeO2, ZrO2 and BaTiO3 were found to be also effective. Since there were a lot of papers on this respect, readers can refer to the literature in Ref. [3]. Further with mesoporous Al2O3 as the insulating phase, the enhancement of conductivity can be more effective, which is satisfactorily explained in the framework of the ideal space-charge model.30 Here, it is worthwhile mentioning “Soggy Sand Electrolytes”.31 The total conductivities are highly increased by virtue of the very high conductivities at the edge of the space charge profiles. This work is of significance owing to evidence of heterogeneous doping mechanism as well as improvement of mechanical behaviour for the polymer electrolytes in the field of solid-state lithium batteries. 
Besides composite electrolytes, composite electrodes are also worth noting. A novel interfacial storage mechanism for lithium in the nanocrystalline boundaries was elucidated by J. Jamnik and J. Maier.32 Later on, many works both in experiment and theory demonstrated valid of the interfacial storage. Li et al. found the Li storage in TiF3 fand VF3, which was attributed to the interfacial effect since neither LiF nor Ti and V could store the Li.11 Yu et al. prepared LiF, Ti and LiF/Ti composite thin films in the same thickness using pulsed laser deposition. Discharge and charge tests revealed that the LiF and Ti films had negligible capacities, while the LiF/Ti composite film showed significant Li storage capacity, which increased with increasing thickness. These results clearly indicate existence of interfacial storage.33 In theory, the first principle calculation proved the reasonability of interface storage from the view point of thermodynamics.5 Such mechanism is beneficial not only to increase the storage capacity at low potential but also to improve the rate performance.
For polycrystalline systems, there have been many good examples demonstrating the SCL effects at grain boundaries in micrometer scale. The details will not be presented here. Readers can refer to previous reports on ZrO2, CeO2 and SrTiO3.9, 10 With respect to the mesoscopic scale, the nanocrystalline SrTiO3 gives direct and unambiguous evidence of space charge overlap as characteristic size effect. Owing to the significant extension of depletion zones for the holes, the bulk impedance signal disappears at about 100 nm grain boundary spacing.8
Heterojunctions in two-phase systems are particularly advantageous on study of the SCL effects at crystalline interfaces owing to the controllable spacing between the two boundaries. CaF2/BaF2 heterolayers prepared by molecular beam epitaxy serve as a nice demonstration of the potential of nanoionics. They show that ion conductivities both parallel and perpendicular to the interfaces increase with decrease in interfacial spacing. This size effect is attributed to the thermodynamically necessary redistribution of the mobile ﬂuoride ions.14,34 On this basis, the striking phenomenon of an upward bending in the effective parallel conductivity as a function of inverse interfacial spacing for low temperatures has been satisfactorily explained by application of a modiﬁed Mott–Schottky model for BaF2.35 This model was further conﬁrmed by measurements perpendicular to the interfaces that offer complementary information on the more resistive parts. This successful comprehensive modeling of parallel and perpendicular conductivities for the whole parameter range gives a nice picture of ion redistribution at the interfaces and the boundary zones overlap as well as the predicted mesoscopic size effect. This mechanism allows achievement of artificial ionically conducting material with anomalous transport properties.34-37
4. Space charge layer effects in all solid state lithium batteries
The SCL effects in ASSLB have been intensively studied by Takada et al. in the all solid state lithium batteries (ASSLB) with Li4GeS4–Li3PS4 (thio-LISICON) as electrolytes and LiCoO2 as cathodes.38-45 Concerning the difference in chemical potential between the sulphide and the oxide, the SCL may forms at the two-phase boundary according to requirement of thermodynamic equilibrium. Further concerning that the oxide is more absorptive with Li than the sulphide, the Li ion may transfer from the sulphide to the oxide, as schematically shown in Figure 3a. Electrons of the mix-conducting oxide will eliminate the concentration of Li interstitials near the boundary, extending thickness of SCL at the oxide side. The defect chemistry situation is depicted in Figure 3b. Since the transport property of the interface is determined by the Li interstitial movement, such carrier redistribution may enlarge the interfacial resistance, increasing the polarization and worsening the rate capability. This phenomenon was indeed proved in experiment as well as in theory.21

[image: image59]
Fig.3 (a) The two-phase boundary of oxide and sulphide; (b) The defect chemistry situation after the formation of SCL; (c) Introduction of ionic-conducting intermediate layer (IL) between the two phases; (d) The defect chemistry situation after the introduction of the IL.
To overcome the shortcomings brought by the SCL as mentioned above, an intermediate layer (IL) with sole ionic-conducting property was supposed to be effective. As shown in Figure 3c, with introduction of such a layer between the two phases, the potential difference between the oxide and the sulphide can be greatly eliminated, leading to reduced Li transfer from the oxide side. With negligible electron concentration in the intermediate layer, the depletion region of Li is also reduced, as shown in Figure 3d. Consequently, the interfacial resistance decreases and the rate capability is enhanced. In experiment, Li4Ti5O12, LiNdO3, LiTaO3, Li2SiO3 thin layers have been used as the intermediate layer between the sulphide and the oxide, and shown effects to reduce the interfacial resistance and increase the power density of the ASSLB.44-47 Interestingly, the Al-enriched domains formed at the LiAlyCo1-yO2 surfaces perform the same functionality as the aforementioned intermediate oxide layers, while with more effective influence on reduction of the interfacial resistance and improvement of rate capability.48 These results are in agreement with the relevant theoretical calculation.21
Although not many, discussions on the SCL effect at interfaces between oxides were also reported. Yamada et al. demonstrated that the nonsintered grain boundary resistance of a highly conducting solid electrolyte (Li1.3Al0.3Ti1.7(PO4)3) could be suppressed by being coated with poorly conducting solid electrolyte (Li2SiO3).49 In addition, Yamada et al. found that at interfaces of solid oxide electrolytes and active materials, lithium-ion transfer across the interfaces occurred, dependent on the potential of the active materials. The Li+ transfer caused change in the ionic conductivity at the interface and, in some cases, changed in the crystal structure. The Li+ transfer would be more critical for batteries with high Li+ conducting solid electrolytes, because the main charge carriers of them are not lithium vacancies but lithium interstitials. The Li+ transfer from such solid oxide electrolytes to cathodes with high electrode potential leads depletion of the charge carriers in the solid electrolytes at the interface and thus increase in the interfacial resistance.50,51 With reduction of SCL effect at the grain boundaries, the total conductivity could be increased. Hitosugi et al. reported the surprisingly low electrolyte/electrode interface resistance in thin-ﬁlm batteries, which is an order of magnitude smaller than that presented in previous reports on all-solid-state lithium batteries as well as smaller than that found in a liquid electrolyte-based batteries. Such low interface resistance was attributed to the fact that the negative SCL eﬀects at the Li3PO4−xNx/LiCoO2 interface were negligible.52
Conclusion and perspective on all solid state lithium batteries
The SCL effects at the interfaces relate to the carrier redistribution near the two-phase boundary, which is led by the SCL potential derived from the requirement of thermodynamic equilibrium at the contact between the two phases. From early experimental phenomena, to qualitative and quantitative understanding, and to interfacial design for manipulation of conductivity by nano technique, many systems including composites, polycrystallines, heterolayer structures have proven important role of the SCL effects in the carrier transport and storage. Especially in research of ASSLIB that has attracted much attention recently, the SCL shows the key influence on the interfacial resistance and thus on the rate capability. Though the SCL at the interface between the sulphide electrolyte and the oxide electrode has been deeply discussed, more relevant effects at the interfaces between the oxide electrolyte and the oxide electrode, between the polymer electrolyte and the oxide electrolyte, and between the polymer electrolyte and the oxide electrode are still in infancy. Existence of such effect either at the electrolyte/cathode interface or at the interfaces inside the composites is one of the key issues for ASSLB, which are currently deemed to be a solution to safety as well as enhancement of energy density in the field of rechargeable lithium battery. Therefore, it is clear that study of SCL related to the ASSLB is significant. More researches in this direction can be expected. 
References

1. C. Wagner, J. Phys. Chem. Solids, 1972, 33, 1051-1059.

2. T. Jow, J.B. Wagner, J. Electrochem. Soc., 1979, 126, 1963-1979.

3. J. Maier, Prog. Solid St. Chem., 1995, 23, 171-263.

4. J. Maier, Nature Mater., 2005, 4, 805-815. 

5. Y. F. Zhukovskii, P. Balaya, E. A. Kotomin, J. Maier, Phys. Rev. Lett., 2006, 96, 058302.

6. H. L. Tuller, Solid State Ionics, 2000, 131, 143-157.

7. J. Schoonman, Solid State Ionics, 2000, 135, 5-19.

8. P. Balaya, J. Jamnik, J. Fleig, J. Maier, Appl. Phys. Lett., 2006, 88, 062109.

9. S. Kim and J. Maier, J. Electrochem. Soc., 2002, 149, J73-J83.

10. X. Guo, J. Maier, J. Electrochem. Soc., 2001, 148, E121-E126.

11. H. Li, G. Richter, J. Maier, Adv. Mater., 2003, 15, 736-739.

12. Y.-G. Guo, J.-S. Lee, J. Maier, Adv. Mater., 2005, 17, 2815-2819.
13. J. Maier, Physical Chemistry of Ionic Materials Ions and Electrons in Solids. Wiley, Chichester 2004. 

14. N. Sata, K. Eberl, K. Eberman, J. Maier, Nature, 2000, 408, 946-949.

15. X.X. Guo, N. Sata, J. Maier, Electrochim. Acta, 2004, 49, 1091-1096.

16. X.X. Guo, J. Maier, Surf. Sci., 2004, 549, 211-216.

17. J. Jamnik, Solid State Ionics, 2006, 177, 2543-2547.

18. A. Tschöpe, E. Sommer, R. Birringer, Solid State Ionics, 2001, 139, 255-265.

19. Y. Gil, O. M. Umurhan, I. Riess, Solid State Ionics, 2007, 178, 1-12.

20. X. Guo, R. Waser, Prog. Mater Sci., 2006, 51, 151-210.

21. J. Haruyama, K. Sodeyama, L. Han, K. Takada, Y. Tateyama, Chem. Mater., 2014, 26, 4248-4255.

22. J. Maier, Ber. Bunsenges. Phys. Chem., 1985, 89, 355-362.

23. J. Maier, J. Electrochem. Soc., 1987, 134, 1524-1535.

24. J. Jamnik, J. Maier, S. Pejovnik, Solid State Ionics, 1995, 75, 51-58.

25. G. Gouy, J. Physique, 1910, 9, 457-468.
26. D.L. Chapman, Phil. Mag., 1913, 25, 475-481.
27. S. M. Sze, Semiconductor Devices. John Wiley & Sons, Ltd., New York 1985.

28. W. Schottky, Halbleiterprobleme. Viewweg, Braunschweig 1954. 

29. C.C. Liang, J. Electrochem. Soc., 1973, 120, 1298-1292.

30. H. Yamada, A.J. Bhattacharyya, J. Maier, Adv. Funct. Mater., 2006, 16, 525-530.

31. A.J. Bhattacharya, J. Maier, Adv. Mater., 2004, 16, 811-814.
32. J. Jamnik, J. Maier, Phys. Chem. Chem. Phys., 2003, 5, 5215-5220.

33. X. Q. Yu, J. P. Sun, K Tang, H. Li, X. J. Huang, L. Dupont, J. Maier, Phys. Chem. Chem. Phys., 2009, 11, 9497-9503.

34. X. X. Guo, I. Matei, J.-S. Lee, J. Maier, Appl. Phys. Lett., 2007, 91, 103102.

35. X. X. Guo, I. Matei, J. Jamnik, J.-S. Lee, J. Maier, Phys. Rev. B, 2007, 76, 125429.
36. X. X. Guo, J. Maier, Adv. Funct. Mater., 2009, 19, 96-101.

37. X. X. Guo, J. Maier, Adv. Mater., 2009, 21, 1-13.
38. Y. Seino, K. Takada, B. C. Kim, L. Zhang, N. Ohta, H. Wada, M. Osada, T. Sasaki, Solid State Ionics, 2005, 176, 2389-2393.

39. B. C. Kim, K. Takada, N. Ohta, Y. Seino, L. Zhang, H. Wada, T. Sasaki, Solid State Ionics, 2005, 176, 2383-2387.

40. T. Matsumura, K. Nakano, R. Kanno, A. Hirano, N. Imanishi, Y. Takeda, J. Power Sources, 2007, 174, 632-636.

41. K. Takada, N. Aotani, K. Iwamoto, S. Kondo, Solid State Ionics, 1995, 79, 284-287.

42. K. Takada, Acta Mater., 2013, 61,759-770.

43. Y. Seino, T. Ota, K. Takada, J. Power Sources, 2011, 196, 6488-6492. 
44. N. Ohta, K. Takada, L. Zhang, R. Ma, M. Osada, T. Sasaki, Adv. Mater., 2006, 18, 2226-2229.

45. N. Ohta, K. Takada, I Sakaguchi, L. Zhang, R. Ma, K. Fukuda, M. Osada, T. Sasaki,  Electrochem. Commun., 2007, 9, 1486-1490.

46. K. Takada, N. Ohta, L. Zhang, K. Fukuda, I. Sakaguchi, R. Ma, M. Osada, T. Sasaki, Solid State Ionics, 2008, 179, 1333-1337.

47. A. Sakuda, H. Kitaura, A. Hayashi, K. Tadanaga, M. Tatsumisago, J. Electrochem. Soc., 2009, 156, A27-A32.
48. X. X. Xu, K. Takada, K. Watanabe, I. Sakaguchi, K. Akatsuka, B. T. Hang, T. Ohnishi, T. Sasaki, Chem. Mater., 2011, 23 , 3798-3804.

49. H. Yamada, D. Tsunoe, S. Shiraishi, G. Isomichi, J. Phys. Chem. C, 2015, 119, 5412-5419.

50. H. Yamada, Y. Oga, I. Saruwatari, I. Moriguchia, J. Electrochem. Soc., 2012, 159, A380-A385.

51. M. Agostini, Y. Aihara, T. Yamada, B. Scrosati, J. Hassoun, Solid State Ionics, 2013, 244, 48-51.

52. M. Haruta, S. Shiraki, T Suzuki, A. Kumatani, T. Ohsawa, Y. Takagi, R. Shimizu, T. Hitosugi, Nano Lett., 2015, 15, 1498-1502.
for   � EMBED Equation.3  ���





for � EMBED Equation.3  ���








1

[image: image61.wmf]*

£

<

l

x

0

_1234263754.unknown

_1234263762.unknown

_1234263766.unknown

_1235548154.unknown

_1239370716.unknown

_1239371017.unknown

_1239371256.unknown

_1508043719.unknown

_1239371085.unknown

_1239370963.unknown

_1235548549.unknown

_1239370270.unknown

_1235548521.unknown

_1234263768.unknown

_1234264104.unknown

_1234265186.unknown

_1234263767.unknown

_1234263764.unknown

_1234263765.unknown

_1234263763.unknown

_1234263758.unknown

_1234263760.unknown

_1234263761.unknown

_1234263759.unknown

_1234263756.unknown

_1234263757.unknown

_1234263755.unknown

_1234263745.unknown

_1234263749.unknown

_1234263751.unknown

_1234263753.unknown

_1234263750.unknown

_1234263747.unknown

_1234263748.unknown

_1234263746.unknown

_1234263737.unknown

_1234263741.unknown

_1234263743.unknown

_1234263744.unknown

_1234263742.unknown

_1234263739.unknown

_1234263740.unknown

_1234263738.unknown

_1234263726.unknown

_1234263734.unknown

_1234263736.unknown

_1234263731.unknown

_1234263722.unknown

_1234263724.unknown

_1234263725.unknown

_1234263723.unknown

_1234263720.unknown

_1234263721.unknown

_1234263716.unknown

_1234263719.unknown

_1234263714.unknown

_1234263715.unknown

_1234263711.unknown

