Figure 1. Skeleton structures of imidazole (ImiH), 1-methyl-imidazole (ImiMe), 2-mercapto-1-methyl-imidazole (SH-ImiMe), benzimidazole (BimH), and 2-mercaptobenzimidazole (SH-BimH). Pyridine- and pyrrole-type N atoms and the numbering of atoms are also indicated.

Figure 2. Structure of Fe(110) surface. Notice two different spacings between adjacent surface Fe atoms, termed short- and long-bridge. The short-bridge distance is a0√3/2, whereas long-bridge distance is a0, where a0 is the equilibrium bcc lattice parameter of Fe bulk. The angles between two short-bridges and between short-bridge and long-bridge are also indicated.

Figure 3. Skeleton structures of thiol and thione tautomers of 2-mercapto-1-methyl-imidazole (top) and 2-mercaptobenzimidazole (bottom). The thiol to thione transformation involves the shifting of blue colored hydrogen atom from the S to the N3 atom. Thiones are more stable than thiols and the corresponding energy differences, calculated at the PBE/plane-wave level of theory, are stated.2

Figure 4. Inhibition efficiency against corrosion of iron in 3 wt.% NaCl solution of imidazole (ImiH) compared to that of (a) 1-methyl-imidazole (ImiMe) and1-methyl-2-mercapto-imidazole (SH-ImiMe), and (b) benzimidazole (BimH) and 2-mercaptobenzimidazole (SH-BimH) as a function of inhibitor concentrations (0.1, 1, and 10 mM). Lines are drawn to guide the eye. ImiH and ImiMe do not inhibit corrosion at 0.1 mM inhibitor concentration, whereas the solubility of SH-BimH is below 10 mM.

Figure 5. Potentiodynamic curves recorded for iron in 3 wt.% NaCl solution, without and with addition of (a) 0.1 mM, (b) 1 mM, and (c) 10 mM of either imidazole (ImiH), 1-methyl-imidazole (ImiMe), 1-methyl-2-mercapto-imidazole (SH-ImiMe), benzimidazole (BimH), or 2-mercaptobenzimidazole (SH-BimH) inhibitor. Curves for imidazole-based inhibitors (ImiH, ImiMe, SH-ImiMe) are shown in upper panels and those of benzimidazole-based inhibitors (BimH, SH-BimH) in bottom panels. dE/dt = 1 mV/s.

Figure 6. Macroscopic images and optical microscopy images of iron sample (a) before immersion and after 30 days immersion in 3 wt.% NaCl solution (b) without and (c) with the addition of 1 mM of either imidazole (ImiH), 1-methyl-imidazole (ImiMe), benzimidazole (BimH), 1-methyl-2-mercapto-imidazole (SH-ImiMe), or 2-mercaptobenzimidazole (SH-BimH). After immersion the specimens were rinsed with deionized water and dried with stream of nitrogen. The values of mean roughness Sa, as obtained by profilometer, are also stated.

Figure 7: Normalized high resolution (a) Fe 2p and (b) O 1s spectra for layers formed during 30 days of immersion of iron in 3 wt.% NaCl solution with and without the addition of 1 mM imidazole (ImiH), 1-methyl-imidazole (ImiMe), 1-methyl-2-mercapto-imidazole (SH-ImiMe), benzimidazole (BimH) and 2-mercaptobenzimidazole (SH-BimH). The take-off angle is 45. Vertical dotted lines denote the position of peaks of reference compounds: (a) dashed: Fe(0), dotted: Fe(II) oxide, dash-dotted: Fe(III) oxide, (b) 1: O2, 2: OH, 3: H2O.

Figure 8: Normalized high resolution (a) C 1s, (b) N 1s and (c) S 2p XPS spectra for layers formed during 30 days of immersion of iron in 3 wt.% NaCl solution with and without the addition of 1 mM imidazole (ImiH), 1-methyl-imidazole (ImiMe), 1-methyl-2-mercapto-imidazole (SH-ImiMe), benzimidazole (BimH) and 2-mercaptobenzimidazole (SH-BimH). The take-off angle is 45. Vertical dotted lines denote the position of peaks of reference compounds: (a) 1: CC, CH, 2: CN (CS), 3: CO, 4: C=N, 5: COO, (b) 1: C=NC, 2: CNHC, and (c) S 2p3/2 / S 2p1/2.

Figure 9. Top and perspective views of optimized standing molecular adsorption modes on Fe(110). From left to right: imidazole (ImiH), 1-methyl-imidazole (ImiMe), benzimidazole (BimH), and thione forms of 1-methyl-2-mercapto-imidazole (S-ImiMeH) and 2-mercaptoimidazole (S-BimH2). Adsorption energies and molecule–surface bond lengths (N–Fe and S–Fe), calculated at 1/20 ML coverage, are also stated. Color coding of atoms is the following: H is white, C is gray, N is sky-blue, S is yellow, and Fe is reddish with color becoming darker as going from surface toward the bulk.

Figure 10. As in Figure 8, but for lying adsorption modes.

Figure 11. “Dehydrogenated” standing adsorption modes on Fe(110); non-mercapto molecules lack the H at C2 atom, whereas mercapto molecules are in thiolate form (which can be seen as thione lacking the H at N1 or as thiol lacking the H at S). Dissociative adsorption energies (Eadsdiss), corresponding to the MolH(g) → Mol(ads) + H(ads) process, and the Mol–Fe(110) binding energies (Eb) are also stated.

Figure 12. “Dehydrogenated” lying adsorption modes on Fe(110); non-mercapto molecules lack the H at N1 atom, whereas mercapto molecules are in thiolate form.