Synthesis, Crystal Structure and Catalytic Property of a Cobalt(II) Complex Derived From 2-Bromo-N’-(2-Hydroxy-5-Methylbenzylidene)Benzohydrazide

Fu-Ming Wang

Key Laboratory of Coordination Chemistry and Functional Materials in Universities of Shandong, Department of Chemistry, Dezhou University, Dezhou Shandong 253023, P. R. China

Email address: wfm99999@126.com

Abstract

With a tridentate Schiff base ligand 2-bromo-N’-(2-hydroxy-5-methylbenzylidene)benzohydrazide (HL) and cobalt nitrate, a cobalt(II) complex was prepared and characterized by elemental analysis, IR spectroscopy and X-ray structure determination. The complex crystallizes in the monoclinic space group P21/c with unit cell dimensions a = 13.406(1) Å, b = 27.443(2) Å, c = 18.142(2) Å, β = 101.147(8)°, V = 6548.5(10) Å3, Z = 4, R1 = 0.0770, and wR2 = 0.1591. Single crystal X-ray diffraction analysis reveals that the Co atom is coordinated by the NOO donor atoms of the Schiff base ligands, in an octahedral coordination. Catalytic oxidation of the complex on some olefins was performed.

Keywords: Schiff base; Cobalt complex; Crystal structure; Catalytic property.

1. Introduction

In recent years, the catalytic oxidation of olefins has aroused much attention in the production of chemicals and fine chemicals since epoxides are key starting materials for a wide variety of oily products.1 Because of the environment friendly nature, H2O2 has been regarded as the first selected oxidant in the oxidation of olefins. Transition metal complexes with various ligands have presented interesting catalytic properties.2 Among the complexes, cobalt species show efficient catalytic oxidation properties.3 In this paper, a new cobalt(II) complex derived from the Schiff base ligand 2-bromo-N’-(2-hydroxy-5-methylbenzylidene)benzohydrazide (HL) was prepared and its catalytic oxidation property was performed.

HL

2. Experimental

2.1. Materials and Methods

5-Methylsalicylaldehyde and 2-bromobenzohydrazide were purchased from Alfa Aesar. Cobalt nitrate and solvents are commercially available and were used without further purification. Elemental analyses for carbon, hydrogen, and nitrogen were carried out with an Elementar Vario EL. Infrared spectra were measured on KBr disks with a Hitachi I-5040 FT-IR spectrophotometer.

2.2. Synthesis of the Complex

5-Methylsalicylaldehyde (0.136 g, 1.0 mmol) and 2-bromobenzohydrazide (0.215 g, 1.0 mmol) were mixed and stirred in methanol (20 mL) for 30 min. Then, cobalt nitrate hexahydrate (0.291 g, 1.0 mmol) dissolved in methanol (20 mL) was added, and stirred for another 30 min. The solution was kept still in air for a few days to slow evaporate, to give brown block-shaped single crystals of the complex. Yield: 32%. Analysis: Found: C 45.27, H 3.13, N 8.97%. Calculated for C60H50Br4Co2N10O15: C 45.36, H 3.17, N 8.82%. IR (KBr, cm-1): ν(O-H), 3451; ν(N-H), 3217; ν(C=N), 1605; ν(NO3), 1377 and 835.

2.3. Catalytic Oxidation Experiment

Catalytic experiment was carried out in a 50 mL glass round-bottom flask fitted with a reflux condenser and placed in an oil bath at prearranged temperature under continuous stirring. The oxidation was carried out as follows: the complex (0.032 mmol) was dissolved in 10 mL 1,2-dichloroethane. Then 10 mmol alkene was added to the reaction mixture and 30 mmol TBHP was added. The reaction mixture was refluxed for 1 h. The reaction products were monitored at periodic time intervals using gas chromatography. The oxidation products were identified by comparison with authentic samples (retention times in GC).

2.4. X-Ray Structure Determination

Data collection for the complex was performed with a Bruker Apex II CCD diffractometer at 298 K. The structure was solved by direct methods with SHELXS-97 and refined by full-matrix least squares (SHELXL-97) on F2.4 All non-hydrogens were refined anisotropically. Hydrogens were placed geometrically and refined with a riding model, with isotropic displacement coefficients U(H) = 1.2 U(C) or 1.5 U(Cmethyl). Br1 atom is disordered over two sites, with occupancies of 0.727 and 0.273. Br2 atom is disordered over two sites, with occupancies of 0.534 and 0.466. Crystallographic data for the complex are summarized in Table 1. Selected bond lengths and angles are listed in Table 2.

CCDC – 1448088 contain the supplementary crystallographic data for this paper. These data can be obtained free of charge from The Cambridge Crystallographic Data Center via www.ccdc.cam.ac.uk/data_request/cif.

Table 1. Crystal data, data collection and structure refinement for the complex

| Molecular Formula | C60H50Br4Co2N10O15 |
| --- | --- |
| Formula weight | 1588.6 |
| Crystal system | Monoclinic |
| Space group | P21/c |
| a (Å) | 13.406(1) |
| b (Å) | 27.443(2) |
| c (Å) | 18.142(2) |
| β (deg) | 101.147(8) |
| V (Å3) | 6548.5(10) |
| Z | 4 |
| Dc (g cm-3) | 1.611 |
| F(000) | 3176 |
| μ (mm-1) | 3.019 |
| θ range (deg) | 2.91-25.50 |
| hkl range | -16 ≤ h ≤ 15 |
|  | -25 ≤ k ≤ 33 |
|  | -19 ≤ l ≤ 21 |
| Measured reflections | 40016 |
| Unique reflection | 11962 |
| Observed reflections [I > 2σ(I)] | 4969 |
| Rint | 0.1238 |
| Parameters | 831 |
| Rastraints | 35 |
| Final R index [I > 2σ(I)] | 0.0770, 0.1591 |
| R index (all data) | 0.2063, 0.2206 |
| Goodness-of-fit on F2 | 0.973 |

Table 2. Selected bond lengths (Å) and bond angles (deg) for the complex

| Co(1)-N(3) | 1.995(6) | Co(1)-N(1) | 2.003(7) |
| --- | --- | --- | --- |
| Co(1)-O(3) | 2.034(6) | Co(1)-O(1) | 2.037(5) |
| Co(1)-O(4) | 2.044(6) | Co(1)-O(2) | 2.083(6) |
| Co(2)-N(7) | 1.985(6) | Co(2)-N(5) | 2.013(7) |
| Co(2)-O(5) | 2.033(5) | Co(2)-O(7) | 2.049(5) |
| Co(2)-O(6) | 2.069(6) | Co(2)-O(8) | 2.119(5) |
| N(3)-Co(1)-N(1) | 166.0(3) | N(3)-Co(1)-O(3) | 88.0(2) |
| N(1)-Co(1)-O(3) | 102.0(3) | N(3)-Co(1)-O(1) | 102.9(2) |
| N(1)-Co(1)-O(1) | 87.2(3) | O(3)-Co(1)-O(1) | 89.1(2) |
| N(3)-Co(1)-O(4) | 80.1(3) | N(1)-Co(1)-O(4) | 90.2(3) |
| O(3)-Co(1)-O(4) | 167.9(2) | O(1)-Co(1)-O(4) | 91.0(2) |
| N(3)-Co(1)-O(2) | 90.8(2) | N(1)-Co(1)-O(2) | 79.4(3) |
| O(3)-Co(1)-O(2) | 91.4(2) | O(1)-Co(1)-O(2) | 166.3(2) |
| O(4)-Co(1)-O(2) | 91.3(2) | N(7)-Co(2)-N(5) | 166.8(3) |
| N(7)-Co(2)-O(5) | 98.4(2) | N(5)-Co(2)-O(5) | 88.6(3) |
| N(7)-Co(2)-O(7) | 87.1(2) | N(5)-Co(2)-O(7) | 104.3(2) |
| O(5)-Co(2)-O(7) | 89.1(2) | N(7)-Co(2)-O(6) | 94.8(2) |
| N(5)-Co(2)-O(6) | 78.7(3) | O(5)-Co(2)-O(6) | 166.7(2) |
| O(7)-Co(2)-O(6) | 90.1(2) | N(7)-Co(2)-O(8) | 78.8(2) |
| N(5)-Co(2)-O(8) | 89.8(2) | O(5)-Co(2)-O(8) | 92.0(2) |
| O(7)-Co(2)-O(8) | 165.9(2) | O(6)-Co(2)-O(8) | 91.9(2) |

3. Results and Discussion

3.1. Chemistry

The complex was prepared by reaction of equimolar quantities of the Schiff base ligand with cobalt nitrate in methanol. Crystals of the complex are stable in air, and soluble in methanol, ethanol, DMF and DMSO, insoluble in water. The molar conductance of the complex is 115 Ω-1 cm2 mol-1, indicating that the complex is a 1:1 electrolyte.

3.2. Infrared Spectra

The complex has been characterized by infrared spectroscopy. The broad band centered at 3451 cm–1 is assigned to the O–H vibrations. The sharp band at 3217 cm–1 is assigned to the N–H vibration of the amino groups. The strong band indicative of the C=N group is observed at 1605 cm–1.5 The bands indicative of the nitrate anions are located at 1377 and 835 cm-1.

3.3. Crystal Structure Description of the Complex

The Co(1) and Co(2) molecular structures of the complex are shown in Figures 1 and 2, respectively. The asymmetric unit of the compound contains two mononuclear cobalt(II) complex molecules, two nitrate anions and one water molecule of crystallization. The Co atoms are coordinated by two phenolate O, two imine N and two carbonyl O atoms from two Schiff base ligands, forming octahedral coordination. The distortion of the octahedral coordination can be observed from the cis and trans coordinate bond angles, viz. 79.4(3)-102.9(2)° and 166.0(3)-167.9(2)° for Co(1), 78.8(2)-104.3(2)° and 165.9(2)-166.8(3)° for Co(2). The bond lengths related to the Co atoms are similar to each other, and also comparable to those observed in cobalt complexes with Schiff base ligands.6 The dihedral angles between the two benzene rings C(1)-C(6) and C(10)-C(15), C(16)-C(21) and C(25)-C(30), C(31)-C(36) and C(40)-C(45), C(46)-C(51) and C(55)-C(60),of the Schiff base ligands are 105.4(5), 74.8(5), 35.9(5), and 62.4(5)°, respectively.

In the crystal structure of the complex, molecules are linked through intermolecular hydrogen bonds (Table 3), to form a network, as shown in Figure 3.

Table 3. Distances (Å) and angles (°) involving hydrogen bonding of the complex

| D–H∙∙∙A | d(D–H) | d(H∙∙A) | d(D∙∙∙A) | Angle(D–H∙∙∙A) |
| --- | --- | --- | --- | --- |
| N(4)–H(4A)∙∙∙N(10)i | 0.86 | 2.64 | 3.46(1) | 161 |
| N(4)–H(4A)∙∙∙O(14)i | 0.86 | 2.61 | 3.27(1) | 135 |
| N(4)–H(4A)∙∙∙O(13)i | 0.86 | 2.00 | 2.86(1) | 170 |
| O(15)–H(15B)∙∙∙O(9)ii | 0.85 | 2.36 | 3.18(2) | 163 |
| O(15)–H(15B)∙∙∙N(9)ii | 0.85 | 2.62 | 3.43(2) | 160 |
| O(15)–H(15B)∙∙∙O(11)ii | 0.85 | 2.23 | 2.90(1) | 135 |
| O(7)–H(7D)∙∙∙O(3) | 0.93 | 1.65 | 2.442(7) | 141 |
| O(1)–H(1A)∙∙∙O(5) | 0.93 | 1.63 | 2.458(7) | 147 |
| N(8)–H(8A)∙∙∙O(12)ii | 0.86 | 1.96 | 2.79(1) | 164 |
| N(6)–H(6A)∙∙∙O(15) | 0.86 | 1.98 | 2.80(1) | 159 |
| N(2)–H(2A)∙∙∙N(9) | 0.86 | 2.69 | 3.41(2) | 142 |
| N(2)–H(2A)∙∙∙O(10) | 0.86 | 1.94 | 2.79(1) | 166 |

Symmetry codes: i: 1 + x, 1/2 – y, –1/2 + z; ii: x, 1/2 – y, –1/2 + z.

Figure 1. The molecular structure of the Co1 complex molecule with 30% probability thermal ellipsoids.

Figure 2. The molecular structure of the Co2 complex molecule with 30% probability thermal ellipsoids.

Figure 3. Molecular packing structure of the complex, viewed along the a axis. Hydrogen bonds are shown as dashed lines.

3.4. Catalytic Property

The catalytic results are given in Table 3. As seen from the results, the products of the reactions are epoxides and the selectivities for these products are 100%. High TONs (turn over numbers = moles of substrate converted per mole of the complex) obtained for the substrates suggest a very high catalytic efficiency for the complex. In general, oxidation of the substrates gave the corresponding epoxides in over 80% yields for various styrene and 71% for cyclohexene.

Table 3. Catalytic oxidation resultsa

| Substrate | Product | Conversion (%)b | TONc |
| --- | --- | --- | --- |
|  |  | 71 | 287 |
|  |  | 83 | 315 |
|  |  | 88 | 353 |
|  |  | 81 | 327 |

a The molar ratio of catalyst:substrate:TBHP is 1:300:1000. The reactions were performed in mixture of CH3OH/CH2Cl2 (V:V = 6:4; 1.5 mL).

b The GC conversion (%) was measured relative to the starting substrate after 1 h.

c TON: turn over number = moles of substrate converted per mole of the complex.

4. Conclusions

A new mononuclear cobalt(II) complex with tridentate Schiff base ligands have been prepared and characterized. Single crystal structure of the complex was determined. The Co atom in the complex is in an octahedral coordination. The complex has effective catalytic oxidation property on some olefins.

5. Acknowledgments

The Department of Chemistry of Dezhou University is acknowledged for financial support.

6. References

- (a) S. Shit, D. Saha, D. Saha, T.N.G. Row, C. Rizzoli. Inorg. Chim. Acta 2014, 415, 103-110; (b) T.R. Amarante, P. Neves, A.C. Gomes, M.M. Nolasco, P. Ribeiro-Claro, A.C. Coelho, A.A. Valente, F.A.A. Paz, S. Smeets, L.B. McCusker, M. Pillinger, I.S. Goncalves. Inorg. Chem. 2014, 53, 2652-2665; (c) A.C. Gomes, S.M. Bruno, M. Abrantes, C.I.R. Magalhaes, I.S. Goncalves, A.A. Valente, M. Pillinger. J. Organomet. Chem. 2014, 760, 205-211; (d) B. Terfassa, J.A. Schachner, P. Traar, F. Belaj, N.C.M. Zanetti. Polyhedron 2014, 75, 141-145; (e) A.J. Musacchio, L.Q. Nguyen, G.H. Beard, R.R. Knowles. J. Am. Chem. Soc. 2014, 136, 12217-12220.

- (a) F. Wang, C.-H. Lu, I. Willner. Chem. Rev. 2014, 114, 2881-2941; (b) L.M.D.R.S. Martins, A.J.L. Pombeiro. Coord. Chem. Rev. 2014, 265, 74-88; (c) A. Quintard, J. Rodriguez. Angew. Chem. Int. Ed. 2014, 53, 4044-4055; (d) K. Riener, S. Haslinger, A. Raba, M.P. Hogerl, M. Cokoja, W.A. Herrmann, F.E. Kuhn. Chem. Rev. 2014, 114, 5215-5272; (e) M. Amini, M.M. Haghdoost, M. Bagherzadeh. Coord. Chem. Rev. 2014, 268, 83-100.

- (a) Y.K. Zhao, J.Q. Lin, Y.D. Liu, B.C. Ma, Y. Ding, M.D. Chen. Chem. Commun. 2015, 51, 17309-17312; (b) M. Khorshidifard, H.A. Rudbari, B. Askari, M. Sahihi, M.R. Farsani, F. Jalilian, G. Bruno. Polyhedron 2015, 95, 1-13; (c) K. Sarma, N. Devi, M. Kalita, B. Sarma, P. Barman. J. Coord. Chem. 2015, 68, 3685-3700; (d) T. Baskaran, R. Kumaravel, J. Christopher, S. Radhakrishnan, A. Sakthivel. Catal. Lett. 2015, 145, 851-859; (e) S.M. Islam, K. Ghosh, R.A. Molla, A.S. Roy, N. Salam, M.A. Iqubal. J. Organomet. Chem. 2014, 774, 61-69; (f) T. Kurahashi, H. Fujii. Inorg. Chem. 2013, 52, 3908-3919.

- G.M. Sheldrick. SHELXL-97, Program for the Refinement of Crystal Structures, Göttingen (Germany): University of Göttingen, 1997.

- R. Pagadala, P. Ali, J.S. Meshram. J. Coord. Chem. 2009, 62, 4009-4017.

- (a) C. Jing, C. Wang, K. Yan, K. Zhao, G. Sheng, D. Qu, F. Niu, H. Zhu, Z. You. Bioorg. Med. Chem. 2016, 24, 270-276; (b) H.A.R. Pramanik, P.C. Paul, P. Mondal, C.R. Bhattacharjee. J. Mol. Struct. 2015, 1100, 496-505; (c) S. Roy, A.K. Maji, D. Sutradhar, S. Choubey, R. Ghosh, B.K. Ghosh. J. Indian Chem. Soc. 2015, 92, 1387-1393; (d) X.-M. Hu, L.W. Xue, G.-Q. Zhao, W.C. Yang. Russ. J. Coord. Chem. 2015, 41, 197-201; (e) M. Ghosh, M. Layek, M. Fleck, R. Saha, D. Bandyopadhyay. Polyhedron 2015, 85, 312-319.