Synthesis, Crystal Structure, and Catalytic Property of Dioxomolybdenum(VI) Complex Derived from 4-Bromo-N’-(4-diethylamino-2-hydroxybenzylidene)benzohydrazide

Li Wang, Yong-Jun Han, Qing-Bin Li, Ling-Wei Xue*

College of Chemistry and Chemical Engineering, Pingdingshan University, Pingdingshan Henan 467000, P.R. China

* Corresponding author. E-mail: pdsuchemistry@163.com

Abstract

A newly synthesized dioxomolybdenum(VI) complex, [MoO2L(MeOH)], where L is the anion of 4-bromo-N’-(4-diethylamino-2-hydroxybenzylidene)benzohydrazide, has been synthesized and characterized. Structure of the complex was characterized by physico-chemical methods and single crystal X-ray determination. The Mo atom in the complex is in octahedral coordination, with three donor atoms of the hydrazone ligand, two oxo groups, and one methanol O atom. The complex has interesting catalytic property for the sulfoxidation reactions. In the presence of the complex, a conversion of 93% for the sulfide to the corresponding sulfoxide was observed within 60 min. After 2 h, the conversion of sulfide was 100%.

Keywords: Dioxomolybdenum; Hydrazone; Crystal structure; Catalytic property; Sulfoxidation

1. Introduction

Molybdenum complexes with multi-dentate ligands have received remarkable attention in recent years for their catalytic properties1 and molecular structures.2 Catalytic oxo transfer properties especially epoxidation and sulfoxidation of dioxomolybdenum complexes are important in industrial. Many types of ligands with various functional groups have been synthesized to prepare molybdenum complexes with the aim of explore new and efficient catalytic materials.3 Salicylaldehyde and its derivatives have been widely used as ligands for the preparation of metal complexes with various applications.4 A large number of molybdenum complexes with Schiff base ligands have been reported.5 Some of the dioxomolybdenum complexes have shown oxygen atom transfer properties as they were found to oxidize thiols, hydrazine, polyketones, and tertiary phosphines.6 Recently, we reported the catalytic property of a dioxomolybdenum(VI) complex.7 As a continuation of such work, we report in this paper the synthesis, structure, and catalytic property of a new dioxomolybdenum(VI) complex, [MoO2L(MeOH)], where L is the anion of 4-bromo-N’-(4-dimethylamino-2-hydroxybenzylidene)benzohydrazide (Scheme 1).

Scheme 1. The hydrazone H2L.

2. Experimental

2.1. Materials and methods

4-Diethylaminosalicylaldehyde, 4-bromobenzohydrazide and MoO2(acac)2 were purchased from Fluka. Other reagents and solvents were analytical grade and used without further purification. The hydrazone was prepared according to the literature method.8 Elemental (C, H, and N) analyses were made on a Perkin-Elmer Model 240B automatic analyzer. IR spectra were recorded on an IR-408 Shimadzu 568 spectrophotometer. 1H NMR data was recorded on a Bruker 300 MHz spectrometer.

2.2. Synthesis of [MoO2L(MeOH)]

MoO2(acac)2 (0.1 mmol, 33.5 mg) was dissolved with methanol (10 mL), to which was added with stirring a methaolic solution (10 mL) of H2L (0.1 mmol, 39.0 mg). The mixture was stirred at reflux for 30 min to give a yellow solution. The solution was slowly evaporated in air to give yellow block-shaped single crystals, which were collected by filtration and dried in vacuum containing anhydrous CaCl2. The yield is 41 mg (75%). Elemental analysis found: C, 41.8; H, 4.1; N, 7.5%, C19H22BrMoN3O5 calcd: C, 41.6; H, 4.0; N, 7.7%.

2.3. X-ray diffraction

Crystal data of the complex were collected with a Bruker Apex II diffractometer. The data were processed with SAINT9 and corrected for absorption using SADABS.10 Multi-scan absorption corrections were applied with ψ scans.11 Structure of the complex was solved by direct method using SHELXS-97 and refined by full-matrix least-squares techniques on F2 using anisotropic displacement parameters.12 All of the non-hydrogen atoms of the complex were refined anisotropically. The H atom of the methanol ligand was located from electronic density maps and refined isotropically. The other hydrogen atoms were located as riding model. Crystallographic data for the complex are summarized in Table 1. Selected bond lengths and angles are listed in Table 2.

Table 1. Crystal and structure refinement data for the complex

| Molecular formula | C19H22BrMoN3O5 |
| --- | --- |
| Molecular weight | 548.2 |
| Crystal system | Monoclinic |
| Space group | P21/c |
| a /Å | 13.9971(8) |
| b /Å | 7.4182(4) |
| c /Å | 21.409(1) |
| β /° | 107.319(1) |
| V /Ǻ3 | 2122.2(2) |
| Z | 4 |
| Dcalc (g cm-3) | 1.716 |
| Crystal dimensions (mm) | 0.21 × 0.20 × 0.18 |
| μ (mm-1) | 2.536 |
| Radiation λ | Mo Kα (0.71073 Ǻ) |
| Tmin/Tmax | 0.6180/0.6582 |
| Reflections measured | 19023 |
| Range/indices (h, k, l) | -16, 16; -8, 8; -25, 24 |
| θ limit (°) | 2.85–25.50 |
| Unique reflections | 3927 [Rint = 0.0301] |
| Observed reflections (I > 2σ(I)) | 3241 |
| Parameters | 268 |
| Restraints | 1 |
| Goodness of fit on F2 | 1.027 |
| R1, wR2 [I  2(I)]a | 0.0299, 0.0673 |
| R1, wR2 (all data)a | 0.0422, 0.0721 |

a R1 = Fo-Fc/Fo, wR2 = [w(Fo2-Fc2)2/w(Fo2)2]1/2

Table 2. Selected bond lengths (Å) and angles (°) for the complex

| Bond lengths |  |  |  |
| --- | --- | --- | --- |
| Mo1-O1 | 1.927(2) | Mo1-O2 | 2.0096(19) |
| Mo1-O3 | 1.686(2) | Mo1-O4 | 2.384(2) |
| Mo1-N1 | 2.228(2) | Mo1-O5 | 1.697(2) |
| Bond angles |  |  |  |
| O1-Mo1-O2 | 149.61(9) | O1-Mo1-N1 | 81.59(8) |
| O5-Mo1-O1 | 102.56(9) | O1-Mo1-O4 | 82.21(9) |
| O3-Mo1-O1 | 99.68(10) | O3-Mo1-O2 | 97.01(10) |
| O3-Mo1-O5 | 105.92(12) | O3-Mo1-N1 | 96.89(10) |
| O5-Mo1-N1 | 155.60(10) | O5-Mo1-O2 | 96.98(9) |
| O2-Mo1-N1 | 71.29(8) | O3-Mo1-O4 | 171.34(10) |
| O5-Mo1-O4 | 81.75(9) | N1-Mo1-O4 | 74.95(8) |
| O2-Mo1-O4 | 77.79(8) |  |  |

2.4. Catalytic oxidation

The dioxomolybdenum(VI) complex (0.001 M) and phenyl methyl sulfide (0.100 M) were dissolved in the mixture of CH2Cl2 and CH3OH (6:4) with 1,3,5-trimethoxybenzene (0.100 M) as the internal standard. The solution was cooled to 283(2) K, to which was added dropwise H2O2 (35% w/w, 0.125 M). An aliquot of the solution (2.0 mL) was quenched with Na2SO3 (0.100 M, 5 mL), then extracted for three times with CH2Cl2 (4 mL). The solvent of the organic phase was removed, and the residue was dissolved in CDCl3 (0.6 mL) and analyzed by 1H NMR to determine the yield.

3. Results and Discussion

The complex was prepared by the reaction of the hydrazone ligand with MoO2(acac)2 in a 1:1 molar ratio (Scheme 2). The crystals of the complex are soluble in DMSO, DMF, MeOH, EtOH and MeCN. Well-shaped single crystals of the complex can be obtained from MeOH.

Scheme 2. The preparation of the complex.

3.1. Crystal structure description of the dioxomolybdenum complex

The molecular structure of the dioxomolybdenum complex is shown in Figure 1. The Mo atom in the complex is coordinated by the phenolic oxygen, imino nitrogen, and enolic oxygen of the hydrazone ligand, two oxo oxygen and one methanol oxygen, forming an octahedral coordination. The hydrazone ligand coordinates to the MoO2 moiety by forming a five- and a six-membered chelate rings. The methanol molecule is weakly coordinated to the Mo atom, as indicated by the long bond value. The equatorial plane defined by atoms O1, O2, N1 and O5 show a high degree of planarity, with mean deviation from the plane of 0.038(3) Å. The Mo1 atom deviates from the least-squares equatorial plane by 0.346(1) Å in the direction of the axial atom O3. The coordinate bond lengths are comparable to those observed in similar complexes.13 The distortion of the octahedral coordination is indicated by the bond angles, ranging from 71.29(8) to 105.92(12)° for the cis angles and from 149.61(9) to 171.34(10)° for the trans angles. The dihedral angle between the two benzene rings of the hydrazone ligand is 0.3(5)°.

In the crystal structure of the complex, the complex molecules are linked through intermolecular hydrogen bonds of types O4–H4···N2i [O4–H4 = 0.85(1) Å, H4···N2i = 2.01(2) Å, O4···N2 = 2.834(3) Å, O4–H4···N2i = 164(4)°; symmetry code for i: – x, 1 – y, – z], to form dimers (Figure 2).

Figure 1. Molecular structure of the complex at 30% probability displacement.

Figure 2. The hydrogen bonds linked dimeric structure of the complex.

3.2. Infrared and electronic spectra

In the IR spectrum of the hydrazone compound (Figure 3), there show stretching bands attributed to C=O, C=N, C–OH and NH at 1634, 1603, 1130 and 3183 cm-1, respectively. In the IR spectrum of the dioxomolybdenum complex (Figure 4), there show two prominent bands at 948 and 850 cm-1, which can be attributed to the MoO2 group.14 The bands due to νC=O and νNH are absent in the dioxomolybdenum complex. This suggests occurrence of keto-imino tautomerization of the hydrazone ligand during coordination to the Mo atom. The typical C=N absorption of the dioxomolybdenum complex is observed at 1595 cm-1.15 The weak bands in low wave numbers can be attributed to the Mo–O and Mo–N vibrations.

Figure 3. IR spectrum of H2L.

Figure 4. IR spectrum of the complex.

The electronic spectrum of the dioxomolybdenum complex recorded in MeCN display strong and medium absorption bands in the region 370–420 and 260–300 nm (Figure 5). These peaks are assigned as charge transfer transitions of the type N(pπ)–Mo(dπ) LMCT and O(pπ)–Mo(dπ) LMCT,16 as the ligand based orbitals are either N or O donor types. The slight change of λmax values within each set of peaks may be due to the difference of electron donating capacity of the hydrazone ligand.

Figure 5. UV spectrum of the complex.

3.3. Catalytic sulfoxidation

The catalytic oxidation test of the dioxomolybdenum complex as catalyst on the oxidation of sulfide under homogeneous conditions using methyl phenyl sulfide as the substrate is shown as Scheme 3. Hydrogen peroxide was used as oxidant in 1.25 equivalent based on the sulfide substrate. Reactions were run with 1 mol% of catalyst based on the substrate at 10 °C. NMR technique was used to monitor the formation of the sulfoxides with 1,3,5-trimethoxybenzene (TMB) as internal standard. The reaction was started by the addition of H2O2. A control reaction under the same condition without the complex present leads to less than 1% sulfide conversion within 4 h. In the presence of the dioxomolybdenum complex, a conversion of 93% for the sulfide to the corresponding sulfoxide was observed within 60 min. After 2 h, the conversion of sulfide was 100%.

Scheme 3. The sulfoxidation process.

4. Supplementary Mateiral

CCDC – 1487659 contain the crystallographic data for the complex. The data can be obtained at http://www.ccdc.cam.ac.uk/const/retrieving.html or from the Cambridge Crystallographic Data Centre (CCDC), 12 Union Road, Cambridge CB2 1EZ, UK; fax: +44(0)1223-336033 or e-mail: deposit@ccdc.cam.ac.uk.

5. Acknowledgments

This research was supported by the National Sciences Foundation of China (No. 20676057 and 20877036) and Top-class foundation of Pingdingshan University (No. 2008010).

6. References

- (a) C. A. Gamelas, A. C. Gomes, S. M. Bruno, F. A. A. Paz, A. A. Valente, M. Pillinger, C. C. Romao, I. S. Goncalves, Dalton Trans. 2012, 41, 3474-3484; (b) L. S. Feng, J. S. Maass, R. L. Luck, Inorg. Chim. Acta 2011, 373, 85-92; (c) M. Bagherzadeh, M. Amini, A. Ellern, L. K. Woo, Inorg. Chem. Commun. 2012, 15, 52-55; (d) S. Rayati, N. Rafiee, A. Wojtczak, Inorg. Chim. Acta 2012, 386, 27-35.

- (a) B. I. Ceylan, Y. D. Kurt, B. Ulkuseven, J. Coord. Chem. 2009, 62, 757-766; (b) M. N. Sokolov, M. A. Mikhailov, P. A. Abramov, V. P. Fedin, J. Struct. Chem. 2012, 53, 197-201; (c) S.-P. Gao, J. Coord. Chem. 2011, 64, 2869-2877.

- (a) M. Ghorbanloo, R. Bikas, G. Malecki, Inorg. Chim. Acta 2016, 445, 8-16; (b) Z. Moradi-Shoeili, M. Zare, M. Bagherzadeh, S. Ozkar, S. Akbayrak, J. Coord. Chem. 2016, 69, 668-677; (c) R. G. Mohamed, F. M. Elantabli, N. H. Helal, S. M. El-Medani, Synth. React. Inorg. Met.-Org. Nano-Met. Chem. 2015, 45, 1839-1850; (d) M. R. Maurya, N. Saini, F. Avecilla, Inorg. Chim. Acta 2015, 438, 168-178; (e) E. Kinoshita, K. Arashiba, S. Kuriyama, A. Eizawa, K. Nakajima, Y. Nishibayashi, Eur. J. Inorg. Chem. 2015, 10, 1789-1794.

- (a) S. Mandal, R. Saha, B. Mahanti, M. Fleck, D. Bandyopadhyay, Inorg. Chim. Acta 2012, 387, 1-7; (b) M. A. Vazquez-Fernandez, M. I. Fernandez-Garcia, A. M. Gonzalez-Noya, M. Maneiro, M. R. Bermejo, M. J. Rodriguez-Douton, Polyhedron 2012, 31, 379-385; (c) F. Habib, P.-H. Lin, J. Long, I. Korobkov, W. Wernsdorfer, M. Murugesu, J. Am. Chem. Soc. 2011, 133, 8830-8833.

- (a) S. Rayati, N. Rafiee, A. Wojtczak, Inorg. Chim. Acta 2012, 386, 27-35; (b) N. K. Ngan, K. M. Lo, C. S. R. Wong, Polyhedron 2012, 33, 235-251; (c) S. Duman, I. Kizilcikli, A. Koca, M. Akkurt, B. Ulkuseven, Polyhedron 2010, 29, 2924-2932; (d) R. D. Chakravarthy, K. Suresh, V. Ramkumar, D. Chand, Inorg. Chim. Acta 2011, 376, 57-63; (e) C. P. Rao, A. Sreedhara, P. V. Rao, M. B. Verghese, K. Rissanen, E. Kolehmainen, N. K. Lokanath, M. A. Sridhar, J. S. Prasad, J. Chem. Soc. Dalton Trans. 1998, 2383-2393.

- (a) M. Mancka, W. Plass, Inorg. Chem. Commun. 2007, 10, 677-680; (b) S. N. Rao, N. Kathale, N. N. Rao, K. N. Munshi, Inorg. Chim. Acta 2007, 360, 4010-4016; (c) R. Dinda, S. Ghosh, L. R. Falvello, M. Tomas, T. C. S. Mak, Polyhedron 2006, 25, 2375-2382.

- X.-M. Hu, L.-W. Xue, C.-X. Zhang, G.-Q. Zhao, Synth. React. Inorg. Met.-Org. Nano-Met. Chem. 2014, 44, 713-718.

- (a) L. Shi, Z.-P. Xiao, Z. Zhuang, Z.-Z. Zhong, H.-L. Zhu, Acta Crystallogr. 2007, E63, o4726; (b) L.-W. Xue, Y.-J. Han, G.-Q. Zhao, Y.-X. Feng, J. Chem. Crystallogr. 2011, 41, 1599-1603.

- Bruker, SMART and SAINT. Area Detector Control and Integration Software; Bruker Analytical X-ray Instruments Inc.: Madison, WI, USA, 1997.

- G. M. Sheldrick, SADABS. Program for Empirical Absorption Correction of Area Detector Data; University of Göttingen: Göttingen, Germany, 1997.

- A. C. T. North, D. C. Phillips, F. S. Mathews, Acta Crystallogr., 1968, A24, 351-359.

- G. M. Sheldrick, SHELXL-97. Program for the Refinement of Crystal Structures; University of Göttingen: Göttingen, Germany, 1997.

- (a) S. N. Rao, K. N. Munshi, N. N. Rao, M. M. Bhadbhade, E. Suresh, Polyhedron 1999, 18, 2491-2497; (b) W.-X. Xu, W.-H. Li, Synth. React. Inorg. Met.-Org. Nano-Met. Chem. 2012, 42, 160-164.

- T. Głowiak, L. Jerzykiewicz, J. M. Sobczak, J. J. Ziółkowski, Inorg. Chim. Acta 2003, 356, 387-392.

- G. Romanowski, M. Wera, Polyhedron 2010, 29, 2747-2754.

- (a) N. R. Pramanik, S. Ghosh, T. K. Raychaudhuri, S. S. Mandal, J. Coord. Chem. 2009, 62, 3845-3582; (b) M. L. H. Nair, D. Thankamani, Russ. J. Coord. Chem. 2010, 36, 259-268.