	Prepared

AgNPs
	Particle Size(nm)
	  Lattice constant ( Å) 
	  Cell volume( Å3) 
	SSA

(m2/g)
	SA:V     ratio
	Crystallinity index Icry

	g1
	16
	4.0529
	66.57
	18.46
	0.35
	~1.0625

	
	
	
	
	
	
	

	g3
	7
	4.0815
	67.99
	40.64
	0.78
	~0.714

	
	
	
	
	
	
	


Table.1. The average particle size, lattice constant, cell volume, surface area to volume (SA: V) ratio, specific surface area (SSA) and crystallinity index of the prepared nanoparticles.

