Electronic Supplementary Information
Mn(II), Zn(II) and Cd(II) complexes based on oxadiazole backbone containing carboxyl ligand: Synthesis, crystal structure, and photoluminescent study

Li-Na Wang, Lin Fu, Jia-Wei Zhu, Yu Xu, Meng Zhang, Qi You, Peng Wang, Jie Qin* 
School of Life Sciences, Shandong University of Technology, Zibo 255049, P. R. China

*Corresponding author: Jie Qin, E-mail: qinjietutu@163.com
Tel.: 0086-533-2780271; Fax: 0086-533-2781329.

Table S1 Selected bond distances (Å) and angles (°) for complex 2.
	Zn1-O4
	2.1208(11)
	Zn1-O2#iii
	2.0722(11)

	Zn1-N1
	2.2111(13)
	S1-C7
	1.7319(17)

	S1-C8
	1.8021(17)
	O2-C9
	1.2576(18)

	O3-C9
	1.2415(19)
	
	

	N1-Zn1-N1#i
	180.00(2)
	O2#iii-Zn1-N1
	90.39(5)

	O4#i-Zn1-N1#i
	91.12(5)
	O2#iii-Zn1-O4
	92.25(4)

	O2#ii-Zn1-O4
	87.75(4)
	O4-Zn1-O4#i
	180.00(10)

	O2#ii-Zn1-N1
	89.61(5)
	O4#i-Zn1-N1
	88.88(5)

	N1-Zn1-N1#i
	180.00(2)
	C7-S1-C8
	98.90(8)


Symmetry transformations used to generate equivalent atoms: (i) -x+2, -y, -z; (ii) -x+1, -y, -z+1; (iii) x+1, y, z-1
[image: image1.jpg]100 moerms

2]
o
]

[=2]
o
]

B
o
I

Transimittance (%)

N
o
I

0 " 1 M 1 A 1 " 1 " 1 A 1 M 1

4000 3500 3000 2500 2000 1500 1000 500
Wavenumber (cm'l)





Figure S1. IR spectra of HL, 1-3.

[image: image2.jpg]



Figure S2. Coordination environment of ZnII in 2. [symmetry codes: (i) -x+2, -y, -z; (ii) -x+1, -y, -z+1; (iii) x+1, y, z-1].
