Synthesis of 2,4,5-Trisubstituted Phenanthroimidazole Derivatives using SBA-Pr-SO3H as a Nanocatalyst
Ghodsi Mohammadi Ziarani,1* Elham Tavaf,1 Vaezeh Fathi Vavsari1 and Alireza Badiei2 
1 Department of Chemistry, Alzahra University, PO Box 1993893973, Tehran, Iran
2 School of Chemistry, College of Science, University of Tehran, PO Box 14155-6455, Tehran, Iran

* Corresponding author: E-mail: gmziarani@hotmail.com, gmohammadi@alzahra.ac.ir
Tel-fax: +98 2188041344

Abstract
An efficient one pot approach for the preparation of 2,4,5-trisubstituted phenanthroimidazole derivatives is described. The three-component reaction between 9,10-phenanthraquinone, benzaldehyde derivatives, and ammonium acetate proceeds in the presence of SBA-Pr-SO3H as a nanoporous solid acid catalyst in short reaction times and good to excellent yields.
Keywords: Trisubstituted phenanthroimidazole; 9,10-Phenanthraquinone; SBA-Pr-SO3H; Nanocatalyst; Heterogeneous catalysis.
1. Introduction

Application of imidazole and their derivatives are unavoidable in the field of medicinal chemistry due to their biologically active properties as biocides,1 platelet aggregation inhibitors,2 analgesics,3 antibacterial,
 ADDIN EN.CITE 

4, 5
 antitumor,
 ADDIN EN.CITE 

6, 7
 and anti-inflammatory.
 ADDIN EN.CITE 

8, 9
 Additionally, derivatives of imidazole conjugated with aromatic rings have been widely used as fluorescent dyes.10 
In recent years, several methods have been reported for the preparation of three-substituted imidazole derivatives from 9,10-phenanthraquinones, benzaldehyde derivatives and ammonium acetate using different catalysts such as I2,11 mercaptopropylsilica,12 zirconium Schiff base,13 iron(III) triflate,14 sulfamic acid15 and ionic liquid modified surface.16
Recently, mesoporous ordered silica materials such as SBA-15 have received more attention in the field of catalysis.
 ADDIN EN.CITE 

17, 18
 As a well ordered hexagonal mesoporous silica, SBA-15 has significant characteristics such as large uniform pore size, high surface area, thick walls, and high thermal stability which makes it a good candidate for preparing organic-inorganic hybrid materials and using as catalysts in different reactions.19 The propyl sulfonic acid modified SBA-15 can behave as an efficient Brønsted acid in organic synthesis. Due to our interest in the field of nano-heterogeneous acidic catalysts,
 ADDIN EN.CITE 

20-23
 and based on different studies on applying SBA-Pr-SO3H in organic synthesis,
 ADDIN EN.CITE 

24-30
 herein we have discovered a green and efficient method for the synthesis of 2,4,5-trisubstituted phenanthroimidazoles 4a-g using SBA-Pr-SO3H. In our previous studies, we have reported the efficient synthesis of benzimidazoquinazolinones31 and 1,2,4,5-tetra substituted imidazoles32 in the presence of SBA-Pr-SO3H.
2. Experimental
2.1. Materials and Instrumentations
All chemicals were obtained commercially and used without further purification. The IR spectra were recorded on KBr disks using a FT-IR Bruker Tensor 27 instrument. Melting points were measured using the capillary tube method with an Electro thermal 9200 apparatus. The 1H NMR and 13C NMR spectra were obtained by a Bruker 400 MHz and 100 MHz, respectively, in either DMSO-d6 or CDCl3 solution. Mass spectra data were also achieved by using a Network mass selective detector 5973 (Agilent) instrument. Scanning electron microscope (SEM) analysis was performed on a PhilipsXL-30 field-emission SEM operated at 16 kV, while TEM was carried out on a Tecnai G2 F30 at 300 kV. Weight change curve in nitrogen was measured on a BAHR Thermo analyse STA 503 with the maximum heating rate of 20 oC/min.
2.2. General procedure for the synthesis of 2,4,5-trisubstituted imidazoles (4a–i)

The mixture of 9,10-phenanthraquinone (0.20 g, 1 mmol), benzaldehyde derivatives (1 mmol), and ammonium acetate (0.31 g, 4 mmol) was stirred in refluxing acetic acid (3 mL) for about 30 min using SBA-Pr-SO3H (0.02 g) as the catalyst. The reaction completion was traced by TLC technique (ethyl acetate/petroleum ether, 2:1). The precipitated product was filtered and dissolved in hot ethanol and DMF to remove the catalyst, and the solvent was evaporated to obtain the pure product. The catalyst was then washed subsequently with a diluted acid solution, distilled water, then acetone, and dried under reduced pressure and reused for several times without significant loss of catalytic activity.33 The physical and spectroscopic data of two new compounds are given below.
2.3. Spectral data of products

2-(2,4-Dimethoxyphenyl)-1H-phenanthro[9,10-d]imidazole (4h)

IR (KBr) (νmax, cm-1): 3523, 3430, 3048, 2987, 2942, 2833, 1935, 1603, 1462, 1371, 1311, 1266, 1204, 1161, 1083, 1022, 923, 835, 747, 714, 564, 434. 1H NMR (400 MHz, DMSO-d6) δ: 3.87 (s, 3H, CH3), 4.03 (s, 3H, CH3), 6.76 (dd, 1H, J=11.5 Hz, J=3 Hz, ArH), 6.80 (d, 1H, J=2.8 Hz, ArH), 7.58-7.74 (m, 4H, ArH), 8.20 (d, 1H, J=11.4 Hz, ArH), 8.62 (d, 1H, J=10.4 Hz, ArH), 8.70 (d, 1H, J=10.5 Hz, ArH), 8.82 (t, 2H, J=10.8 Hz, ArH), 12.57 (s, 1H, NH) ppm. 13C NMR (100 MHz, DMSO-d6) δ: 55.5, 55.9, 98.5, 105.9, 111.8, 111.9, 121.9, 122.4, 122.5, 123.7, 123.9, 125, 126.6, 126.8, 126.9, 127, 127.3, 127.4, 131.1, 136.2, 147.3, 157.8, 161.6 ppm. MS (m/z, %):  354 (M+, 100), 336(33), 321(47), 309(23), 267(24), 190(20), 177(28), 163(13), 137(22).
2-(2,6-Dichlorophenyl)-1H-phenanthro[9,10-d]imidazole (4i)

IR (KBr) (νmax, cm-1): 3063, 2973, 2904, 2845, 2737, 1948, 1702, 1602, 1548, 1481, 1437, 1327, 1191, 1153, 1041, 954, 880, 784, 740, 617, 531, 432. 1H NMR (400 MHz, DMSO-d6) δ: 7.60-7.75 (m, 7H, ArH), 8.36 (d, 1H, J=10.4 Hz, ArH), 8.56 (d, 1H, J=10.3 Hz, ArH), 8.81-8.88 (m, 2H, ArH), 13.82 (s, 1H, NH) ppm. 13C NMR (100 MHz, DMSO-d6) δ: 121.7, 122, 122.4, 123.8, 124.2, 125.3, 125.6, 127.1, 127.14, 127.3, 127.5, 127.8, 128.4, 130.7, 132.5, 135.7, 136.5, 144.2 ppm. MS (m/z, %): 362 (M+, 100), 336(9), 190(86), 171(18), 163(53), 136(18).

3. Results and Discussion
The reaction of 9,10-phenanthraquinone 1, 4-chlorobenzaldehyde 2a, and ammonium acetate 3 was selected for optimizing conditions and investigating the role of nanocatalyst SBA-Pr-SO3H (Scheme 1). In order to study the solvent effect, different solvents were tested including solvent-free system at ambient temperature and 120 ºC, refluxing in water, ethanol and/or acetic acid as green solvents. As the result shown in Table 1, the best yield was obtained under refluxing in acetic acid in the presence of SBA-Pr-SO3H (0.02 g). On the other hand, to indicate the catalyst effect, the results of different catalyst were compared with SBA-Pr-SO3H under modified conditions (Figure 1). As it is clear, SBA-Pr-SO3H led to both shorter reaction time and higher yields. After that, several aromatic aldehydes were applied for the synthesis of other 2,4,5-trisubstituted phenanthroimidazoles (Figure 2) which are listed in Table 2. 

[image: image1.emf]O

O

+

H

O

+ NH

4

OAC

1

2a

3

N

H

N

Cl

4a

Cl

Different

conditions


Scheme 1. Model reaction of 9,10-phenanthraquinone 1, 4-chlorobenzaldehyde 2a, and ammonium acetate 3 for the synthesis of 4a.
Table 1: Optimizing the reaction conditions for the synthesis of 4a.
	Entry
	Catalyst
	Solvent
	Condition
	Time (min)
	Yield (%)

	1
	SBA-Pr-SO3H
	-
	r.t.
	24 h
	Trace

	2
	SBA-Pr-SO3H
	-
	120 °C
	N. R.
	80

	3
	SBA-Pr-SO3H
	H2O
	Reflux
	>5 h
	-

	4
	SBA-Pr-SO3H
	EtOH
	Reflux
	>5 h
	73

	5
	SBA-Pr-SO3H
	CH3COOH
	Reflux
	5
	95

	6
	-
	CH3COOH
	Reflux
	10
	90


[image: image2.png]300

200 -

100 -

Time (min)

Yiled (%)

SILLP

SBA-Pr-SO;H




Figure 1. Comparison of two factors (reaction times and product yields) for the synthesis of product 4 using different catalysts including I2,11 mercaptopropylsilica (MPS),12 p-toluenesulfonic acid (p-TSA),13 NH2SO3H,15 supported ionic liquid-like phase (SILLP),16 and SBA-Pr-SO3H.
[image: image3.png]



Figure 2. Schematic synthesis of 2,4,5-trisubstituted imidazoles.
Table 2: Synthesis of 2,4,5-trisubstituted imidazoles in the presence of SBA-Pr-SO3H under reflux conditions in acetic acid.
	Entry
	R
	Product
	Time (min)
	Yield (%)
	mp (°C)
	mp (Lit.)

	1
	4-Cl
	
[image: image4.emf]N HN

Cl

4a


	10
	95
	263-265
	275-276 14

(Sakaino 1971)


	2
	4-F
	
[image: image5.emf]N HN

F

4b


	20
	96
	205-208
	-

	3
	4-OMe
	
[image: image6.emf]N HN

O

4c


	10
	95
	265-267
	265-257 34

	4
	4-Me
	
[image: image7.emf]N HN

CH

3

4d


	10
	97
	292-295
	290-292 35

	5
	4-OH
	
[image: image8.emf]N HN

OH

4e


	20
	97
	>300
	350-352 14

	6
	3-NO2
	
[image: image9.emf]N HN

NO

2

4f


	20
	90
	278-280
	271-272 36

	7
	2,4-(Cl)2

	
[image: image10.emf]N HN

Cl

Cl

4g


	10
	94
	242-244
	245-246 15

	8
	2,4-(OMe)2

	
[image: image11.emf]N HN

O

O

4h


	20
	93
	203-205
	New

	9
	2,6-(Cl)2

	
[image: image12.emf]N HN

Cl Cl

4i


	20
	90
	230-232
	New


The proposed mechanism is shown in Scheme 2. Accordingly, the carbonyl group of aldehydes 2a-i is protonated upon the acidic sites of SBA-Pr-SO3H. Afterward, the activated carbonyl will be susceptible to the nucleophilic attack of ammonia, produced by ammonium acetate 3, and gives intermediate 4'. Condensation of 9,10-phenanthraquinone 1 with intermediate 4' through an imination process and proton replacement of intermediate 4'' produces the desired products 4a-i.
[image: image13.png]



Scheme 2. The proposed mechanism for the synthesis of 4a-i.
SBA-15 was synthesized through the reported method.33 Then, its internal surfaces were modified using (3-mercaptopropyl)trimethoxysilane following oxidation with H2O2 in methanol provided SBA-Pr-SO3H. The latter was then characterized via different techniques including TGA, and SEM and TEM images. The weight reduction in TGA analysis (Figure 3) in the temperature range of 200-600 °C, indicated that the amount of propyl sulfonic acid groups were grafted onto the pores of silica material and its amount is 1.2 mmol/g. The mass loss before 200 °C is for the adsorbed water onto the pores of SBA-Pr-SO3H. SEM image of SBA-Pr-SO3H showed same morphology as obtained for SBA-15 proving this process didn’t change the structure of SBA-15 (Figure 4). TEM image also demonstrated the presence of channels onto the SBA-Pr-SO3H structure which were not collapsed after modification. 
[image: image14.png]105

100

ES

(%) WsPm

4

2

75

400 600 800

Temperature (°C)

200




Figure 3. TGA curve of SBA-Pr-SO3H.
[image: image15.jpg]R 9=
.BkY X18.0K 3.880sm



[image: image16.emf]
Figure 4. The SEM (left) and TEM (right) images of SBA-Pr-SO3H.
4. Conclusion
In conclusion, we have developed a novel three-component reaction leading to 2,4,5-trisubstituted phenanthroimidazoles 4 from 9,10-phenanthraquinones, benzaldehyde derivatives and ammonium acetate. The high yields of products, mild reaction conditions, the ease of purification, and the ability of recycling the heterogonous nanocatalyst SBA-Pr-SO3H make this as an ecologically friendly procedure for the synthesis of 4. This protocol not only provides an effective methodology for the preparation of the product but also expands the new pathway for employing green catalysts to design other similar multicomponent reactions. 
5. Acknowledgements
We gratefully acknowledge the financial support from the Research Council of Alzahra University and University of Tehran.
This research did not receive any specific grant from funding agencies in the public, commercial, or not-for-profit sectors.
6. References
1.
T. Maier, R. Schmierer, K. Bauer, H. Bieringer, H. Burstell, B. Sachse, 1-Substituted imidazole-5-carboxylic acid derivatives, their preparation and their use as biocides, US Patent Number 4820335 A, 1989.

2.
P. Needleman, A. Raz, J. A. Ferrendelli, M. Minkes, Proc. Natl. Acad. Sci. 1977, 74, 1716-1720. http://dx.doi.org/10.1073/pnas.74.4.1716
3.
Ü. Uçucu, N. G. Karaburun, İ. Işikdağ, Il Farmaco 2001, 56, 285-290. http://dx.doi.org/10.1016/S0014-827X(01)01076-X
4.
M. Antolini, A. Bozzoli, C. Ghiron, G. Kennedy, T. Rossi, A. Ursini, Bioorg. Med. Chem. Lett. 1999, 9, 1023-1028. http://dx.doi.org/10.1016/S0960-894X(99)00112-2
5.
L. H. Jawaharmal, S. Narwal, G. Singh, D. Saini, A. Kaur, S. Narwal, Indo Global J. Pharm. Sci. 2012, 2, 147-156.

6.
L. Wang, K. W. Woods, Q. Li, K. J. Barr, R. W. McCroskey, S. M. Hannick, L. Gherke, R. B. Credo, Y.-H. Hui, K. Marsh, R. Warner, J. Y. Lee, N. Zielinski-Mozng, D. Frost, S. H. Rosenberg, H. L. Sham, J. Med. Chem. 2002, 45, 1697-1711. http://dx.doi.org/10.1021/jm010523x
7.
J. C. Lee, J. T. Laydon, P. C. McDonnell, T. F. Gallagher, S. Kumar, D. Green, D. McNulty, M. J. Blumenthal, J. R. Keys, S. W. Land vatter, J. E. Strickler, M. M. McLaughlin, I. R. Siemens, S. M. Fisher, G. P. Livi, J. R. White, J. L. Adams, P. R. Young, Nature 1994, 372, 739-746. http://dx.doi.org/10.1038/372739a0
8.
T. Corell, G. Hasselmann, Acta Pharmacol. Toxicol. 1983, 53, 288-296. http://dx.doi.org/10.1111/j.1600-0773.1983.tb03425.x 
9.
I. K. Khanna, R. M. Weier, Y. Yu, X. D. Xu, F. J. Koszyk, P. W. Collins, C. M. Koboldt, A. W. Veenhuizen, W. E. Perkins, J. J. Casler, J. L. Masferrer, Y. Y. Zhang, S. A. Gregory, K. Seibert, P. C. Isakson, J. Med. Chem. 1997, 40, 1634-1647. http://dx.doi.org/10.1021/jm9700225
10.
K. Skonieczny, A. I. Ciuciu, E. M. Nichols, V. Hugues, M. Blanchard-Desce, L. Flamigni, D. T. Gryko, J. Mater. Chem. 2012, 22, 20649-20664. http://dx.doi.org/10.1039/C2JM33891B
11.
H. Behmadi, M. Roshani, S. M. Saadati, Chin. Chem. Lett. 2009, 20, 5-8. http://dx.doi.org/10.1016/j.cclet.2008.09.047 
12.
C. Mukhopadhyay, P. K. Tapaswi, M. G. B. Drew, Tetrahedron Lett. 2010, 51, 3944-3950. http://dx.doi.org/10.1016/j.tetlet.2010.05.102
13.
S. Damavandi, Synth. React. Inorg., Met.-Org., Nano-Met. Chem. 2011, 41, 1274-1277. http://dx.doi.org/10.1080/15533174.2011.594839
14.
S. Damavandi, R. Sandaroos, Heterocycl. Communi 2011, 17, 121-124. http://dx.doi.org/10.1515/hc.2011.028
15.
H.-N. Peng, X.-M. Peng, D.-G. Zheng, F. Yu, M. Rao, Heterocycl. Communi 2011, 17, 223-226. http://dx.doi.org/10.1515/HC.2011.040
16.
M. Saffari Jourshari, M. Mamaghani, F. Shirini, K. Tabatabaeian, M. Rassa, H. Langari, Chin. Chem. Lett. 2013, 24, 993-996. http://dx.doi.org/10.1016/j.cclet.2013.06.005
17.
G. Mohammadi Ziarani, N. Lashgari, A. Badiei, J. Mol. Catal. A: Chem. 2015, 397, 166-191. http://dx.doi.org/10.1016/j.molcata.2014.10.009
18.
G. Mohammadi Ziarani, N. Lashgari, A. Badiei, Curr. Org. Chem. 2016, Corrected Proof, In Press. http://dx.doi.org/10.2174/1385272820666160525123600 
19.
F. Hoffmann, M. Cornelius, J. Morell, M. Fröba, Angew. Chem. Int. Ed. 2006, 45, 3216-3251. http://dx.doi.org/10.1002/anie.200503075
20.
V. Fathi Vavsari, G. Mohammadi Ziarani, S. Balalaie, A. Latifi, M. Karimi, A. Badiei, Tetrahedron 2016, 72, 5420-5426. http://dx.doi.org/10.1016/j.tet.2016.07.034
21.
M. Rahimifard, G. Mohammadi Ziarani, A. Badiei, Res. Chem. Intermed. 2016, 42, 6327-6336. http://dx.doi.org/10.1007/s11164-016-2465-3
22.
G. Mohammadi Ziarani, L. Seyedakbari, S. Asadi, A. Badiei, M. Yadavi, Res. Chem. Intermed. 2016, 42, 499-509. http://dx.doi.org/10.1007/s11164-015-2036-z
23.
G. Mohammadi Ziarani, M. Shakiba Nahad, N. Lashgari, A. Badiei, Acta Chim. Slov. 2015, 62, 709-715. http://dx.doi.org/10.17344/acsi.2014.972
24.
V. Fathi Vavsari, G. Mohammadi Ziarani, A. Badiei, S. Balalaie, J. Iran. Chem. Soc. 2016, 13, 1037-1043. http://dx.doi.org/10.1007/s13738-016-0817-y
25.
P. Gholamzadeh, G. Mohammadi Ziarani, A. Badiei, A. Abolhassani Soorki, N. Lashgari, Res. Chem. Intermed. 2013, 39, 3925-3936. http://dx.doi.org/ 10.1007/s11164-012-0909-y
26.
P. Gholamzadeh, G. Mohammadi Ziarani, A. Badiei, Z. Bahrami, Eur. J. Chem. 2012, 3, 279-282. http://dx.doi.org/10.5155/eurjchem.3.3.279-282.630
27.
N. Lashgari, G. Mohammadi Ziarani, A. Badiei, M. Zarezadeh-Mehrizi, J. Heterocycl. Chem. 2014, 51, 1628-1633. http://dx.doi.org/10.1002/jhet.1746
28.
G. Mohammadi Ziarani, A. Badiei, M. Azizi, N. Lashgari, J. Chin. Chem. Soc. 2013, 60, 499-502. http://dx.doi.org/10.1002/jccs.201200530
29.
G. Mohammadi Ziarani, N. H. Mohtasham, A. Badiei, N. Lashgari, J. Chin. Chem. Soc. 2014, 61, 990-994. http://dx.doi.org/ 10.1002/jccs.201300538
30.
G. Mohammadi Ziarani, N. Lashgari, S. Faramarzi, A. Badiei, Acta Chim. Slov. 2014, 61, 574-579.
31.
G. Mohammadi Ziarani, A. Badiei, Z. Aslani, N. Lashgari, Arabian J. Chem. 2015, 8, 54-61. http://dx.doi.org/10.1016/j.arabjc.2011.06.020
32.
G. Mohammadi Ziarani, A. Badiei, N. Lashgari, Z. Farahani, J. Saudi Chem. Soc. 2016, 20, 419-427. http://dx.doi.org/10.1016/j.jscs.2013.01.005
33.
G. Mohammadi Ziarani, S. Ghorbi, P. Gholamzadeh, A. Badiei, Iran. J. Catal. 2016, 6, 229-235.
34.
E. K. Dora, B. Dash, C. S. Panda, J. Indian Chem. Soc. 1979, 56, 620-624.
35.
L. Weiying, L. Lingliang, Y. Lin, C. Zengmei, C. Bingbing, T. Wen, Org. Lett. 2008, 10, 5577-5580. http://dx.doi.org/10.1021/ol802436j
36.
Y. Sakaino, H. Kakisawa, K. Arita, M. Kouno, H. Morishima, Tetrahedron 1973, 29, 1185-1191. http://dx.doi.org/10.1016/0040-4020(73)80099-7


Cover Picture
[image: image17.jpg]SBA-Pr-SO;H





13

_1541658911.cdx

_1541658913.cdx

_1541658916.cdx

_1541659837.cdx

_1541658917.cdx

_1541658914.cdx

_1541658912.cdx

_1541658909.cdx

_1541658910.cdx

_1541658908.cdx

