Electronic Supplementary Information
1D, 2D and 3D supramolecular frameworks self-assembled from a hydrazone ligand and azide salts: syntheses, structural diversity, and luminescent properties

Peng Wang†, Yu-Shan Wu†, Xiao-Meng Han, Shan-Shan Zhao, Jie Qin* 

School of Life Sciences, Shandong University of Technology, Zibo 255049, P. R. China

*Corresponding author: Jie Qin, E-mail: qinjietutu@163.com
Tel.: 0086-533-2780271; Fax: 0086-533-2781329.
† These authors contributed equally to this work.
Table S1 Selected bond distances (Å) and angles (°) for complex 2.
	Zn1-N6
	2.002(2)
	Zn1-N3
	2.051(2)

	Zn1-O1
	2.1146(17)
	Zn1-N5#i
	2.1253(19)

	Zn1-N1
	2.190(2)
	C7-N4
	1.326(3)

	C7-O1
	1.275(3)
	C5-N3
	1.287(3)

	N6-N7
	1.193(3)
	N7-N8
	1.157(3)

	N3-Zn1-N1
	75.51(8)
	N3-Zn1-O1
	75.54(7)

	N6-Zn1-O1
	100.56(8)
	N6-Zn1-N1
	105.09(8)

	N6-Zn1-N5#i
	98.23(8)
	N3-Zn1-N5#i
	106.81(8)

	O1-Zn1-N5#i
	94.34(8)
	N5#i-Zn1-N1
	95.12(8)

	N6-Zn1-N3
	154.85(9)
	O1-Zn1-N1
	151.02(7)

	C7-N4-N3
	108.59(19)
	N7-N6-Zn1
	123.87(19)

	N8-N7-N6
	176.2(3)
	C4-C5-N3
	113.6(2)


Symmetry transformations used to generate equivalent atoms: (i) –x+1/2, y-1/2, -z-1/2.
[image: image1.png]Transimittance (%)

100

~
(3]
]

a
o
T

N
3,
T

4000

3500

3000 2500 2000 1500
Wavenumber (cm'l)

1000

500




Figure S1. IR spectra of complexes 1-3.

[image: image2.png]



Figure S2. Coordination environment of ZnII in 2. [symmetry codes: (i) –x+1/2, y-1/2, -z-1/2]
[image: image3.png]



Figure S3. 1D zigzag chain structure of 2.
3

