Diaquabis(2,2’-dipyridylamine)M(II) terephthalate dihydrates, M(II) = Ni, Co: synthesis, crystal structures, thermal and magnetic properties

Lidija Radovanović,1,* Jelena Rogan,2 Dejan Poleti,2 Marko V. Rodić,3 Zvonko Jagličić,4
1 Innovation Centre - Faculty of Technology and Metallurgy, University of Belgrade, Karnegijeva 4, 11000 Belgrade, Serbia

2 Department of General and Inorganic Chemistry, Faculty of Technology and Metallurgy, University of Belgrade, Karnegijeva 4, 11000 Belgrade, Serbia

3 Faculty of Sciences, University of Novi Sad, Trg Dositeja Obradovića 3, 21000 Novi Sad, Serbia

4 Faculty of Civil and Geodetic Engineering & Institute of Mathematics, Physics and Mechanics, University of Ljubljana, Jamova 2, 1000 Ljubljana, Slovenia
e-mail: lradovanovic@tmf.bg.ac.rs
[image: image1.png]



Figure S1. Structural fragment of 2 with atomic numbering scheme (hydrogen atoms are omitted for the sake of clarity). The thermal ellipsoids are plotted at the 30% probability level. Symmetry codes: (i): –x+1, y, –z+1/2, (ii): –x+1, –y+2, –z.

[image: image2.png]06

O 5ii





Figure S2. The network of hydrogen bonds (presented by dashed lines) in 2. Hydrogen atoms are omitted for the sake of clarity.
[image: image3.png]



Figure S3. Projections of the crystal packing of 2 in almost ac plane. The π-π interactions between structural fragments are presented by purple lines.
[image: image4.png](LLL) ®

¢ Ni (JCPDS 04-0850)

(0zz)®

(002)®

3

1
80

70

T
60

40

(‘n "e) AjIsuayu|

20 (°)




Figure S4. XRPD pattern of Ni obtained after thermal decomposition of 1 in N2.

[image: image5.png]100 -

Mass Loss, Y%
AN (@)) o0
o o o
] ] ]

N
o
|

\t'

20

T T
I o

N

(@)

Heat Flow, W g

T
I
N
o

J
200

I v I v I
400 600 800
Temperature, °C

J
1000




Figure S5. TGA and DSC curves for 2 obtained at heating rate of 10 °C min–1 in flowing N2 (exo up).
[image: image6.png](LLL)®

e Co (JCPDS 15-0806)

(002)®

(0zz)e®

(‘n "e) AjIsualu|

70

60

50

40

20 (°)




Figure S6. XRPD pattern of Co obtained after thermal decomposition of 2 in N2.
3

