Legends to Tables

- Table 1. Elemental analysis, physical and surface characterization of PBP

- Table 2. Kinetic parameters biosorption of 2,4,6-TCP on PBP

- Table 3. Isotherm parameters for the biosorption of 2,4,6-TCP on PBP

Table 1. Elemental analysis, physical and surface characterization of PBP

| Parameter |  | Value |
| --- | --- | --- |
| Odor |  | None |
| Color |  | Light Brownish |
| Weight loss (%) |  | 42.6 |
| Apparent (bulk) density (g/cm3) |  | 0.318 |
| Moisture content (%) |  | 5 |
| Ash content (%) |  | 5.62 |
| BET surface area (m2/g) |  | 0.104 |
| Multi point BET surface area (m2/g) |  | 1.410 |
| Pore radius (A0) |  | 22.35 |
| Carbon (%) |  | 76.41 |
| Hydrogen (%) |  | 5.35 |
| Nitrogen (%) |  | 6.78 |

Table 2. Kinetic parameters biosorption of 2,4,6-TCP on PBP

| Parameter | Initial concentration of 2,4,6-trichlorophenol (mg/L) |  |  |  |
| --- | --- | --- | --- | --- |
|  | 100 | 200 | 300 | 400 |
| q(e, exp) (mg/g) | 85.90 | 158.47 | 247.20 | 329.21 |
| Pseudo-first-order-kinetic model |  |  |  |  |
| q(e, cal) (mg/g) | 61.14 | 105.59 | 128.54 | 130.49 |
| k1( min-1 ) | 0.022 | 0.016 | 0.017 | 0.014 |
| R2 | 0.979 | 0.974 | 0.994 | 0.999 |
| qt (%) | 44 | 54.31 | 69.59 | 83.80 |
| Pseudo-second-order-kinetic model |  |  |  |  |
| q(e, cal) (mg/g) | 96.74 | 168.06 | 253.08 | 321.73 |
| k2 (g/mg/min ) | 4.6 × 10-4 | 2.6 × 10-4 | 2.8 × 10-4 | 3.3 × 10-4 |
| R2 | 0.999 | 0.998 | 0.997 | 0.997 |
| qt (%) | 1.37 | 2.24 | 2.95 | 3.49 |
| Elovich model |  |  |  |  |
| q(e, cal) (mg/g) | 83.67 | 144.15 | 231.13 | 302.41 |
| 1/b (mg/g) | 20.49 | 35.57 | 42.64 | 40.72 |
| R2 | 0.999 | 0.999 | 0.995 | 0.986 |
| qt (%) | 0.50 | 0.63 | 0.95 | 1.18 |
| Weber-Morris |  |  |  |  |
| kid | 5.92 | 10.32 | 12.41 | 11.96 |
| C | 22.12 | 37.06 | 102.4 | 178.7 |
| R2 | 0.979 | 0.987 | 0.989 | 0.998 |
| qt (%) | 3.06 | 2.36 | 1.51 | 0.38 |

Table 3. Isotherm parameters for the biosorption of 2,4,6-TCP on PBP

| Isotherms | Constants |  | R2 | qe(%) |
| --- | --- | --- | --- | --- |
| Langmuir | qm (mg/g) | b (L/mg) |  |  |
|  | 289.09 | 0.002 | 0.999 | 2.43 |
| Freundlich | KF ((mg/g)(L/mg)1/n) | n |  |  |
|  | 0.565 | 1.030 | 0.999 | 1.48 |
| Dubinin-Radushkevich | qs (mmol/g) | E (kJ/mol) |  |  |
|  | 4.84 | 7.60 | 0.997 | 3.51 |