Supporting information
Electrochemical detection of nitrite in food based on poly- (3,4-ethylenedioxythiophene) doped with Fe3O4 nanoparticles loaded carboxylated nanocrystalline cellulose

 Guiyun Xu,a Mingming Zhanga and Xijuan Yua*
aKey Laboratory of Sensor Analysis of Tumor Marker, Ministry of Education, College of Chemistry and Molecular Engineering, Qingdao University of Science and Technology, Qingdao 266042, China.

*Corresponding author. Tel:+ 86 532 84022681; Fax: + 86 532 84023927; 

E-mail: xjuanyu@qust.edu.cn
Fig S1. Zeta potentials of NCC (a), CNCC (b) and Fe3O4-CNCC (c).

[image: image6.png]Current / pA

4004A,, 1504B
3509w A
1 /
300-75250 Y ' 120
2503 m
<
3 904
200- 025 0.30 035 040 045 050 :
1504 Scanrate/ (V/s)"” g
£ 60+
100 3
(§]
50 304
04 S
50 04
-100 T T T T T T T T T T T T T T T T T
04 05 06 07 08 09 10 11 03 04 05 06 07 08 09 1.0 11 12 13

Potential / V Potential / V




Fig S2. XRD patterns of CNCC (a) and Fe3O4-CNCC (b). 

[image: image2.png]Intensity (a.u.)

i; “
H !
* E ~/*\/ |
(022) &W\—
° = ZO(D::M’ “ °
| (042)
(400) (333)
‘ N
‘ ‘
| ! I
I
T T T !
20 40 60 80

20 (Degree)




Fig S3. DPV curves of different electrodes in PBS (0.2 M, pH 7.4) in the presence of 5.0 mM nitrite with the quiet time of 2 s: bare GCE (a), PEDOT/CNCC/GCE (b), PEDOT/Fe3O4-CNCC/GCE (c).

[image: image3.png]Current / pA

80 -

60 -

40

20 -

0 -

0.5

0.6

0.7

0.8

1
0.9 1.0
Potential / V

1.1

1.2

1.3

14




Fig S4. (A) CVs of the PEDOT/Fe3O4-CNCC/GCE in PBS (0.2 M, pH 7.4) in the presence of 5.0 mM nitrite at different scan rates from 0.05 to 0.19 V/s. The inset is the linear relationship between peak currents and scan rates; (B) DPV curves of PEDOT/Fe3O4-CNCC/GCE in PBS (0.2 M, pH 7.4) in the presence of 5.0 mM nitrite (a) and then in PBS (0.2 M, pH 7.4) without the addition of nitrite (b).

[image: image4]
Fig S5. Amperometric response to successive addition of 0.1 mM nitrite (a), 0.5 mM AA (b), 0.5 mM DA (c), 1.0 mM UA (d), 1 mM sodium citrate (e), 1 mM sodium benzoate (f) and a second addition of 0.1 mM nitrite (a) of the PEDOT/Fe3O4-CNCC/GCE in PBS (0.2 M, pH 7.4). 

[image: image5.png]Current / pA

-5 4

T T T T T T T I v I
0 100 200 300 400 500
Time /s

I
600





[image: image1.png]Total Counts

50000

40000

30000 -

20000

10000 -

0

-150

T
-100

-.’;0 0 50
Zeta Potential (mV)

T
100

150



