Adsorptive removal of cationic and anionic dyes from aqueous solutions by using eggshell household waste as biosorbent

Eszter Rápó1, Robert SZÉP2, Ágnes KERESZTESI2, Maria SUCIU3, Szende TONK1*

1Faculty of Sciences and Arts, Sapientia Hungarian University of Transylvania, Calea Turzii no. 4, RO-400193, Cluj-Napoca, Romania (corresponding author: tonkszende@gmail.com Tel.: +40 744 767 794)

2Faculty of Economics, Sapientia Hungarian University of Transylvania, Piaţa Libertăţii no. 1, RO-530104, Miercurea-Ciuc, Romania

3National Institute for Research and Development of Isotopic and Molecular Technologies, Electron Microscopy Integrated Laboratory, 67-103 Donath Str., 400293, Cluj Napoca, Romania

Abstract

In the last years the adsorption processes were proven to be effective and easy to use techniques to clean the polluted waste water. The purpose of this research is to examine the biosorption method on organic indicators (Methylene Blue, Malachite Green, Congo Red and Bromphenol Blue) in aqueous medium by using chicken eggshell. The adsorption process was investigated in static circumstance. We examined the initial change of concentration (10-50 mg/l), the pH effect on the adsorption process, the equilibrium process, and the sorption kinetics. With scanning electron microscope, we examined the morphology and texture of the eggshell, furthermore we conducted EDX micro analysis and ecotoxicological tests. Our results support the influence of the parameters on the sorption process.

Keywords

adsorption; eggshell; cationic dye; anionic dye

INTRODUCTION

The World Economic Forum has consecutively assessed the water crisis as one of the major global risks over the past five years. In 2016, the water crisis was determined as the global risk of highest concern for people and economies for the next ten years.1 In global scale it is estimated that 80% of wastewater is released to the environment without adequate treatment.2 Water pollution is highly affected by industrial development. Textile industry uses dyes to color their products producing wastewater containing organic matter with strong color.3 Due to low level dye-fiber fixation approximately 15% of the total dyestuff produced annually is lost during the dyeing process and comes out with their waste water.4,5 The removal of dyes from water becomes environmentally important because small quantities can be toxic to natural waters causing allergic reactions, skin irritation, cancer, mutations, its color is highly visible and inhibits sunlight penetration into waters like streams, rivers, lakes.6 For this reason, the effective removal of these dyes by using clean-up technologies is an outstanding task. Adsorption is a well-known equilibrium separation process and an effective method for water decontamination applications.7 Eggshell could be a low-cost adsorbent for dye removal from wastewater because dye molecules can bind to the porous structure of eggshell (17000 pores) having large surface area.8–10 Eggs are the most common and widely used natural food on Earth, only in the US 50 billion eggs are consumed per year.11

Materials and Methods

Preparation of dye

Methylene Blue (MB) and Malachite Green (MG) cationic dyes were purchased from Loch-Ner.s.r.o., Chech Republic and Loba Chemie, Wien-Fischamend, Austria, respectively and were used without any further purification treatment. Whereas anionic dyes Congo Red and Bromphenol Blue (BPB) were purchased from Merck KGaA, Germanz and Loba Chemie Wien-Fischamend respectively. Chemical structures and characteristics of all four dyes are summarized in Table 1.

Table 1. Description of indicators used in experiment

| Characteristics | Congo Red | Bromphenol Blue | Methylene Blue | Malachite Green |
| --- | --- | --- | --- | --- |
| Chemical formula | C32H22N6Na2O6S2 | C19H10Br4O5S | C16H18ClN3S | C23H25ClN2 |
| M (g/mol) | 696.66 | 669.96 | 373.91 | 364.91 |
| anionic/cationic | anionic | anionic | cationic | cationic |
| Previous biosorption study | 12,13 | 14,15 | 16,17 | 7,18 |

Stock solutions of dyes were prepared by dissolving 1 g of each dye in 1 L deionized water. During adsorption experiments 1g/L stock solution was diluted to obtain the needed concentration.

Preparation of adsorbent

The used chicken eggshell as biosorbent was gathered in from household, kitchen waste. The shells were firstly washed in tap water than in deionized (MilliQ) water. The cleaned eggshell was dried in drying cabinet (Memmert UN75 PLUS) at 80ºC than powdered and sieved at 160 µm size fraction geologist sieve. During biosorption experiments 3-3 g of powdered shell was used without any chemical or physical treatment.

Effect of initial dye concentration

The sorption of indicator dyes on chicken eggshell’s surface was studied in aqueous solutions using 250 mL Erlenmeyer flasks where 100 mL dye solutions were constantly mixed (VARIOMAG Electronisher MULTIPOINT HP multi-magnetic shaker) with 3 g of biosorbent (160 µm particle size) at 750 rpm, room temperature (T=20±1ºC) and without initial pH adjustment. Spectrophotometer was used to periodically measured the dyes concentrations at λmax=497,580,664,619 respectively for Congo Red, BPB, MB, MG using calibration curve as measuring technique for quantitative analysis.

In each case the samples supernatant was centrifuged (Hettick Zentrifugen Mikro 20) for 5 minutes at 10000 rotation/min. after which the maximum absorption was measured by spectrophotometer.

In order to investigate the effect of concentration on adsorption, 100 mL of Congo Red, BPB, MB, MG solutions were mixed with 3 g of powdered eggshell at different initial concentrations between 10-50 mg/L. In each case three parallel experiments were executed.

Effect of pH

Due to the fact that the solutions’ pH highly affects not only the aqueous chemistry but also the biosorbents’ active sites, the removal of Congo Red, BPB, MB, MG from aqueous solution was investigated at different pH between 2-10. pH was adjusted with 0.1N NaOH and 0.1N HCl. During the experiment constant parameters were: c=30 mg/L, 3 g of 160 µm particle sized biomass, 750 rpm, T=20±2ºC.

SEM and EDX analytical measurement

The texture and morphology of chicken eggshell before and after treatment with dyes was analyzed using Scanning electron microscopy (JEOL(USA)JSM5510 LV SEM). Elemental studies were also carried out using Energy dispersive spectroscopy.

Bioconcentration factor

BCF is a value that gives the dyes’ accumulation efficiency in eggshell. It was calculated based on the dye concentrations in the eggshell and the dissolved dye concentration of aquatic solution.

BCF=cindicator on eggshellcindicator in water									                (1)

Ecotoxicological tests – the effect of dyes on seedling growth

Based on Hungarian standard MSZ 21978/8-85 the toxicological effect of Congo Red, BPB anionic and MB, MG cationic dyes was studied on lettuce and mustard seeds. During experiments 25 seeds were put in autoclaved (at 120ºC) Petri-dishes and 5-5 mL dye solution was added at different concentrations (10, 30, 50, 1000 mg/L). The two simultaneous set of samples were put in a dark chamber for 3 days, where the temperature was kept constant T=20±2ºC. After the passing days the length of the seeds roots were measured and the number of seedling was also examined. With the help of the equation below, by knowing the length of the seeds (using the averages of the 25 seed length) the root growth inhibition was calculated.

X=K-MK*100											                (2)

Where: X – Root growth inhibition, K – root length of control seeds (mm), M – root length of dye contaminated seeds (mm).

Results and discussions

Effects of initial indicator dye concentration

During our research the effect of Congo Red, BPB anionic and MB, MG cationic indicators uptake by chicken eggshell household waste was examined using different initial dye concentrations between 10-50 mg/L. Figure 1 shows the efficiency and quantity in equilibrium of various dyes at different initial concentration where 3 g eggshell powder of 160 μm particle size was constantly shaken at 750rpm with 100 mL solution at room temperature (T=20±2ºC) without pH adjustment (pHCR=8.05, pHBPB=2.7, pHMB=3.95, pHMG=2.76). With the increase of initial dye concentration in case of Congo Red, MB and MG, the adsorption capacity also increased, whereas in case of BPB there is no such trend.

Figure 1. Effect of initial dye concentration for Congo Red (a), BPB (b), MB (c), MG (d) (Ci=0-50 mg/L, 3 g biomass, 160 µm, 700 rpm, pHCongo=8.05; pHBPB= 2.70; pHMB=3.95; pHMG=2.76, T=20±1oC)

Effect of solution pH

The pH of aqueous solution can highly affect the biosorbents’ (eggshell) surface charge. In acidic media, the surface of the adsorbent is protonated while in a basic medium its surface deprotonates. During our research the adsorption processes were studied by varying the aqueous solutions’ pH, ranging between 2-10. As seen in figure 2. Congo Red dyes’ highest adsorption efficiency was obtained at pH=2, but in all cases E was above 93%. BPB dyes’ highest efficiency was also at pH=2 (E=67%). For MB the adsorption was most efficient at pH=10, achieving 75% efficiency, while the lowest was at pH=2 where E=14%. MG is similar to Congo Red dye, with a high percentage efficiency at all pHs. Thus it can be said that BPB anionic dye preferred acidic medium, while MB cationic dye preferred the basic medium. Whereas there is no significant change in case of Congo Red and MG, because the efficiency was high at all pHs. Similar results were obtained by Zeroual et al., 2006; Iqbal and Ashiq, 2010; Salleh et al., 2011; Zulfikar and Setiyanto, 2013; Tiwari et al., 2015; El-Dars et al., 2015.3,14,19–22

Figure 2. Effect of pH for indicators: Congo Red (a), BPB (b), MB (c), MG (d) (Ci=30 mg/L, 1.5 g biomass, 160 µm, 700 rpm, T=20±1oC)

SEM and EDX

Scanning electron microscopy photographs were taken in order to examine the shape of the samples’ particle, size of appeared aggregates, porosity and texture before and after adsorption with eggshell biomass. Figure X shows the SEM of the control sample (160 μm sized eggshell without adsorption) and four dye treated samples with 50 mg/L dye solutions. It can be seen that the porous, cross-linked structure of eggshell disappears in comparison to the control sample (Figure 3.a) in case of MB, MG, Congo Red, this is due to the fact that the eggshell has incorporated the color into its “caverns”. On the other hand, in case of BPB (Figure 3.e) some of the cross-linked structure is saturated, in other parts smaller or larger aggregates have appeared, but the cross-linked structure, characteristic to eggshell structure, is still visible. This can be explained in the following way: when comparing the result with the amount of bounded material, we can see that BPB has the smallest value (ci=50 mg/L, qe=0.06 mg/g), so we can conclude that there are still free binders and the eggshells’ crystal grid structure is still visible.

Figure 3. a. control eggshell, 50 mg/L b. MB, c. MG, d. Congo Red, e. BPB adsorbed eggshell household waste

In order to examine the elemental composition of the eggshell both for control and dye adsorbed samples X-ray spectroscopy (EDX) was carried out. From Table 2 it can be assumed that the control sample contains mostly carbon, oxygen and calcium. This was expected because eggshell is made of calcium carbonate (approx. 94%). Samples contaminated with dye not only contain elements specific to eggshell but also elements gained from the dye they were adsorbed with, we can see that new elements appeared, some completely disappeared while others only decreased.

Table 2. Eggshells’ elemental composition, results obtained were computed from 9 data (Cdye= 50 mg/L, 160 μm)

| Elements | Wt(%) control eggshell | Wt(%) MB | Wt(%) MG | Wt(%) Congo Red | Wt(%) BPB |
| --- | --- | --- | --- | --- | --- |
| C | 22.944 ± 9,144 | 25.169 ± 2.617 | 24.662 ± 6.016 | 23.504 ± 5.877 | 25.092 ± 6.607 |
| N | 0.314 ± 0.735 | 0 | 0 | 0 | 0 |
| O | 43.990 ± 10.782 | 46.110 ± 1.241 | 47.633 ± 6.553 | 45.058 ± 2.076 | 47.050 ± 8.348 |
| Na | 0.063 ± 0.108 | 0.046 ± 0.044 | 0.063± 0.067 | 0.096± 0.046 | 0.050 ± 0.079 |
| F | 0 | 0.870 ± 0.688 | 1.763 ± 1.693 | 2.390 ± 0.805 | 1.520 ± 1.726 |
| Mg | 0.445 ± 0.237 | 0.328 ± 0.036 | 0.312 ± 0.040 | 0.358 ± 0.034 | 0.192 ± 0.217 |
| Al | 0.429 ± 0.541 | 0.340 ± 0.072 | 0.403 ± 0.180 | 0.366 ± 0.111 | 0.690 ± 0.720 |
| Si | 0 | 0 | 0.008 ± 0.020 | 0.018 ± 0.040 | 0 |
| P | 0.084 ± 0.219 | 0.084 ± 0.051 | 0.107± 0.045 | 0.096 ± 0.026 | 0.085 ± 0.069 |
| S | 0.175 ± 0.328 | 0.236 ± 0.030 | 0.2370 ± 0.213 | 0.238 ± 0.058 | 0.385 ± 0.196 |
| Ca | 29.245 ± 9.553 | 26.750 ± 1.265 | 28.765 ± 5.136 | 27.864 ± 3.337 | 28.973 ± 5.117 |
| Cu | 0 | 0.020 ± 0.020 | 0.015 ± 0.023 | 0.008 ± 0.018 | 0 |
| K | 0.015 ± 0.048 | 0 | 0 | 0 | 0 |
| Br | 0 | 0 | 0 | 0 | 0.130 ± 0.162 |

Figure 4 is a graphical representation of the distribution of trace elements summarized in Table 2. We can see clearly the decrease of Mg while the increase of Sulphur. Furthermore, Sulphur as keystone of dyes can be seen in each sample, while nitrogen is eliminated. In the case of BPB, the presence of bromine proves the eggshells’ adsorption ability. Results obtained demonstrate that even in small concentrations (50 mg/L) the elemental composition of the eggshell can change when is used for dye adsorption.

Figure 4. Appearance of trace elements in eggshell before and after adsorption

Bioconcentration factor

Figure 5 shows that BCF decreases with the increase of dye concentration in case of Congo Red while BCF increases in case of MG, clearly demonstrating that eggshell is a promising biosorbent to remove indicators.10 On the other hand, there is no significant change in the presence of BPB and MB.

Figure 5. Bioconcentration factor

Ecotoxicological test

During research the toxicity of each indicator was studied by carrying out seed germination, seedling growth test for salad (lettuce) and mustard seeds. Four different concentrations were used beside the control sample. After 72 h. the length of each seeds’ root was measured and 2x25 measurements’ arithmetic mean was calculated and summarized in tables.

For Congo Red in Table 3 it is obvious that for lettuce seed the inhibition of germination can reach 80%, while for mustard seed negative values were obtained. The growth of the seed roots can be explained by the presence of nitrogen in the dye. Moreover, from the 25 seeds more were germinated in case of mustard than in case of lettuce.

Table 3 shows that the degree of germination is increased by increasing the concentration in case of BPB. The inhibition grows with concentration increase, in high concentrations (1 g/L) for lettuce reaches 100% and for mustard 99.85%.

In case of MB for lettuce seed the inhibition is around 30% for 10 mg/L concentration, the inhibition increases with the increase of dye concentration. For mustard seed, the values are much lower. During experiments the mustard seed became blue and the seeds also discolored.

Both for the mustard and lettuce seed the inhibition was high in case of MG, more than 88% was obtained even at low concentration (10 mg/L) for mustard seed, whereas in case of lettuce seed more seeds germinated. Mustard seeds have become colored and around them (in the inhibition zone) the dye was discolored.

Table 3. Seedling growth test containing root growth inhibition data, as the standard method required results obtained were computed from 2 parallel experiments (Ci= 10-1000 mg/L, T=20oC, t=72h)

| Dye | Congo Red |  | BPB |  | MB |  | MG |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Concentration (mg/L) | Lettuce (%) | Mustard (%) | Lettuce (%) | Mustard (%) | Lettuce (%) | Mustard (%) | Lettuce (%) | Mustard (%) |
| 10 | -35,75 | -5,31 | 24,84 | 45,75 | 30,37 | 20,25 | 88,68 | 63,36 |
| 30 | 68,88 | -25,74 | 43,43 | 69,42 | 49,09 | 10,81 | 93,67 | 83,44 |
| 50 | 82,62 | -21,87 | 54,97 | 78,79 | 79,66 | 17,43 | 97,17 | 83,16 |
| 1000 | 36,83 | 18,28 | 100 | 99,85 | 99,19 | 74,14 | 100 | 97,25 |

Figure 5 shows mustard and lettuce seed sprouts. On the left (Figure 6.a,d) side seeds were in control solution while on the right (Figure 6.b,c) side seeds were placed in 50 mg/L MG solution. It can be seen that the sprouts are healthy and long (lettuce 40 mm, mustard 70 mm), while in the dye solution the seeds were colorful and small (barely 10 mm). It is also noteworthy that the control had at least 20 sprouts out of 25 seeds, while in the dye solution it was much less. These observations apply in each case. All in all, we can conclude that seed germination is dye and plant dependent.

Figure 6. Mustard (a, b) and lettuce (c, d) seeds before (a, d) and after (b, c) seed growth test

Adsorption kinetic models

Experimental data were analyzed using various kinetic models to describe the mechanism of adsorption process of Congo Red, BPB anionic and MB, MG cationic dyes on chicken eggshell household waste. Linearized graphics are only present in case of MB, but the others show similar trends. The pseudo-first-order (Lagergen) plot is shown in Figure 6.a. From the intercept and slope of the straight lines’ plot qe (quantity in equilibrium) and k1 (Lagergen rate constant) was calculated and listed in table 4 for all four indicators.

Pseudo-second-order (Ho&McKay) plot is shown in figure 6. b. an as in case of pseudo-first- order kinetic model qe (quantity in equilibrium) and k2 (equilibrium rate constant) was calculated from strait lines’ intercepts and slopes. Table 4 not only shows the kinetic models’ specific parameters but also the linear regression coefficients. Based on received data in all cases pseudo-second-order kinetic model describes the adsorption process.

Figure 7. Pseudo-first (a) and pseudo-second (b) order kinetic models in case of MB

Table 4. Adsorption kinetics (Ci=10-50 mg/L, 3 g biomass, 160 μm, 700 rpm, T=20±2oC).

| MB |  | Pseudo-first-order |  |  | Pseudo-second-order |  |  | CongoRed |  | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C | qe | k1 | qe | R2 | k2 | qe | R2 | C | qe | k1 | qe | R2 | k2 | qe | R2 |
| (mg/L) | (exp) | (1/t) | (calc) |  | (g/mg×t) | (calc) |  | (mg/L) | (exp) | (1/t) | (calc) |  | (g/mg×t) | (calc) |  |
|  | (mg/g) |  | (mg/g) |  |  | (mg/g) |  |  | (mg/g) |  | (mg/g) |  |  | (mg/g) |  |
| 10 | 0.20 | -0.04 | 0.11 | 0.118 | -5.59 | 0.61 | 0.997 | 10 | 0.33 | -0.06 | 0.36 | 0.604 | 0.71 | 0.99 | 0.996 |
| 20 | 0.44 | -0.03 | 0.09 | 0.159 | 0.42 | 1.91 | 0.999 | 20 | 0.63 | -0.04 | 0.53 | 0.847 | 0.42 | 1.91 | 0.999 |
| 30 | 0.76 | -0.12 | 0.61 | 0.714 | 0.24 | 2.75 | 0.999 | 30 | 0.92 | -0.02 | 0.65 | 0.742 | 0.24 | 2.75 | 0.999 |
| 40 | 0.88 | -0.08 | 0.33 | 0.292 | 0.18 | 3.73 | 0.999 | 40 | 1.24 | -0.03 | 0.91 | 0.844 | 0.18 | 3.73 | 0.999 |
| 50 | 1.07 | -0.07 | 0.29 | 0.144 | 0.12 | 4.67 | 0.999 | 50 | 1.53 | -0.01 | 0.77 | 0.555 | 0.12 | 4.67 | 0.999 |
| MG |  | Pseudo-first-order |  |  | Pseudo-second-order |  |  | BPB |  | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| C | qe | k1 | qe | R2 | k2 | qe | R2 | C | qe | k1 | qe | R2 | k2 | qe | R2 |
| (mg/L) | (exp) | (1/t) | (calc) |  | (g/mg×t) | (calc) |  | (mg/L) | (exp) | (1/t) | (calc) |  | (g/mg×t) | (calc) |  |
|  | (mg/g) |  | (mg/g) |  |  | (mg/g) |  |  | (mg/g) |  | (mg/g) |  |  | (mg/g) |  |
| 10 | 0.39 | 0.03 | 0.05 | 0.022 | -5.92 | 1.07 | 0.999 | 10 | 0.04 | -0.02 | 0.06 | 0.731 | 2.45 | 0.11 | 0.995 |
| 20 | 0.71 | -0.02 | 0.12 | 0.137 | -36.46 | 2.14 | 0.999 | 20 | 0.07 | -0.03 | 0.29 | 0.262 | 0.21 | 0.42 | 0.919 |
| 30 | 1.11 | -0.08 | 0.25 | 0.276 | 8.89 | 3.30 | 0.999 | 30 | 0.09 | -0.07 | 0.55 | 0.935 | 0.25 | 0.68 | 0.991 |
| 40 | 1.48 | -0.03 | 0.28 | 0.050 | -18.53 | 4.31 | 0.999 | 40 | 0.08 | -0.03 | 0.61 | 0.946 | 0.11 | 0.73 | 0.997 |
| 50 | 1.59 | -0.05 | 0.18 | 0.073 | -34.70 | 4.71 | 0.999 | 50 | 0.06 | -0.06 | 0.39 | 0.978 | 0.40 | 0.52 | 0.976 |

Similar results were obtained by Rani et al. where they studied Congo Red biosorption on coconut residual fiber.12 Mudyawabikwa et al. studied MB removal by activated carbon made from tobacco stems.23 They affirm that the study of kinetics of this process is really important “since it is a depiction of adsorbate uptake rate and also controlling parameter to the adsorption process residual time”. Pseudo-second-order kinetic model described the adsorption process in case of MG using nanowires loaded activated carbon as biosorbent and in case of BPB using bentonite carbon composite material.14,24

Adsorption isotherm models

Equilibrium processes can be characterized by adsorption isotherm models. In order to characterize the adsorption process and to determine the amount of adsorption, four different isotherm models (Langmuir, Freundlich, Temkin, Dubinin-Radushkevich) were used for all four dyes’ equilibrium data, obtained after adsorption with eggshell.

Table 5 contains the calculated parameters characteristic to each isotherm model. Due to the fact that B – Temkin constant is less than 20 kJ/mol and E – energy is less than 8 kJ/mol the adsorption is mostly physical in nature.

Table 5. Adsorption isotherm models calculated constants for indicator adsorption onto eggshell surface (Ci=10-100 mg/L, 3 g biomass, 160 μm, 700 rpm, T=20±2oC)

|  | Langmuir |  |  | Freundlich |  |  | Dubinin-Radushkevich |  |  | Temkin |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | KL | qmax | R2 | n | Kf | R2 | β | E | R2 | AT | B | R2 |
|  | (L/mg) | (mg/g) |  |  | (mg(1−1/n)L1/n/g) |  | (mol2 kJ2) | (kJ/mol) |  | (L/g) | (J/mol) |  |
| MB | 0.04 | 0.87 | 0.911 | 0.78 | 36.90 | 0.930 | 9×10-6 | 0.24 | 0.990 | 2.36 | 2×10-5 | 0.989 |
| MG | 0.33 | 2.13 | 0.856 | 2.09 | 1.46 | 0.965 | 3×10-7 | 1.29 | 0.955 | 2.53 | 7×10-5 | 0.961 |
| CongoRed | 3.75 | 1.22 | 0.999 | 2.50 | 1.02 | 0.996 | 4×10-8 | 3.54 | 0.854 | 2.66 | 2×10-6 | 0.917 |
| BPB | 0.59 | 0.04 | 0.827 | 1.02 | 1.23 | 0.811 | 8×10-7 | 2.89 | 0.755 | 2.13 | 2×10-7 | 0.803 |

As shown in Table 5 MB fits the Dubinin-Radushkevich isotherm model more closely, which indicates that chemical adsorption also occurs, ion exchange happens, similar results were obtained using walnut as biosorbent for MB removal.25 In case of MG the liner regression coefficients are very near values but it aligned closer to Freundlich isotherm model, Santhi et al. got Freundlich isotherm as well by studying MG adsorption on prawn waste.26 In case of BPB and Congo Red the adsorption process can be described by Langmuir isotherm model. Similar results to Congo Red : 27,28 and to BPB: 19,29,15.

Conclusions

The present study compared two anionic (Congo Red, Bromphenol Blue) and two cationic (Methylene Blue Malachite Green) dyes’ adsorption properties on eggshell surface. By studying the effect of pH, results demonstrate that anionic dyes adsorb better in acidic while cationic dyes in basic medium. Highest efficiency occurred at pH=2 for Congo Red and BPB (98.71, 67.61%) while for MB and MG in basic medium (75.10, 98.18%). SEM images show that the porous, cross-linked structure of eggshell disappeared after dye adsorption in case of Congo Red, MB, MG. From EDX measurements it is obvious that eggshell is mostly made of CaCO3 and after adsorption process the amount of sulphur, chromium and brome increased in samples. With the help of seed germination test, the different effect of each dye on lettuce and mustard seed growth was investigated, where the phytotoxic test was plant and dye dependent. For all four dyes the adsorption mechanism was best described by pseudo-second-order kinetic model. In case of MB Dubinin-Radushkevich, MB-Freundlich, BPB, Condo Red Langmuir isotherm model fitted better the adsorption data.

References

1 	The United Nations World Water Development Report - Facts and figures. http://unesdoc.unesco.org/images/0024/002475/247553e.pdf

2 	The United Nations World Water Development Report - Executive summary, http://unesdoc.unesco.org/images/0024/002475/247552e.pdf.

3 	M. A. M. Salleh, D. K. Mahmoud, W. A. W. A. Karim, A. Idris, Desalination 2011, 280, 1-13, DOI: 10.1016/j.desal.2011.07.019.

4 	R. Dutta, T. V. Nagarjuna, S. A. Mandavgane, J. D. Ekhe, Ind. Eng. Chem. Res. 2014, 53, 18558-18567, DOI: 10.1021/ie5030003.

5 	R. B. Arfi, S. Karoui, K. Mougin, A. Ghorbal, Euro-Mediterr. J. Environ. Integr. 2017, 2, 20, DOI: 10.1007/s41207-017-0032-y.

6 	M.-S. Chiou, P.-Y. Ho, H.-Y. Li, Dyes Pigments 2004, 60, 69-84, DOI: 10.1016/S0143-7208(03)00140-2.

7	C. Indolean, S. Burcă, A. Măicăneanu, Acta Chim. Slov. 2017, 64, 513-521, DOI: 10.17344/acsi.2017.3271.

8 	W. T. Tsai, J. M. Yang, C. W. Lai, Y. H. Cheng, C. C. Lin, C. W. Yeh, Bioresour. Technol. 2006, 97, 488-493, DOI: 10.1016/j.biortech.2005.02.050.

9 	P. S. Guru, S. Dash, Adv. Colloid Interface Sci. 2014, 209, 49-67, DOI: 10.1016/j.cis.2013.12.013.

10 S. Tonk, C. Majdik, S. Robert, M. Suciu, E. Rápó, B. Nagy, A. Gabriela Niculae, Rev. Chim. -Buchar.- Orig. Ed.- 2017, 68, 1951.

11 How many chickena are there in the United States? How many eggs do they produce? Just the facts here., http://www.ansc.purdue.edu/faen/poultry%20facts.html, accessed November 26, 2017.

12 K. C. Rani, A. Naik, R. S. Chaurasiya, K. S. M. S. Raghavarao, Water Sci. Technol. 2017, 75, 2225-2236, DOI: 10.2166/wst.2017.109.

13 N. F. El-Harby, S. M. A. Ibrahim, N. A. Mohamed, Water Sci. Technol. 2017, 76, 2719-2732, DOI: 10.2166/wst.2017.442.

14 F. El-Dars, H. M Ibrahim, H. A. B. Farag, M. Zakaria Abdelwahhab, M. Shalabi, Int. J. Sci. Eng. Res. 2015.

15 S. Dhananasekaran, R. Palanivel, S. Pappu, J. Adv. Res. 2016, 7, 113-124, DOI: 10.1016/j.jare.2015.03.003.

16 O. Hamdaoui, M. Chiha, Acta Chim. Slov. 2007, 54, 407-418.

17 D. Caparkaya, L. Cavas, Acta Chim. Slov. 2008, 55, 547-553.

18 H. Mei Chen, J. Liu, X. Zhong Cheng, Y. Peng, Adv. Mater. Res. 2012, 573–574, 63-67, DOI: 10.4028/www.scientific.net/AMR.573-574.63.

19 Y. Zeroual, B. S. Kim, C. S. Kim, M. Blaghen, K. M. Lee, Water. Air. Soil Pollut. 2006, 177, 135-146, DOI: 10.1007/s11270-006-9112-3.

20 M. J. Iqbal, M. N. Ashiq, J. Chem. Soc. Pak. 2010, 32, 419-428.

21 M. A. Zulfikar, H. Setiyanto, ‘Study of the adsorption kinetics and thermodynamic for the removal of Congo Red from aqueous solution using powdered eggshell’, 2013.

22 D. P. Tiwari, S. K. Singh, N. Sharma, Appl. Water Sci. 2015, 5, 81-88, DOI: 10.1007/s13201-014-0171-0.

23 B. Mudyawabikwa, H. H. Mungondori, L. Tichagwa, D. M. Katwire, Water Sci. Technol. 2017, 75, 2390-2402, DOI: 10.2166/wst.2017.041.

24 M. Ghaedi, E. Shojaeipour, A. M. Ghaedi, R. Sahraei, Spectrochim. Acta. A. Mol. Biomol. Spectrosc. 2015, 142, 135-149, DOI: 10.1016/j.saa.2015.01.086.

25 Removal of Methylene Blue from Aqueous Solution Using Agricultural Residue Walnut Shell: Equilibrium, Kinetic, and Thermodynamic Studies, https://www.hindawi.com/journals/jchem/2017/8404965/, accessed October 13, 2017.

26 D. T. S. Dr.T.Santhi, S. Manonmani, T. Smitha, K. Mahalakshmi, Rasayan J. Chem. 2009, 2, 813-824.

27 P. D. Saha, S. Chowdhury, M. Mondal, K. Sinha, Sep. Sci. Technol. 2011.

28 J. Liu, X. Z. Cheng, P. Qin, M. Y. Pan, Adv. Mater. Res. 2012, 599, 391-399, DOI: 10.4028/www.scientific.net/AMR.599.391.

29 A. A. El-Zahhar, N. S. Awwad, E. E. El-Katori, J. Mol. Liq. 2014, 199, 454-461, DOI: 10.1016/j.molliq.2014.07.034.