Figure Legends
Fig. 1   Cross linking condensation reaction of polyvinyl alcohol with borax
Fig. 2 FTIR spectra of PVA-PES composite membrane specimens cross linked with 0.2% and 0.5%    borax as cross-linking agent   used in the present study
Fig. 3 TGA thermograms of PVA-PES composite membrane specimens cross linked with 0.2% and 0.5% borax as cross-linking agent used in the present study 
Fig. 4. Differencial Scanning Calorimetry thermograms of the prepared composite membranes used in the present study
Fig. 5. Wide angle X ray diffraction pattern of the borax cross-linked PVA-PES composites membranes used in the present study with two different borax concentrations viz 0.2% and 0.5%
Fig. 6. Scanning electron micrographs of the top surface and cross sections of the uncrosslinked PVA-PES composite, and PVA-PES composite membrane specimens doped with 0.2% and 0.5% of borax crosslink  (a: uncrosslinked PVA –PES top surface, magnification: 3500; b: uncrosslinked PVA-PES cross section, magnification: 250; c: PVA-PES-0.2% borax top surface, magnification: 2500; d:PVA-PES-0.2% borax cross section, magnification 250; e: PVA-PES-0.5% borax top surface, magnification: 2500; f: PVA-PES-0.5% borax cross section, magnification: 350)
Fig. 7. AFM images of the uncrosslinked and cross linked PVA-PES membranes used in the present study (a: PVA-PES uncrosslinked; b: PVA-PES-0.2% borax; c: PVA-PES-0.5% borax)
Fig. 8. Percentage degree of swelling as a function of feed water concentration at a constant temeprature
Fig. 9   Total pervaporation flux and separation factor as a function of feed flow rate in the pervaporation of EG-water system (Temperature: 45 oC, Feed concentration: 80% Ethylene glycol by volume)
Fig. 10. Water and ethylene glycol diffusion coefficient as a function of feed flow rate in the pervaporation of EG-water mixture (Temperature: 45 oC, Feed concentration: 80% Ethylene glycol by volume)
Fig.11 Water and ethylene glycol permeability as a function of feed temperature

[image: image21.png]Heat Flow (mW)
o

—> (PVA-PES)

(PVA-PES, 0.2% Borax)

(PVA-PES, 0.5% Borax)

Temperature (°C}

250 300

[} 5 10 15 20 25
Time (Min})

30

35

45




Fig. 1 
[image: image2.png]100

Transmittance (%)

(PVA-PES, 0.2% Borax)

(PVA-PES, 0.5% Borax)

4000.0

3600 3200 2800 2400 2000 1800 1600 1400

‘Wave Number (cm™)




Fig. 2
[image: image3.png]Weight (%)

(PVA-PES)

(PVA-PES, 0.2% Borax)

(PVA-PES, 0.5% Borax) <

30 100 200 300 400 500 600
Temperature (°C)




Fig. 3 

[image: image1.emf]
Fig. 4

[image: image20.png]Intensity (Arbitrary)

(PVA-PES, 0.5% Borax)

(PVA-PES, 0.2% Borax)

Position (20)







Fig. 5. 

	[image: image4.png]ﬁ dwel | WV [mode | det | meg ] |spot| WD | 6901 | —30ym -
& 45ps | 5.00KkV | None | LVD [ 3500x |35 | 5.6mm | 11:30:35AM PVA  SICART






	[image: image5.jpg]dwell
3 s

HV
20.00 kV

mag

250 x

det
LVD

spot
5.0

WD
10.5 mm

7/16/2016
11:49:31 AM

T e —

(PVA)O






	[image: image6.jpg]PVA/2% B






	[image: image7.jpg]%

dwell

1yus

HV
5.00 kv

mode
SE

det
ETD

mag

250 x

spot WD
3.5 | 6.0 mm

6/9/2017
11:51:20 AM

T e —

PVA/2% BORAX






	[image: image8.jpg]mag [ | spo /2017
2500x% |3 11:20:55 AM PVA/4% B




	[image: image9.jpg]6/9/2017
11:55:44 AM

PVA/4% BORAX







Fig. 6 
	[image: image10.jpg]2 Axis, nm
00

150

%





	[image: image11.jpg]3.1 1FHeight

350

00

250

200

150

100






	[image: image12.jpg]g
S
2
<
N

(=]
(<]
(]





	[image: image13.jpg]Y Axis,um

3.1 1FHeight

3.0

2.0

2.0 3.0
X Axis,um

4.0

5.0

200

100

50

Z Axis,nm





	[image: image14.jpg]Z Axis, nm
120
9

Y Axis, um
5.0

5.0 ¢o

X Axis, um




	[image: image15.jpg]Y Axis,um

4.1 1FHeight

4.0

3.0

2.0

1.0

by

[1]
°p

1.0

. LY
2.0 3.0 4.0
X Axis,um

5.0

150

100

50

Z Axis,nm






Fig. 7
[image: image16.png]100

< (PVA-PES, 0.2% Borax)
80 A (PVA-PES, 0.5% Borax)
O(PVA-PES, Uncrosslinked)
o0
Z
= 60
H
s
g 3
g w0
R
20
2z
0 T T T T
0 20 40 60 80 100

Feed water concentration (vol %)




Fig. 8. 
[image: image17.png]Total flux, m3(STP)/m?2h

15

12

(PVA-PES, 0.2% Borax, Total flux)
(PVA-PES, 0.5% Borax, Total flux)
(PVA-PES, Uncrosslinked, Total flux)
(PVA-PES, 0.2% Borax, Sep.Factor)
(PVA-PES, 0.5% Borax, Sep.Factor)
(PVA-PES, Uncrosslinked, Sep.Factor)

0.01

0.02

0.03 0.04 0.05 0.06

Feed flowrate (m3/h)

0.07

Separation Factor




Fig. 9
[image: image18.png]Water Diffusion Coefficient (D, x 10 19), m?/s

2.5

15

0.5

PVA-PES, 0.2% Borax, Water Diff. Coefficient)
PVA-PES, 0.5% Borax, Water Diff. Coefficient)
PVA-PES, Uncrosslinked, Water Diff. Coefficient)
PVA-PES, 0.2% Borax, EG Diff. Coefficient)
PVA-PES, 0.5% Borax, EG Diff. Coefficient)
PVA-PES, Uncrosslinked, EG Diff. Coefficient)

0.01 0.02 0.03 0.04 0.05 0.06

Feed flowrate (m3/h)

2.5

15

0.5

EG Diffusion Coefficient (D¢ x 10 19), m%/s




Fig.10. 
[image: image19.png]Water Permeability (Barrer)

20

16

12

(PVA-PES, 0.2% Borax, Water Permeability)
(PVA-PES, 0.5% Borax, Water Permeability)
(PVA-PES, Uncrosslinked, Water Permeability)
(PVA-PES, 0.2% Borax, EG Permeability)
(PVA-PES, 0.5% Borax, EG Permeability)
(PVA-PES, Uncrosslinked EG Permeability)

25 35 45 55 65

Feed temperature (°C)

75

20

16

12

EG Permeability (Barrer)




Fig.11
a





b





e





c





d





f





a





b





c








2

