Supplementary materials

Adsorptive removal of fluoride from the water by iron permeated activated carbon derived from the Citrus limetta pulp waste

Mohd. Ibrahim1, Adil Siddique1, Jiwan Singh1*, D.P. Singh1, Janardhan Reddy Koduru2**

1Department of Environmental Science, Babasaheb Bhimrao Ambedkar University, Lucknow-226025, India

2Department of Environmental Engineering, Kwangwoon University, Seoul 139-701, Republic of Korea

# *Corresponding Author-email (J. Singh)-jiwansingh95@gmail.com

**Corresponding author. E-mail: reddyjchem@gmail.com (J. R. Kuduru); Tel: 82-2-940-5496

Fig. S1 Effect of various parameters (a) contact time, (b) different pH (c) biosorbent dose of ACP- 250 (d) ACP-500 for the removal of fluoride.

Fig. S2 (a, b) Intraparticle diffusion model, (c, d) adsorption thermodynamics of ACP-250 and ACP-500

Table S1: Quantitative elements distribution in weight percentage determined from EDX Analysis of ACP-250 and ACP-500

| Elements | Weight percentage |  |
| --- | --- | --- |
|  | ACP-250 (%) | ACP-500 (%) |
| Carbon(C) | 50.27 | 57.98 |
| Oxygen(O) | 6.78 | 29.63 |
| Chlorine (Cl) | 27.49 | 4.14 |
| Iron (Fe) | 9.94 | 4.46 |
| Calcium(Ca) | 0.98 | 0.35 |
| Bismuth(Bi) | -0.46 | - |
| Zirconium (Zr) | 4.99 | - |
| Magnesium(Mg) | - | 0.76 |
| Silicon (Si) | - | 2.68 |
| Total | 100.00 | 100.00 |

Table S2: Thermodynamics parameters of removal of fluoride by ACP-250 and ACP-500

| Adsorbent | Temperatures (K) | ΔGO(KJ mol-1) | ΔHO(KJ mol-1) | ΔSO(J mol-1K-1) |
| --- | --- | --- | --- | --- |
| ACP-250 |  |  |  |  |
|  | 289 | 0.298 | 29.6 | -102.0 |
|  | 308 | 2.547 |  |  |
|  | 318 | 3.048 |  |  |
|  | 328 | 3.442 |  |  |
| ACP-500 |  |  |  |  |
|  | 289 | -2.099 | 46.7 | -150.0 |
|  | 308 | -0.462 |  |  |
|  | 318 | 1.238 |  |  |
|  | 328 | 2.311 |  |  |

Table S3 Cost comparison of biosorbent for the fluoride adsorption

| Adsorbent | Cost (US $/kg) | References |
| --- | --- | --- |
| Activated alumina | ῀1.5 | [1] |
| Activated alumina | ῀2.3 | [2] |
| Amorphous alumina | ῀70 | [2] |
| Activated carbon | ῀25 | [2] |
| Hydrous bismuth oxide | ῀59 | [3] |
| ACP | ῀12.58 | Present study |

- Maliyekkal SM, Sharma AK, Philip L. Manganese-oxide-coated alumina: a promising sorbent for defluoridation of water. Water Res. 2006;40:3497–3506.

- Rubel JF, Shupe JF, Leone HP, Leone NC (Eds.). The Removal of Excess Fluoride from Drinking Water by the Activated Alumina Method, Paragon Press, Salt Lake City. 1983;345.

- Srivastav AL, Singh PK, Srivastava V, Sharma YC. Application of a new adsorbent for fluoride removal from aqueous solutions. J. Hazard. Mater. 2013;263:342– 352.