Table 1 Comparison of rate constant (k) for the catalyzed and uncatalyzed degradation of Rh6G

and MO.

| Rate constant (catalysis)(min-1) | Rate constant (uncatalysis)(min-1) | Dye | Entry |
| --- | --- | --- | --- |
| 0.126 | 0.049 | Rhodamine 6G | 1 |
| 0.222 | 0.014 | Methyl Orange | 2 |

Table 2 Optimization of degradation conditions for Rh6G at room temperature.

| Rate constant (min-1) | NaBH4 (mg L-1) | Ag/HNT (g l-1) | Entry |
| --- | --- | --- | --- |
| 0.010 | 4 | 0.0002 | 1 |
| 0.083 | 4 | 0.0005 | 2 |
| 0.126 | 4 | 0.0010 | 3 |
| 0.234 | 4 | 0.0250 | 4 |
| 0.014 | 1.5 | 0.0250 | 5 |
| 0.083 | 4 | 0.0250 | 6 |
| 0.207 | 8 | 0.0250 | 7 |
| 0.184 | 16 | 0.0250 | 8 |

Table 3 Optimization of degradation conditions for MO at room temperature.

| Rate constant (min-1) | NaBH4 (mg L-1) | Ag/HNT (g l-1) | Entry |
| --- | --- | --- | --- |
| 0.085 | 4 | 0.0002 | 1 |
| 0.188 | 4 | 0.0005 | 2 |
| 0.222 | 4 | 0.0010 | 3 |
| 0.229 | 4 | 0.0250 | 4 |
| 0.061 | 1.5 | 0.0250 | 5 |
| 0.221 | 4 | 0.0250 | 6 |
| 0.236 | 8 | 0.0250 | 7 |
| 0.330 | 16 | 0.0250 | 8 |

Table 4 Rate constant (k) for the reduction of Rh5G and MO involving various nanocatalysts.

| Refs | Time (min) | Rate constant (min-1) | NaBH4 (µmol) |  | Dye (µmol) |  | Catalyst (mg L-1) | Entry |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 25 | 1.5 | 0.33 | 7 |  | Rh6G 0.18 |  | silver-nanoshells 0.001 | 1 |
| 59 | 35 | 0.09 | 0.27 |  | MO 2.40 |  | Ag/tannic acid 0.004 | 2 |
| 60 | 15 | 0.19 | 30 |  | MO 0.20 |  | AgNPs 0.0001 | 3 |
| 61 | 8 | 0.30 | 550 |  | MO 0.76 |  | Ag/ZeoliteX 0.060 | 4 |
| This work | 30 | 0.21 | 10 |  | Rh6G 0.02 |  | Ag/HNT 0.025 | 5 |
| This work | 30 | 0.222 | 10 |  | MO 0.03 |  | Ag/HNT 0.025 | 6 |