Synthesis, Characterization and DFT Studies of Two New π-conjugated Pyridine-based Tetrathiafulvalene Derivatives
Zhi-Gang Niu,1 Li-Rong He,1 Lin Li,1 Wen-Feng Cheng,1 Xiao-Yan Li,1 Hao-Hua Chen1 and Gao-Nan Li1,2,*
1 College of Chemistry and Chemical Engineering, Hainan Normal University, Haikou 571158, China

2 State Key Laboratory of Coordination Chemistry, School of Chemistry and Chemical Engineering, Nanjing University, Nanjing 210093, China
Supporting materials
Table S1 Crystallographic data and structure refinement details for compound 2a.
	Empirical formula
	C21H15NS8

	Mr
	537.90

	Crystal system
	Triclinic

	Space group
	P
[image: image1.wmf]1



	a (Å)
	8.813(3)

	b (Å)
	11.082(3)

	c (Å)
	12.620(4)

	( (°)
	88.805(5)

	( (°)
	80.440(5)

	( (°)
	75.680(5)

	V (Å3)
	1177.3(6)

	Z
	2

	Dcalcd (Mg/m3)
	1.517

	F(000)
	552

	T / K
	293(2)

	((Mo-K()/ mm(1
	0.769

	index ranges
	(10 ≤ h ≤ 9

	
	(13 ≤ k ≤ 11

	
	(14 ≤ l ≤ 14

	Reflections collected
	5872

	Independent reflections
	4051

	Rint
	0.0296

	Absorption correction
	multi-scan

	Data/restraints/parameters
	4051 / 79 / 290

	GOF (F2)
	1.017 

	R1a, wR2b (I >2((I))
	0.0484, 0.1176

	R1a, wR2b (all data)
	0.0622, 0.1245

	Largest diff. peak/hole / e Å(3
	0.356/(0.258


a R1 = (((Fo( ( (Fc((/(|Fo(. b wR2 = [(w(Fo2 ( Fc2)2/(w(Fo2)]1/2
Table S2 Selected bond lengths (Å) and bond angles (◦) for compound 2a.

	
	X(ray
	Calculated

	Bond length (Å)

	S(1)-C(8)
	1.742(3)
	1.8171

	S(1)-C(15)
	1.779(3)
	1.8790

	S(2)-C(7)
	1.734(3)
	1.8211

	S(2)-C(9)
	1.782(3)
	1.8840

	S(3)-C(6)
	1.752(3)
	1.8479

	S(3)-C(7)
	1.750(3)
	1.8383

	S(4)-C(6)
	1.760(3)
	1.8486

	S(4)-C(8)
	1.759(3)
	1.8388

	S(5)-C(4)
	1.761(3)
	1.8532

	S(5)-C(5)
	1.739(3)
	1.8399

	S(6)-C(3)
	1.763(3)
	1.8529

	S(6)-C(5)
	1.749(3)
	1.8399

	S(7)-C(1)
	1.693(8)
	1.9068

	S(7)-C(4)
	1.801(8)
	1.8205

	S(8)-C(2)
	1.790(4)
	1.9068

	S(8)-C(3)
	1.737(3)
	1.8205

	C(3)-C(4)
	1.342(5)
	1.3391

	C(5)-C(6)
	1.337(4)
	1.3330

	C(7)-C(8)
	1.329(5)
	1.3318

	C(9)-C(15)
	1.343(4)
	1.3416

	N(1)-C(11)
	1.367(7)
	1.3473

	C(10)-N(1)
	1.319(4)
	1.3564

	C(16)-C(17)
	1.383(4)
	1.4065

	C(17)-C(18)
	1.359(5)
	1.3949

	Bond angle (◦)

	C(8)-S(1)-C(15)
	100.85(15)
	99.431

	C(7)-S(2)-C(9)
	99.48(15)
	97.628

	C(7)-S(3)-C(6)
	93.55(16)
	93.095

	C(8)-S(4)-C(6)
	92.62(15)
	92.867

	C(5)-S(5)-C(4)
	93.95(15)
	94.163

	C(5)-S(6)-C(3)
	93.96(15)
	94.162

	S(5)-C(5)-S(6)
	113.51(17)
	111.734

	S(3)-C(6)-S(4)
	113.33(18)
	112.625

	C(10)-N(1)-C(11)
	116.3(5)
	118.823

	N(1)-C(10)-C(14)
	122.0(4)
	121.767

	C(11)-C(12)-C(13)
	119.0(6)
	118.413

	C(17)-C(16)-C(21)
	118.9(3)
	118.900

	C(18)-C(17)-C(16)
	120.7(3)
	120.432

	C(18)-C(19)-C(20)
	119.6(4)
	119.754


_1437813665.unknown

