Two trans-dicyanidechromium(III)-containing building blocks and one chiral copper(II) compound have been employed to assemble cyanide-bridged heterometallic complexes, resulting in three chiral cyanide-bridged Cr(III)–Cu(II) complexes, {[Cu(S,S/R,R-Chxn)2Cr(bpb)(CN)2]ClO4}2·CH3OH·H2O(1,2), {[Cu(R/R-Chxn)2Cr(bpClb)(CN)2][Cr(bpClb)(CN)2]}·CH3OH·2H2O (3). All the three complexes have been characterized by elemental analysis, IR spectroscopy and X-ray structure determination. Single X-ray diffraction analysis shows that the complexes 1-3 belong to cyanide-bridged cationic binuclear structure type with ClO4- or the anionic cyanide building block as balance anion for complexes 1,2 or 3, respectively. Investigation of the magnetic properties of complexes 1-3 reveals the weak ferromagnetic coupling between the neighboring Cr(III) and Cu(II) ions through the bridging cyanide group.
[image: image1.png]



[image: image2.png]Jour _.:Eo\_.Ex

490

o
o
T

430

2.74

1.8+

T
o
(=}
low o/ W

M

0.0

300

200

100

T/K




