SUPPLEMENTARY MATERIAL TO

Adsorption of Cr (III) and Cd (II) ions using mesoporous cobalt-ferrite nanocomposite from synthetic wastewater

Iman Khoshkerdar1 and Hossein Esmaeili*2

1 Department of Chemical Engineering, Dashtestan Branch, Islamic Azad University, Dashtestan, Iran

2Department of Chemical Engineering, Bushehr Branch, Islamic Azad University, Bushehr, Iran

Table S-1: BET analysis of CFNC

| Specifications | units | value |
| --- | --- | --- |
| Special surface of the adsorbent | /g2m | 17.8358 |
| Apertures surface area | /g2m | 24.144 |
| Average volume of pores | /g3 cm | 11.117 |
| Average diameter of pores | nm | 7.5315 |
| Pores radius | nm | 1.21 |

Table S-2: Effect of buffer types on adsorption of Cr (III) and Cd (II) ions using CFNC from aqueous solutions.

| Cr (III) adsorption efficiency | Cd (II) adsorption efficiency | Types of buffer |
| --- | --- | --- |
| 80 | 75.5 | citrate )Citric acid( |
| 60.7 | 60.3 | phosphate |
| 96.4 | 95 | maleic acid |
| 87.4 | 88.9 | phthalate hydrogen potassium |

Table S-3: Effect of electrolyte types on adsorption of Cr (III) and Cd (II) ions using CFNC from aqueous solutions.

| Cr (III) adsorption efficiency | Cd (II) adsorption efficiency | Type of electrolyte |
| --- | --- | --- |
| 93 | 94 | NaNO3 |
| 95 | 95.6 | KCl |
| 97.4 | 100 | NaCl |
| 91 | 96 | CaCl2 |

Isotherms study

In this study, Langmuir and Freundlich isotherm models are used to explain adsorption process of chromium (III) and cadmium (II) ions using CFNC.

Langmuir isotherm model states that adsorption of metal ions occurs on a single and homogeneous layer of adsorbent without any interaction between adjoining sites. This model expresses the information about the adsorption capacity as well as the equilibrium behavior of the adsorption process.1-2 The linear form of Langmuir equation is like below:

(S-1)

Where Ce, qe, qmax and KL are equilibrium concentration of metal ion in solution (mg/L), equilibrium adsorption capacity (mg/g), maximum adsorption capacity (mg/g) and Langmuir constant or adsorption energy (L/g), respectively. Moreover, a constant parameter namely separation factor (RL) is defined as equation S-2:

(S-2)              Ceqe=Ceqmax+1kLqmax

In this equation, Ci is initial concentration of metals ion (mg/g). If RL>1, RL=0, RL=1 and 0<RL<1, the process is categorized as undesirable, irreversible, linear and desirable, respectively.1

Another adsorption model is Freundlich isotherm model. This model is applied to describe multi-layer adsorption on heterogeneous surfaces. The linear form of this model is as follows:

(S-3)

KF is a constant depending on adsorption capacity and n is an empirical parameter related to adsorption intensity.2 In Freundlich isotherm, for n>1, adsorption process is undesirable and in condition 1<n<10, adsorption process is desirable.3 Fig. S-1 (a) and (b) is drawn to Langmuir isotherm to remove cadmium (II) and chromium (III) ion sequentially. Also, in Fig. S-2 (a) and (b) linear equations are shown to remove cadmium (II) and chromium (III) ion with CFNC with Freundlich isotherm model.

Fig. S-1: Langmuir linear isotherm plots related to the adsorptions of a) cadmium (II), b) chromium (III) using CFNC from aqueous solutions.

Fig. S-2: Freundlich linear isotherm plots related to the adsorptions of a) cadmium (II), b) chromium (III) using CFNC  from aqueous solutions.

Kinetic study

Kinetic studies of adsorption processes show the interactions between metal ions in aqueous solution and the adsorbent. In this study, in order to explain adsorbent kinetic behavior, pseudo first-order and pseudo second-order kinetic models were applied.1-2

The linear form of pseudo first-order and pseudo second-order kinetic models are presented using equations S-4 and S-5, respectively.

(S-4)

(S-5)

Where, qt (mg/g), K1 (1/min) and K2 (g/mg.min ) are the value of cadmium (II) and chromium (III) ion at time t, adsorption constant of pseudo first-order kinetics and pseudo second-order, sequentially.1-2, 4 Fig. S-3 shows the effect of time (t) against log(qe-qt) for pseudo first-order kinetic model. Also, the effect of time (t) against t/qt for the pseudo second-order kinetic model is shown in Fig. S-4. Additionally, constants and parameters of pseudo first-order and pseudo second-order kinetic models for adsorption of cadmium (II) and chromium (III) ions using CFNC are tabulated in Tables S-4 and S-5.

Fig. S-3: pseudo-first and pseudo- second order model plots related to the adsorptions of  cadmium (II) using CFNC  from aqueous solutions.

Fig. S-4: pseudo-first order synthetic and pseudo- second order model plots related to the adsorptions of  chromium (III) using CFNC  from aqueous solutions.

Table S-4: Pseudo-first and pseudo- second order synthetic model constants cadmium (II).

| mg/L 75 | mg/L 60 | mg/L 40 | 20 mg/L | parameters | Models |
| --- | --- | --- | --- | --- | --- |
| 11.86 | 11.85 | 8.35 | 12.4 | qcal | Pseudo firest-oreder kinetic |
| 229.55 | 219.55 | 177.05 | 84.55 | qexp |  |
| 0.9885 | 0.9786 | 0.9798 | 0.9781 | 2 R |  |
| 0.035 | 0.042 | 0.048 | 0.15 | 1k |  |
| 0.41 | 0.49 | 0.4 | 1.86 | 1h |  |
| 0.43 | 0.43 | 0.52 | 0.728 | qcal | Pseudo second-order kinetic |
| 229.55 | 219.55 | 177.05 | 84.55 | qexp |  |
| 0.4207 | 0.7647 | 0.7168 | 0.2633 | 2 R |  |
| 3-10*1 | 3-10*1 | 4-10*2 | 4-10*1 | 2k |  |
| 2.077 | 3.086 | 10.33 | 3.086 | 2h |  |

Table S-5: Pseudo-first and pseudo- second order synthetic model constants chromium (III).

| mg/L 60 | mg/L 40 | mg/L 20 | parameters | models |
| --- | --- | --- | --- | --- |
| 12.206 | 13.70 | 8.49 | qcal | pseudo-first order model |
| 249.55 | 179.55 | 95 | qexp |  |
| 0.9712 | 0.8538 | 0.9798 | 2 R |  |
| 0.035 | 0.084 | 0.063 | 1k |  |
| 0.427 | 1.15 | 0.534 | 1h |  |
| 99.009 | 357.14 | 169.49 | qcal | pseudo- second order model |
| 249.55 | 179.55 | 95 | qexp |  |
| 0.3982 | 0.8344 | 0.1802 | 2 R |  |
| 3-10*2 | 4-10*62 | 4-10*6 | 2k |  |
| 19.6 | 7.90 | 1.72 | 2h |  |

Thermodynamic studies

To calculate the changes of Gibbs free energy ∆G°, entropy ΔSo and enthalpy ΔHo, equations S-6 and S-7 were used:5

(S-6)                     
                                         (S-7)

Where: R, T(K) and Kd (qe/ce) are gas universal constant, temperature and distribution coefficient, respectively. Constants and thermodynamic parameters are presented in Table S-6.

Table S-6: Thermodynamic properties for cadmium (II) and chromium (III) adsorption

| ∆S (J/mol.K) | ∆H (kJ/mol) |  | ∆G (kj/mol) | KC | Temperature/K | heavy metal ion |
| --- | --- | --- | --- | --- | --- | --- |
| 147.85 | 39.37 | -1.82 |  | 2.25 | 278 | cadmium (II) |
|  |  | -3.23 |  | 3.86 | 288 |  |
|  |  | -4.31 |  | 5.92 | 293 |  |
|  |  | -5.73 |  | 10.17 | 298 |  |
| 133.91 | 34.36 | -2.86 |  | 2.25 | 278 | chromium (III) |
|  |  | -4.2 |  | 3.86 | 288 |  |
|  |  | -4.87 |  | 5.92 | 293 |  |
|  |  | -5.54 |  | 10.17 | 298 |  |

References

1. F. S. Sarvestani, H. Esmaeili, B. Ramavandi. 3 Biotech. 2016, 6, 251. DOI: 10.1007/s13205-016-0570-z.

2. R. Foroutan, H. Esmaeili, S. M. D. Rishehri, F. Sadeghzadeh, S. R. Mirahmadi, M. Kosarifard, B. Ramavandi. Data Brief. 2017, 12, 485-492. DOI: 10.1016/j.dib.2017.04.031.

3. P. Bartczak, M. Norman, Ł. Klapiszewski, N. Karwańska, M. Kawalec, M. Baczyńska, T. Jesionowski. Arab. J. Chem. 2015. DOI: 10.1016/j.arabjc.2015.07.018.

4. B. S. Zadeh, H. Esmaeili, R. Foroutan, Indones. J. Chem. 2018, 18, 265-271. DOI: 10.22146/ijc.28789.

5. A. Teimouri, H. Esmaeili, R. Foroutan, B. Ramavandi. Korean J. Chem. Eng. 2018, 35, 479-488. DOI: 10.1007/s11814-017-0311-y.

*Corresponding Author: E-mail Address: esmaeili.hossein@gmail.com & esmaeili.hossein@iaubushehr.ac.ir