Supplementary Materials for “Adsorption Mechanism of Congo Red on Mg–Al-layered Double Hydroxide Nanocompound”

Tables:

Table S1- Relative magnitude of region I and sections IIA and IIB for adsorption of CR on Mg-Al-LDH nanocompound in water, 0.1 M NaCl and alkaline solutions at 308–328 K.

| Solvent | T (K) | Region I | Section IIA | Section IIB |
| --- | --- | --- | --- | --- |
|  |  | (MP site) |  | (003 site) |
| Water | 308 | 0.20 | 0.19 | 0.61 |
|  | 318 | 0.21 | 0.28 | 0.51 |
|  | 328 | 0.34 | 0.36 | 0.30 |
| 0.1 M NaCl | 318 | 0.14 | 0.18 | 0.68 |
| pH=10 | 318 | 0.09 | 0.22 | 0.69 |
| pH=11 | 318 | 0.09 | 0.37 | 0.53 |
| pH=12 | 318 | 0.11 | 0.32 | 0.57 |
| pH=13 | 318 | 0.14 | 0.58 | 0.29 |

Table S2- Experimental , ,,, and  values and coefficients of the KASRA equation for kinetics of CR adsorption on

Mg-Al-LDH nanocompound at different temperatures and in various shaking rates and initial CR concentrations (Complete data).

| Solvent | T |  | rpm |  |  |  |  | KASRA region 1 (1st curve) |  |  |  |  |  |  | KASRA region 2 (1st curve) |  |  |  |  |  | KASRA region 2 (3rd curve) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to thermodynamic |  |  |  |  |  |  | ARIAN region I (MP Site) |  |  |  |  |  |  |  | ARIAN section IIA (MP Site) |  |  |  |  |  |  |  |  |  |  |
| Water | 318 | 0.01 | 100 |  | (150,13.9) |  |  |  |  | –0.45 |  | 1.93 |  | (5,4.1) |  | –8.0×10-4 |  |  | 0.12 |  | – | – |  |  | – |
|  |  |  |  | KASRA region 1 (1st curve) |  |  |  |  |  |  |  |  |  |  | KASRA region 2 (2nd curve) |  |  |  |  |  | KASRA region 2 (3rd curve) |  |  |  |  |
| Corresponding to thermodynamic |  |  |  | ARIAN region I and section IIA(MP Site) |  |  |  |  |  |  |  |  |  |  | ARIAN section IIB (003 Site) |  |  |  |  |  | ARIAN section IIB (003 Site) |  |  |  |  |
| Water | 308 | 0.06 | 100 |  | (180,48.0) |  |  |  |  | –3.54 |  | 6.44 |  | (20,10.3) |  | –2.5×10-3 |  |  | 0.43 |  | – | – |  |  | – |
|  | 318 | 0.06 | 100 |  | (150,49.2) |  |  |  |  | –5.70 |  | 16.62 |  | (20,27.7) |  | –0.002 |  |  | 0.30 |  | – | – |  |  | – |
|  | 318 | 0.09 | 100 |  | (150,74.2) |  |  |  |  | –20.40 |  | 35.30 |  | (5,30.5) |  | –0.003 |  |  | 0.51 |  | – | – |  |  | – |
|  | 318 | 0.06 | 70 |  | (180,57.0) |  |  |  |  | –3.52 |  | 11.29 |  | (5,19.8) |  | –0.002 |  |  | 0.40 |  | – | – |  |  | – |
|  | 318* | 0.06 | 30 |  | (180,54.4) |  |  |  |  | –1.52 |  | 10.84 |  | (5,14.4) |  | –0.002 |  |  | 0.40 |  | – | – |  |  | – |
|  | 328 | 0.06 | 100 |  | (30,54.3) |  |  |  |  | –14.66 |  | 33.00 |  | (3,37.7) |  | –0.05 |  |  | 1.21 |  | – | – |  |  | – |
| 0.1M NaCl | 318 | 0.06 | 100 |  | (210,60.1) |  |  |  |  | –11.69 |  | 14.52 |  | (3,9.9) |  | –0.008 |  |  | 0.71 |  | (120,43.2) | –5.4×10-4 |  |  | 0.22 |
| pH=10 | 318 | 0.06 | 100 |  | (180,41.5) |  |  |  |  | –29.94 |  | 19.36 |  | (5,6.9) |  | –0.034 |  |  | 0.80 |  | (50,16.1) | –0.004 |  |  | 0.44 |
| pH=12* | 318 | 0.06 | 100 |  | (120,30) |  |  |  |  | –0.25 |  | 2.53 |  | (40,15.4) |  | –0.002 |  |  | 0.25 |  | – | – |  |  | – |
| pH=13* | 318 | 0.06 | 100 |  | (240,26) |  |  |  |  | –0.06 |  | 0.87 |  | (50,7.5) |  | –3×10-4 |  |  | 0.13 |  | – | – |  |  | – |

Units of,and are in mg g-1 min-2 and those of , and  are in mg g-1 min-1. Units of , and are in min and those of ,and are in mg g-1. In region 1,  and  are equal to zero. Except for 0.01 mM of CR, there is a TRAK between each two successive kinetic curves (Table 4). *There is a TD (time delay) before the first curve (Table 4).

Table S3- Coefficients of the intraparticle diffusion equation for kinetics of CR adsorption on Mg-Al-LDH nanocompound at different temperatures and in various shaking rates and initial CR concentrations (Complete data).

| Solvent | T |  |  | rpm |  |  | KASRA region 1 (1st curve) |  |  |  | KASRA region 2 (1st curve) |  |  |  |  |  | KASRA region 2 (3rd curve) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) | (mM) |  |  |  |  | TD |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to thermodynamic |  |  |  |  |  | ARIAN region I (MP Site) |  |  |  |  |  | ARIAN section IIA (MP Site) |  |  |  |  |  |  |  |  |  |  |
| Water | 318 | 0.01 |  |  |  | 100 | – | 1.85 | 0.11 |  |  |  |  | (5,4.1) | 1.00 | 2.0 |  | – |  |  | – | – |
|  |  |  |  |  | KASRA region 1 (1st curve) |  |  |  |  |  |  |  | KASRA region 2 (2nd curve) |  |  |  |  |  | KASRA region 2 (3rd curve) |  |  |  |
| Corresponding to thermodynamic |  |  |  |  | ARIAN region I and section IIA (MP Site) |  |  |  |  |  |  |  | ARIAN section IIB (003 Site) |  |  |  |  |  | ARIAN section IIB (003 Site) |  |  |  |
| Water | 308 |  | 0.06 |  |  | 100 | – | 4.36 | –0.27 |  | (20,10.3) |  |  |  | 4.25 | –6.4 | – |  |  |  | – | – |
|  | 318 |  | 0.06 |  |  | 100 | – | 15.5 | –1.2 |  | (20,27.7) |  |  |  | 2.8 | 16.1 | – |  |  |  | – | – |
|  | 318 |  | 0.09 |  |  | 100 | – | 21.7 | 0.94 |  | (5,30.5) |  |  |  | 4.5 | 20.6 | – |  |  |  | – | – |
|  | 318 |  | 0.06 |  |  | 70 | – | 11.4 | –0.94 |  | (5,19.8) |  |  |  | 3.3 | 14.1 | – |  |  |  | – | – |
|  | 318 |  | 0.06 |  |  | 30 | 0-0.5 | 20.9 | –15.3 |  | (5,14.4) |  |  |  | 3.8 | 4.7 | – |  |  |  | – | – |
|  | 328 |  | 0.06 |  |  | 100 | – | 25.9 | –1.2 |  | (3,37.7) |  |  |  | 4.5 | 30.9 | – |  |  |  | – | – |
| 0.1M NaCl | 318 |  | 0.06 |  |  | 100 | – | 8.6 | –0.06 |  | (3,9.9) |  |  |  | 4.3 | 3.2 | (120,43.2) |  |  |  | 4.9 | –10.5 |
| pH=10 | 318 |  | 0.06 |  |  | 100 | – | 7.5 | 0.2 |  | (5,6.9) |  |  |  | 2.8 | 0.7 | (50,16.1) |  |  |  | 4.7 | –16.1 |
| pH=12 | 318 |  | 0.06 |  |  | 100 | 0-2 | 8.0 | –9.9 |  | (40,15.4) |  |  |  | 3.2 | –5.3 | – |  |  |  | – | – |
| pH=13 | 318 |  | 0.06 |  |  | 100 | 0-5 | 2.8 | –6.0 |  | (50,7.5) |  |  |  | 2.3 | –9.4 | – |  |  |  | – | – |

Units of and  are in mg g-1 min-0.5 and mg g-1. Units of  and  are in min and those of  and are in mg g-1 and . Boundary points coordinates of diffusion regions,, are similar to those of the KASRA model,  in Table S2. Except for 0.01 mM of CR, there is a TRAK between each two successive kinetic curves (Table 4). Unit of TD (time delay) is in min.

Table S4-Coefficients of the first curve (region 1) and second curve (region 2including parts 2a and 2b) of the ISO equation for kinetics of CR adsorption on different sites of Mg-Al-LDH nanocompound at 308–328 K (Complete data).

| Solvent | T |  |  | rpm |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  | (mM) |  |  |  | (mM,min,mg g-1) |  |  |  |  | (min,mg g-1) |  |  |  | (mM,min,mg g-1) |
| Corresponding to thermodynamic |  |  |  |  | ARIAN region I (MP Site) |  |  |  |  | ARIAN section IIA (MP Site) |  |  |  |  |  |  |
| Water | 318 |  | 0.01 | 100 |  | 6.34×104 | (5,4.1) | 3.05×104 |  |  |  | (90,11.6) | 6.81×104 |  |  | (0.006,150,13.9) |
|  |  |  |  | KASRA region 1 (1st curve) |  |  |  |  | KASRA region 2 (2nd or 2nd and 3rd curves) |  |  |  |  |  |  |  |
| Corresponding to thermodynamic |  |  |  | ARIAN region I and section IIA (MP Site) |  |  |  |  |  |  | ARIAN section IIB (003 Site) |  |  |  |  |  |
| Water |  | 308 | 0.06 | 100 |  | 1.75×105 | (0.058,3,9.9) | 1.57×104 |  |  |  | (90,36.0) | 2.35×104 |  |  | (0.043,150,48.0) |
|  |  | 318 | 0.06 | 100 |  | 5.01×105 | (0.051,3,25.2) | 2.00×104 |  |  |  | (90,43.1) | 4.76×104 |  |  | (0.039,150,49.2) |
|  |  | 318 | 0.09 | 100 |  | 1.22×106 | (0.080,2,29.4) | 1.64×104 |  |  |  | (90,63.9) | 5.97×104 |  |  | (0.063,150,74.2) |
|  |  | 318 | 0.06 | 70 |  | 3.18×105 | (0.053,3,18.9) | 1.64×104 |  |  |  | (90,46.9) | 3.72×104 |  |  | (0.038,180,56.2) |
|  |  | 318** | 0.06 | 30 |  | 2.15×105 | (0.054,2,14.6) | 1.13×104 |  |  |  | (60,33.1) | 3.69×104 |  |  | (0.038,180,54.4) |
|  |  | 328 | 0.06 | 100 |  | 7.37×105 | (0.047,2,36.8) | 1.13×105 |  |  |  | (20,51.9) | 6.33×105 |  |  | (0.039,30,54.3) |
| 0.1M NaCl |  | 318 | 0.06 | 100 |  | 3.65×105 | (0.057,1,8.7) | 2.72×104 |  |  |  | (2nd TRAK)* |  | 2.93×104 | (0.039,210,60.1) |  |
| pH=10 |  | 318 | 0.06 | 100 |  | 5.26×105 | (0.058,0.8,6.3) | 5.33×104 |  |  |  | (2nd TRAK)* |  | 2.16×104 | (0.044,180,41.5) |  |
| pH=12** |  | 318 | 0.06 | 100 |  | 5.67×104 | (0.056,10,12.1) | 4.90×103 |  |  |  | (50,16.8) | 1.59×104 |  |  | (0.049,120,30.0) |
| pH=13** |  | 318 | 0.06 | 100 |  | 1.77×104 | (0.058,20,6.4) | 5.22×103 |  |  |  | (180,21.6) | 2.51×104 |  |  | (0.050,240,26.0) |

,  and  are CR concentration, time and adsorption capacity at the beginning of the TRAK between nth and (n+1)th kinetic curves, respectively (corresponding to ,  and in the last curve). ,  and  are CR concentration, time and adsorption capacity at the beginning of the plateau. Except for 0.01 mM of CR solution which there is one kinetic curve, there is a TRAK between each two successive kinetic curves (Table 4). * values of 2nd TRAKs in 0.1M NaCl and pH=10 solutions are (0.045,90,41.8) and (0.054,30,15.5), respectively and their dimensions are in (mM, min, mg g-1) and in these cases there are totally three kinetic curves (Table 4). Units of ,  and  are in mg g-1 M-1 min-1.

Figures:

Fig. S1. EDS spectra of (a) CR-adsorbed Mg-Al-LDH and Mg-Al-LDH after contact with alkaline solutions at pHs of (a) 10 and (b) 12 and (13).

Fig. S1 (a)

Fig. S1 (b)

Fig. S1 (c)

Fig. S2- BET diagrams of (a) Mg-Al-LDH, (b) CR-adsorbed Mg-Al-LDH and (c) Mg-Al-LDH in contact with solution at pH=13.

Fig. S2(a)

Fig. S2(b)

Fig. S2(c)