Supplementary online material

Comparison of the NMR and the Acid Value Determination Methods for Quality Control of Input Polysorbates

Ema Valentina Brovča,b, Stane Pajka, Roman Šinkb, Janez Mravljaka,*

aThe Chair of Pharmaceutical Chemistry, University of Ljubljana, Faculty of Pharmacy, Aškerčeva 7, SI-1000 Ljubljana, Slovenia

bDrug Product Analytical Development, Lek d.d., Kolodvorska 27, SI-1234 Mengeš, Slovenia

*Corresponding author. phone.: +386 1 4769500; fax: +386 1 4258031.

E-mail address: janez.mravljak@ffa.uni-lj.si (J. Mravljak).

Corresponding author

Contents

Spiked 1H NMR spectra 							2, 3

Solvent comparison: 1H NMR spectra 					4 – 7

Free fatty acid determination: 1H NMR spectra                                     8

Acid value determination 						            8, 9

1H NMR

Fig S1. 1H NMR spectra of PS 20 samples with LA spiking, recorded in CD3OD.

Fig S2. 1H NMR spectra of PS 80 samples with OA spiking, recorded in CD3OD.

Solvent comparison

Fig S3. 1H NMR spectra of PS 20 samples, recorded in DMSO-d6.

Fig S4. 1H NMR spectra of PS 80 samples, recorded in DMSO-d6.

Fig S5. 1H NMR spectra of PS 20 samples, recorded in CDCl3.

Fig S6. 1H NMR spectra of PS 80 samples, recorded in CDCl3.

Free fatty acid determination

Equation S1. Calculation of the proportion of FFA molecules relative to the total content of FA molecules [%].

% FA=∫FFA∫FFA+∫estrified FA∙100

∫ FFA = integral value for free fatty acids [/]

∫ esterified FA = integral value for esterified fatty acids = 1 [/]

Table S1. Values of FFAs ∫ and of the proportions of FFA in samples of PS 20 with different levels of LA spiking.

| % spiked FA in PS 20 | ∫ for FFAs | % FFAs |
| --- | --- | --- |
| 0.00% | 0.052 | 4.94 |
| 1.02% | 0.113 | 10.15 |
| 2.03% | 0.170 | 14.53 |
| 3.01% | 0.239 | 19.29 |
| 4.02% | 0.313 | 23.84 |
| 4.99% | 0.393 | 28.21 |

Table S2. Values of FFAs ∫ and of the proportions of FFA in samples of PS 80 with different levels of OA spiking.

| % spiked FA PS 80 | ∫ for FFAs | % FFAs |
| --- | --- | --- |
| 0.00% | 0.097 | 8.84 |
| 0.81% | 0.131 | 11.58 |
| 1.98% | 0.161 | 13.87 |
| 3.01% | 0.193 | 16.18 |
| 3.98% | 0.257 | 20.45 |
| 5.02% | 0.294 | 22.72 |

Acid value determination

Equation S2. Values of IA were calculated using the following equation, considering the mass of weighed samples and the consumption of 0.1 M NaOH solution.

IA=5.610∙VNaOH∙fm

VNaOH = volume of 0.1 M NaOH solution [mL]

f = factor of the volumetric NaOH solution [/]

m = weight of the individual sample [g]

When calculating values of IA, the factor of the volumetric NaOH solution that represents the ratio between the prepared and the required concentration of the NaOH solution was taken into account. Three repetitions of the determination of IA for each sample were carried out and the average of three measurements taken.

Table S3. IA values of the PS 20 samples with LA spiking.

| % spiked LA in PS 20 | IA Tukaj vnesite enačbo. |
| --- | --- |
| 0.00% | 0.80 |
| 1.02% | 3.6 |
| 2.03% | 6.5 |
| 3.01% | 9.2 |
| 4.02% | 12.0 |
| 4.99% | 14.7 |

Table S4. IA values of the PS 80 samples with OA spiking.

| % spiked OA in PS 80 | IA |
| --- | --- |
| 0.00% | 1.5 |
| 0.81% | 3.1 |
| 1.98% | 5.4 |
| 3.01% | 7.5 |
| 3.98% | 9.4 |
| 5.02% | 11.4 |