Synthesis and Characterization of High-Efficiency Red Phosphorescent Iridium(III) Complexes with 1-(4-(trifluoromethyl)phenyl)isoquinoline Ligand

Zheng Zhao,1 Xiao-Han Yang,1 Zi-Wen Tao,1 Han-Ru Xu,1 Kai Liu,1 Guang-Ying Chen,2 Zheng-Rong Mo,2 Shui-Xing Wu,1 Zhi-Gang Niu1,2 and Gao-Nan Li1,*
1 Key Laboratory of Electrochemical Energy Storage and Energy Conversion of Hainan Province, College of Chemistry and Chemical Engineering, Hainan Normal University, Haikou 571158, China
2 Key Laboratory of Tropical Medicinal Plant Chemistry of Ministry of Education, Hainan Normal University, Haikou 571158, China
Table S1. Frontier orbital energy and electron density distribution for complexes 2a(2b.
	Complex
	Orbital
	Energy (eV)
	Ir (%)
	Cyclometalated ligand (%)
	Ancillary ligand (%)

	2a
	LUMO+1
	-2.070
	4.82
	92.90
	2.28

	
	LUMO
	-2.176
	4.24
	93.75
	2.01

	
	HOMO
	-4.908
	13.88
	10.38
	75.74

	
	HOMO-1
	-5.343
	47.00
	35.09
	17.91

	2b
	LUMO+1
	-2.106
	5.01
	92.18
	2.81

	
	LUMO
	-2.219
	4.10
	93.39
	2.52

	
	HOMO
	-5.205
	24.74
	17.20
	58.06

	
	HOMO-1
	-5.446
	36.62
	31.32
	32.06

	
	HOMO-2
	-5.840
	34.89
	26.89
	38.22

	
	HOMO-3
	-5.971
	36.65
	36.81
	26.54


[image: image1.png]=01

0.0

Lo

2.0

3.0

40

6.0

£1 (ppm)




Fig. S1. 1H NMR spectrum of complex 2a in CDCl3 (400 MHz).
[image: image2.png]RS T Y

0.0

Lo

2.0

3.0

40

6.0

£1 (ppm)




Fig. S2. 1H NMR spectrum of complex 2b in CDCl3 (400 MHz).
