Opis  nowości

Nienasycone żywice poliestrowe są zazwyczaj utwardzane w roztworze styrenu  z udziałem  inicjatora takiego jak nadtlenek lub wodoronadtlenek. Trzeciorzędowe aminy zmniejszają energię aktywacji rozkładu nadtlenku i prowadzą do inicjacji układu utwardzania w niskiej temperaturze. Niestety, nienasycone żywice poliestrowe z rozpuszczoną w nich aminą mają niską trwałość przy przechowywaniu. Lepsza stabilność ma układ, w którym amina jest chemicznie włączana do struktury poliestru, już na etapie jej syntezy. Aktywator aminowy jest wówczas bardzo równomiernie rozłożony w poliestrze. Takie wbudowanie  jest możliwe, gdy amina ma dwie lub więcej grup funkcyjnych, np. hydroksylowych  zdolnych do reakcji z kwasami karboksylowymi lub  bezwodnikami kwasowymi. W tej pracy opisano nowe aminy trzeciorzędowe z grupami hydroksylowymi , które można stosować jako modyfikatory i przyspieszacze dla nienasyconych żywic poliestrowych. Wytwarza się je w reakcjach tlenku etylenu lub tlenku propylenu z fenyleno-1,2-diaminą. Przedstawiono wyniki badań nad ich wpływem na zachowanie żelowania (zmniejszenie czasu żelowania w zależności od ilości wbudowanego akceleratora aminowego) i stabilność nienasyconych żywic poliestrowych.

The unsaturated polyester resins are usually cured in a styrene solution with an initiator such as peroxide or hydroperoxide. In low temperature curing of unsaturated polyester, cobalt or vanadium salts as well as tertiary amines are used most often. Tertiary amines reduce the activation energy of peroxide decomposition and lead to the initiation of the low temperature curing system. Unfortunately, unsaturated polyester resins with amine dissolved in them have low storage stability. Better stability has a system in which the amine is chemically incorporated into the polyester structure at the stage of its synthesis. The amine activator is then very evenly distributed in the polyester. Such incorporation is possible when the amine has two or more functional groups (e.g. hydroxyls groups) capable of reacting with carboxylic acids or acid anhydrides. This work describes new tertiary amines with hydroxyl groups that can be used as modifiers and accelerators for unsaturated polyester resins. They are prepared in reactions of ethylene oxide or propylene oxide with phenylene-1,2-diamine. The results of research on their influence on gelation behavior (reduction of gelling time depending on the amount of amine accelerator incorporated) and stability of unsaturated polyester resins have been presented.
Tertiary amines reduce the activation energy of peroxide decomposition and lead to the initiation of the low temperature curing system of polyester resins. Unfortunately, unsaturated polyester resins with amine dissolved in them have low storage stability. Better stability has a system in which the amine is chemically incorporated into the polyester structure at the stage of its synthesis. This work describes new tertiary amines with hydroxyl groups  incorporated into the polyester structure. They can be used as modifiers and accelerators for unsaturated polyester resins. They are prepared in reactions of ethylene oxide or propylene oxide with phenylene-1,2-diamine.
