Table 1.	Adsorption capacities of various adsorbents.

| Adsorbent | Adsorption Capacity (mg/g) | Adsorption Temperature (℃) | CO2 Purity | Sources |
| --- | --- | --- | --- | --- |
| 35%ODA/SG600 | 15.61 | 25 | 99 % | 15 |
| MEA/AC | 15.40 | 25 | 15 % | 16 |
| Raw kenaf | 27.46 | 30 | 99.99 % | 17 |
| 50%MEA-Kenaf | 34.36 | 30 | 99.99 % | 17 |
| 50%TEPA-Kenaf | 40.22 | 30 | 99.99 % | 17 |
| MCM-41 | 35.00 | 25 | n.a | 10 |
| Fe2O3/MCM-41 | 38.40 | 25 | n.a | 10 |
| NiO | 14.14 | 25 | 99 % | 25 |
| CeO2 | 48.00 | 25 | > 99.5 % | 30 |
| Fe2O3 | 17.00 | 25 | 99 % | 31 |
| SiO2 | 33.73 | 25 | 99 % | 32 |
| 1%[bmim][CF3SO3]/SiO2 | 66.71 | 25 | 99 % | 32 |
| 10%NiO/[emim][HSO4]/SiO2 | 48.80 | 25 | 99 % | 33 |
| 10%[emim][HSO4]/SiO2 | 26.70 | 25 | 99 % | 33 |
| 10%ChCl:U/SG200 | 22.30 | 30 | 99 % | 34 |
| ChCl:U/AC | 39.40 | 25 | 15 % in N2 | 35 |

Table 2.	Vibrational frequencies IR spectroscopy of various MO/AC.

| Vibrational modes | This study (cm-1) | Reference (cm-1) |
| --- | --- | --- |
| O-H Stretching | 3406 | 3412 |
| C=O stretching | 1716 | 1716 |
| C=C Stretching | 1634 | 1633 |
| C=C Stretching | 1560 | 1550 |
| C-H Bending | 1388 | 1390 |
| C-O Stretching | 1130 | 1130 |
| C-H Stretching | 600 | 600 |
| Ce-O | 470 | 459 |

Table 3.	The textural characteristics of the adsorbents.

| Adsorbent |  | AC | CeO2/AC | ZnO/AC | Co3O4 /AC |
| --- | --- | --- | --- | --- | --- |
| Surface area | SBET (m2/g) | 1043.6 | 763.4 | 792.9 | 838.5 |
|  | Smeso (m2/g) | 171.0 | 254.1 | 280.4 | 302.2 |
|  | Smicro (m2/g) | 872.6 | 509.4 | 512.5 | 536.3 |
| Pore Volume | Vtotal (cm3/g) | 0.46 | 0.42 | 0.45 | 0.47 |
|  | Vmicro (cm3/g) | 0.35 | 0.21 | 0.21 | 0.22 |
| Average pore diameter (nm) |  | 1.8 | 2.2 | 2.3 | 2.2 |

where SBET is surface area by BET method; Smic is micropore surface area by t-plot method; Vtotal is single point total pore volume; Vmicro is micropore volume by the t-plot method

Table 4.	Adsorption capacities of various sorbents.

| Adsorbent | Adsorption Capacity (mg/g) | Adsorption Temperature (℃) | CO2 Purity | Sources |
| --- | --- | --- | --- | --- |
| AC | 52.01 | 30 | 99 % | This study |
| CeO2/AC | 52.78 | 30 | 99 % | This study |
| ZnO/AC | 52.06 | 30 | 99 % | This study |
| Co3O4/AC | 43.17 | 30 | 99 % | This study |
| ACCe-HT | 37.66 | 30 | 20 % | 47 |
| ACCu-HT | 25.74 | 30 | 20 % | 47 |
| Mg-MCs-12 | 53.68 | 40 | 15 % in N2 | 28 |

Table 5.	Kinetic parameters of CO2 adsorption onto CeO2/AC.

| Kinetic model | Parameter | Temperature (℃) |  |
| --- | --- | --- | --- |
|  |  | 30 | 50 |
|  | qe(act) (mg/g) | 52.78 | 40.56 |
| Pseudo-first order kinetic | qe(cal) (mg/g) | 9.87 | 8.78 |
|  | k1(1/min) | 0.2308 | 0.2132 |
|  | R2 | 0.9178 | 0.8777 |
|  | Relative error (%) | 81.29 | 78.34 |
| Pseudo-first order kinetic | qe(cal) (mg/g) | 53.47 | 41.67 |
|  | k2 (g/mg min) | 0..0546 | 0.0389 |
|  | h (mg/g min) | 156.14 | 67.57 |
|  | R2 | 0.9994 | 0.9622 |
|  | Relative error (%) | 1.32 | 2.74 |

where qe(act) = actual adsorption capacity; qe(cal) = calculated adsorption capacity