The effect of hydrogen bonding and azomethine group orientation on liquid crystal properties in benzylideneaniline compounds

Figure 1: The torsion angle for benzylidine aniline compounds

Figure 2: The general structures for the prepared Schiff bases

Figure 3: The structure of (1-6a) compounds and hydrogen atoms numbers

Figure 4:  structure of (1-6b)  compounds and hydrogen atoms numbers

Table1:Mesomorphic data and structures for compounds 1-6b

| Comp. | Phase transition | TSm | TN |
| --- | --- | --- | --- |
| 1b | Cr 197.4 I | - | - |
| 2b | Cr 166 Sm 197.7 N 268.3 I | 31.7 | 70.6 |
| 3b | Cr 224 Sm 263.5 N 278 I | 39.5 | 14.5 |
| 4b | Cr 225.2 Sm 247.9 N 276 I | 22.7 | 28.1 |
| 5b | Cr 242.1 N 266.3 I | - | 24.2 |
| 6b | Cr 202.9 N 291.8 I | - | 88.9 |

Figure 5: A schematic of the hydrogen bond in the compounds 1-6a and 1-6b

Figure 6: The dipole moment and the torsion angle for compounds 1-6a

Figure 7: The dependence of melting points on size of substituent atoms

Figure 8: Polarized optical micrographs for: (a) compound 2b (smectic at 166 °C); (b) compound 2b  (nematic, schlieren at 197.7 °C); (c) compound 3b (smectic at 224 °C), (d) compound 3b (nematic, schlieren at 263.5 °C); (e) compound 4b (smectic, at 225.2 °C); (f) compound 4b (nematic, schlieren at 247.9 °C); (g) compound 5b (nematic, schlieren , at 242.1 °C); (h) compound 6b (nematic, Schlieren at 202.9 °C).

Figure 9. Hydrogen bonds in compounds 2-4b in the smectic and nematic  phases

Figure 10: The hydrogen bond for compounds (5 and 6b in the nematic  phase