Supplementary Material:

GO/PAMAM as a high capacity adsorbent for removal of Alizarin Red S: Selective separation of dyes

Authors: Mohammad Rafia, Babak Samiey,a,* Chil-hung Chengb

Address: aDepartment of Chemistry, Faculty of Science, Lorestan University, Khoramabad 68137–17133, Lorestan, Iran

bDepartment of Chemical Engineering, Ryerson University, M5B 2K3, Toronto, Ontario, Canada

Corresponding Author: Babak Samiey

E-mail: babsamiey@yahoo.com , samiey.b@lu.ac.ir

Fig. S1a

Fig. S1b

Fig. S1c

Fig. S1. BET isotherms of (a) pristine GO/PAMAM, (b) ARS–adsorbed GO/PAMAM at pH=2 and (b) ARS–adsorbed GO/PAMAM modified at pH=0.

Fig. S2a                                                               Fig. S2b

Fig. S2. SEM images of (a) pristine GO/PAMAM and (b) GO/PAMAM modified at pH=0.

Fig. S3. EDS spectra of GO/PAMAM and GO/PAMAM modified in 1M HCl at pH=0.

Fig. S4. Nitrogen, carbon and hydrogen mass percentages of pristine GO/PAMAM.

Fig. S5. (a) (1) 5×10–2 mM ARS, (2) 5×10–2 mM MB, (3) 5×10–2 mM MB+GO/PAMAM, (4) 5×10–2 mM MB+ 5×10–2 mM ARS and (5) 5×10–2 mM MB+5×10–2 mM ARS+GO/PAMAM, (b) (1) 5×10–2 mM ARS, (2) 5×10–2 mM AO, (3) 5×10–2 mM AO+GO/PAMAM, (4) 5×10–2 mM AO+ 5×10–2 mM ARS and (5) 5×10–2 mM AO+5×10–2 mM ARS+GO/PAMAM, (c) (1) 5×10–2 mM ARS, (2) 5×10–2 mM Th, (3) 5×10–2 mM Th+GO/PAMAM, (4) 5×10–2 mM Th+ 5×10–2 mM ARS and (5) 5×10–2 mM Th+5×10–2 mM ARS+GO/PAMAM, (d) (1) 5×10–2 mM ARS, (2) 5×10–2 mM PY, (3) 5×10–2 mM PY+GO/PAMAM, (4) 5×10–2 mM PY+ 5×10–2 mM ARS and (5) 5×10–2 mM PY+5×10–2 mM ARS+GO/PAMAM, (e) (1) 5×10–2 mM ARS, (2) 2.5×10–2 mM MEB, (3) 2.5×10–2 mM MEB+GO/PAMAM, (4) 2.5×10–2 mM MEB+ 5×10–2 mM ARS, (5) 2.5×10–2 mM MEB+5×10–2 mM ARS+GO/PAMAM and (f) (1) 5×10–2 mM ARS, (2) 5×10–2 mM JG, (3) 5×10–2 mM JG+GO/PAMAM (4) 5×10–2 mM JG+5×10–2 mM ARS (5) 5×10–2 mM JG+5×10–2 mM ARS+GO/PAMAM at pH=2 and room temperature. 0.001 g GO/PAMAM was used in each test as adsorbent.

Tables:

Table S1- Parameters obtained from the Henry’s law and and values for adsorption of ARS on GO/PAMAM nanocompound in water, alkaline and acidic solutions at 100 rpm and 308–328 K.

| Solvent | T |  | Henry’s law |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | (K) | A | K | R2 | (mM) | (mg g–1) |
| pH=0 | 318 | 2.23 | 3.32×107 | 0.97 | 2.25×10−3 | 72.7 |
| pH=0.3 | 318 | 0.45 | 8.41×106 | 0.99 | 1.29×10−2 | 107.9 |
| pH=1 | 318 | 4.91 | 7.19×107 | 0.99 | 3.56×10−3 | 252.6 |
| pH=2 | 308 | 5.38 | 4.95×107 | 0.99 | 4.45×10−3 | 222.7 |
|  | 318 | –4.77 | 3.22×107 | 0.99 | 4.81×10−3 | 154.7 |
|  | 328 | –4.99 | 1.09×107 | 0.98 | 7.03×10−3 | 133.7 |
| pH=3 | 318 | –2.21 | 3.09×107 | 0.98 | 4.96×10−3 | 154.2 |
| pH=5 | 318 | –1.28 | 2.47×106 | 0.99 | 3.15×10−2 | 79.1 |
| pH=10 | 318 | 0.75 | 5.70×106 | 0.98 | 3.74×10−3 | 21.4 |
| pH=13 | 318 | 0.37 | 3.50×106 | 0.97 | 6.19×10−3 | 21.7 |
| pH=14 | 318 | 0.88 | 1.71×106 | 0.99 | 1.32×10–2 | 23.3 |

Dimensions of A and K are in mg g–1 and mg g–1 M–1, respectively. Henry’s law for experimental data is as

Table S2- Parameters obtained from the Temkin and Langmuir equations and and values for adsorption of ARS on GO/PAMAM nanocompound in water, alkaline and acidic solutions at 100 rpm and 308–328 K.

| Solvent | T |  | Temkin |  |  | Langmuir |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  |  |  | R2 |  | K | R2 |  | (mM) | (mg g–1) |  |
| pH=0 |  | 318 | 54.1 | 1.55×106 | 0.99 | 250.0 | 2.00×105 | 0.98 |  | 0.16 |  | 291.1 |
| pH=0.3 |  | 318 | 108.0 | 1.96×105 | 0.98 | 500.0 | 2.22×104 | 0.99 |  | 0.21 |  | 380.4 |
| pH=1 |  | 318 | 119.0 | 2.26×106 | 0.97 | 574.7 | 2.16×105 | 0.96 |  | 0.18 |  | 759.6 |
| pH=2 |  | 308 | 111.1 | 1.73×106 | 0.99 | 613.5 | 1.26×105 | 0.98 |  | 0.25 |  | 636.7 |
|  |  | 318 | 147.5 | 6.19×105 | 0.97 | 724.6 | 5.45×104 | 0.98 |  | 0.18 |  | 633.2 |
|  |  | 328 | 235.5 | 2.85×105 | 0.99 | 1941.7 | 1.17×104 | 0.94 |  | 0.18 |  | 919.3 |
| pH=3 |  | 318 | 141.7 | 7.45×105 | 0.98 | 751.9 | 2.68×102 | 0.97 |  | 0.23 |  | 754.2 |
| pH=5 |  | 318 | 39.4 | 2.39×105 | 0.97 | 200.0 | 2.50×104 | 0.98 |  | 0.38 |  | 544.3 |
| pH=10 |  | 318 | 23.4 | 7.29×105 | 0.98 | 142.9 | 7.00×104 | 0.98 |  | 3.2×10–2 |  | 72.6 |
| pH=13 |  | 318 | 14.7 | 6.66×105 | 0.97 | 58.8 | 8.50×104 | 0.98 |  | 2.5×10–2 |  | 42.8 |
| pH=14 |  | 318 | 79.9 | 9.94×104 | 0.99 | –38.0 | –2.9×104 | 0.98 |  | 3.4×10–2 |  | 63.7 |

Dimension of  and is in mg g-1. Dimension ofand K is in M–1.

Table S3- Parameters obtained from the Temkin and Langmuir equations and  and  values for adsorption of ARS on GO/PAMAM nanocompound in water, alkaline and acidic solutions at 100 rpm and 308–328 K.

| Solvent | T | Temkin |  |  |  | Langmuir |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  |  | R2 |  |  | K | R2 | (mM) | (mg g–1) |
| pH=0 | 318 | – | – | – | – |  | – | – | 0.16 | 291.1 |
| pH=0.3 | 318 | 332.1 | 1.58×104 | 0.95 | 1831.5 |  | 1.31×103 | 0.93 | 0.37 | 575.6 |
| pH=1 | 318 | 1127.0 | 1.08×104 | 0.98 | –9174 |  | –3.99×102 | 0.96 | 0.27 | 1182.6 |
| pH=2 | 308 | 888.9 | 7.39×103 | 0.99 | –5848 |  | –3.59×102 | 0.99 | 0.38 | 929.4 |
|  | 318 | 599.6 | 1.60×104 | 0.99 | 2188.2 |  | 2.34×103 | 0.97 | 0.41 | 1027.6 |
|  | 328 | 526.6 | 2.36×104 | 0.96 | 2257.3 |  | 2.77×103 | 0.95 | 0.49 | 1275.2 |
| pH=3 | 318 | 878.0 | 9.26×103 | 0.97 | 7633.6 |  | 4.44×102 | 0.95 | 0.39 | 1091.5 |
| pH=5 | 318 | 9148.0 | 7.32×103 | 0.97 | –333.0 |  | –3.00×103 | 0.95 | 0.38* | 544.3* |
| pH=10 | 318 | 63.9 | 9.98×104 | 0.96 | 500.0 |  | 6.67×103 | 0.96 | 6.5×10−2 | 112.5 |
| pH=13 | 318 | 113.4 | 5.86×104 | 0.99 | –125.0 |  | –1.00×104 | 0.94 | 4.7×10−2 | 114.0 |
| pH=14 | 318 | – | – | – | – |  | – | – | – | – |

Unit of  and is in mg g–1. Unit of and K is in M-1. *At pH=5, mM and  mg g-1 and the third region (region IIC) starts after this point. The Temkin parameters of this section are mg g–1 and M–1 and its Langmuir parameters are  mg g-1 and  M–1. In this region,  mM  and  mg g–1.

Table S4- Relative magnitude of regions I and II (sections IIA, IIB and IIC) for adsorption of ARS on GO/PAMAM nanocompound in water, alkaline and acidic solutions at 100 rpm and 308–328 K.

| Solvent | T (K) | Region I | Section IIB | Section IIC |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| pH=0 | 318 | 0.25 | 0.75 | – | – |  |  |
| pH=0.3 | 318 | 0.19 | 0.45 | 0.39 | – |  |  |
| pH=1 | 318 | 0.21 | 0.31 | 0.36 | – |  |  |
| pH=2 | 308 | 0.19 | 0.35 | 0.45 | – |  |  |
|  | 318 | 0.14 | 0.42 | 0.44 | – |  |  |
|  | 328 | 0.10 | 0.62 | 0.28 | – |  |  |
| pH=3 | 318 | 0.13 | 0.51 | 0.35 | – |  |  |
| Solvent | T (K) | Region I | Section IIA | Section IIB | Section IIC |  |  |
| pH=5 | 318 | 0.12 | 0.08 | 0.62 | 0.15 |  |  |
| Solvent | T (K) | Region I | Section IIA | Section IIB |  |  |  |
| pH=10 | 318 | 0.19 | 0.46 | 0.35 |  | – |  |
| pH=13 | 318 | 0.19 | 0.18 | 0.63 |  | – |  |
| pH=14 | 318 | 0.37 | 0.63 | – |  | – |  |

| Solvent | T |  |  | rpm |  |  |  |  | KASRA region 1 (1st curve) |  |  |  |  |  |  | KASRA region 2 (1st curve) |  |  |  | KASRA region 2 (2nd curve) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to thermodynamic |  |  |  |  |  |  |  | ARIAN region I |  |  |  |  |  |  |  | ARIAN section IIA |  |  |  | ARIAN section IIB |  |  |  |  |  |  |
| pH=0A | 318 | 0.25 | 100 |  |  | (270,206.3) |  |  |  |  | –0.048 |  | 2.79 |  | (45,73.7) |  | –4.0×10-3 | 1.29 |  |  | – | – |  |  | – |  |
| pH=2 | 318 | 0.07 | 100 |  |  | (180,202.2) |  |  |  |  | –0.23 |  | 9.16 |  | (45,181.8) |  | –2.0×10-3 | 0.32 |  |  | – | – |  |  | – |  |
| (0.1 M NaCl) 318 |  | 0.07 | 100 |  |  | (420,174.0) |  |  |  |  | –0.47 |  | 6.88 |  | (10,44.8) |  | –1.6×10-3 | 0.64 |  |  | – | – |  |  | – |  |
|  | 308 B | 0.70 | 100 |  |  | (360,991.9) |  |  |  |  | –10.40 |  | 61.00 |  | (5,169.9) |  | –0.11 | 8.24 |  |  | (90,469.2) | –0.012 |  |  | 3.94 |  |
|  | 318 B | 0.70 | 100 |  |  | (420,965.9) |  |  |  |  | –14.28 |  | 71.25 |  | (5,184.2) |  | –0.13 | 8.35 |  |  | (60,449.2) | –0.006 |  |  | 2.99 |  |
|  | 328 B | 0.70 | 100 |  |  | (300,960.1) |  |  |  |  | –16.94 |  | 88.84 |  | (5,232.6) |  | –0.14 | 11.32 |  |  | (90,681.0) | –0.004 |  |  | 1.96 |  |
|  | 318 B | 0.70 | 70 |  |  | (360,815.4) |  |  |  |  | –4.00 |  | 34.13 |  | (9,120.6) |  | –0.08 | 6.95 |  |  | (60,402.8) | –0.002 |  |  | 1.85 |  |
|  | 318 B | 0.70 | 40 |  |  | (480,893.4) |  |  |  |  | –2.40 |  | 23.70 |  | (10,120.1) |  | –0.11 | 7.54 |  |  | (90,376.7) | –0.004 |  |  | 2.70 |  |
| pH=3C | 318 | 0.70 | 100 |  |  | (480,931.5) |  |  |  |  | –8.45 |  | 63.88 |  | (5,213.8) |  | –0.11 | 10.07 |  |  | (60,585.1) | –0.002 |  |  | 1.67 |  |
|  |  |  |  |  | KASRA region 1 (1st curve) |  |  |  |  |  |  |  |  |  |  | KASRA region 2 (2nd curve) |  |  |  |  | KASRA region 2 (3rd curve) |  |  |  |  |  |
| Corresponding to thermodynamic |  |  |  |  | ARIAN region I and section IIA |  |  |  |  |  |  |  |  |  |  | ARIAN section IIB |  |  |  |  | ARIAN section IIC |  |  |  |  |  |
| pH=5D | 318 | 1.00 | 100 |  |  | (360,577.8) |  |  |  |  | –1.19 |  | 12.32 |  | (10,61.8) |  | –0.106 |  | 7.83 |  | (120,362.5) | –0.006 |  |  |  | 1.97 |
| pH=10E | 318 | 0.07 | 100 |  |  | (480,90.4) |  |  |  |  | –0.65 |  | 5.85 |  | (30,27.1) |  | –4.0×10–4 |  | 0.23 |  | – | – |  |  |  | – |
| pH=13F | 318 | 0.07 | 100 |  |  | (120,109.0) |  |  |  |  | –0.95 |  | 9.60 |  | (15,53.7) |  | –4.0×10–3 |  | 0.75 |  | – | – |  |  |  | – |

Table S5- Experimental , , , ,  and  values and coefficients of the KASRA equation for kinetics of ARS adsorption on GO/PAMAM at different temperatures and in various shaking rates and initial ARS concentrations (complete data).

Units of ,  and  are in mg g-1 min-2 and those of ,  and  are in mg g–1 min–1. Units of , and   are in min and those of ,  and  are in mg g–1. In region 1,  and  are equal to zero. AAdsorption of  occurs on  and  sites in the kinetic curve, respectively. BAdsorption of  occurs on  and  sites in the first curve and on  site in the second curve. CAdsorption of  occurs on  and  sites in the first curve and on  site in the second curve. DAt pH=5, data in three boxes from left to right belong to the adsorption of on Ph sites (1st kinetic curve), onsites (2nd kinetic curve) and  on  sites (3rd kinetic curve), respectively. EAdsorption of  occurs on  site in the first curve and on  site in the second curve. FAdsorption of  occurs on  site in the first curve and on  site in the second curve.

Table S6- Coefficients of the intraparticle diffusion equation for kinetics of ARS adsorption on GO/PAMAM at different temperatures and in various shaking rates and initial ARS concentrations (complete data).

| Solvent | T |  |  |  |  |  |  | rpm |  |  |  | KASRA region 1 (1st curve) |  |  |  |  |  | KASRA region 2 (1st curve) |  |  |  |  |  | KASRA region 2 (2nd curve) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  |  | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | TRAK |  |  |  |  |  |  | TRAK |
| Corresponding to thermodynamic |  |  |  |  |  |  |  |  | ARIAN region I |  |  |  |  |  |  |  |  |  |  | ARIAN section IIA |  |  | ARIAN section IIB |  |  |  |  |  |  |
| pH=0 |  | 318 |  | 0.25 |  |  | 100 |  |  |  |  | 11.2 |  | –3.06 |  | (45,73.7) |  |  |  | 14.1 | –12.6 | – | – |  | – | – |  |  | – |
| pH=2 |  | 318 |  |  | 0.07 |  | 100 |  |  |  |  | 32.6 |  | –24.0 |  | (45,181.8) |  |  |  | 3.2 | 161.3 | – | – |  | – | – |  |  | – |
| (0.1 M NaCl) |  | 318 |  |  | 0.07 |  | 100 |  |  |  |  | 19.2 |  | –15.5 |  | (10,44.8) |  |  |  | 8.4 | 10.5 |  |  |  |  |  |  |  |  |
|  |  | 308 B |  |  | 0.70 | 100 |  |  |  |  | 97.1 |  | –40.2 |  | (5,169.9) |  |  |  | 44.3 |  | 71.6 | – | (90,469.2) |  | 56.2 | –31.1 |  |  | – |
|  |  | 318 B |  |  | 0.70 | 100 |  |  |  |  | 82.5 |  | –1.9 |  | (5,184.2) |  |  |  | 50.7 |  | 69.5 | – | (60,449.2) |  | 45.4 | 92.7 |  |  | – |
|  |  | 328 B |  |  | 0.70 | 100 |  |  |  |  | 105.7 |  | –0.7 |  | (5,232.6) |  |  |  | 65.0 |  | 101.9 | – | (90,681.0) |  | 37.9 | 308.7 |  |  | – |
|  |  | 318 B |  |  | 0.70 | 70 |  |  |  |  | 66.3 |  | –32.3 |  | (9,120.6) |  |  |  | 52.5 |  | –4.6 | – | (60,402.8) |  | 35.3 | 138.4 |  |  | – |
|  |  | 318 B |  |  | 0.70 | 40 |  |  |  |  | 43.8 |  | –11.8 |  | (10,120.1) |  |  |  | 38.4 |  | 34.0 | – | (90,376.7) |  | 44.9 | –36.8 |  |  | – |
| pH=3 |  | 318 | 0.70 |  |  | 100 |  |  |  |  | 119.4 |  | –53.2 |  | (5,213.8) |  |  |  | 71.6 |  | 30.9 | – | (60,585.1) |  | 24.9 | 403.3 | – |  |  |
| pH=5* |  | 318 | 1.00 |  |  | 100 |  |  |  |  | 24.9 |  | –15.6 |  | (10,61.8) |  |  |  | 75.0 |  | –180.4 | – | (30,237.0) |  | 70.1 | 30.9 | 90–120 |  |  |
| KASRA region 1 (1st curve) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | KASRA region 2 (2nd curve) |  |  |  |  |  |  |
| Corresponding to thermodynamic |  |  |  |  |  |  |  |  |  | ARIAN region I and section IIA |  |  |  |  |  |  |  |  |  |  |  |  | ARIAN section IIB |  |  |  |  |  |  |
| pH=10 |  | 318 | 0.07 |  |  | 100 |  |  |  |  | 7.7 |  | 2.0 |  | – |  |  |  | – |  | – | 10–30 | (30,27.1) |  | 4.0 | 3.29 |  | – |  |
| pH=13 |  | 318 | 0.07 |  |  | 100 |  |  |  |  | 19.8 |  | –9.4 |  | – |  |  |  | – |  | – | 10–15 | (15,53.7) |  | 7.8 | 22.8 |  | – |  |

Units of and  are in mg g-1 min–0.5 and min–0.5. Units of  and  are in min and those of  and  are in mg g–1 and . Boundary points coordinates of diffusion regions, , are similar to those of the KASRA model,  in Table S7. *Data in the boxes from left to right belong to the first and second kinetic curves and third kinetic curve (corresponding to the ARIAN section IIC) starts after TRAK in the range of 90–120 min and for that and  are 36.3 mg g-1 min–0.5 and -45.4 min–0.5, respectively. AAdsorption of  occurs on  and  sites in the kinetic curve, respectively. BAdsorption of  occurs on  and  sites in the first curve and on  site in the second curve. CAdsorption of  occurs on  and  sites in the first curve and on  site in the second curve. DAt pH=5, data in three boxes from left to right belong to the adsorption of on Ph sites (1st kinetic curve), onsites (2nd kinetic curve) and  on  sites (3rd kinetic curve), respectively. EAdsorption of  occurs on  site in the first curve and on  site in the second curve. FAdsorption of  occurs on  site in the first curve and on  site in the second curve.

Table S7- Coefficients of region 1 and region 2 (parts 2a and 2b) of the ISO equation for kinetics of ARS adsorption on different sites of GO/PAMAM at 308–328 K (complete data).

| Solvent | T |  |  |  | rpm | KASRA regions 1 and 2 (1st curve) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to thermodynamic |  |  |  |  |  | ARIAN region I and section IIA |  |  |  |  |  |  |  |  |  |
| pH=0A |  | 318 | 0.25 |  | 100 |  | 2.83×104 | 0.99 | (45,73.7) |  | 8.43×103 | 0.99 | (120,140.9) | 2.32×104 | 0.96 | – |
| pH=2 |  | 318 |  | 0.07 | 100 |  | 3.91×105 | 0.99 | (45,181.8) |  | 1.87×105 | 0.97 | Adsorption only on Ph site |  |  | – |
| (0.1 M NaCl) 318 |  |  |  | 0.07 | 100 |  | 6.46×104 | 0.99 | (10,44.8) |  | 9.33×104 | 0.98 | Adsorption only on Ph site |  |  | – |
|  |  | 318 B |  | 0.70 | 100 |  | 4.85×104 | 0.99 | (5,169.9) |  | 1.83×104 | 0.99 | (20,267.9) | 3.89×104 | 0.99 | (0.59,90,469.2) |
|  |  | 318 B |  | 0.70 | 100 |  | 5.50×104 | 0.99 | (5,184.2) |  | 1.70×104 | 0.99 | (25,290.4) | 7.11×104 | 0.99 | (0.556,60,449.2) |
|  |  | 328 B |  | 0.70 | 100 |  | 8.50×104 | 0.99 | (5,232.6) |  | 2.88×104 | 0.98 | (30,469.9) | 7.84×104 | 0.98 | (0.521,90,681.0) |
|  |  | 318 B |  | 0.70 | 70 |  | 3.19×104 | 0.99 | (90,163.7) |  | 1.66×104 | 0.99 | (20,227.6) | 2.99×104 | 0.96 | (0.606,60,402.8) |
|  |  | 318 B |  | 0.70 | 40 |  | 2.68×104 | 0.99 | (6,95.8) |  | 1.53×104 | 0.97 | (15,160.6) | 3.19×104 | 0.99 | (0.59,90,376.7) |
| pH=3C |  | 318 |  | 0.70 | 100 |  | 1.35×104 | 0.99 | (5,213.8) |  | 6.23×103 | 0.99 | (20,342.8) | 1.35×104 | 0.99 | (0.563,60,585.1) |
| pH=5D |  | 318 | 1.00 |  | 100 |  | 1.78×104 | 0.99 | (0.97,10,61.8)** |  | 1.75×104 | 0.99 | (30,237.0) | 1.11×104 | 0.98 | (0.85,90,362.2) |
| pH=10E |  | 318 | 0.07 |  | 100 |  | 1.98×105 | 0.99 | – | – |  | – | – | – | – | (6.32×10–2,10,25.7) |
| pH=13F |  | 318 | 0.07 |  | 100 |  | 2.35×105 | 0.98 | – | – |  | – | – | – | – | (5.79×10–2,10,51.6) |

,  and  are ARS concentration, time and adsorption capacity at the end of adsorption on a type of adsorption site, respectively (corresponding to ,  and  in the last curve). ,  and  are ARS concentration, time and adsorption capacity at the beginning of the plateau. Units of ,  and , are in min–1. Units of , ,  and  are in min–1. Units of , ,  and  are in mg g–1.  and  are in mM. **This parenthesis shows data of ending point for adsorption of ARS– on Ph sites.

Continuation of Table S7

Coefficients of region 1 and region 2 (parts 2a and 2b) of the ISO equation for kinetics of ARS adsorption on different sites of GO/PAMAM at 308–328 K (complete data).

| Solvent | T |  |  |  | rpm | KASRA region 2 (2nd curve) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to thermodynamic |  |  |  |  |  | ARIAN section IIB |  |  |  |  |  |  |  |  |
| pH=0A |  | 318 |  | 0.25 | 100 |  | – | – | – | – | – |  | – | (0.196,270,206.3) |  |
| pH=2 |  | 318B |  | 0.07 | 100 |  | – | – | – | – | – |  | – | (2.27×10–2,180,202.2) |  |
| (0.1M NaCl) |  | 318B |  | 0.07 | 100 |  | – | – | – | – | – |  | – | (2.42×10–2,420,174.0) |  |
|  |  | 318 |  | 0.70 | 100 |  | (0.59,90,469.2) | 1.40×104 | 0.99 | (180,742.1) | 5.39×104 |  | 0.99 | (0.49,360,991.9) |  |
|  |  | 318 |  | 0.70 | 100 |  | (0.556,60,449.2) | 1.39×104 | 0.99 | (240,811.1) | 7.86×104 |  | 0.99 | (0.418,420,965.9) |  |
|  |  | 328 |  | 0.70 | 100 |  | (0.521,90,681.0) | 9.81×103 | 0.98 | (150,766.8) | 2.21×104 |  | 0.96 | (0.391,300,960.1) |  |
|  |  | 318 |  | 0.70 | 70 |  | (0.606,60,402.8) | 6.12×103 | 0.96 | (210,616.0) | 1.22×104 |  | 0.99 | (0.533,360,815.4) |  |
|  |  | 318 |  | 0.70 | 40 |  | (0.59,90,376.7) | 8.76×103 | 0.99 | (240,690.6) | 6.57×104 |  | 0.98 | (0.204,480,893.4) |  |
| pH=3C |  | 318 |  | 0.70 | 100 |  | (0.563,60,585.1) | 7.73×103 | 0.99 | (120,693.5) | 1.15×104 |  | 0.99 | (0.482,480,931.5) |  |
| pH=5D* |  | 318 |  | 1.00 | 100 |  | (0.85,90,362.2)* | 7.81×103 | 0.98 | (240,514.8) | 1.77×104 |  | 0.98 | (0.814,360,577.8) |  |
| pH=10E |  | 318 |  | 0.07 | 100 |  | (6.32×10–2,10,25.7) | 3.70×103 | 0.99 | (120,43.8) | 9.25×103 |  | 0.99 | (4.89×10–2,480,90.4) |  |
| pH=13F |  | 318 |  | 0.07 | 100 |  | (5.79×10–2,10,51.6) | 3.59×104 | 0.99 | (60,83.0) | 1.14×105 |  | 0.98 | (5.21×10–2,180,110.0) |  |

* Third kinetic curve (corresponding to the ARIAN section IIC) starts after passing TRAK (in the range of 90–120 min) and ending it. AAdsorption of  occurs on  and  sites in the kinetic curve, respectively. BAdsorption of  occurs on  and  sites in the first curve and on  site in the second curve. CAdsorption of  occurs on  and  sites in the first curve and on  site in the second curve. DAt pH=5, data in three boxes from left to right belong to the adsorption of on Ph sites (1st kinetic curve), onsites (2nd kinetic curve) and  on  sites (3rd kinetic curve), respectively. EAdsorption of  occurs on  site in the first curve and on  site in the second curve. FAdsorption of  occurs on  site in the first curve and on  site in the second curve.