Supporting Information

Elaboration of lamellar and nanostructured materials based on manganese: Efficient adsorbents for removing heavy metals

Amina Amarray,1 Sanae El Ghachtouli,1* Mohammed Ait Himi,1 Mohamed Aqil,2 Khaoula Khaless,3 Younes Brahmi,2 Mouad Dahbi,2 Mohammed Azzi1

1 Laboratoire Interface Matériaux – Environnement, Faculté des Sciences Ain-Chock, Université Hassan II de Casablanca, B.P 5366 Maarif, Casablanca, Maroc.

2 Materials Science and Nano-engineering Department, Mohammed VI Polytechnic University (UM6P), Ben Guerir, Morocco.

3 Department of Chemical and Biochemical Sciences, Green Process Engineering CBS. Mohammed VI Polytechnic University, Ben Guerir, Morocco.

* Corresponding author: E-mail address: s.elghachtouli@gmail.com.

Supporting Figures

- (b)

(c)

Figure S1. N2 adsorption-desorption isotherms of (a) Na-MnO2, (b) Cocoon-MnO2 and (c) Urchin-MnO2

Figure S2. Comparative study of Cd(II) and Pb(II) removal efficiencies by Na-MnO2, Urchin-MnO2 and Cocoon-MnO2

Figure S3. Langmuir isotherm plot for Pb(II) and Cd(II) adsorption onto Na-MnO2, Urchin-MnO2 and Cocoon-MnO2

Figure S4. Amount of Na+ released during the removal of Pb(II) and Cd(II) ions by Na- MnO2 material

Figure S5. Amount of K+ released during the removal of Pb(II) and Cd(II) ions by Urchin-MnO2 and Cocoon-MnO2

Supporting Tables

Table S1: Porous structure parameters of the Na-MnO2, Urchin-MnO2 and Cocoon-MnO2

|  | Analysis of pore distribution (BJH) (%) | Average pore diameter of adsorption/desorption (Å) (BJH) | Cumulative volume of adsorption/desorption (BJH) (cm3/g) 17Å<d< 3000Å |
| --- | --- | --- | --- |
| Na-MnO2 | Micropores: 17.39 Mesopores: 52.17 Macropores: 30.44 | 66.630/75.844 | 0.0817/0.1232 |
| Urchin-MnO2 | Micropores: 13.63 Mesopores: 54.54 Macropores: 31.82 | 60.657/64.581 | 0.1121/0.1327 |
| Cocoon-MnO2 | Micropores: 14.29 Mesopores: 52.38 Macropores: 33.33 | 59.014/59.290 | 0.1040/0.1189 |

Table S2: Kinetic parameters for adsorption of Pb(II) and Cd(II) on manganese oxides materials

| Pb(II) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Na-MnO2 qexp= 15.76mg/g | Urchin-MnO2 qexp= 12.04mg/g |  | Cocoon-MnO2 qexp= 14.85mg/g |  |
| Pseudo-first order |  |  |  |  |
| qe= 1.33 mg/g | qe= 1.0087 mg/g |  | qe= 3.752 mg/g |  |
| Kt= 0.0184 min-1×g/mg | Kt= 0.0101min-1×g/mg |  | Kt= 0.0239 min-1×g/mg |  |
| R2= 0.9996 | R2= 0.8821 |  | R2= 0.8787 |  |
| Pseudo-second order |  |  |  |  |
| qe= 14.81 mg/g | qe= 12.06 mg/g |  | qe= 14.92 mg/g |  |
| K= 0.058 min-1×g/mg | K= 0.0846 min-1×g/mg |  | K= 0.0478min-1×g/mg |  |
| R2= 0.9998 | R2= 0.9999 |  | R2= 0.9997 |  |
| Cd(II) |  |  |  |  |  |
| Na-MnO2 qexp= 15.13 mg/g |  | Urchin-MnO2 qexp= 10.44 mg/g |  | Cocoon-MnO2 qexp= 12.57 mg/g |  |
| Pseudo-first-order |  |  |  |  |  |
| qe= 2.029 mg/g |  | qe= 2.110 mg/g |  | qe= 8.230 mg/g |  |
| Kt= 0.0177 min-1×g/mg |  | Kt= 0.0026 min-1×g/mg |  | Kt= 0.1308 min-1×g/mg |  |
| R2= 0.8960 |  | R2 = 0.9881 |  | R2= 0.9204 |  |
| Pseudo-second-order |  |  |  |  |  |
| qe = 15.25 mg/g |  | qe= 10.58 mg/g |  | qe= 12.75 mg/g |  |
| K= 0.0192 min-1×g/mg |  | K= 0.0133min-1×g/mg |  | K= 0.043 min-1×g/mg |  |
| R2= 0.9990 |  | R2= 0.9969 |  | R2 = 0.9985 |  |

Table S3: Isotherm parameters for Langmuir, Freundlich and Temkin models

|  | Langmuir isotherm |  |  | Freundlich isotherm |  |  | Temkin isotherm |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | R2 | qm (mg/g) | b | R2 | KF | n | RT/bT | KTKKK KT | R2 |
|  | Pb(II) |  |  |  |  |  |  |  |  |
| Urchin-MnO2 | 0.9844 | 263.85 | 2.435×10-3 | 0.9476 | 45.760 | 4.88 | 19.120 | 205.250 | 0.9825 |
| Cocoon-MnO2 | 0.9820 | 209.64 | 4.146×10-3 | 0.6992 | 34.300 | 6.378 | 10.734 | 909.730 | 0.5783 |
| Na-MnO2 | 0.9409 | 297.62 | 2.290 ×10-3 | 0.8882 | 35.930 | 3 | 26.635 | 0.087 | 0.6829 |
| Cd(II) |  |  |  |  |  |  |  |  |  |
| Urchin-MnO2 | 0.9981 | 191 | 3.032×10-3 | 0.8029 | 0.8366 | 1.185 | 26.661 | 0.442 | 0.5607 |
| Cocoon-MnO2 | 0.9499 | 171.53 | 5.322×10-3 | 0.7745 | 0.650 | 1.291 | 13.178 | 3.027×10-3 | 0.7975 |
| Na-MnO2 | 0.9655 | 199 | 4.635×10-3 | 0.9087 | 2.085 | 1.598 | 31.972 | 8.168×10-4 | 0.7482 |