Table 1. Fitting parameters and goodness of fit for three different isotherm models (Langmuir, Freundlich and Temkin) applied to the experimental adsorption data

| Adsorbents | Langmuir |  |  |  | Freundlich |  |  | Temkin |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Q max (mg/g) |  | KL | R2 | n | KF | R2 | B | KT | R2 |
| OFIP | 20.8 | 0.245 |  | 0.99 | 3.244 | 6.157 | 0.95 | 3.306 | 6.36 | 0.96 |
| Ac-OFIP | 42.02 | 6.102 |  | 0.99 | 5.437 | 25.84 | 0.90 | 3.563 | 8.32 | 0.98 |

Table 2. RL as a function of the initial concentration of Manganese

| Cinitial (mg/l) | 5.55 | 13.875 | 19.425 | 27.75 | 55.5 | 83.25 |
| --- | --- | --- | --- | --- | --- | --- |
| RL (OFIP) | 0.424 | 0.227 | 0.173 | 0.128 | 0.068 | 0.046 |
| RL (Ac-OFIP) | 0.028 | 0.011 | 0.008 | 0.005 | 0.002 | 0.001 |

Table 3. Values of the thermodynamic parameters of the manganese adsorption at different temperatures by OFIP and Ac-OFIP.

| Adsorbent | Temperature/K | KF | ΔG°/kJ.mol-1 | ΔH°/kJ.mol-1 | ΔS°/KJ.mol-1. K-1 |
| --- | --- | --- | --- | --- | --- |
| OFIP | 293 298 303 308 313 | 0.2262 0.2670 0.3248 0.4248 0.3807 | 3.6210 3.2717 2.8330 2.1925 2.5128 | 26.30 | 0.077 |
| Ac-OFIP | 293 298 303 308 313 | 0.8158. 0.9605. 1.3654. 2.9303. 1.7770. | 0.4958 0.0998 -0.7845 -2.7530 -1.4961 | 54.79 | 0.183 |

Table 4. R2 and constant values of the kinetics parameters of the manganese adsorption at different time by OFIP and Ac-OFIP.

| Adsorbent | Pseudo-First-Order | Pseudo-Second-Order | Elovich Model | Intraparticle Diffusion |
| --- | --- | --- | --- | --- |
| OFIP | R2 0.961 Qe (The) 11.61 Qe (exp) 10.92 K1 0.150 | R2 0.996 Qe (The) 11.61 Qe (exp) 14.12 K2 0.006 | R2 0.979 a 4.553 b 0.311 | R2 0.938 ki 1,298 C 2,465 |
| Ac-OFIP | R2 0.986 Qe (The) 28.14 Qe (exp) 17.65 K1 0.156 | R2 0.998 Qe (The) 28.14 Qe (exp) 31.06 K2 0.005 | R2 0.974 a 22.536 b 0.192 | R2 0.946 ki 2.118 C 13.373 |

Table 5. Comparison of the maximum Mn(II) adsorption capacities with other adsorbents.

| Adsorbents | Capacity (mg/g) | Reference |
| --- | --- | --- |
| Pecan nut shell | 103.8 | Vaghetti et al.46 |
| Crab shell particles | 69.9 | Vijayaraghavan et al.47 |
| Ac-OFIP | 42.03 | This study |
| OFIP | 19.50 | This study |
| Natural zeolitic tuff | 10 | Rajic et al.48 |
| Black carrot residues | 5.17 | Güzel et al.49 |
| Activated carbon immobilized Bytannic acid | 1.73 | Uçer et al.50 |
| Kaolinite | 0.44 | Yavuz et al.51 |
| Pithacelobium dulce carbon | 0.41 | Emmanuel et al.7 |