Table1 Basal spacing d001 and 2θ  angle for each cation

| Mt-M | Mt-Na+ | Mt-Fe3+ | Mt-Fe2+ | Mt-Co2+ | Mt-Cr3+ | Mt-Cu2+ | Mt-Ni2+ |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2θ (°) | 5.84 | 6.24 | 6.18 | 6.27 | 6.1 | 7.19 | 6.1 |
| d001 (Å) | 15.12 | 14.15 | 14.28 | 14.08 | 14.48 | 12.28 | 14.48 |

Table 2 Values of cation exchange capacity

| Mt-M | C.E.C (meq/100g) |
| --- | --- |
| Mt-Cu2+ | 47.40 |
| Mt-Co2+ | 111.60 |
| Mt-Ni2+ | 50.60 |
| Mt-Fe2+ | 112.60 |
| Mt-Fe3 + | 108.10 |
| Mt-Cr3+ | 45.10 |

Table 3 Effect of the exchanged cation on Biginelli reaction

| Catalyst | Time (h) | Yield (%) |
| --- | --- | --- |
| Mt-Na+ (raw material) | 32 | 13 |
| Mt-Cu2+ | 7 | 20 |
| Mt-Co2+ | 9 | 57 |
| Mt-Ni2+ | 9 | 20 |
| Mt-Fe2+ | 7 | 34 |
| Mt-Fe3+ | 8 | 60 |
| Mt-Cr3+ | 10 | 24 |
| HCl | 7 | 56 |
| Without catalyst | 11 | 16 |

Table 4 Effect of the catalyst amount on the yield of the reaction

| Catalyst | Catalyst amount (%) | Time (h) | Yield (%) |
| --- | --- | --- | --- |
| Mt-Fe3+ | 20 | 8 | 60 |
| Mt-Fe3+ | 40 | 7 | 68 |
| Mt-Fe3+ | 50 | 7 | 76 |
| Mt-Fe3+ | 60 | 7 | 86 |
| Mt-Co2+ | 20 | 9 | 57 |
| Mt-Co2+ | 40 | 8 | 62 |
| Mt-Co2+ | 50 | 8 | 69 |
| Mt-Co2+ | 60 | 8 | 73 |

Table 5 Effect of the Solvent on the yield of the reaction

|  | Mt-Fe3+ |  | Mt-Co2+ |  |
| --- | --- | --- | --- | --- |
| Solvent | Time (h) | Yield (%) | Time (h) | Yield (%) |
| Ethanol | 7 | 76 | 8 | 69 |
| Water | 7 | 44 | 8 | 36 |
| Toluene | 5 | 62 | 7 | 65 |
| Glacial acetic acid | 5 | 82 | 6 | 77 |

Table 6 Effect of introduction order of reagents

|  | First step |  | Second step |  | Yield (%) |
| --- | --- | --- | --- | --- | --- |
|  | Reagents | operating condition | Reagents | operating condition |  |
| process 1 | Benzaldehyde + Mt-Fe3+ | Stirring, 2h | ethylacetoacetate + urea | Reflux, 7h | 68 |
| Process 2 | Ethylacetoacetate + Mt-Fe3+ | Stirring, 2h | Benzaldéhyde + urea | Reflux, 6h | 81 |
| Process 3 | urea + Mt-Fe3+ | Stirring, 2h | Benzaldéhyde + ethylacetoacetate | Reflux, 5h | 81 |

Table 7 Comparison between Mt-Fe3+ and other catalysts reported in the literature

| Catalyst | Time |  | Yield (%) in ethanol |
| --- | --- | --- | --- |
| Mt-Fe3+ (our study) | 5 h |  | 81 |  |
| PS-PEG-SO3H60 | 10 h |  | 80 |
| PPF-SO3H61 | 8 h |  | 81 |
| Nafion-Ga62 | 1 h |  | 84 |
| ZnO@SBA-1563 | 150 mn | 96 |  |
| Co phthalocyanines64 | 16 h |  | 10 |
| NHC copper complexes65 | 24 h |  | 39 |
| Hf(OTf)466 | 9 h |  | 88 |