Supplementary Material

Physico-chemical properties of the pyrolytic residue obtained by different treatment conditions of meat and bone meal

Marija Zupančič, Nataša Čelan Korošin*

Faculty of Chemistry and Chemical Technology, University of Ljubljana, Večna pot 113, 1000 Ljubljana, Slovenia

*Corresponding author details: Email: Natasa.Celan@fkkt.uni-lj.si, Tel: +386 1 479 8524

Total numbers of tables: 2

Total numbers of figures: 0

Table S1. Hygroscopic moisture and ash content in MBM and T1ABC samples.

| Sample | Hygroscopic moisture/% | Ash content/% |
| --- | --- | --- |
| MBM | 3.20 | 27.12 |
| T1H005 | 2.96 | 57.41 |
| T1H010 | 3.70 | 60.00 |
| T1H020 | 2.90 | 61.00 |
| T1H050 | 3.81 | 64.88 |
| T1H100 | 2.96 | 66.64 |

Table S2. Semi-total concentrations of elements in the MBM and T1H005 samples (the mean of triplicates ± standard deviation).

| Sample | Unit | MBM | T1H005 |
| --- | --- | --- | --- |
| Cr | mg kg─1 | 0.53 ± 0.06 | 1.36 ± 0.08 |
| Ni | mg kg─1 | 0.35 ± 0.01 | 0.90 ± 0.02 |
| Cu | mg kg─1 | 2.7 ± 0.1 | 6.9 ± 0.1 |
| Zn | mg kg─1 | 58.8 ± 0.9 | 151 ± 1 |
| As | mg kg─1 | 0.09 ± 0.01 | 0.19 ± 0.02 |
| Mo | mg kg─1 | 0.31 ± 0.01 | 0.70 ± 0.05 |
| Cd | mg kg─1 | 0.020 ± 0.002 | 0.035 ± 0.007 |
| Pb | mg kg─1 | 1.16 ± 0.04 | 2.97 ± 0.06 |
| Fe | mg kg─1 | 289 ± 10 | 799 ± 2 |
| Ca | g kg─1 | 78.3 ± 4 | 161 ± 1 |
| Mg | g kg─1 | 1.14 ± 0.04 | 2.8 ± 0.5 |
| Na | g kg─1 | 12.4 ± 0.3 | 28.6 ± 0.6 |
| K | g kg─1 | 6.0 ± 0.2 | 12.5 ± 0.5 |
| P | g kg─1 | 21.5 ± 0.9 | 48.4 ± 0.6 |