Fabrication of Zirconium Silicate Reinforced Superhydrophobic Coating for the Evaluation of Corrosion-Resistance

Mubarak Ali Muhamadh Basha1* and Sathiya Srinivasan1

Department of Chemistry, Chikkaiah Naicker College, Erode-638004. Tamilnadu, India.

*Corresponding author Email: mubarakscience@gmail.com  Hand phone: +91- 94433 12819

Total number of pages: 08

Total number of Figures: 06

Total number of Table: 01

Fig. S1: Effect of (a) The concentration of zirconium silicate (b) The anodizing voltage (c) The anodizing temperature (d) The anodization reaction time on growth kinetics of the coating.

Fig. S2: SEM images of SO, Zr1, Zr2, Zr3 and Zr4 coatings.

Fig. S3: Influence of zirconium silicate concentrations SO, Zr1, Zr2, Zr3, Zr4 on microhardness of the coating.

Fig. S4: Representative EDX spectra of SO and Zr3 coating.

Fig. S5: Tafel polarization plots for SA1 and SA2 for bare aluminium and anodized aluminium coatings immersed in a 3.5 percent NaCl solution.

Fig. S6: Nyquist plot curves associated with SA1 and SA2 anodized aluminium Coatings that have been submerged in a 3.5 percent NaCl solution.

Table. S1: Tafel polarisation examinations of bare aluminium, SO, and different Zr anodic coatings anodized at room temperature for 65 minutes yielded corrosion parameters.

| Sample | Open Circuit Potential (V) | Corrosion Potential Ecorr(V) | Corrosion Current Icorr(µAcm-2) | Corrosion resistance Rp (Ωcm-2) |
| --- | --- | --- | --- | --- |
| Bare Al | -0.699 | -0.715 | 1.27 x10-4 | 5173.3 |
| SO | -0.57 | -0.611 | 4.82x10-6 | 15051 |
| Zr1 | 0.189 | -0.578 | 5.91x10-6 | 21932 |
| Zr2 | 0.672 | -0.511 | 1.92x10-6 | 23535 |
| Zr3 | 0.761 | -0.428 | 6.14 x 10-7 | 68956 |
| Zr4 | 0.745 | -0.501 | 4.109x10-7 | 64371 |