100nm

30nm

Fig. 1. TEM images of carbon supported RuNP catalyst

Fig. 2. Cyclic voltammogramms at CPE (thin solid line) and CPE-RuNP modified carbon paste electrodes (A). Influence of the starting potential and scanning domain on the cyclic voltammograms at CPE-RuNP (2.5:1) modified electrode (B). Experimental conditions: electrolyte, 0.15 M phosphate buffer (pH 7); starting potential, -1 vs. Ag/AgCl, KClsat (A, B thin black solid line), 0 V vs. Ag/AgCl, KClsat (B, thick red line); scan rate, 50 mV/s.

| Fig. 3. Influence of the scan rate on the electrochemical response of CPE-RuNP (2.5:1) electrode (A); cathodic current vs.v1/2 dependence of the process (IIc) occurring at different CPE-RuNP modified electrodes (B). Experimental conditions: see figure 2A, error bar for 4 similar measurements |  |
| --- | --- |

Fig. 4. Electroreduction of 3 mM H2O2 at CPE-RuNP modified electrode (A) and CPE (B). Experimental conditions: electrolyte, 0.15 M phosphate buffer (pH 7) (A, B solid line); starting potential, -1 vs. Ag/AgCl, KClsat (A); scan rate, 50 mV/s; graphite:RuNP ratio, see inset legend.

Fig. 5. Cyclic voltammograms at CPE-RuNP (2.5:1) modified electrode at different concentrations of H2O2 (A). Calibration curve of CPE and CPE-RuNP modified electrodes (B). Experimental conditions: see fig. 4.

Fig. 6. Calibration curves for H2O2 electroreduction at CPE and CPE-RuNP modified electrodes. Inset: I vs. time dependence for additions of 0.01 mM H2O2 at CPE-RuNP (2.5:1) modified electrode. Experimental conditions: electrolyte, 0.15 M phosphate buffer (pH 7); applied potential, -0.1 vs. Ag/AgCl, KClsat; rotation speed, 500 rpm

Table 1. Cathodic current intensity dependence on the RuNP amounts in the modified electrodes at fixed values of potential. Experimental conditions: see Fig. 2A.

| Electrode | Ic / A |  |  |
| --- | --- | --- | --- |
|  | Ec = -0.1 V | Ec = -0.3 V | Ec = -0.5 V |
| CPE-RuNP(2.5 : 1)* | -0.48 10-4 ± 0.19 10-4 | -1.26 10-4 ± 0.22 10-4 | -2.54 10-4 ± 0.38 10-4 |
| CPE-RuNP(2.5 : 2)* | -2.00 10-4 ± 0.57 10-4 | -3.17 10-4 ± 0.49 10-4 | -4.71 10-4 ± 0.68 10-4 |
| CPE-RuNP(2.5 : 3)** | -2.45 10-4 ± 1.24 10-4 | -3.69 10-4 ± 1.18 10-4 | -5.71 10-4 ± 1.16 10-4 |

where: * values are mean of 4 measurements; ** values are mean of 3 measurements; Ec is expressed as V vs. Ag/AgCl, KClsat

Table 2. Analytical parameters for CPE-RuNPs modified electrodes. Experimental conditions: see Fig. 6

| Electrodes | Cyclic voltammetry [H2O2] 1 5 mM | Amperometry [H2O2] 0.01 0.1 mM |  |
| --- | --- | --- | --- |
|  | Sensitivity (A/mM) R/n | Sensitivity (A/mM) R/n | LOD*/mM |
| CPE | 0.12 10-5  8.3 10-8 0.9846/4 | 0.13 10-5  8.1 10-8 0.9923/6 | 5.43 10-3 |
| CPE-RuNP(2.5 : 1) | 5.02 10-5  0.43 10-5 0.9640/6 | 4.59 10-5  0.11 10-5 0.9976/11 | 3.78 10-3 |
| CPE-RuNP(2.5 : 2) | 10.79 10-5  0.95 10-5 0.9626/6 | 3.16 10-5  0.17 10-5 0.9878/11 | 8.62 10-3 |
| CPE-RuNP(2.5 : 3) | 12.38 10-5  1.09 10-5 0.9626/6 | 7.88 10-5  0.35 10-5 0.9912/11 | 7.37 10-3 |

*the detection limit was calculated as the ratio between the 3Sa/b where: Sa is the standard deviation of the intercept of the linear regression, and b is the slope of the linear regression (I = a+ b [H2O2]), when the signal/noise ratio is 3.