Figure 1

Figure 1. Structures of Acid blue 29 (a) and Ponceau xylidine (b).

Figure 2

Figure 2. FTIR spectrum of n-Fe2O3 particles.

Figure 3

Figure 3. EDX analysis of n-Fe2O3 particles.

Figure 4

Figure 4. Characterisation of n-Fe2O3 particles: a. TEM image; b. Particle size distribution; c. XRD diffractogram; d. Magnetization curve.

Figure 5

Figure 5. Effect of [HP] (a) and catalyst loading (b) on the absorption spectra: [AB] = [PX] = 0.15 mM; pH= 3; treatment period = 90 min; equilibrium period = 90 min.

Figure 6

Figure 6. Effect of catalyst load on the m-CODeffof mixture of dyes (AB+PX): [HP] = 7.0 mM; [AB] = [PX] = 0.15 mM; pH= 3; equilibrium period = 90 min; treatment period= 90 min.

Figure 7

Figure 7. Effect of residual HP on CODeff of mixture of dyes (AB+PX). Inset: consumption of HP with time. [AB] = [PX] = 0.15 mM; [n-Fe2O3 ] = 4.0 g/L; [HP] = 7.0 mM; pH= 3; equilibrium period = 90 min.

Figure 8

Figure 8. Effect of particle size of catalyst on m-CODeff (a) and reusability of catalyst (b): [AB] = [PX] = 0.15 mM; equilibrium period = 90 min; pH= 3.

Figure 9

Figure 9.  TEM images of n-Fe2O3 particles after different cycles of treatment: [AB] = [PX] = 0.15 mM; [n-Fe2O3] = 4.0 g/L; [HP] = 7.0 mM; treatment period = 300 min; pH = 3.

Figure 10

Figure 10. COD removal kinetics in n-Fe2O3 /HP system: (a) with interference due to HP from 120 min to 300 min (inset: from 0-60 min); (b) Without interference due to HP from 120 to 300 min (inset: from 0-60 min).

Figure 11

Figure 11. Kinetics of HP consumption in n-Fe2O3 /HP system from 120 min to 300 min. (Inset: from 05 min to 60 min)

Figure 12

Figure 12. CFU and light loss (%) in n- Fe2O3/ HP system:  [AB] = [PX] = 0.15 mM; pH of treatment = 3; pH of E. coli growth = 7; [n- Fe2O3] = 4.0 g/L; [HP] = 7.0 mM.