Table 1

Table 1. Optimization of operational parameters of mixture of dyes for n-Fe2O3 /HP and n-Fe2O3 /SPS systems: [AB] = [PX] = 0.15 mM;      [n-Fe2O3 ] = 0.4 g/L; [m-Fe2O3 ] = 0.6 g/L; [HP] = [SPS] = 7.0 mM; pH= 3; treatment period = 90 min.

| Catalyst |  |  |  |  | Oxidant |  |  |  |  | pH |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| [n-Fe2O3 ] (g/L) | Decolorization (%) |  |  |  | [Oxidant] (mM) | Decolorization (%) |  |  |  | pH | Decolorization (%) |  |  |  |
|  | n-Fe2O3 /HP system |  | n-Fe2O3 /SPS system |  |  | n-Fe2O3 /HP system |  | n-Fe2O3 /SPS system |  |  | n-Fe2O3 /HP system |  | n-Fe2O3 /SPS system |  |
|  | AB | PX | AB | PX |  | AB | PX | AB | PX |  | AB | PX | AB | PX |
| 0.1 | 62.0 | 51.7 | 39.9 | 15.8 | 5.0 | 66.1 | 54.3 | 94.3 | 79.7 | 3.0 | 95.0 | 91.4 | 97.0 | 91.4 |
| 0.2 | 82.4 | 72.0 | 47.1 | 23.1 | 6.0 | 86.1 | 84.4 | 96.5 | 89.2 | 5.9 | No decolorisation was observed |  | 95.4 | 84.5 |
| 0.4 | 95.0 | 91.4 | 88.2 | 64.3 | 7.0 | 95.0 | 91.4 | 97.0 | 91.4 | - |  |  | - | - |
| 0.6 | 95.2 | 91.0 | 97.0 | 91.4 | 8.0 | 93.4 | 90.0 | 93.8 | 85.5 | 9.0 |  |  | 94.2 | 82.8 |
| 0.8 | 94.2 | 91.0 | 92.2 | 72.9 | 9.0 | 91.2 | 85.9 | 93.0 | 76.9 | 11.0 |  |  | 25.6 | 03.0 |
| 1.0 | 95.2 | 91.4 | 89.5 | 66.4 | - | - | - | - | - | - | - | - | - | - |

Table 2

Table 2. COD removal efficiency of mixture of dyes (AB+PX): [AB] = [PX] = 0.15 mM;   [n-Fe2O3 ] = 4.0 g/L; [HP] = 7.0 mM; pH= 3; equilibrium period = 90 min.

| Treatment period (Min) | Decolorisation (%) |  | Consumption of [HP] (%) | m-CODeff (%) | CODeff (%) |
| --- | --- | --- | --- | --- | --- |
|  | AB | PX |  |  |  |
| 10 | 71.6 | 65.3 | 64.0 | 4.1 | 31.3 |
| 30 | 83.6 | 77.6 | 64.0 | 6.1 | 33.2 |
| 60 | 97.9 | 96.9 | 67.2 | 10.9 | 35.7 |
| 120 | 100.0 | 100.0 | 76.3 | 29.3 | 45.1 |
| 180 | 100.0 | 100.0 | 87.3 | 47.4 | 58.8 |
| 240 | 100.0 | 100.0 | 95.4 | 55.7 | 74.9 |
| 300 | 100.0 | 100.0 | 98.9 | 72.1 | 83.1 |
| 360 | 100.0 | 100.0 | 99.8 | 78.2 | 83.8 |

m-CODeff – COD removal efficiency in the presence of residual HP

CODeff – COD removal efficiency in the absence of residual HP

Table 3

Table 3. COD removal and HP consumption rate constants for the mixture of dyes (AB+PX) by n-Fe2O3 / HP system at different time intervals

| Time scale | Rate constant (10-3min-1) |  | R2 |  |
| --- | --- | --- | --- | --- |
|  | COD removal rate constants |  |  |  |
|  | HP interference | No HP interference | HP interference | No HP interference |
| 0-60 (min) | 1.49 | 1.32 | 0.98555 | 0.99926 |
| 120-300 (min) | 7.94 | 6.73 | 0.98394 | 0.99036 |
| Time scale | HP consumption rate constants |  |  |  |
| 0 - 60 min | 1.96 |  | 0.8813 |  |
| 120 -300 min | 17.17 |  | 0.9684 |  |

Table 4

Table 4. Ions and intermediate products identified by ion chromatography

| Sr. No. | Ions |  | Intermediate products |  |
| --- | --- | --- | --- | --- |
|  | R.T (min) | Name | R. T (min) | Name |
| 1 | 4.27 | Na+ | 1.54 | Formic acid |
| 2 | 4.54 | NH4+ | 2.63 | Malonic acid |
| 3 | 2.12 | NO2- | 2.81 | Maleic acid |
| 4 | 3.65 | NO3- | 3.37 | Fumaric acid |
| 5 | 4.26 | CO32- | 2.95 | Not identified |
| 6 | 5.56 | SO42- | 3.86 | 3- Amino phenol |
| 7 | --- | --- | 4.57 | 2- Amino phenol |
| 8 | --- | --- | 7.91 | Phenol |