Synthesis and spectral studies of some homo dinuclear lanthanide(III) complexes of a mesogenic Schiff-base

Prem Kumar Shrestha and Pawan Raj Shakya*

Department of Chemistry, Padma Kanya Multiple Campus, Tribhuvan University, Kathmandu, Nepal

∗Corresponding author, E-mail: pawansh2003@yahoo.com

Tel.: +977-1-4218218

Abstract

A mesogenic Schiff-base, N,N’-di-(4-decyloxysalicylidene)-1’,8’-diamino-3’,6’-dioxaoctane (H2L) and a series of homo dinuclear lanthanide(III) complexes of the type [Ln2(LH2)3(NO3)4](NO3)2, (Ln = La, Pr, Nd, Sm, Eu, Gd, Tb, Dy, and Ho) were synthesized and characterized by elemental analysis, mass spectrometry, FTIR, and NMR spectral techniques. The IR and NMR spectral evidences imply bonding of a neutral bidentate H2L species through two phenolate oxygen atoms in its zwitterionic form to LnIII, rendering the overall geometry of the complexes as a seven-coordinate polyhedron – possibly distorted mono-capped octahedron. Differential scanning calorimetry (DSC) and polarizing optical microscopic (POM) studies reveal mesogenic properties (Smectic-X, Smectic-A and nematic mesophases) in the ligand over a wide range of temperature but none mesomorphism in the LnIII complexes synthesized under this study. Luminescence studies exhibit emissions of H2L and TbIII complex.

Keywords: Mesogenic Schiff-base; LnIII Complexes; Zwitterionic-coordination; Mono-capped octahedron; Luminescence

- Introduction

Lanthanide(III) complexes have received much attention due to their potential scientific applications in design of various luminescent metallomesogens1,2, chemosensors1,3 and photoluminescence materials and devices4. Schiff-base ligands having N and/or O donor atoms may assemble coordination architectures in which the LnIII ions can promote Schiff-base condensation5. Mesomorphisms (an anisotropic liquid) in Schiff-base ligands, may be obtained by their careful design in which the molecular order is in between the crystalline and isotropic liquid state.6 By incorporating LnIII ions into the mesogenic Schiff-base, one can obtain useful metallomesogens for the design of emissive LCDs.

The mesogenic properties of the ligands may often be influenced by the nature of coordinated metal ions.7,8 A metallomesogen has the greater tendency to exhibit intermolecular dative coordination in solid state.7,9 The design of metallomesogens is rather difficult because of their high coordination numbers incompatible with the structural anisotropy, the basics for showing liquid crystalline behavior.9 However, the columnar type of LnIII ion containing metallomesogens was first synthesized by Piechocki et al.10 in 1985 followed by the first calamitic LnIII ion containing metallomesogens by Galyametdinov et al.11 in 1991. Lanthanide(III) complexes with high coordination number may be obtained by choice of nitrate as the counter-ion  because it can coordinate in a bi-dentate fashion. In continuation of our earlier work on metallomesogens12-17 we now report here synthesis and spectral studies of a mesogenic Schiff-base (having terminal alkoxy chain next to benzene ring) and of some homo dinuclear LnIII complexes.

2. Experimental

2.1. Starting materials

All the required reagents of analytical grade (AR) were obtained from commercial sources and used without further purification; 1-bromodecane, 2,4-dihydroxybenzaldehyde and 1,8-diamino-3,6-dioxaoctane are from Sigma–Aldrich, USA; all the Ln(NO3)3.xH2O salts are from Indian Rare Earths Ltd. and KI and KHCO3 are from Merck. The organic solvents obtained from commercial vendors were dried using standard methods.18

2.2. Synthesis

Experimental details given in Scheme 1 show synthesis of N,N’-di-(4-decyloxysalicylidene)-1’,8’-diamino-3’,6’-dioxaoctane (H2L), 2, by a two-step process, alkylation of 2,4-dihydroxybenzaldehyde with 1-bromodecane followed by condensation with 1,8-diamino-3,6-dioxaoctane. The LnIII complexes, [Ln2(LH2)3(NO3)4](NO3)2 (Ln = La, Pr, Nd, Sm, Eu, Gd, Tb, Dy, and Ho), 3, were synthesized by reacting the H2L and appropriate metal nitrate in solution state at room temperature.

Scheme 1. Reaction steps involved in the synthesis of 4-decyloxysalicylaldehyde, 1; N,N’-di-(4-decyloxysalicylidene)-1’,8’-diamino-3’,6’-dioxaoctane (H2L), 2, and LnIII complexes, 3.

2.2.1. Preparation of 4-decyloxysalicylaldehyde, 1

Equimolar amounts of 2,4-dihydroxy benzaldehyde (50 mmol, 6.91 g) and 1-bromodecane (50 mmol, 10.4 mL) were mixed with 100 mL of dry acetone and added potassium bicarbonate (55 mmol, 5.51 g). The reaction mixture was refluxed for 30 h in the presence of KI (0.1–0.2 g) as a catalyst. Insoluble solids were removed through hot filtration and subsequently, the filtrate was made neutral by adding 6N hydrochloric acid little at a time and extracted the product twice with 100 mL portions of CHCl3. A straw-yellow solid was obtained upon concentration of the chloroform extracts which was purified by column chromatography over SiO2 by eluting first with n-hexane and then with a mixture of n-hexane and chloroform (v/v, 1/1). The product, 4-decyloxysalicylaldehyde (1) was obtained in the form of a white solid upon evaporation of this purified extract; yield: 68% (9.47 g).

2.2.2. Synthesis of N,N’-di-(4-decyloxysalicylidene)-1’,8’-diamino-3’,6’-dioxaoctane (H2L), 2

A mixture of absolute ethanolic solutions of 4-decyloxysalicylaldehyde, 1, (8.34 g, 30 mmol in 50 mL) and 1,8-diamino-3,6-dioxaoctane (2.22 g, 15 mmol in 15 mL) was refluxing together for 1.5 h in the presence of a few drops of glacial acetic acid. Yellow colored solid, 2, was obtained after the resulting mixture left overnight which was filtered off under suction, thoroughly washed with cold ethanol and dried at room temperature. Yield: 74% (7.43 g), m.p.165 oC. Anal. Calcd for C40H64N2O6 (%): C, 71.82; H; 8.64; N, 4.19. Found (%): C, 71.85; H, 9.65; N, 4.21. 1H NMR (300 MHz; DMSO-d6; J (Hz), ppm) (Figure S1) δ = 0.853 (t, J = 5.7, 3H, –CH3), 1.729 – 1.255 (m, 16H, –(CH2)8 –), 3.507 (t, J = 6.6, 2H, –NCH2), 3.955 (t, J = 6.3, 2H, –OCH2), 6.278 (d, J = 11.4, 1H, Ar–H), 6.329 (s, 1H, Ar–H), 7.191 (d, J = 8.7, 1H, Ar–H), 8.322 (s, 1H, –N=CH), 13.804 (s, br, 1H, ph–OH); 13C{1H}NMR: (75.45 MHz; DMSO-d6; ppm) (Figure S2) δ = 165.39, 163.82, 162.36, 132.45, 111.70, 105.56, 101.40, 67.27; FAB Mass (m/e, fragment, % intensity): the molecular ion as base peak (668, M+, 100) generates simultaneously four fragments, M1-M4; M1: 349, C10H21OC6H3(OH)CH=NC2H4OCH2CH2+, 28%; M2: 321, C10H21OC6H3(OH)CH=NCH2CH2O+, 25%; M3: 305, C10H21OC6H3(OH)CH=NCH2CH2+, 35%; M4 (generated from M3): 164, (OH)C6H3(OH)CH=NCH2CH2+, 25%; IR (cm-1, KBr disk): 3458 (–OH), 1628 (─C=N), 1150 (─Cph─O).

2.2.3. Synthesis of LaIII complex, [Ln2(LH2)3(NO3)4](NO3)2, 3

Mixing of THF solutions of H2L (2.01 g, 3.0 mmol in 30 mL) and of La(NO3)3 6H2O (0.87 g, 2.0 mmol in 20 mL) under magnetic stirring turned the resultant solution cloudy after 15 min. A light yellow colored solid separated upon continuous stirring for 3 h at room temperature was filtered off under suction, washed repeatedly with cold methanol, and dried over fused CaCl2 in a desiccator. Yield: 65% (1.73 g) as yellow solid; m.p. 245 oC (decompose); Anal. Calcd for La2C120H192N12O36 (%): C, 54.25; H, 7.28; N, 6.33; La, 10.46; Found (%): C, 54.30; H, 7.30; N, 6.37 and La, 10.51; 1H NMR (300 MHz; DMSO-d6; J (Hz), ppm) (Figure S3) δ = 0.881 (t, J = 5.4, 3H, –CH3), 1.712-1.287 (m, 16H, –(CH2)8–), 3.540 (t, J = 6.3, 2H, –NCH2), 3.982 (t, J = 6.3, 2H, –OCH2), 6.341 (d, J = 6.6, 1H, Ar–H), 6.358 (s, 1H, Ar–H), 7.223 (d, J = 8.7, 1H, Ar–H), 8.356 (s, 1H, –N=CH), 9.272 (s, br, 1H, –N+H); 13C{1H}NMR: (75.45 MHz; DMSO-d6; ppm) (Figure S4) δ = 166.07, 162.61, 164.02, 132.75, 111.67, 105.64, 101.56, 67.35; IR (cm−1, KBr disk): 3046 (ν–N+H), 1658 (ν–C=N), 1124 (ν–Cph–O).

All the other LnIII complexes (Ln = Pr, Nd, Sm, Eu, Gd, Tb, Dy, and Ho) were synthesized in an analogous way by using the appropriate hydrated salt of LnIII nitrate; the physical properties and the analytical data of all the complexes are given in Table 1 while the NMR data of the ligand (H2L) and the LaIII complex are presented as supplementary data. Infrared spectral data of the ligand and complexes are given in Table 2; the data of two representative complexes are given below: [Gd2(LH2)3(NO3)4](NO3)2: IR (cm−1, KBr disk): 3026 (–N+H), 1654 (–C=N), 1124 (–Cph–O); [Ho2(LH2)3(NO3)4](NO3)2: IR (cm-1, KBr disk): 3038 (–N+H), 1654 (─C=N), 1124 (─Cph─O).

2.3. Physical measurements

The LnIII ions in the complexes were determined complexometrically by titrating against the standard EDTA solution using xylenol orange as a metal ion indicator. The elemental contents (C, H and N) were analyzed on an Exeter Analyzer, Model CE-440 CHN. Bruker Av III HD (DRX) 300 MHz FT-NMR multinuclear spectrometer was used to record the 1H and 13C NMR spectra while Bruker IFS66 FTIR spectrometer recorded IR spectra within the 4000–400 cm−1 region using KBr pellets. Mass spectra were recorded on JEOL SX-102 FAB mass spectrometer. UV–vis spectra were recorded on Shimadzu spectrophotometer, model Pharmaspec-UV 1700. The molar conductance of the complexes was determined in 10-3 M solutions on a digital conductivity meter (Model alpha-06, ESICO International) using a commercial conductivity ‘dip cell’ of cell constant, 1.03. Magnetic susceptibility measurements were made at room temperature on a Cahn–Faraday balance using Hg[Co(NCS)4] as the calibrant. Mesophases were identified by the optical textures using an Olympus BX60 Polarizing Optical Microscope (POM) equipped with a Linkam THMS600 hot stage and a Linkam TMS93 programmable temperature controller (heating and cooling rates of 2oC/min). Differential Scanning Calorimetry (DSC) studies were made on a Mettler-Toledo DSC822e module (scan rate 10°C/min under a helium flow, aluminum cups). Fluorescence measurements were recorded at room temperature in a mixed solvent of CHCl3/DMSO solutions (3:1 v/v; 10-4 mol L-1; λex, 380 nm) on a Perkin Elmer LS-45 luminescence spectrometer (10 nm slit width on both excitation and emission).

3. Results and discussion

| Table 1. General and analytical data of H2L and of LnIII metal complexes. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| H2L/complex formula weight (empirical formula) | Colour, yield | m.p. (oC) | Found (Calcd.)% |  |  |  | μeff (van Vleck) value, B.M. |
|  |  |  | C | H | N | M |  |
| H2L, 668.95 (C40H64N2O6) | Yellow, 74% | 165 | 71.85 (71.82) | 9.65 (9.64) | 4.21 (4.19) | - | - |
| [La2(LH2)3(NO3)4](NO3)2 2656.68 (La2C120H192N12O36) | Light yellow, 65% | 245d | 54.30 (54.25) | 7.30 (7.28) | 6.37 (6.33) | 10.51 (10.46) | Diamag. |
| [Pr2(LH2)3(NO3)4](NO3)2 2660.69 (Pr2C120H192N12O36) | Light yellow, 66% | 242d | 54.15 (54.12) | 7.28 (7.27) | 6.38 (6.32) | 10.66 (10.59) | 3.90 (3.40-3.60) |
| [Nd2(LH2)3(NO3)4](NO3)2 2667.35 (Nd2C120H192N12O36) | Light yellow, 72% | 238d | 54.10 (54.03) | 7.28 (7.26) | 6.28 (6.30) | 10.90 (10.82) | 3.94 (3.50-3.60) |
| [Sm2(LH2)3(NO3)4](NO3)2 2679.59(Sm2C120H192N12O36) | Light yellow, 69% | 240d | 53.82 (53.79) | 7.26 (7.22) | 6.30 (6.27) | 11.30 (11.22) | 1.87 (1.50-1.60) |
| [Eu2(LH2)3(NO3)4](NO3)2 2682.80 (Eu2C120H192N12O36) | Light yellow, 74% | 255d | 53.75 (53.72) | 7.23 (7.21) | 6.32 (6.27) | 11.37 (11.33) | 4.56 (3.40-3.60) |
| [Gd2(LH2)3(NO3)4](NO3)2 2693.37(Gd2C120H192N12O36) | Light yellow, 70% | 258d | 53.49 (53.51) | 7.23 (7.19) | 6.29 (6.24) | 11.71 (11.68) | 10.84 (7.80-8.00) |
| [Tb2(LH2)3(NO3)4](NO3)2 2696.72 (Tb2C120H192N12O36) | Light yellow, 67% | 260d | 53.47 (53.45) | 7.21 (7.18) | 6.28 (6.23) | 11.86 (11.79) | 11.84 (9.40-9.60) |
| [Dy2(LH2)3(NO3)4](NO3)2 2703.87 (Dy2C120H192N12O36) | Light yellow, 70% | 257d | 53.35 (53.30) | 7.20 (7.16) | 6.27 (6.22) | 12.09 (12.02) | 12.47 (10.40-10.50) |
| [Ho2(LH2)3(NO3)4](NO3)2 2608.73 (Ho2C120H192N12O36) | Light Yellow, 68% | 258d | 53.22 (53.21) | 7.19 (7.14) | 6.26 (6.21) | 12.25 (12.18) | 14.36 (10.30-10.50) |
| d = decomposition |  |  |  |  |  |  |  |

3.1. Properties of the complexes

The analytical data on elemental analyses, general behavior and some important physical properties of the LnIII complexes are given in Table 1. The LnIII complexes synthesized under the study are of the type [Ln2(LH2)3(NO3)4](NO3)2 indicating 2:3 metal to ligand stoichiometry with nitrate groups present both outside and within the coordination sphere. The molar conductivity measurements in 10-3 M DMF solutions (110 – 125 Ω-1 cm2 mol-1) of the LnIII complexes imply 2:1 electrolytic behavior.19

3.2. FAB-mass spectral study of H2L

The formation of the Schiff-base ligand (H2L), in addition to the IR and NMR spectral techniques to be discussed later, was further confirmed by the FAB mass spectrum. The molecular ion peak as well as base peak that corresponds to the m/e value of 668, matches with the molecular weight of the ligand (668.95) having the molecular formula, C40H64N2O6. The 100% intensity of the molecular ion peak as the base peak is as expected for the molecule on the basis of its predominant aromatic character; the major fragment peaks (m/e = 349, 321, 305, 164) are due to C10H21OC6H3(OH)CH=NC2H4OCH2CH2+, C10H21OC6H3(OH)CH=NCH2CH2O+, C10H21OC6H3(OH)CH=NCH2CH2+, and (OH)C6H3(OH)CH=NCH2CH2+ species respectively.

3.3. IR spectral studies

The important infrared spectral data of H2L and its LnIII complexes are presented in Table 2.

| Table 2. IR Spectral data* (cm-1) of H2L and of LnIII metal complexes |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H2L/Complexes | (O-H) phenol | ν (N+H) | (C=N) | (C─O) phenolic | ν(NO3) |  |  |  |  |
|  |  |  |  |  | ν5 | Ionic | ν1 | ν2 | ν5- ν1 |
| H2L | 3458 b | - | 1628 s | 1150 m | - | - | - | - | - |
| [La2(LH2)3(NO3)4](NO3)2 | - | 3046w | 1656 | 1124 | 1470 | 1386 | 1290 | 794 | 180 |
| [Pr2(LH2)3(NO3)4](NO3)2 | - | 3042 | 1654 | 1118 | 1469 | 1386 | 1294 | 794 | 175 |
| [Nd2(LH2)3(NO3)4](NO3)2 | - | 3040 | 1654 | 1126 | 1470 | 1380 | 1292 | 791 | 178 |
| [Sm2(LH2)3(NO3)4](NO3)2 | - | 3042 | 1654 | 1124 | 1470 | 1382 | 1292 | 792 | 180 |
| [Eu2(LH2)3(NO3)4](NO3)2 | - | 3030 | 1654 | 1124 | 1468 | 1381 | 1288 | 793 | 181 |
| [Gd2(LH2)3(NO3)4](NO3)2 | - | 3026 | 1654 | 1124 | 1467 | 1372 | 1290 | 791 | 177 |
| [Tb2(LH2)3(NO3)4](NO3)2 | - | 3036 | 1654 | 1122 | 1471 | 1378 | 1294 | 792 | 177 |
| [Dy2(LH2)3(NO3)4](NO3)2 | - | 3028 | 1654 | 1126 | 1472 | 1378 | 1292 | 793 | 180 |
| [Ho2(LH2)3(NO3)4](NO3)2 | - | 3038 | 1654 | 1124 | 1470 | 1382 | 1290 | 794 | 180 |
| * Spectra recorded as KBr pellets; b: broad; w: weak; s: sharp; m:medium |  |  |  |  |  |  |  |  |  |

The broad absorption, centered at 3458 cm-1 and characteristic of ν(O–H)phenolic20 involving considerable H-bonding, disappears in spectra of the complexes due to shifting of the phenolic proton to the azomethine nitrogen, resulting in formation of the zwitterion. The weak/medium intensity bands of the H2L centered at 1150 cm-1 are assigned to ν(C–O)phenolic. The strong intensity band appearing at 1628 cm-1, which is assignable21 to ν(C=N) of azomethine, undergoes a hypsochromic shift in all the complexes on account of zwitterion formation. Thus, the complexation of the H2L to LnIII results in migration of phenolic protons onto the two uncoordinated imino nitrogen atoms, which then are intramolecularly hydrogen bonded to metal-bound phenolate oxygen atoms to give the zwitterionic structure, N+–H….O–. Such zwitterionic behavior is in consistent with the study of Binnemans et al.22 who also reported similar observation for acyclic Schiff-base lanthanide complexes. The band frequencies of ν(C=N) shifting to higher wave numbers upon complexation, also provide further evidence implying the presence of the C–N+ and the non-involvement of nitrogen in complex formation.23 Further, the present complexes are characterized by a strong band at 1656–1654 cm-1 due to ν(C=N) and a weak broad band at 3046–3026 cm-1 due to H-bonded N+–H….O– vibration of the protonated imine.23 Thus, the above evidence supports for none involvement of bonding between lanthanide and the imine nitrogen; instead the ligand coordinates to the LnIII ions via the negatively charged phenolic oxygen.

The LnIII complexes also exhibit three additional characteristic bands of the vibrational modes of the coordinated nitrate groups (C2v symmetry) at 1472–1467, 1294–1288, and 794–791 cm-1.24 Besides, the mono- and bidentate chelating nitrates in the complexes may be distinguished on the basis of the profile and separation of the modes associated with asymmetric nitrate vibrations. Accordingly, a bidentate coordinated nitrate is indicated by the magnitude of splitting (181–175 cm-1) at higher energies.24,25 The non-coordinated nitrate present in the ionization sphere is supported by additional bands at 1386–1372 cm-1.

3.4. 1H and 13C NMR spectral studies

A comparison of 1H NMR spectral data of the ligand with that of the LaIII complex shows the phenolic –OH signal (δ, 13.804) that appear in the ligand, disappears later upon complexation. Further, the 1H NMR spectral data imply the shifting of phenolic protons to the two uncoordinated imino nitrogen atoms, which give zwitterionic structure (=N+–H….O–) by intramolecularly hydrogen-bonding to the metal-bound phenolate oxygen atoms; as such is designated as LH2.26 Besides, the LaIII complex (δ, 8.356) shows a signal corresponding to the imine hydrogen, –CH=N, that got broadened when compared with that of the ligand (δ, 8.322). Further, the LaIII complex shows a new signal, characteristic of –N+H resonance, at 9.272 δ while such a signal is absent in the ligand. The results are in accordance with similar observations made by Binnemans et al.,27 on metallomesogens, [Ln(LH)3(NO3)3], where LH = 4-alkoxy-N-alkyl-2-hydroxy benzaldimine. Thus, the metal complex has its’ Schiff base ligand existing in a zwitterionic form, with the phenolic oxygen deprotonated and the imine nitrogen protonated (scheme 2), as supported evidently by IR and NMR spectral data.

Scheme 2. Depiction of migration of phenolic protons to imine nitrogens of the ligand, H2L, during the formation of zwitter ion.

The 13C{1H} NMR spectral data show a significant shift of the –NCH signal (δ, 165.39 in case of H2L and δ, 166.07 in the LaIII complex) implying the two phenolate oxygen atoms of H2L bonded to LaIII in the zwitterionic form. The carbons directly attached to the phenolate group showed similar shifts while those for the other carbon signals were of lower magnitude.

3.5. Magnetic and electronic spectral studies

The µeff values (at room temperature) of all the LnIII complexes (Table 1) under the present study have been found to be higher than the reported van Vleck values. These abnormal µeff values, attributed to metal–metal interactions, are in good agreement with similar complexes reported in literatures.28-30

| Table 3. Electronic spectral data of the selected metal complexes of H2L. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Pr(III) |  |  |  | Nd(III) |  |  |
| Transitions/ Bonding parameters | λmax (cm-1) aq. ion |  | λmax (cm-1) complex | Transitions/ Bonding parameters | λmax (cm-1) aq. ion | λmax (cm-1) complex |
| 1G4← 3H4 | 9900 |  | 9800 | 4F3/2 ← 4I9/2 | 11,450 | 11,435 |
| 1D2*← | 16850* |  | 16,840 | 4F5/2 ← | 12,500 | 12,484 |
| 3P0 ← | 20800 |  | 20,760 | 4S3/2, 4F7/2 ← | 13,500 | 13,430 |
|  |  |  |  | 4F9/2 ← | 14,800 | 14,694 |
|  |  |  |  | 2H11/2 ← | 15,900 | 15,850 |
|  |  |  |  | 2G7/2*← | 17,400* | 17,196 |
|  |  |  |  | 4G7/2 ← | 19,100 | 19,015 |
| β |  |  | 0.993 |  |  | 0.995 |
| b1/2 |  |  | 0.059 |  |  | 0.050 |
| %δ |  |  | 0.705 |  |  | 0.503 |
| η |  |  | 0.003 |  |  | 0.002 |
| Sm(III) |  |  |  | Dy(III) |  |  |
| 6F9/2←6H5/2 |  | 9200 | 9174 | 6H7/2 ←6H15/2 6F9/2 ← | 9100 | - |
| 6F11/2 ← |  | 10,500 | 10,352 |  |  |  |
| 4G5/2 ← |  | 17,900 | - | 6H5/2 ← | 10,200 | 10,156 |
| 6P7/2* ← |  | 26,750* | 26,197 | 6F7/2 ← | 11,000 | 10,952 |
| 4D7/2 |  | 29,100 | 29,185 | 6F5/2 ← | 12,400 | 12,392 |
|  |  |  |  | 4F7/2 ← | 25,800 | 25,828 |
| β |  |  | 0.991 |  |  | 0.998 |
| b1/2 |  |  | 0.067 |  |  | 0.032 |
| %δ |  |  | 0.908 |  |  | 0.200 |
| η |  |  | 0.004 |  |  | 0.001 |
| *Hypersensitive band. |  |  |  |  |  |  |

The electronic spectra of only the PrIII, NdIII, SmIII, and DyIII complexes (Table 3) were recorded in qualitative solution state from 200 to 1100nm, in view of their ability to show hypersensitive bands. The considerable red shifts in the λmax values of the above complexes compared to those of the corresponding aqua ions31 are attributed to the Nephelauxetic effect32 which is regarded as a measure of covalency of the bonding between the metal ions and the ligands. Various bonding parameters (Table 3), viz., Nephelauxetic ratio (β), bonding parameter (b1/2), Sinha’s parameter (%δ), and covalency angular overlap parameter (η), calculated by the procedures as reported33, suggest a weak covalent nature of the metal–ligand bonds.

Figure 1. Proposed Polyhedron (Mono-capped Octahedron) for [Ln2(LH2)3(NO3)4](NO3)2 :

Ln =  La, Pr, Nd, Sm, Eu, Gd, Tb, Dy and Ho

Based on the above spectral evidences, the seven-coordinate geometry, possibly in a distorted mono-capped octahedron (Figure 1) may be proposed to all the present complexes in which the mesogenic Schiff-base, N,N’-di-(4-decyloxysalicylidene)-1’,8’-diamino-3’,6’-dioxaoctane (H2L), 2, coordinates to the LnIII ions in a neutral bidentate fashion.

3.6 Optical and thermal studies

The DSC (recorded in the second heating and cooling cycle with heating rate of 10oC/min) and POM (heating and cooling rates of 2oC/min) were employed to study liquid crystalline (mesogenic) properties of the ligand and those of the LnIII complexes. The corresponding transition temperatures, enthalpy, and entropy changes are given in Table 4.

| Table 4. Thermodynamic data (transition temp., enthalpy and entropy changes). |  |  |  |  |
| --- | --- | --- | --- | --- |
| Ligand | Transitiona | Tb (C) | Hb (kJ mol-1) | S (J mol-1 K-1) |
| H2L | Cr – SmX | 91.84 | 10.62 | 29.11 |
|  | SmX– SmA | 116.96 | 10.52 | 26.98 |
|  | SmA – N | 131.93 | 16.52 | 40.80 |
|  | N – I | 162.85 | 6.09 | 13.97 |
|  | I – N | 148.53 | 2.39 | 5.67 |
|  | N – SmX | 141.73 | 1.12 | 2.70 |
|  | SmX – Cr | 89.96 | 20.20 | 55.65 |
| aCr: Crystal; SmX: Smectic-X; SmA: Smetic-A; N: Nematic; I-Isotropic liquid bData as obtained from the DSC cycle |  |  |  |  |

The POM study revealed optical textures of the H2L (Figure 2) implying smectic-X (SmX), smectic-A (SmA) and nematic (N) mesophases while none of the LnIII complexes reported here exhibited mesomorphism. The non-mesomorphism in the LnIII complexes may be attributed to very high thermal energy required to melt completely the alkoxy chains of the complexes. Under the given situation of high energy level, the layered structure in the complexes breaks down prior to the alkoxy chains, losing thereby the mesogenic properties of the materials.27

Figure 2. Optical textures of Schiff-base (H2L): (a) Smectic-X (SmX), (b) Smectic-A (SmA)

and (c) Nematic (N)

3.7. Luminescence studies

The H2L shows fluorescence (Figure 3a) with an emission band at 410 nm due to intra-ligand transition and the TbIII complex (Figure 3b) with four typical metal-centered emission bands at 490 nm (5D4→7F6), 547 nm (5D4→7F5), 620 nm (5D4→7F3), and 685 nm (5D4→7F0) respectively.34

Figure 3. The fluorescence spectra of (a) H2L and (b) TbIII complex.

Under the same experimental conditions, the observed fluorescence intensities of the SmIII, EuIII and DyIII complexes were observed to be weak (spectra not shown) and their emission spectra also did not show any bands characteristic of metal-centered emission. Thus, it may be inferred that the H2L is likely to be a suitable organic chelator to absorb energy and transfer the same to TbIII ion, implying the well-known intramolecular energy transfer mechanism exhibited by lanthanide Schiff-base complexes.35

4. Conclusion

The mesogenic (SmX, SmA and N) Schiff-base, N,N’-di-(4-decyloxysalicylidene)-1’,8’-diamino-3’,6’-dioxaoctane (H2L), coordinates to LnIII ions (Ln = La, Pr, Nd, Sm, Eu, Gd, Tb, Dy, and Ho) as a neutral bidentate species to yield seven-coordinate non-mesogenic complexes of the formula, [Ln2(LH2)3(NO3)4](NO3)2, the polyhedron being possibly distorted mono-capped octahedron. The neutral bidentate H2L coordinates to LnIII in a zwitterionic form through two phenolate oxygen atoms along with bonding of nitrato groups in similar bidentate fashion. Luminescence of the H2L and TbIII complex arises due to intra-ligand and metal-centered emissions respectively.

Acknowledgements

One of the authors, P.R. Shakya gratefully acknowledges the University Grants Commission (UGC), Kathmandu, Nepal, for research fellowship.

References

1. 	D. Parker, R.S. Dickins, H. Puschmann, C. Crossland, J.A.K. Howard, Chem. Rev. 2002, 102, 1977–2010; DOI: 10.1021/cr010452+

2. 	C. Piguet, J.C.G. Bunzli, B. Donnio, D. Guillon, Chem. Commun. 2006, 3755–3768; DOI: 10.1039/B605737C

3. 	L.J. Charbonniere, R. Ziessel, M. Montalti, L. Prodi, N. Zaccheroni, C. Boehme, G. Wipff, J. Am. Chem. Soc. 2002, 124, 7779–7788; DOI: 10.1021/ja0200847

4.  	H.J. Zhang, R.H. Gou, L. Yan, R.D. Yang, Spectrochim. Acta Part A 2007, 66, 289–294; DOI: 10.1016/j.saa.2006.02.054

5.		M. Tsiouri, N. Hadjiliadis, T. Arslan, B.M. Kariuki, J.C. Plakatouras, Inorg. Chem. Commun. 2006, 9, 429-432; DOI:10.1016/j.inoche.2005.12.018

6.		K. Lodewyckx, R.V. Deun, K. Binnemans, Mater. Sci. Eng. C 2001, 18, 217-221; DOI:10.1016/S0928-4931(01)00361-7

7.		A.M. Giroud-Godquin, P.M. Maitlis, Angewandte Chemie 1991, 30, 375-402; DOI:10.1002/anie.199103751

8.		D.W. Bruce, In Inorganic Materials, 2nd ed.; Bruce, D.W., O’Hare, D., Eds.; Wiley: Chichester, Chapter 8, 1996, pp 405–490.

9. 		K. Binnemans, K. Lodewyckx, Angewandte Chemie 2001, 13, 248–244; DOI:10.1002/1521-3773(20010105)40:1<242::AID-ANIE242>3.0.CO;2-O

10.		C. Piechocki, J. Simon, J.J. Andre, D. Guillon, P. Petit, A. Skoulios, P. Weber, Chem. Phys. Lett. 1985, 122, 124-128; DOI:10.1016/0009-2614(85)85490-7

11.		Y.G. Galyametdinov, G.I. Ivanova, I.V. Ovchinnikov, Bulletin of the Academy of Sciences of the USSR Division of Chemical Science, 1991, 40, 1109-1115.

12.		P.R. Shakya, A.K. Singh, T.R. Rao, Spectrochim. Acta A 2011, 79, 1654-1659; DOI:10.1016/j.saa.2011.05.030

13.		P.R. Shakya, A.K. Singh, T.R. Rao, Mater. Sci. Eng. C 2012, 32, 1906-1911; DOI:10.1016/j.msec.2012.05.039

14.		P.R. Shakya, A.K. Singh, T.R. Rao, J. Coord. Chem. 2012, 65, 3519-3529; DOI:10.1080/00958972.2012.719225

15.		P.R. Shakya, A.K. Singh, T.R. Rao, Synth. Rect. Inorg. Met. Org. Chem. 2014, 44, 739-747; DOI:10.1080/15533174.2013.790056

16.		A.K. Singh, S. Kumari, P.R. Shakya, T.R. Rao, Mater. Sci. Eng. C 2011, 31, 1111-1114; DOI:10.1016/j.msec.2011.04.006

17.		P.K. Shrestha, P.R. Shakya, J. Nepal Chem. Soc. 2020, 41, 16-25; DOI:10.3126/jncs.v41i1.30509

18.		A. Weisberger, F.S. Praskver, Organic Solvents, International Publishers Inc., New York, 1956, p. 1263.

19.		W.J. Geary, Coord. Chem. Rev. 1971, 7, 81-122; DOI:10.1016/S0010-8545(00)80009-0

20.		R.M. Silverstein, F.X. Webster, Spectrometric Identification of Organic Compounds, 6th Ed., John Wiley & Sons Inc., New York, 2002.

21.		N.B. Colthup, L.H. Daly, S.E. Wiberley, Introduction to Infrared and Raman Spectroscopy, 3rd Ed., Academic Press, New York, 1990.

22.		K. Binnemans, D.W. Bruce, S.R. Collinson, R. Van Deun, Y.G. Galyametdinov, F. Martin, Philos. Trans. R. Soc. Lond., Ser. A 1999, 357, 3063-3077; DOI:10.1098/rsta.1999.0481

23.		K. Binnemans, R. van Deun, Christiane G. Walrand, W. Haase, D.W. Bruce, L. Malykhina, Y.G. Galyametdinov, Mater. Sci. Eng. C 2001, 18, 247-254; DOI:10.1016/S0928-4931(01)00369-1

24.		B. Keshavan, P.G. Chandrashekara, N.M. Made Gowda, J. Mol. Struct. 2000, 553, 193-197; DOI:10.1016/S0022-2860(00)00551-2

25.		J. Nawrocka, V. Patroniak, J. Alloys Compd. 2004, 380, 159-162; DOI:10.1016/j.jallcom.2004.03.079

26.		P. Bag, U. Flörke, K. Nag, Dalton Trans. 2006, 26, 3236-3248; DOI:10.1039/B516306D

27.		K. Binnemans, Y.G. Galyametdinov, R. van Deun, D.W. Bruce, S.R. Collison, A.P. Polishchuk, I. Bikechantaev, W. Hasse, A.V. Prosvirin, L. Tinchurina, I. Litvinov, A. Gubajdullin, A. Rakhamatullin, K. Uytterhoeven, L. VanMeervelt, J. Am. Chem. Soc. 2000, 122, 4335-4344; DOI:10.1021/ja993351q

28.		W. Plass, G. Fries, Z. Anorg, Allg. Chem. 1997, 623, 1205–1207;  DOI:10.1002/zaac.19976230804

29.		J.P. Costes, F. Dahan, A. Dupuis, S. Lagrave, J.P. Laurent, Inorg. Chem. 1998, 37, 153–155; DOI:10.1021/ic9712481

30.		J.P. Costes, A. Dupuis, J.P. Laurent, Inorg. Chim. Acta 1998, 268, 125–130; DOI:10.1016/S0020-1693(97)05628-4

31.		R. Reisfeld, C.K. Jorgensen, Lasers and Excited States of Rare Earths, SpringerVerlag, Berlin, 1977.

32.		W.T. Carnall, P.R. Fields, K. Rajnak, J. Chem. Phys. 1968, 49, 4424–4442;  DOI:10.1063/1.1669893

33. 	T.R. Rao, P.A. Kumar, Synth. Rect. Inrg. Met. Org. Chem. 1995, 25, 1011-1026; DOI:10.1080/15533179508218277

34.		T. Gao, P.F. Yan, G.M. Li, G.F. Hou, J.S. Gao, Inorg. Chim. Acta 2008, 361, 2051–2058; DOI:10.1016/j.ica.2007.10.021

35. 	R.D. Archer, H. Chen, L.C. Thompson, Inorg. Chem. 1998, 37, 2089–2095; DOI:10.1021/ic960244d