Synthesis and Application of Silica Supported Calix[4]arene Derivative as Processing Aid Agent for Decreasing Rolling Resistance of Rubber Compounds Used in Tire Tread Formulation

Seyedeh Nazanin Sadat-Mansouri,1 Nasrin Hamrahjou,1 Saeed Taghvaei-Ganjali,1,* Reza Zadmard2

1 Chemistry Department, IA-University, North Tehran Branch, Tehran 1651153311, Iran

2 Chemistry and Chemical Engineering Research Center of Iran, Tehran, Iran

* Corresponding author: s_taghvaei@iau-tnb.ac.ir

Phone: +989128588434

Abstract

One of the most important properties in rubber compounds used in tire is rolling resistance. There are a lot of ways to reduce this parameter both in construction improvement of tire and changing in rubber compound formulation specially in tire tread formulation. Rubber scientists try to introduce new processing aid agents beyond the traditional tire components for reducing the rolling resistance. In this study a unique structure of silica supported calix[4]arene (SS-CSC[4]A) has been synthesized and applied as processing aid agent in tire tread formulation. Fourier-transform infrared spectroscopy (FTIR), Nuclear Magnetic Resonance (1HNMR and 13CNMR), 29Si CP/MAS spectroscopy, thermal gravimetric analysis (TGA), elemental analysis and acid-base titration were used to characterize the structure of it. Scanning Electron Microscopy (SEM) use to investigate the effect of prepared material on qualification of filler dispersion in rubber matrix. The viscoelastic properties of prepared rubber compound were measured by Dynamic Mechanical Thermal Analysis (DMTA) which showed the great decrease in rolling resistance of rubber compound based on SS-CSC[4]A as processing aid agent. The mechanical and rheological properties of obtained tread rubber compound measured by tensometer and MDR rheometer. The results showed no sensible changes in these properties.

Keywords: Rolling resistance; tire tread compound; silica supported calix[4]arene; dynamic mechanical thermal analysis; processing aid agent; wet grip.

- Introduction

Styrene-butadiene rubbers (SBRs) are a group of synthetic elastomer which consist of styrene and butadiene units.1 These rubbers have a huge contribution in the production of car tires2 because of their unique properties of excellent abrasion resistance and good aging stability.3, 4 It is notable that the ratio of styrene and butadiene has an important role in the properties of final product.

SBR and BR are used as elastomers because of their amorphous structures. Absence of crystalline structures in these polymers gives rise to the low mechanical properties which hinders their uses.5 One of the most effective ways to improve the mechanical properties of these polymers is to prepare their compounds with the addition of fillers such as carbon black or silica.6 Although, the addition of such a rigid additive to the SBR and BR blends can increase their mechanical strength, it can complicate the processability, decrease the adhesion and rises the friction between the tires and the surface which results in the high rolling resistance, heat build-up and fuel consumption.7, 8

As a best of our knowledge, high performance rubber tread is in high demand, for example, high wet skid resistance (WSR) and low rolling resistance, which is in line with the concept of "green tires".9 Thus, it is necessary to find alternative processing aid agents for using in rubber compounds to reduce heat build-up and rolling resistance. Generally, the processing aid agents used in rubber industry are regular according to their hydrocarbons length and structure, polymers with low molecular weight, resins, fatty acids, and other hydrocarbon compounds.10 Recently, Song11 has reported a silica-based processing aid agent, utilizing terpene phenol resin (TPR) which enhanced the mechanical and fatigue properties, Kukreja et al.12 found that adding palm oil in an NBR rubber matrix improved the aging resistance and plasticizing efficiency, Asharf et al.13 reported that poly (methyl methacrylate) (PMMA) compounds with palm oil exhibited enhanced mechanical properties. Veiga et al.14 investigated the replacement of carbon black by silica-organosilane coupling agent system and the number of processing steps on the mechanical properties, rolling resistance, and wet grip of truck tire treads. Hua et al.15 studied the effect of vinyl and phenyl group content on the physical, dynamic and mechanical properties of HVBR and SSBR. Mensah et al.16 explored the physico-mechanical properties of variable rubber blends including epoxide natural rubber (ENR), polybutadiene rubber (BR), and solution polymerized styrene-butadiene rubber (SBR) filled by silanized silica and carbon black mixtures.

Calix[n]arenes are basket shaped (vase-shaped) macro cyclic or cyclic oligomers composed of repeating para-alkyl phenolic monomers linked by methylene bridges to form a hydrophobic cavity and are simply functionalized both at the upper rim and lower rim. These compounds are based on hydroxyl alkylation product of aldehydes and phenols with defined upper rim, lower rim and a central annulus.17

Taghvaei-Ganjali and colleagues employed calix[4]arenes and their derivatives in sensors,18 construction of polyurethane foams,19 membrane electrode,20 improvement of mechanical properties and thermal stability of polyurethane composite21 and removal agents for ions.22 As other researchers have reported, calix[n]arene derivatives can be used as heterogeneous catalytic system,23 binders24 and for detection of tryptophan.25

Our research group studied the use of calix[4]arene derivatives as sorbent,26 filler,27 tackifier resin,28 anti-reversion agent29 in rubber industry. Li et al. investigated the effect of phenolic antioxidants based on calixarene on the antioxidative properties of natural rubber.30 Malekzadeh et al.31 studied the influence of a silane coupling agent based on calix[4]arene on the properties of nano-silica filled rubber compound. As could be seen, the possible influence of calix[n]arenes as a processing aid agent on tire tread performance has not been examined in present literatures.

In the present study, a novel calixarene silica based 5, 11, 13, 17-tetrahydroxy 25, 26, 27, 28-tetrakis[chlorosulfonyl]calix[4]arene-bonded silica gel (SS-CSC[4]A), has been synthesized and applied as processing aid agent in BR/SBR based rubber compounds in order to decreasing of heat build-up as well as rolling resistance.

- Experimental

2. 1. Materials

Emulsion polymerized styrene butadiene rubber (E-SBR1502) was provided by Takhte Jamshid Petrochemical Company (Iran) and high-cis polybutadiene rubber 96% (BR) was purchased from Arak Petrochemical Company (Iran). N-330 carbon black was supplied by Pars Company (Iran). Aromatic oil (290, dark brown) was purchased from Iranol Company (Iran). The Hydrocarbon Resin (C5) was provided by Lesco Chemical (China). p-tert-Butylphenol was purchased from Merck (Germany) and applied without any purification and another three types of resins (C9, G90 and SP1068) were supplied by Taizhou Huangyan Donghai Chemical Company (China). N-cyclohexyl-2-benzothiazole sulfonamide (CBS), 1, 3-Diphenylguanidine (DPG) and 2, 2, 4-trimethyl-1, 2-dihydroquinoline (TMQ) and sulfur were supplied by Taizhou Huangyan Donghai Chemical Company (China).  N-isopropyl-N'-phenyl-p-phenylene (IPPD) was provided by Nocil (India). The silica (Ultrasil VN3) was purchased from Evonik Company (Germany). Bis[3-(triethoxysilyl)propyl]tetrasulfide (TESPT) was purchased from Shin-Etsu company (Japan). stearic acid (PALMAC 1600) was supplied by Acidchem Company (Malaysia) and Zinc oxide (ZnO) was manufactured by Sepid Oxide Shokuhie Company (Iran). Paraffin wax was supplied by Behran Company (Iran). N-(cyclohexylthio) phethalimide (PVI) was purchased from Changde Dingyuan (China). Silica supported calix[4]arene derivative was synthesized in our research group32. All analytical grades of the reagents and solvents used in this study were provided by Merck Company (Germany) and were analytical pure grades.

2. 2. Synthesis

Synthetic strategy for preparation of silica supported calix[4]arene derivative (SS-CSC[4]A) according to our published papar32 has been illustrated in Figure 1.

Figure 1. The synthetic strategy for silica supported calix[4]arene.

2.2.1. Synthesis of p-tert-Butyl calix[4]arene (1)

p-tert-Butyl calix[4]arene was synthesized according to previously described method by Gutsche and Iqbal.33

Yield: 62%; mp: 342–344 °C; ATR-FTR: υmax (cm–1) = 3169, 2955, 1200, 1401; 1H NMR (400 MHz, CDCl3), δ(ppm): 1.21 (s, 36H, CH(CH3)3), 3.51 (d, 4H, ArCH2Ar, J 12.8 Hz), 4.26 (d, 4H, ArCH2Ar, J 12.8 Hz), 7.06 (s, 8H, Ar–H), 10.34 (s, 4H, OH); 13C NMR: (100 MHz, CDCl3), δ(ppm): 31.3, 32.4, 34.0, 126.2, 128.4, 144.5, 146.6.

2.2.2. Synthesis of Chlorosulfonyl-Calix[4]arene (2)

Chlorosulfonyl-Calix[4]arene (CSC[4]A) was prepared in accordance with the previously method described by Coquiere et al.34 with some modification. A mixture of p-tert-butylcalix[4]arene (2 mmol) and dichloromethane (25 mL) were placed in a three necked 100 mL round-bottom flask equipped with a magnetic stirrer, reflux condenser and septum. The mixture was stirred for 15 min at room temperature in an inert atmosphere of nitrogen gas. Chlorosulfonic acid (5 mL) was slowly added by syringe at a rate to keep the temperature between 0 and 5 ◦C. When the addition of chlorosulfonic acid was finished, the solution mixture was refluxed for 2 h under vigorous stirring. After cooling, dry ether (30 mL) was added and the resulting oil after separating was triturated several times with methanol. CSC[4]A as a tan powder was given.

Yield 50%; mp > 230 ◦C; ATR-FTIR: υmax (cm–1) = 2881, 2829, 1455, 1936, 650, 455-1000. 1H NMR: (500 MHz, DMSO-d6, TMS), δ(ppm): 3.94 (8H, s, ArCH2Ar), 7.39 (8H, s, Ar–H) and 11.39 (4H, s, 8OH); 13C NMR: (125 MHz, DMSO-d6), δ(ppm): 138.3 (ArC–SO2), 30.4 (ArCH2Ar); MS-FAB: m/z 817.0 (M+, calcd 817.5)

2.2.3. Synthesis of Silica Supported Calix[4]arene derivative (SS-CSC[4]A) (3)

5 g of mesoporous silica gel was activated by refluxing with concentrated sulfuric acid and nitric acid [4:1] at 140 ◦C for 4 h to remove any adsorbed metal ions. The solution was filtered and obtained white powder was washed with distilled water until the neutral pH was gained. The residual solid was washed with acetone, methanol and dichloromethane, respectively and dried in an oven at 300 ◦C for 2 h to remove adsorbed surface water and maximize the number of silanol groups on the surface. Activated silica gel was put in a stream of dry nitrogen for 1 h and was used immediately.

100 mL round-bottom flask, equipped with a reflux condenser, a gas inlet tube for conducting of HCl gas over silver nitrate solution was used. It was charged with 50 mL anhydrous xylene, 1.5 g of activated silica gel and 1 g of CSC[4]A. The mixture was allowed to reflux under continuous stirring and a dry nitrogen atmosphere at 140 ◦C for 72 h. It was mentioned in order to prevent the crashing of silica gel particles and as a result changing the special surface area of silica particle during the reaction, was not used mechanical stirring in this reaction. Instead, the stirring was done by bubbling of nitrogen gas over the reaction mixture. After carrying out the reaction, the suspension was vacuum filtered using a sintered glass funnel (porosity 3) and the residue was washed in sequence with dichloromethane (5 mL), diethyl ether (5 mL), methanol (5 mL) and hexane (5 mL). The unreacted CSC[4]A inside the pores of silica gel was extracted with acetone at reflux temperature for 12 h in a soxhlet system. The acetone solution was checked by thin layer chromatography and there was no evidence of unreacted CSC[4]A. The final product as dried in an oven at 150 ◦C for 12 h and kept in the desiccator.

SS-CSC[4]A was characterized by various physical techniques such as elemental analysis for C and Si, ATR-FTIR spectra for functional group confirmation, TGA for confirmation of covalently anchored organic groups and Solid-State 29Si CP/MAS (cross-polarization/magic-angle spinning) NMR for the conformation of chemically bonding between silica gel and CSC[4]A.

The percentage of carbon, sulfur, hydrogen which was obtained from elemental analysis and resulting acidic properties of SS-CSC[4]A are given in Table 1. The carbon and sulfur content were assigned to the loading of CSC[4]A over silica gel. The bonded amount was found to be 92.82 µmol/g (0.219 µmol/m2) according to the carbon content shown in Table 1. Further, the sulfur content of SS-CSC[4]A was 0.36 mmol/g. The number of H+ determined by acid-base titration was 0.17 mmol/g in the hydrolyzed sample. This value is half of the sulfur content, indicating that only two ester units took place onto SS-CSC[4]A and two acidic sites exist on the surface.

Table 1. The results of elemental analysis and titration of SS-CSC[4]A.

| Compound | Elemental analysis |  |  |  | Titration |
| --- | --- | --- | --- | --- | --- |
|  | %C | %H | %S | Bonded amount (µmol/g) | Acid capacity (mmol H+/g) |
| SS-CSC[4]A | 3.11 | 0.45 | 1.15 | 92.82 | 0.17 |

The TGA curve of SS-CSC[4]A shows two distinct stages of weight loss. The first weight loss is between 30 ◦C and 130 ◦C is attributed to the physically adsorbed water.35 The second weight loss is observed between 160 ◦C and 900 ◦C which can be related to the decomposition of calixarene, corresponding to 92.82 µmol of CSC[4]A content per gram of silica.

FT-IR spectra was taken for a bare silica gel, CSC[4]A and SS-CSC[4]A. The major peaks of bare silica gel spectrum are: (a) a large broad band between 3200 and 3400 cm−1 attributed to the presence of the OH stretching frequency of the surface silanol group and adsorbed water (b) an intense peak at 1000-1250 cm−1 related to the antisymmetric Si–O–Si (siloxane) stretching in the amorphous silica (c) a band near 800 cm−1 is associated with the symmetric Si–O–Si stretching (d) a peak in the region 1600-1650 cm−1 is due to the bending mode of associated water molecules (e) the appearance of a peak at 900 cm−1 is related to Si–OH bending frequency. The infrared spectrum of the SS-CSC[4]A presented the same set of bands related to the silica gel, however some additional bands at 2883, 2827, 1457, 1936 and 650 which are assigned to the methylene asymmetric stretching, methylene symmetric stretching, C–H bending mode, benzene ring and C–S stretching mode respectively. Also, the appearance of the several peaks in the region between 1000 and 1500 cm−1 is a characteristic adsorption band of calixarenes. So, It is possible that the characteristic peaks of S=O group in compound SS-CSC[4]A which can be seen at 950-1040 cm−1, overlapped with the strong broad band of siloxane in the compound SS-CSC[4]A. It is reasonable to mention here, because of the intense and broad band of siloxane in the region 1100 cm−1, the intensities of the other bands in the spectrum are relatively small. To clarify the spectrum between 1200 and 4000 cm−1, it was scaled up and magnified to show the differences more clearly. Considering the possible heterogeneity in the thickness of samples and the changes in the infrared beam positions, the band area of Si–OH bending frequency at 900 cm−1 after and before immobilization were calculated using the silica band at 1100 cm−1 as a reference band. The decrease of a absorbance in the 900 cm−1 band region of SS-CSC[4]A in comparison with the spectrum of bare silica gel indicates that the Si–O–H vibration was affected due to the immobilization. These results which are obtained from IR spectrum are closely in agreement with published data.36-38

Direct evidence for chemical attachment of macrocyclic functionalized CSC[4]A to silica surface was done by 29Si CP/MAS solid state NMR. Normally, the spectra of the bare silica gel shows three resonance peaks at −90, −100 and −110 ppm correspond to germinal silanol (Si(OH)2, Q2), free silanol (SiOH, Q3) and siloxane (SiOSi, Q4) respectively.39 Because the resolution of the spectra is not sufficient to distinguish these signals, only one broad band was seen in the spectra. As a result of the introduction of functionalized calixarenes, the cross polarized 29Si-MAS NMR spectra displayed unsymmetrical pattern when compared to the bare silica material.40, 41 These results indicated the covalent-attachment of organic groups on the silica surface.

2.3. Preparation of rubber compounds

In this study seven tire tread compounds were prepared. The formulation of compounds is shown in Table 2. All compounds were mixed by two-roll mill (Hiva Machinery Company, Iran) according to ASTM D3182 and Vulcanization were done in 160 ᵒC.

Table 2. Tire Tread Compound Formulations.

| Ingredient | Component content (phr*) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | C | D | E | F | G |
| BR | 30 | 30 | 30 | 30 | 30 | 30 | 30 |
| SBR | 70 | 70 | 70 | 70 | 70 | 70 | 70 |
| Carbon Black N330 | 45 | 45 | 45 | 45 | 45 | 45 | 45 |
| Silica | 20 | 20 | 20 | 20 | 20 | 20 | 20 |
| Silane (TESPT) | 1 | 1 | 1 | 1 | 1 | 1 | 1 |
| ZnO | 3 | 3 | 3 | 3 | 3 | 3 | 3 |
| Stearic acid | 2 | 2 | 2 | 2 | 2 | 2 | 2 |
| Sulfur | 1.6 | 1.6 | 1.6 | 1.6 | 1.6 | 1.6 | 1.6 |
| P.Wax | 2 | 2 | 2 | 2 | 2 | 2 | 2 |
| IPPD | 1.5 | 1.5 | 1.5 | 1.5 | 1.5 | 1.5 | 1.5 |
| TMQ | 1 | 1 | 1 | 1 | 1 | 1 | 1 |
| Aromatic oil | 37 | 37 | 37 | 37 | 37 | 37 | 37 |
| CBS | 1.4 | 1.4 | 1.4 | 1.4 | 1.4 | 1.4 | 1.4 |
| DPG | 2 | 2 | 2 | 2 | 2 | 2 | 2 |
| PVI | 0.3 | 0.3 | 0.3 | 0.3 | 0.3 | 0.3 | 0.3 |
| Aliphatic hydrocarbon Resins (C5) | — | 2 | — | — | — | — | — |
| Aromatic hydrocarbon Resins (C9) | — | — | 2 | — | — | — | — |
| Coumarone Indene Resin (G90) | — | — | — | 2 | — | — | — |
| Phenolic Tackifying Resin (SP1068) | — | — | — | — | 2 | — | — |
| Para tert butyl phenol | — | — | — | — | — | 2 | — |
| SS-CSC[4]A | — | — | — | — | — | — | 2 |

*phr represented the mass parts per 100 mass parts of BR/SBR blend.

2.4. Characterization

    - Cure Characteristics

Rheometric properties of tire tread compounds such as scorch time (ts2), cure time (tc90), minimum torque (ML), maximum torque (MH) and cure rate index (CRI) were measured at 160 °C using a Monsanto Moving Die Rheometer (MDR 2000) made by HIWA company according to ASTM D5289 standard. The curing characteristics of compounds have been shown in Table 3.

Table 3. The results of curing behavior of rubber compounds.

| Sample | ML (dN.m) | MH (dN.m) | MH-ML (dN.m) | Tc90 (Min) | TS2 (Min) | CRI (dN.m) |
| --- | --- | --- | --- | --- | --- | --- |
| A | 1.343 ± 0.213 | 7.570 ± 0.121 | 6.227 ± 0.234 | 13.672 ± 0.223 | 7.06 ± 0.211 | 15.125 ± 0.444 |
| B | 1.655 ± 0.111 | 8.277 ± 0.154 | 6.621 ± 0.054 | 14.721 ± 0.358 | 7.729 ± 0.276 | 14.301 ± 0.591 |
| C | 1.655 ± 0.132 | 8.139 ± 0.148 | 6.483 ± 0.229 | 13.823 ± 0.311 | 7.203 ± 0.257 | 15.106 ± 0.213 |
| D | 1.655 ± 0.112 | 8.691 ± 0.076 | 7.035 ± 0.211 | 14.125 ± 0.298 | 6.967 ± 0.122 | 13.972 ± 0.274 |
| E | 1.793 ± 0.163 | 8.415 ± 0.181 | 6.621 ± 0.017 | 13.832 ± 0.301 | 6.767 ± 0.130 | 14.156 ± 0.479 |
| F | 1.793 ± 0.224 | 8.691 ± 0.159 | 6.897 ± 0.326 | 15.46 ± 0.388 | 7.667 ± 0.199 | 12.832 ± 0.395 |
| G | 1.793 ± 0.194 | 8.691 ± 0.271 | 6.897 ± 0.077 | 14.682 ± 0.390 | 7.428 ± 0.295 | 13.784 ±0.565 |

2.4.2. Mechanical Properties

The mechanical properties of tire tread compounds including tensile strength and stress at 100% elongation (M100), 300% elongation (M300), and elongation at break were investigated by a Universal Testing Machine (model; M350-5kN, Testometric Company, UK) according to the ASTM D412 test method. Dumbbell-shaped specimens (2 mm thickness, 25 mm width and 100 mm length) were cut from molded sheets. The average values of the measured quantities and their standard deviations were reported in Table 4.

Table 4. The results of mechanical properties of rubber compounds.

| Sample | Processing aid agent | Tensile strength (MPa) | Elongation at break (%) | Modulus @ 100% (MPa) | Modulus @ 300% (MPa) |
| --- | --- | --- | --- | --- | --- |
| A | Blank | 13.179 ± 0.876 | 647.693 ± 28.251 | 1.742 ± 0.027 | 5.042 ± 0.038 |
| B | C5 | 13.227 ± 0.726 | 725.75 ± 24.344 | 1.493 ± 0.056 | 4.273 ± 0.096 |
| C | C9 | 14.251 ± 0.44 | 746.179 ± 4.855 | 1.529 ± 0.085 | 4.436 ± 0.158 |
| D | G90 | 14.958 ± 0.252 | 736.452 ± 4.583 | 1.729 ± 0.045 | 4.897 ± 0.105 |
| E | SP-1068 | 14.549 ± 0.13 | 754.237 ± 6.797 | 1.820 ± 0.053 | 4.824 ± 0.086 |
| F | P-tert | 13.897 ± 0.319 | 745.163 ± 38.728 | 1.564 ± 0.131 | 4.443 ± 0.300 |
| G | SS-CSC[4]A | 14.175 ± 0.306 | 712.71 ± 23.45 | 1.762 ± 0.109 | - ± 0.230 |

2.4.3. Dynamic Mechanical Thermal Analysis (DMTA)

Dynamic mechanical thermal properties of tire tread compounds were examined by using a dynamic mechanical thermal analyzer (DMTA; Tritec-2000; England) at a temperature range from -140 °C to 90 °C with tension mode deformation and a frequency of 1.0 Hz according to ASTM E1640. The results have been shown in Tables 5 and 6.

Table 5. The results of dynamic mechanical thermal properties of rubber compounds A-G.

| CLD (mol/m2) | E' 30 °C (Mpa) | E'R (Mpa) | E'G (MPa) | Tan δ (max) | Tg (°C) | Processing aid agent | Sample |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.3466 | 10.31 | 3.134 | 2.64E+03 | 0.5328 | -44.2 | Blank | A |
| 0.5990 | 11.31 | 5.421 | 2.73E+03 | 0.5324 | -44.3 | C5 | B |
| 0.6460 | 10.71 | 5.841 | 2.69E+03 | 0.5505 | -44.0 | C9 | C |
| 0.5393 | 11.27 | 4.876 | 2.29E+03 | 0.5116 | -40.8 | G90 | D |
| 0.8293 | 15.89 | 7.498 | 2.61E+03 | 0.4891 | -43.9 | SP-1068 | E |
| 0.5563 | 10.87 | 5.030 | 2.44E+03 | 0.5188 | -44.0 | P-tert | F |
| 0.5112 | 10.53 | 4.622 | 2.68E+03 | 0.5369 | -44.5 | SS-CSC[4]A | G |

Table 6. tan δ at various temperature for compounds A-G derived by DMTA.

| tan δ @ |  |  |  |  | Processing aid agent | Sample |
| --- | --- | --- | --- | --- | --- | --- |
| -10 °C | 0 °C | 25 °C | 60 °C | 90 °C |  |  |
| 0.1773 | 0.1735 | 0.1668 | 0.1517 | 0.1627 | Blank | A |
| 0.1646 | 0.1549 | 0.1441 | 0.1176 | 0.1068 | C5 | B |
| 0.1739 | 0.1648 | 0.1413 | 0.1079 | 0.0922 | C9 | C |
| 0.1797 | 0.1741 | 0.1615 | 0.1460 | 0.1321 | G90 | D |
| 0.1694 | 0.1672 | 0.1590 | 0.1512 | 0.1357 | SP-1068 | E |
| 0.1760 | 0.1717 | 0.1571 | 0.1326 | 0.1243 | P-tert | F |
| 0.1746 | 0.1681 | 0.1564 | 0.1359 | 0.1378 | SS-CSC[4]A | G |

2.4.4. Scanning Electron Microscopy (SEM)

The degree of filler dispersion was explored by scanning electron microscopy (SEM, Philips-XL 30, Netherlands) with an accelerating voltage of 25 kV. The samples were supper-coated with gold to increase their electric conductivity before the examination.

3. Results and Discussions

  - . Curing Characteristics

The cure properties that include scorch time (ts2), optimum cure time (tc90), maximum and minimum torque (MH and ML), the difference in torque (ΔM=MH-ML), and the cure rate index (CRI) of different tire tread compounds (A-G) are shown in Figures 2-4 and Table 3.

These data show that there are no significant changes in rheological properties of rubber compounds by changing in processing aid agents.

Figure 2. Optimum Curing Time [tc90] and Scorch time [ts2] of rubber samples containing various processing aid agents with MDR rheometer.

Figure 3. Minimum Torque [ML], Maximum Torque [MH] and MH-ML of rubber samples containing various processing aid agents with MDR rheometer.

Figure 4. Cure Rate Index [CRI] of rubber samples containing various processing aid agents with MDR rheometer.

3.2. Mechanical Properties

In order to investigate the mechanical properties, the results of Tensile strength, Elongation at break, modulus at 100% and modulus at 300% after optimum vulcanization can be seen in Figures 5-7 and the values of these results are given in Table 4.

The results of mechanical properties of rubber compounds A-G show that SS-CSC[4]A acts as C9 resins according to aromatic behavior and there are slightly increasing in tensile strength and elongation at break in comparison with blank compound A without any significant changing in modulus %100 and %300.

Figure 5. Elongation at break of rubber samples containing various processing aid agents.

Figure 6. Tensile strength of rubber samples containing various processing aid agents.

Figure 7. Stress at 100% and 300% of rubber samples containing various processing aid agents.

3.3. DMTA

Dynamic mechanical thermal analysis (DMTA) of tire tread compounds due to prediction tire tread performance, mainly rolling resistance as an indicator of fuel consumption efficiency, is important in tire industry. For this purpose, the dependence of the loss factor (tan 𝛿) on temperature at a constant frequency could be characterized. Therefore, the tan δ values at about 90 °C, 60 °C, 25 °C, 0 °C and -10 °C are used to consider heat build-up, rolling resistance, dry grip, wet grip and ice grip, respectively.15, 42-50 The loss factor that is the ratio between the loss modulus to storage modulus (tan δ = E"/E'), is related to macromolecule’s movements and phase transition in the polymers.50-52 The lower value of tan δ at 60 °C, 90 °C causes lower rolling resistance and lower heat build-up, and therefore lower fuel consumption efficiency. On the other hand, the higher value of tan δ at low temperatures (-10 °C, 0 °C, 25 °C) indicates better grip properties of tire on the roads surface.53, 54 Figures 8-10 and Tables 5-6 represent the influence of different processing aid agents on tire tread performance and dynamic properties for tire tread compounds A-G.

As shown in Figure 10 and Table 5, C and E compounds had the highest and the lowest values of tan δmax (peak of the tan δ). The almost same values of tan δmax for the G and the blank compounds demonstrate that the amount of rubber chains participating in the glass transition for both compounds is in the same order.55 Regarding to this fact the value of E' at 30 °C directly relates to the dry handling property of a tire56, the highest value of E' at 30 °C for the E compound indicates that the compound possessed the best dry handling property. The E' value at 30 °C for the G compound increased about 2.1% compared to the obtained parameter for the blank compound. The value of cross-linking density (CLD) parameter in Equation (1) was obtained by the following equation55:

| CLD = E'/3RT | (1) |
| --- | --- |

where E', R, and T are corresponded to the minimum storage modules, the universal gas constant, and the absolute temperature at the rubbery plateau zone, respectively.

Based on the Equation (1), the higher value of E' at the rubbery region results in a higher degree of cross linking density. Therefore, from Table 5 it can be clearly seen that the E compound possessed the highest modulus at rubbery and so the highest degree of cross linking density. The higher E' value at the rubbery zone for the G compound compared to the blank compound led to the increment of the cross linking density (about 47.5%) for the SS-CSC[4]A containing compound. The value of E' at the glassy region for the G compound was about 1.5% more than the blank compound indicating the stronger structural interactions of SS-CSC[4]A in G compound with the matrix.

Tg is another parameter that can be obtained from the DMTA analysis. As can be seen, the lowest and highest values of Tg respectively belong to the G and E compounds. The Tg of tire tread compound decreases from -44.2 °C to -44.5 °C when there is SS-CSC[4]A. To understand the reason, the SS-CSC[4]A structure and its effect on silica particle dispersion has been studied. SS-CSC[4]A is a calixarene, that the cavity of its can relieve the force on itself by moving its flexible bonds, then it is accepted that when SS-CSC[4]A is added as mobile macromolecule to compound with cured chain, Tg must be decreased. On other hand, the addition of SS-CSC[4]A to compound provides better silica dispersion and more interaction between rubber chain and silica particle, which means we have to provide more energy for chain movement and this energy must be provided by higher temperature. According to results, there is a trade-off between increasing and decreasing Tg when SS-CSC[4]A is added to compound, DMTA results show a 0.3 °C decrease in Tg, so the SS-CSC[4]A flexible bonds is the Tg controller.

In general, it is expected that with a gradual decrease in Tg, the values of tan δ will be increased. But as can be seen in results, Tan δ values is lower than the blank compound at all temperatures in the presence of SS-CSC[4]A. In high temperature when the temperature is well above Tg, the movement of the chains is very fast and long range. Regardless of the flexible structure, with presence of SS-CSC[4]A as an external factor makes it difficult to move the polymer chain, so tan δ values were decreased.

According to Figure 10 and Table 6, the values of tan δ at 60 ᵒC and 90 ᵒC of compound G are decreased compared to blank compound A, where the rolling resistance and heat build-up decreased by 11.6% and 18.1%, respectively. Which means the fuel consumption efficiency and heat build-up performance of compound G containing SS-CSC[4]A are improved. The fuel consumption of a passenger car will be reduced by 1-2% if the rolling resistance of tire is reduced by 10%, according to the literatures.57-59

But in lower temperature due to better dispersion of the silica particle and more interaction between matrix and filler, moving and relaxing becomes harder for the polymer chain, as a result tan δ values were decreased. As a result grip decreases in G compound compared to blank compound, which is a weak point of using SS-CSC[4]A in tire tread compounds.

Consequently, the use of SS-CSC[4]A as a processing aid agent in tire tread compounds, regardless of improvement of grip properties, is beneficial for reducing rolling resistance. This is because of better filler dispersion, stronger rubber-filler interaction, higher crosslink density and lower filler-filler interaction.

Figure 8. Storage modulus (E') versus temperature curves of rubber samples containing various processing aid agent.

Figure 9. Loss factor (tan δ) versus temperature curves of rubber samples containing various processing aid agent.

Figure 10. Loss factor (tan δ) values at different temperature of rubber samples containing various processing aid agent.

3.4. SEM Analysis

For investigating of the SS-CSC[4]A effect on silica dispersion in rubber compound, the SEM analysis was done in compound A (Blank) and G (SS-CSC[4]A) as processing aid agent, are shown in Figure 12. As can be seen the presence of SS-CSC[4]A lead to better dispersion of silica particle in the rubber matrix.

According to the structure of SS-CSC[4]A, there is dual structural behavior. A fair dispersity to the silica as filler via lower rim silica supported moiety and good physical connection to rubber matrix via upper rim moiety of aromatic based calixarene. As a result, better silica disperses is observed in the rubber matrix in the presence of SS-CSC[4]A as dispersing agents.

Figure 11. SS-CSC[4]A molecular structure.

Compound G

Compound A

Figure 12. SEM images of compounds A and G.

4. Conclusion

In this study in order for improvement of rolling resistance and heat build-up of tire tread formulation a unique processing aid agent, SS-CSC[4]A was synthesized. FTIR, and NMR proved the structure of SS-CSC[4]A. DMTA results showed a reduction in rolling resistance (11.6%) and heat build-up (18.1%), due to the effect of SS-CSC[4]A on silica dispersion and interaction between matrix and filler. SEM results showed a great silica dispersion when there is SS-CSC[4]A in compound, and the tensile test did not illustrate any tangible changes for compound containing SS-CSC[4]A. On the other hand, rheological properties showed a slight increase in cure parameters because of the interaction enhancement between uncured polymeric chain, filler and macromolecule SS-CSC[4]A.

5. References

1. J. G. Speight, (Ed.): Handbook of industrial hydrocarbon processes, Gulf Professional Publishing, 2019.

2. D. De, D. De, Mater. Sci. Appl. 2011, 2, 05, 486-496. DOI: 10.4236/msa.2011.25066.

3. R. Chawla, S. Sharma, J. Mol. Model. 2018, 24, 4, 1-9. DOI: 10.1007/s00894-018-3636-5.

4. Y. Li, P. Cheng, E. A. Siddig, C. Han, Road Mater. Pavement Des. 2020, 21, 7, 1902-1917. DOI: 10.1080/14680629.2019.1574234.

5. R. Sengupta, S. Chakraborty, S. A. Bandyopadhyay, S. Dasgupta, R. Mukhopadhyay, K. Auddy, A. S. Deuri, Polym. Eng. Sci. 2007, 47, 11, 1956-1974. DOI: 10.1002/pen.20921.

6. S. S. Choi, B. H. Park, H. Song, Polym. Adv. Technol. 2004, 15, 3, 122-127. DOI: 10.1002/pat.421.

7. S. K. Peddini, C. P. Bosnyak, N. M. Henderson, C. J. Ellison, D. R. Paul, Polymer 2014, 55, 1, 258-270. DOI: 10.1016/j.polymer.2013.11.003.

8. R. P. Kumar, K. M. Nair, S. Thomas, S. C. Schit, K. Ramamurthy, Compos. Sci. Technol. 2000, 60, 9, 1737-1751. DOI: 10.1016/S0266-3538(00)00057-9.

9. R. Huang, Q. Pan, Z. Chen, K. Feng, Appl. Sci. 2020, 10, 13, 4478. DOI: 10.3390/app10134478.

10. N. C. Kim, S. H. Song, Int. J. Polym. Sci. 2019, 2019, 1-9. DOI: 10.1155/2019/9123635.

11. S. H. Song, Appl. Sci. 2020, 10, 20, 7244. DOI: 10.3390/app10207244.

12. T. R. Kukreja, R. C. Chauhan, S. Choe, P. P. Kundu, J. Appl. Polym. Sci. 2003, 87, 10, 1574-1578. DOI: 10.1002/app.11490.

13. S. M. Ashraf, S. Ahmad, U. Riaz, M. Alam, H. O. Sharma, J. Macromol. Sci., Part A: Pure Appl. Chem. 2005, 42, 10, 1409-1421. DOI: 10.1080/10601320500206903.

14. V. D. A. Veiga, T. M. Rossignol, J. D. S. Crespo, L. N. Carli, J. Appl. Polym. Sci. 2017, 134, 39, 45334. DOI: 10.1002/app.45334.

15. J. Hua, K. Liu, Z. Wang, J. Geng, X. Wang, J. Appl. Polym. Sci. 2018, 135, 12, 45975. DOI: 10.1002/app.45975.

16. B. Mensah, B. Agyei-Tuffour, E. Nyankson, Y. D. Bensah, D. Dodoo-Arhin, J. K. Bediako, B. Onwona-Agyeman, A. Yaya, Int. J. Polym. Sci. 2018, 2018, 1-12. DOI: 10.1155/2018/2473286.

17. W. Sliwa, C. Kozlowski, (Ed.): Calixarenes and resorcinarenes: synthesis, properties and applications, John Wiley & Sons, 2009. DOI: 10.1002/anie.200903182.

18. M. Hosseini, M. Rahimi, H. B. Sadeghi, S. Taghvaei-Ganjali, S. D. Abkenar, M. R. Ganjali, Int. J. Environ. Anal. Chem. 2009, 89, 6, 407-422. DOI: 10.1080/03067310802713195.

19. M. S. Mirmoeini, M. M. A. Nikje, M. Rasouli‐Saniabadi, S. Taghvaei‐Ganjali, Macromol. Symp. 2017, 373, 1600101. DOI: 10.1002/masy.201600101.

20. S. Taghvaei-Ganjali, R. Zadmard, M. Zeyaei, K. Rahnama, F. Faridbod, M. R. Ganjali, Res. Lett. Org. Chem. 2009, 2009, 1-5. DOI: 10.1155/2009/601089.

21. S. Taghvaei-Ganjali, M. Rasouli-Saniabadi, M. S. Mirmoeini, J. Inclusion Phenom. Macrocyclic Chem. 2015, 83, 1, 45-52. DOI: 10.1007/s10847-015-0539-2.

22. M. Nouri, S. Mozafari, S. Taghvaei-Ganjali, Iran. JOC. 2011, 3, 4, 807-809.

23. A. B. Chenari, M. Saber-Tehrani, M. Mamaghani, M. Nikpassand, J. Inclusion Phenom. Macrocyclic Chem. 2019, 94, 1, 45-53. DOI: 10.1007/s10847-019-00894-x.

24. K. D. Daze, C. E. Jones, B. J. Lilgert, C. S. Beshara, F. Hof, Can. J. Chem. 2013, 91, 11, 1072-1076. DOI: 10.1139/cjc-2013-0186.

25. T. T. Pang, L. M. Du, H. L. Liu, Y. L. Fu, Can. J. Chem. 2014, 92, 1139-1144. DOI: 10.1139/cjc-2014-0150.

26. Z. Servati, M. Saber-Tehrani, S. Taghvaei-Ganjali, R. Zadmard, J. Porous Mater. 2018, 25, 5, 1463-1474. DOI: 10.1007/s10934-018-0559-6.

27. H. Mohamadi, F. Motiee, M. Saber-Tehrani, S. Taghvaei-Ganjali, Russ. J. Appl. Chem. 2019, 92, 6, 809-816. DOI: 10.1134/S1070427219060107.

28. H. M. Pekachaki, S. Taghvaei-Ganjali, F. Motiee, M. Saber-Tehrani, Rubber Chem. Technol. 2019, 92, 3, 467-480. DOI: 10.5254/rct.19.81510.

29. H. Mohamadi, F. Motiee, S. Taghvaei-Ganjali, M. Saber-Tehrani, Acta Chim. Slov. 2021, 68, 1, 128-136. DOI: 10.17344/acsi.2020.6225.

30. H. Li, Y. Zhong, W. Wu, L. Zhang, X. Lai, X. Zeng, J. Appl. Polym. Sci. 2017, 134, 31, 45144. DOI: 10.1002/app.45144.

31. M. Malekzadeh, H. Nouri, M. Farahani, JACR. 2010, 3, 41-45.

32. S. Taghvaei-Ganjali, R. Zadmard, M. Saber-Tehrani, Appl. Surf. Sci. 2012, 258, 16, 5925-5932. DOI: 10.1016/j.apsusc.2011.09.019.

33. C. D. Gutsche, M. Iqbal, Org. Synth. 2003, 68, 234-234. DOI: 10.1002/0471264180.os068.29.

34. D. Coquière, H. Cadeau, Y. Rondelez, M. Giorgi, O. Reinaud, J. Org. Chem. 2006, 71, 11, 4059-4065. DOI: 10.1021/jo052605p.

35. S. Radi, A. Attayibat, A. Ramdani, M. Bacquet, Eur. Polym. J. 2008, 44, 10, 3163-3168. DOI: 10.1016/j.eurpolymj.2008.07.021.

36. M. Tabakci, J. Inclusion Phenom. Macrocyclic Chem. 2008, 61, 1, 53-60. DOI: 10.1007/s10847-007-9392-2.

37. H. Huang, C. Zhao, Y. Ji, R. Nie, P. Zhou, H. Zhang, J. Hazard. Mater. 2010, 178, 1-3, 680-685. DOI: 10.1016/j.jhazmat.2010.01.140.

38. R. Tian, J. Sun, H. Zhang, M. Ye, C. Xie, J. Dong, J. Hu, D. Ma, X. Bao, H. Zou, Electrophoresis 2006, 27, 4, 742-748. DOI: 10.1002/elps.200500630.

39. T. M. Suzuki, T. Nakamura, E. Sudo, Y. Akimoto, K. Yano, Microporous Mesoporous Mater. 2008, 111, 1-3, 350-358. DOI: 10.1016/j.micromeso.2007.08.008.

40. D. W. Sindorf, G. E. Maciel, J. Am. Chem. Soc. 1983, 105, 12, 3767-3776.

41. E. F. Vansant, P. Van Der Voort, K. C. Vrancken, (Ed.): Characterization and chemical modification of the silica surface, Elsevier, Amsterdam, 1995.

42. X. Zhao, K. Niu, Y. Xu, Z. Peng, L. Jia, D. Hui, L. Zhang, Composites, Part B. 2016, 107, 106-112. DOI: 10.1016/j.compositesb.2016.09.073.

43. X. Liu, S. Zhao, X. Zhang, X. Li, Y. Bai, Polymer 2014, 55, 8, 1964-1976. DOI: 10.1016/j.polymer.2014.02.067.

44. M. H. R. Ghoreishy, S. Taghvaei, R. Z. Mehrabian, Iran. J. Sci. Technol. 2011, 24, 4, 329-337.

45. C. Sirisinha, P. Sae‐oui, K. Suchiva, P. Thaptong, J. Appl. Polym. Sci. 2020, 137, 20, 48696. DOI: 10.1002/app.48696.

46. U. Thepsuwan, P. Sae‐oui, C. Sirisinha, P. Thaptong, J. Appl. Polym. Sci. 2019, 136, 4, 46987. DOI: 10.1002/app.46987.

47. P. Sae-Oui, K. Suchiva, C. Sirisinha, W. Intiya, P. Yodjun, U. Thepsuwan, Adv. Mater. Sci. Eng. 2017, 2017, 1-8. DOI: 10.1155/2017/2476101.

48. P. J. Martin, P. Brown, A. V. Chapman, S. Cook, Rubber Chem. Technol. 2015, 88, 3, 390-411. DOI: 10.5254/rct.15.85940.

49. Y. Gui, J. Zheng, X. Ye, D. Han, M. Xi, L. Zhang, Composites, Part B. 2016, 85, 130-139. DOI: 10.1016/j.compositesb.2015.07.001.

50. H. Roshanaei, F. Khodkar, M. Alimardani, Iran. Polym. J. 2020, 29, 10, 901-909. DOI: 10.1007/s13726-020-00850-4.

51. S. Ahmadi Shooli, M. Tavakoli, J. Macromol. Sci., Part B: Phys. 2016, 55, 10, 969-983. DOI: 10.1080/00222348.2016.1230464.

52. S. Ahmadi-Shooli, M. Tavakoli, J. Macromol. Sci., Part B: Phys. 2019, 58, 7, 619-633. DOI: 10.1080/00222348.2019.1574428.

53. M. Harper, J. Tardiff, D. Haakenson, M. Joandrea, M. Knych, SAE Int. J. Veh. Dyn. Stab. and NVH 2017, 1, 2, 179-189. DOI: 10.4271/2017-01-1502.

54. S. Ezzoddin, A. Abbasian, M. Aman-Alikhani, S. Taghvaei-Ganjali, Iran. Polym. J. 2013, 22, 9, 697-707. DOI: 10.1007/s13726-013-0168-9.

55. P. Thaptong, P. Sae‐Oui, C. Sirisinha, J. Appl. Polym. Sci. 2016, 133, 17, 43342. DOI: 10.1002/app.43342.

56. T. Mondal, A. K. Bhowmick, R. Ghosal, R. Mukhopadhyay, Polymer 2018, 146, 31-41. DOI: 10.1016/j.polymer.2018.05.031.

57. J. Barrand, J. Bokar, SAE Int. J. Passeng. Cars - Mech. Syst. 2008, 1, 1, 9-17. DOI: 10.4271/2008-01-0154.

58. C. F. S. Gabriel, A. D. A. P. Gabino, A. M. F. de Sousa, C. R. G. Furtado, R. C. R. Nunes, J. Elastomers Plast. 2019, 51, 7-8, 712-726. DOI: 10.1177/0095244318819196.

59. P. Sae-oui, K. Suchiva, U. Thepsuwan, W. Intiya, P. Yodjun, C. Sirisinha, Rubber Chem. Technol. 2016, 89, 2, 240-250. DOI: 10.5254/rct.15.84859.