Synthesis, characterization, and investigation of mesomorphic properties of a new 2,5-bis-(4-alkanoyloxybenzylidene) cyclopentan-1-one

Figure 1: General structure of chalcone

Scheme1. Synthetic route for synthesis of B2-B10 compounds

Figure 2: FT IR spectrum for chalcone A.

Figure 3: 1H NMR spectrum for chalcone A.

Figure 4: DSC of compound B5 during heating/cooling cycles

Table 1. Phase transitions and transition enthalpy for chalcone ester under heating and cooling cycle

| Comp. | Transition Temperatures, οC (ΔH, KJ mol-1) ΔT/ΔS |  |
| --- | --- | --- |
|  | Heating | Cooling |
| B5 | Cr 103.26 (0.0829) SA 174.25 (17.22) SC 193.48 (0.994) I Cr 70.99/0.0002 SA 19.23/ 0.038 SC -/ 0.002 I | I 167.38 (0.61) SC 146.77 (26.0) Cr |
| B6 | Cr 68.62 (3.058) N 168.70 (23.01) I Cr 100.08/0.008 N -/ 0.052 I | I 100.89 (10.26) Cr |
| B7 | Cr 103.91 (3.39) N 164.10 (17.59) I Cr 60.19/ 0.009 N - / 0.040 I | I 142.23 (9.55) Cr |
| B8 | Cr1 87.88 (6.30) Cr2 106.95 (1.08) SA 134.28 (0.71) N 173.42 (16.94) I Cr1 19.07/ 0.017 Cr2 27.33/ 0.002 SA 39.14 / 0.0004 N - / 0.037 I | I 147.54 (13.51) Cr |
| B9 | Cr1 122.92 (1.72) Cr2 132.27 (0.36) N 166.99 (23.15) I Cr1 9.35/0.0043 Cr2 34.72/0.0009 N -/0.0526 I | I 150.77 (17.63) Cr |
| B10 | Cr1 21.01/0.0096 Cr2 51.25/0.0019 SA 32.78/0.018 SC 8.84/0.0273 N -/0.0055 I | I 145.58 (10.51) Cr |

Figure 5: Polarized optical micrographs for: (a) compound B5 (SC at 174.25 °C); (b) compound B6  (N, at 68.62 °C); (c) compound B7 (N, mosaic at 103.91 °C), (d) compound B8 (SA, at 106.95 °C); (e) compound B9 (N, Schlieren, at 132.27 °C); (f) compound B10 (N, mosaic at 164.30 °C).

Figure 6: Relationship of isotropization and nematic phase range with the number of carbon atoms