Dear Sir,

Re: Manuscript Id: Ms. No. 7567

I submit you a revised version of our manuscript “Enhanced Adsorption of Methylene Blue by Chemically Modified Materials Derived from Phragmites australis Stems

Environmental Engineering Research” for publication in Acta Chimica Slovenica.

I thank you for giving me the opportunity to revise this manuscript and appreciate the time given by you and each reviewer. Agreeing with the reviewer’s suggestion, efforts have been made to incorporate throughout the paper.

The authors thank reviewer for all remark points. The comments provided by the reviewers were extremely insightful and enabled us to improve the quality of our manuscript significantly. Agreeing with the reviewer’s suggestion, point-by-point has been incorporated throughout the revised manuscript. To make the changes easier to identify, major changes made in the original manuscript have been highlighted in green colour and additional content with the yellow colour. Some minor changes (some phrases) have been modified/changed/added have been highlighted in red colour.

I trust that the revisions in the manuscript and our accompanying responses may make this manuscript suitable for publication in Acta Chimica Slovenica.

Looking forward to hearing from you at your earliest convenience.

Yours sincerely,

Enclosures:

- Summary sheet of changes made in the original manuscript

- Point-by-point responses of the reviewers comments.

1. Summary sheet of changes made in the original manuscript

| Section name in original manuscript | Changes made and reflected in revised manuscript | Remarks |
| --- | --- | --- |
| Full revised manuscript | English was thoroughly checked and corrected by a native English speaker. | As suggested by reviewer A, C and editor |
| Introduction | Some sentences have been added | As suggested by reviewer C |
| Materials and methods | - Title: “Adsorption mechanisms” has been added (2.5.2) | As suggested by reviewer A |
| Results | - Title: “Intra-particle diffusion and film diffusion models” has been added - Figure: “Plots of intra-particle diffusion model for the adsorption of MB dye onto SA-RPB at 203; 313 and 323 K” (Figure 6), and “Fig. 7. Boyd plots for MB adsorption by SA-RPB at 303, 313, and 323 K” have been added. - The title names of figures have been also modified - Table: “Intra-particle diffusion model constant for MB adsorption by SA-RPB at different temperatures” (Table 4) has been added - Some contents have been added | As suggested by reviewer A |
| Discussion | Some contents have been modified |  |
| References | None |  |

2. Point-by-point responses of the reviewers comments

Reviewer A:

Comments for the authors:

This paper presents the adsorption of MB onto chemically modified Phragmites australis biomass. The paper needs improvements. The experimental data should be checked. Some clarifications should be made (see my comments).

Answer:

The authors thank reviewer for all remark points. The comments provided by the reviewers were extremely insightful and enabled us to improve the quality of our manuscript significantly. Agreeing with the reviewer’s suggestion, point-by-point has been incorporated throughout the revised manuscript.

Comment:

3.3.3. Effects of initial MB concentration and adsorption isotherms: “More than 94% MB was absorbed using 125 and 150 mg/L concentrations, and the dye equilibrium adsorptioncapacity (qe) decreased at higher concentrations (Fig. 6(a))”.

Attention! Please check your results. The dye equilibrium adsorption capacity (qe) should increase with increasing initial dye concentration.

Answer:

Thank you for paying attention to this fragment. It was our mistake. In this revised manuscript, the sentence has been corrected:

“More than 94% MB was absorbed at 125 and 150 mg/L concentrations, and the MB equilibrium adsorption capacity (qe) increased with higher initial dye concentrations”. (line 403-405)

Comment:

In order to study the effect initial concentration, the experiments should be carried out using a fixed biomass quantity, stirring rate, same temperature but varying the initial MB concentration. In order to study the effect of temperature, the experiments should be carried out using a fixed biomass quantity, stirring rate, same initial MB concentration but varying
the temperature. The experiments were performed as described above? I don’t understand why did you used for the isotherm modeling the experimental data obtained after studying the effects of initial MB and temperature. From fig 6 seems that the data were combined and used for isotherm modeling. You have to choose one set of data (the data from initial
MB concentration or temperature) for isotherm modeling. If you choose temperature, please use the experimental data obtained using the same initial MB concentration. Please check your data and make the necessary corrections. The data should be modelled again using the considered isotherm models. Please check also the data used for kinetic modeling.

Answer:

The authors thank reviewer for all remark points. In this submission, some sentences have been added: in subtitles 2.5.3 and 3.3.4. Some contents have been modified.

Line 271-272: “Adsorption isotherm tests were performed by adding 0.1 g SA-RPB into 100 mL MB at a concentration range of 125 - 300 mg/L”.

Line 399-401: “The effects of initial MB concentration (from 125 to 300 mg/L) on adsorption were determined by 0.1 g/L SA-RPB, at pH 6.5 and 303 K. Adsorption isotherms were analyzed at different initial MB concentrations, reflecting MB removal by SA-RPB (Fig. 8(a))”.

We focused on the temperature of 303 K, using different concentrations of MB. Data of temperatures 313 and 323 K have been deleted/modified.

Figure 6 (Figure 8 in this revised manuscript) has been modified.

Table 4 (Table 5 in this revised manuscript) has been modified.

Comment:

Pg. 16: Please explain the results obtained from Dubinin–Radushkevitch and Temkin isotherm.

Answer:

The authors thank reviewer for the suggestion. In this revised manuscript, the contents have been added (lines 427-433).

“Non-linear regression of the Temkin model fitted well with the experimental data with high R2(T) and low χ2(T) (Table 5). BT was 21.47 J/mol at 303K, reflecting the endothermic nature of adsorption. The R2(DR) value generated by Dubinin–Radushkevitch isotherm (Table 5) was significantly lower than those of other isotherms mentioned above. This result shows that the MB adsorption by SA-RPB was not well-aligned with the Dubinin–Radushkevitch isotherm. Moreover, mean energy of sorption (E) calculated from this model was 0.615 kJ/mol at 303 K, which proved the endothermic nature of adsorption”.

Comment:

Table 3. Please use the same format for the units (for eg. 1/min instead of min-1). Also, please correct the unit for k2 parameter. Please check the entire paper and correct where it is necessary.  
Answer:

It is our mistake which has been corrected in this submission.

Comment:

3.3.6. Possible mechanism of MB adsorption onto SA-RPB: The experimental data should be analyzed using intra-particle diffusion model of Weber and Morris and film diffusion model to determine the controlling mechanism of MB adsorption.

The authors thank reviewer for the suggestion. Weber and Morris and film diffusion model are important in determining absorption process. In this revised manuscript, the contents have been added:

- Title: 2.5.2. Adsorption mechanisms (lines 144-166)

- Title: 3.3.3. Intra-particle diffusion and film diffusion models (lines 364-397)

Comment:

3.4 Reusability: Why ethanol was used for MB desorption instead of 0.1 M HCl? Using diluted HCl the number of positively charged sites on the biomass increases. Thus, the desorption efficiency of MB dye increase due to the electrostatic repulsion between positively charged sites on the biomass and cationic MB molecules.

Answer:

The authors thank reviewer for the suggestion. During the experiments, HCl was used beside ethanol; however, the result was not significantly different. Therefore, ethanol which is common chemical and easy to handle is applied.

Comment:

3.4 Reusability: “The regeneration results showed that the adsorption capacity decreased by approximately 7% after four desorption–adsorption cycles compared with the first batch experiment”. As the number of desorption–adsorption cycles increases the removal efficiency decreases. I suggest investigating the adsorption performance of the adsorbent for MB sorption after six adsorption-desorption cycles or until three consecutive cycles exhibit similar removal efficiencies.

Answer:

Thanks for your suggestion. Authors spent more time to do the experiment, and the result of six cycles have been added in this submission:

Lines 529-531: “The regeneration results showed that the adsorption capacity decreased by approximately 7% after four desorption–adsorption cycles compared with the first batch experiment”.
------------------------------------------------------
------------------------------------------------------
Reviewer C:

Comments for the authors:

Paper could be accepted for publication after a minor revision, taking into account the suggestions presented in the Review report.

The topic of the paper is current and refers to the adsorption of methylene blue dye using an adsorbent obtained from Phragmites australis Stems. Generally, the manuscript is interesting, the experimental procedures were well designed and the article is correctly written. Paper could be accepted for publication after a minor revision, taking into account the following suggestions:

Answer:

The authors thank reviewer for all remark points. The comments provided by the reviewers were extremely insightful and enabled us to improve the quality of our manuscript significantly. Agreeing with the reviewer’s suggestion, point-by-point has been incorporated throughout the revised manuscript.

Comment:

1. In the Introduction section the novelty of the work must be better highlighted and clearly presented.

Answer:

The authors thank reviewer for the suggestion. In this revised manuscript, some contents have been added/modified:

Lines 62-64: “Some recent studies have used raw materials or raw materials modified with NaOH to treat MB.26,27 For instance, plant materials modified with citric acid (CA) show good potential for wastewater treatment”.

Lines 69-73: “It wildly grows all year round throughout the country of Viet Nam, especially in wetlands. In this study, the biomass of P. australis modified with NaOH and followed by esterification using citric acid (NaOH-then-CA treatment) was investigated in adsorbing MB from aqueous solutions. In addition, the effects of environmental parameters on MB adsorption by raw and modified adsorbents were evaluated”.

Comment:

2. Figure 3(b) - the experimental conditions of absorption must be specified.

Answer:

The authors thank reviewer for the suggestion, the title of Fig. 3 has been modified:

Lines 304-306: “Fig. 3. (a) Plots of point of zero charges of RPB, S-RPB, and SA-RPB (1.0 g/L adsorbent at different pH values); (b) percentage removal efficiency values for MB on RPB, S-RPB, and SA-RPB samples (150 mg/L MB at 6.5 pH value)”

Comment:

3. The resolution of Figure 6 needs to be improved.

Answer:

The authors thank reviewer for this remark point, the Figure 6 (Figure 8 in this revised manuscript) has been improved

4. Please careful check the English language. Some sentences are not well structured and some grammatical errors appear in the manuscript.

Comment:

The authors thank reviewer for the suggestion, English gramma has been checked and corrected.

Thank you for all,

Sincerely.