Supporting Information

Hybrid Polymer Composite of Prussian Red Doped Polythiophene for

Adsorptive Waste Water Treatment Application

Mohd Mustafa1, Shabnum Bashir1, Syed Kazim Moosvi2, Mohd. Hanief Najar3, Mubashir Hussain Masoodi4 * Masood Ahmad Rizvi1*

1Department of Chemistry, University of Kashmir, Hazratbal Srinagar, 190006, J&K, India.

2Department of School Education, Government of Jammu and Kashmir, Srinagar, Jammu and Kashmir, India.

3Department of Chemistry, Government College of Engineering & Technology, Safapora 193504, Jammu and Kashmir, India.

4Department of Pharmaceutical Sciences, University of Kashmir, Hazratbal Srinagar, 190006, J&K, India.

email:masoodku2@gmail.com, mubashir@kashmiruniversity.ac.in

Fig.S1(a) Effect of contact time on adsorption capacity of PTP/PR nanocomposite (20mg) for MG adsorption (10-25 mg/L in 30mL)at 298K,(b) Effect of initial concentrations on adsorption capacity of MG solution (30 mL) on PTP/PR nanocomposite (20mg), at 298K.

Fig.S2 Effect of PTP/PR adsorbent dosage (10-30 mg) towards adsorptive removal 	of (MG) dye(10mg/L in 30 mL) at 298K.

Fig.S3 Particle diameter calculations from DLS plot of PTP/PR nanocomposite at different adsorbent dosage (10-30 mg)

Fig.S4 FT-IR spectral changes of PTP/PR nanocomposite before and after adsorption 	of MG  dye.

Fig.S5 Supramolecular interaction for MG adsorption on PTP/PR nanocomposite schematically

Table S1: Intraparticle diffusion model parameters for MG adsorption at various initial concentrations(conditions: adsorbent dosage of 20mg in 30 mL solution,298K)

| C0 (mg/l) | Kid1mg/(g/min0.5) | C1mg/g) | R2 | Kid2 mg/(g/min0.5) | C2( mg/g) | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| 10 | 2.4 | 0.75 | 0.84 | 0.05 | 13.5 | 0.81 |
| 15 | 3.54 | 1.11 | 0.84 | 0.05 | 20.46 | 0.76 |
| 20 | 4.66 | 1.44 | 0.84 | 0.17 | 26.29 | 0.74 |
| 25 | 5.8 | 1.82 | 0.84 | 0.07 | 33.67 | 0.98 |