## Slide 1
60% decomposition
99%
decomposition
Figure 1. PTP/PR composite characterization (from selected peak picking) using FTIR spectra.
Figure 2.Thermogravimetric analysis plots showing PR enhanced thermal stability of PTP polymer.

## Slide 2
20nm
PR nanoparticles
PTP
Inset-1
Inset-2
B
Figure 3. X-ray diffraction pattern of PTP & PTP/PR nanocomposite (A). TEM image of PTP/PR nanocomposite (B) spherical shaped PR nanoparticles of PTP/PR nanocomposite (inset-1).Gaussian histogram fitting plot for particle size distribution (inset-2)
A

## Slide 3
Figure 4.N2 adsorption-desorption isotherms of PR, PTP and PTP/PR nanocomposite.Pore size distribution curves, Effect of PR Wt% on the surface area, pore volume of PTP/PR

## Slide 4
C
B
A
D
Figure 5. Kinetic models for data fitting of MG adsorption onto PTP/PR adsorbent (20mg in 30mL solution at 298K):(A) Pseudo-first order (B) Pseudo-second order (C) Elovich kinetic models (D) Intraparticle diffusion model

## Slide 5
(A)
(B)
(C)
Figure 6. Adsorption isotherms of MG on PTP/PR nanocomposite; (A) Langmuir (B) Freundlich (C)Temkin

## Slide 6
(A)
(B)
Figure7 (A) Temperature effect on MG (10 mg/L, 30 mL) adsorption on 20 mg PTP/PR composite (B) Van’t Hoff plot

## Slide 7
Chart: Time(min.)
| 20 | 40 | 60 | 80 | 100 | 120
pH 7 | 13.8855 | 13.92 | 13.9785 | 13.9935 | 14.1135 | 14.127
pH 4 | 13.254 | 13.359 | 13.4355 | 13.467 | 13.473 | 13.479
(A)
(B)
A
Figure 8. (A) Effects of solution pH on adsorption of MG (10 mg/L, 30 mL) onto the 20 mg of PTP/PR nanocomposite at 298 K.(B) Zeta potential studies of PTP/PR over pH range of 2-12.

## Slide 8
Chart: 
| C.R | M.O | RhB | M.G
 | 0.307 | 0.4 | 0.6 | 0.93
Chart: 
| deionised water | Real sample | tap water
 | 0.926 | 0.958 | 0.906
Figure 9.Adsorptive efficiency of PTP/PR towards: (A) real time samples (B) representative dyes from different dye classes.

## Slide 9
A
B
B
C
Figure 10.Comparative Cyclic Voltammograms of PR and PTP/PR at constant and increasing scan rates (A,B, C), (D,E) Linear relationship of peak currents with square root of scan rate
D
E

## Slide 10
Figure 10.Comparative Nyquist plots for PR and PTP/PR nanocomposite.

## Slide 11
Chart: Time(min)
| 5 | 10 | 15 | 20 | 25 | 30
Photocatalysis | 21 | 32 | 43 | 52 | 58 | 59
Adsorption | 31 | 47 | 65 | 75 | 80 | 93
Synergistic | 45 | 61 | 73 | 81 | 88 | 98
Figure 11. The synergistic effect of photocatalysis and adsorption for MG dye attenuation by PTP/PR nanocomposite

## Slide 12
(a)
(b)
Fig.S1(a) Effect of contact time on adsorption capacity of PTP/PR nanocomposite (20mg) for MG adsorption (10-25 mg/L in 30mL) at 298K,(b) Effect of initial concentrations on adsorption capacity of MG solution (30 mL) on PTP/PR nanocomposite (20mg), at 298K.
Fig.S2 Effect of PTP/PR adsorbent dosage (10-30 mg) towards adsorptive removal of (MG) dye(10mg/L in 30 mL) at 298K.

## Slide 13
Fig.S3 Particle diameter calculations from DLS plot of PTP/PR nanocomposite at different adsorbent dosage (10-30 mg)

## Slide 14
Fig.S4 FT-IR spectral changes of PTP/PR nanocomposite before and after adsorption of MG dye.