Supporting Information

Modified activated carbon with pistachio nut shells as an excellent surface to the preparation of copper magnetic nanocomposite and its application as recoverable catalyst for C-S coupling reaction 

Vajihe Nejadshafiee*, Ehsan Ghonchepour†, Hojatollah Khabazzadeh, Shahrzad Mahdavi Aliabad, Fatemeh Hassani Bagheri, and Mohammad Reza Islami‡
Chemistry Department, Shahid Bahonar University of Kerman, Kerman 76169, Iran.
Table of content page

Characterization of Cu-MAC@C4H8SO3H                                                                   S2

General procedure for synthesis of aryl thioquinazoline derivatives                          S5

1H and 13C NMR and CHN analysis of aryl thioquinazoline                                       S9
Characterization

FT-IR spectra were recorded on a commercial spectrophotometer (Bruker Tensor 27 FT -IR). 1H and 13C NMR spectra were recorded on a Bruker 400 Ultrashield NMR Magnet (400 MHz for 1H NMR) with TMS as the internal standard. Powder X-ray diffraction (XRD) spectra were recorded at room temperature with a Philips X-Pert 1710 diffractometer using Co Kα (λ=1.78897 Å) at a voltage of 40 Kv and a current of 40 mA and data were collected from 10° to 90° (2θ) with a scan speed of 0.02° s. The morphology of the catalyst was studied using scanning electron microscopy (SEM; Philips XL 30 and S-4160) with coated gold equipped with dispersive X-ray spectroscopy capability. Thermogravimetric analysis (TGA) and differential thermal analysis (DTA) were performed using a thermal analyzer with a heating rate of 20°C min in a temperature range of 25–1100°C under flowing compressed nitrogen. The magnetic property of the catalyst was measured with a vibrating sample magnetometer (VSM).

The FT-IR spectrum of the AC exhibits the bands corresponding to the functionalities containing hydroxyl─OH group (~3442 cm-1), carboxyl C=O group (~1719 cm-1), C=C (~1577 cm-1), C─O group (~1384 cm-1) (Fig. 1a). The presence of Fe─O band (~673 cm-1) in the FT-IR spectrum of Fe3O4 NPs@AC confirms that the Fe3O4 NPs located on the AC structure (Fig. 1b). In the Fig 1C, the new bands observed at 2919 cm-1 and 1036 cm-1 due to stretching vibrations of sp3 C─H and C─S bands respectively which prove 1,4-butane sultone loaded on the MAC@C4H8SO3H. Furthermore, the FT-IR spectrum of Cu-MAC@C4H8SO3H NCs exhibits a new absorption band at 583 cm−1 due to the presence of copper onto structure (Fig. S1d). 

[image: image1.emf]N

N

O

S


Fig. S1. FTIR spectra of (a) AC, (b) MAC (c) MAC@C4H8SO3H and (d) Cu-MAC@C4H8SO3H NCs.

Fig. S2 illustrates the XRD patterns of AC, MAC and MAC@C4H8SO3H. A broad diffraction peak was obtained at 2θ=25.31° for AC due to the plane of amorphous activated carbon. In XRD patterns of MAC, some peaks were appeared at 30.51°, 35.81°, 43.51°, 54.15°, 57.46°, 63.06 and 74.60° were related to the cubic spinel structure of magnetic nanoparticles. The XRD pattern of MAC@C4H8SO3H was almost similar to the MAC but the intensity of pecks decreased which could be related to immobilizing of C4H8SO3H onto MAC.

[image: image2.emf]N

N

O

S

OMe


Fig. S2. XRD patterns of (a) AC, (b) MAC and MAC@C4H8SO3H.

The morphology of AC, MAC and MAC@C4H8SO3H were deduced by TEM analysis and the TEM images were shown in Fig. S3.

The mesoporous structure of AC was observed by TEM (Fig. 3a). The TEM images of MAC and MAC@C4H8SO3H show that the Fe3O4 nanoparticles are coated onto AC (Fig. S3b-c). 
From Fig. S3b and c show that the particle size of MAC@C4H8SO3H is larger than MAC (from 30 to 50 nm, respectively), which could be due to the immobilization of 1,4-butane soltune onto the surface of the MAC. 

[image: image3.emf]N

N

O

S

Me


Fig. S3. TEM images of, (a) AC (b) MAC (c) MAC@C4H8SO3H NCs.

Thermal stability was studied by thermal gravimetric analysis of AC, MAC, MAC@C4H8SO3H and Cu-MAC@C4H8SO3H NCs in Fig. S4.

The thermal gravimetric analysis of AC displayed a weight loss below at temperatures of 175 °C, 200-400 °C, and 500-750 °C, which could be ascribed to the loss of adsorbed water (15.43 %), exclusion of oxygenated functional groups (8.85 %), and ultimately to the decomposition of AC (72.48 %), respectively (Fig. S4a). The TGA curve of MAC showed a weight loss about 51.14 % (Fig. 4b). For MAC@C4H8SO3H a weight loss occurred at 160-350 °C about 4.45 %, resulting from the pyrolysis of C4H8SO3H functional groups (Fig. S4c). Also, about 40.0 % of MAC and H3NSO3-MAC NCs retained at 750 °C, due to the remaining iron oxide. 

The TGA curve of Cu-MAC@C4H8SO3H showed an increase in temperature to 950 ºC which is related to the coordination of Cu(II) ions with the active sites of MAC@C4H8SO3H surface. Also, Cu-MAC@C4H8SO3H retained about 64.0 % of its weight at 950 °C, due to the residual of copper oxide and iron oxide (Fig. S4d).

[image: image4.emf]N

N

O

S

NO

2


Fig. S4. TGA plots of (a) AC, (b) MAC (c) MAC@C4H8SO3H and (d) Cu-MAC@C4H8SO3H NCs.
The magnetization curves of the MAC, MAC@C4H8SO3H and Cu-MAC@C4H8SO3H NCs are exhibited in Fig. S5. The saturation magnetization of the MAC and MAC@C4H8SO3H NCs was 21.73 and 16.33 emu g−1 respectively that this decrease in saturation magnetization can be attributed to the loading of C4H8SO3H on the MAC. Also, the saturation magnetization of the Cu-MAC@C4H8SO3H NCs was 14.23 emu g−1. This observed decrease in magnetic property was due to the loading of copper onto the surface of MAC@C4H8SO3H NCs.

[image: image5.emf]N

N

O

S

Br


Fig. S5. Magnetization curves of MAC, MAC@C4H8SO3H NCs and Cu-MAC@C4H8SO3H NCs.

The presence of Fe3O4, sulfamic acid and copper groups on the AC surface was further conﬁrmed by the EDS analysis of the MAC@C4H8SO3H and Cu-MAC@C4H8SO3H NCs (Fig. S6). 

[image: image6.png]MAgnetization (emu/g)

= mac
© MAC@HNSOH
4 MAC@HNSO H-Cu

Applied Field (Oe)

Intensity (a.u.)

20 (degeres)





Fig. S6. EDS pattern of a) MAC@C4H8SO3H NCs and b) Cu-MAC@C4H8SO3H NCs.

General procedure for the synthesis of aryl thioquinazoline derivatives in the presence of Cu-MAC@C4H8SO3H NCs

To a solution of arylhalide compound (0.5 mmol), 2-mercapto-3-phenylquinazolin-4(3H)-one (0.5 mmol) and 0.75 mmol K2CO3 in 1.5 mL DMF, was added 20 mg of Cu-MAC@C4H8SO3H as a catalyst. The mixture was heated and stirred at 110°C for 4 h. The progress of the reaction was monitored by TLC. After 4 h, the nanoparticles were separated by an external magnet from the reaction mixture and washed with DI water and diethyl ether repeatedly. Then, 50 ml of water was added to the reaction mixture and extracted with CH2Cl2 (2×25 mL) and dried over Na2SO4. The solvent was removed under reduced pressure to give the crude product. The residue was subjected to column chromatography using n-hexane and ethyl acetates an eluent to afford pure product.
3-phenyl-2-(phenylthio) quinazoline-4-(3H)-one (3a). IR (KBr): 3057, 2921, 1691, 1626, 1541, 1465, 1295, 1257, 1202, 767 cm-1, 1H NMR (400 MHz, CDCl3) (σ, ppm): 8.24 (s, 1H, ArH), 7.58- 7.56 (m, 4H, ArH), 7.42-7.33 (m, 4H, ArH); 13C NMR (100 MHz, CDCl3) (σ, ppm): 161.9, 157.1, 147.7, 136.0, 135.7, 134.4, 130.0, 129.7, 129.6, 129.3, 129.0, 128.6, 127.1, 126.7, 125.9, 119.9. Anal. calcd for C20H14N2OS (330.40): C 72.70, H 4.27, N 8.48, S 9.70; found: C 72.77, H 4.55, N 8.15, S 9.88.

2-((4-methoxyphenyl)thio-3-phenylquinazoline-4-(3H)-one (3b). IR (KBr): 3065, 1728, 1626, 1573, 1468, 1250, 1173, 690 cm-1. 1H NMR (400 MHz, CDCl3) (σ, ppm): 8.22 (s, 1H, ArH), 7.63- 7.61 (m, 3H, ArH), 7.60-7.58 (m, 2H, ArH), 7.45-7.42 (m, 4H, ArH), 7.37-7.352 (m, 2H, ArH). 7.45-7.42 (m, 4H, ArH), 6.95 (d, 1H, ArH), 3.85 (s, 1H, OCH3); 13C NMR (100 MHz, CDCl3) (σ, ppm): 161.9, 160.7, 157.7, 147.7, 137.3, 135.9, 134.3, 129.9, 129.6, 129.2, 126.9, 125.8, 119.8, 119.1, 114.6, 55.3. Anal. calcd for C21H16N2O2S (360.43): C 69.98, H 4.47, N 7.77, S 8.90; found: C 69.84, H 4.54, N 7.97, S 8.50. 
3-phenyl-2-(p-tolylthio)quinazoline-4-(3H)-one (3c). IR (KBr): 3066, 1682, 1573, 1464, 1256, 1197, 766 cm-1. 1H NMR (400 MHz, CDCl3) (σ, ppm): 8.23 (s, 1H, ArH), 7.65- 7.57 (m, 3H, ArH), 7.45-7.42 (m, 4H, ArH), 7.37-7.36 (m, 3H, ArH), 7.26-7.23 (m, 2H, ArH), 2.42 (s, 1H, CH3); 13C NMR (100 MHz, CDCl3) (σ, ppm): 162.1, 157.6, 147.9, 139.9, 136.2, 135.3, 130.1, 129.9, 129.4, 127.2, 126.8, 126.0, 120.1, 21.5. Anal. calcd for C21H16N2OS (344.43): C 73.23, H 4.68, N 8.13, S 9.31; found: C 72.99, H 4.67, N 8.23, S 9.10.

2-((4-nitrophenyl)thio)-3-phenylquinazoline-4-(3H)-one (3d). IR (KBr): 3104, 2974, 2925, 1690, 1548, 1511, 1466, 1343, 1258, 1050, 769 cm-1. 1H NMR (400 MHz, CDCl3) (σ, ppm): 8.27-8.25 (m, 2H, ArH), 8.23 (m, 1H, ArH), 7.76-7.74 (m, 2H, ArH), 7.68 (m, 1H, ArH), 7.62-7.61 (m, 2H, ArH), 7.44-7.42 (m, 4H,ArH), 7.37-7.35 (m, 1H, ArH); 13C NMR (100 MHz, CDCl3) (σ, ppm): 161.0, 154.5, 147.7, 146.7, 136.5, 134.3, 135.0, 134.2, 129.8, 129.3, 128.6, 125.9, 123.2, 119.5. Anal. calcd for C20H13N3O3S (344.43): C 63.99, H 3.49, N 11.19, S 8.54; found: C 63.77, H 3.44, N 11.31, S 8.84.

2-((4-bromophenyl)thio)-3-phenylquinazoline-4-(3H)-one (3e). IR (KBr): 3067, 1695, 1549, 1466, 1260, 1110, 765 cm-1. 1H NMR (400 MHz, CDCl3) (σ, ppm): 8.23 (m, 1H, ArH), 7.66-7.64 (m, 1H, ArH), 7.61-7.58 (m, 2H, ArH), 7.57-7.55 (m, 2H, ArH), 7.43-7.36 (m, 7H,ArH); 13C NMR (100 MHz, CDCl3) (σ, ppm): 161.6, 156.2, 147.4, 137.0, 135.6, 132.0, 129.6, 129.0, 127.5, 126.9, 126.5, 125.9, 124.1, 119.8. Anal. calcd for C20H13BrN2O3S (409.30): C 58.69, H 3.20, N 6.84, S 7.83; found: C 58.92, H 3.24, N 6.91, S 7.55. 
Copy of 1H NMR, 13C NMR & CHNS of the synthesized compounds.

3-phenyl-2-(phenylthio) quinazoline-4-(3H)-one (3a).
[image: image7.jpg]Entensity (a.u.)

1t (@)

Fe

Fe

3 4 5 6 7 8 38
Energy (keV)




2-((4-methoxyphenyl)thio-3-phenylquinazoline-4-(3H)-one (3b).
[image: image8.jpg]Entensity (a.u.)

(o)

Fe

5

e
w

Energy (keV)

4 5 6 4 8 9




3-phenyl-2-(p-tolylthio)quinazoline-4-(3H)-one (3c).
[image: image9.jpg]MAgnetization (emu/g)

20 |

30

30 4

[
.
A

MAC
MAC@C,H,SOH
Cu-MAC@C H,SOH

20 -

ey

T
15000

T T T T T T
10000 5000 J 5000 10000 15000
Applied Field (Oe)




2-((4-nitrophenyl)thio)-3-phenylquinazoline-4-(3H)-one (3d).
[image: image10.jpg]Transmittance (%)

(@)

(c)

(b)

v
(@) Fe-
OH C=0 \C= c
40'00 35'00 30'00 25'00 20‘00 1 5'00 1 0‘00 560

Wavenumber (cm 1)





2-((4-bromophenyl)thio)-3-phenylquinazoline-4-(3H)-one (3e).
[image: image11.jpg]200 nm





� EMBED ChemDraw.Document.6.0  ���





� EMBED ChemDraw.Document.6.0  ���





� EMBED ChemDraw.Document.6.0  ���





� EMBED ChemDraw.Document.6.0  ���





� EMBED ChemDraw.Document.6.0  ���








* Corresponding author. Tel: +98 034 31312200, E-mail address: nejadshafiee@sci.uk.ac.ir


† � HYPERLINK "mailto:Ghonchepoor@gmail.com" �Ghonchepoor@gmail.com�





‡ mrislami@uk.ac.ir





12

[image: image12.jpg]Weight (%)

= AC
e MAC
wl 4 MAC@CMH,SOH

v Cu-MAC@C H,SOH

80 4

60 -

0

204

0 T T T T T
o 200 400 600 800 1000

Temperature (°C)



[image: image13.jpg]— EK-1_11-Mar-2019_060

¥ Inyding 29961

€ uaboipAH e0v'g

[min]

20

15

400+

300

abeyop

Time



[image: image14.jpg]STANDARD FLUORINE PARAMETERS SIRRRRREEERRRARSRACISRRRRARRR Shu400
T W bbbl L LT S i
[ Parameter Ve
1 DataFile Name 1300
|2 orgn varian
3 Specvometer 1200
|4 sovent cids
| |5 Temperature 50
‘s Pulse Sequence. s2pul i
7 Nomberofsans 1
8 Recewer Gan =2 1000
|o Rematnosey Lo
) 10 pudse vidtn 00000 -
i |11 AcqustionTime 20480
2 AcustonDate 019027141415
ModfatonDate 2013025714158 | [800
|14 ‘Spectrometer Frequency 500.02
15 Spectal vickh s000.0 s
lonestFrequeney 9983
17 uceus W
| Acquired Size 16384 600
| 19 Spectral Size: 32768
T
400
f 300
200
100
\_;/ ilg
g ——
::;ESEE&Q {100
13 12 1 10 9 s 7 5 4 3 2 1 0 2

s
1 (oom)



[image: image15.emf]N

N

O

S

[image: image16.jpg]B2 ossmmmasessssee Peremeter e
Gradient Shimming 35 $5S:5SRR2335RSE 1 Data Fie Name.
Eniieininiey
[ == 2 Origin Varian
3 Spectometer o
4 Sohent cids
5 Tenperatire 0
& puse sequence s
7 Nomberofscans 100
§ Recever Gan 2
9 Relatoneey 10000
10 e Vi 0.0000
11 Acqison Tme Lot24
[l t 12 Acquisition Date 2018-12-16T11:16:08
13 ModfcatonDate 2015-12-16T1 15314
13 Spectrometer Frequency 125.74
15 SpectralVidth 132
16lovestFrequeney 18670
17 uceus 1
18 Acqured sze 70
19 Sectralsie ess36
i i
.
'
20 220 20 200 190 180 170 160 150 140 130 120 10 100 90

f1 (ppm)

45

40

35

30

25



[image: image17.jpg]SNNIBRIRSIITIILARARES Parameter Valve
STANDARD FLUORINE PARAMETERS GRS 1 Data Fie Name
2 orign Varian
3 Specrometer inova
4 Solvent 3
i 5 Temperatire 20

6 Puise Sequence szl
7 Number of Scans 5
8 Receiver Gan #
9 Relaxaton Delay 10000

| \ e aF o

. I AcqistonTme 20460
12 Acquiston Date 21902257 12:5239
13 Modfication Date 2019-02-25T12:53:06
14 Specirometer Frequency 500.02
15 Speciral Width a000.0
16 Lowest Frequency  -1001.3
17 Nudleus H
18 Acquired Size 16384
19 Specira Size 32768

T gl &

13 12 1 10 8 7 5 1

2200

F2100

2000

1900

1800

F1700

1600

F1s00

1400

1300

1200

F1100

1000

900

800

700

600

500

400

300

200

100




[image: image18.jpg]Parameter Value

STANDARD FLUORINE PARAMETERS S35 ShEIEiiEfEiii t Daaie tone 100
Vi e [ v
|3 spectometer inova
[+ o o N
|5 Temperatre 20
|6 Pulse sequence s2pul
|7 tomberofscans 1892
|8 Receter Gan » 80
|5 ReasctionDday 10000
| 10 pule viatn 0.0000
| 11 Acquisiton e 10424
| 12 Acqusition ate 902 sTizsas | [70
| 13 vodcationDate  019.02257 13157258
| 14 Spectometer Frequency 125.74
s e a2 ©
| 16 Lonest Frequeney 65673
| 17 huges 13
| 18 Acqured size 768
|19 e s 50

55 a8 fatn St} vioSt Dot o B SO0 [etpylte, fofpaodl el 76 (GG B 0y B ped by oo oid
1 (ppm;



[image: image19.jpg]— EK-2_11-Mar-2019_058

b Inydns 21261

€ ueBoipiH e9v'g

1 ueBoN 00€'L

20

15

)

[mv]

abejo

[rin.]

Time



[image: image20.emf]N

N

O

S

OMe

[image: image21.jpg]t8s0

800

750

700

650

600

550

500

Fas0

400

350

F300

250

200

F1s0

100

Ve
st
st
s
e
we
e
e
ere
b
e
e
e
ase
ise
03¢
o9e
ove
7
19
e
25
e
ase
eve
e9e
e
sve

e
e
ecn
i

STANDARD FLUORINE PARAMETERS

=

[

b1
::
st
oz
e
TeE

o

10

1

12

D)



[image: image22.jpg]65

60

ie—

ey
7

orozr
arser
Twaer
vaozt
et
evcr
Vet
a6
arocr

Isva
scsaf
ccan

STANDARD FLUORINE PARAMETERS

-10

0 2 10

40

20 210 20 10 18 170 160 130 40 130 120 10 100 S 8 70
1 (pom)

230



[image: image23.emf]N

N

O

S

Me

[image: image24.jpg]— BK3_11-Mar-2019_059

b NS 15961

€ usbopfH orr's.

5001
400
E

abejop,

2009
1001
o

5

10

[min]

=



[image: image25.jpg]1000

e
we
we
e
e
e
i
e
e
e
192
19
ase
2
ave
be
vie
ace
ern
ecn
ves
seo
seo
see
s
e
P

STANDARD FLUORINE PARAMETERS

200
200
70
600
500
400
300
200
100

1 (pom)

10

11

12

13




[image: image26.jpg]STANDARD FLUORINE PARAMETERS 3 F Bfsfgzzzszasas o
Parameter Value [TV SN e
1 Dota Fie Name
55
2 orign Varian
3 Spectrometer inova
4 Sovent cad3 Lso
5 Temperature 20
6 Puse Sequence szl
7 Number of Scans: 1 b 5 .
8 Receiver Gain 2 '
9 Relaxation Delay 10000 |
10 Puise Width 0.0000
11 Acquiston Time 2080 0
12 Acquiston Date 21802257 14:14:15
13 Modfication Date  2019-0225T14:14:48
14 Specirometer Frequency 500,02 33
15 Speciral Width 8000.0
16 LowestFrequensy 10014
17 Nudleus ™ i 30
18 Acguired Size 16384
19 Spectral Sze 32768
25
L
[ 20
15
10
|
5

B0 m U S0 SR A i el s L G M BENF G B6 W H W W X om WoW W
1 (ppm;



[image: image27.jpg]— EK-4_11-Mar-2019_061

| usboIN L06°L

¥ nydng 059°61.

€ ueBoIAH 035’8

20

15

)

V]

obejop

200
1004

[min]



[image: image28.emf]N

N

O

S

NO

2

[image: image29.jpg]600
550
500
450

400

350

300

250

200
150
100
50
0

st
st
ot
e
e
we
e
sse
st
s
st
19¢
2ye

v
vz =
ave

o
fitog =

STANDARD FLUORINE PARAMETERS

s
1 (pom)

12 11 10

13



[image: image30.jpg]STANDARD FLUORINE PARAMETERS

12908
12752
12638
12646
12597
12415
1o

13700
13567
7700
7680
7658

Parameter Value

1 DataFie Name

2 orgn Varian
3 Spectrometer inova

4 Solvent a3

5 Temperature 20

6 Pulse Sequence 2ol

7 Number of Scans. 2000

8 Receiver Gan EY

5 Relaxation Delay 10000

10 Puse Width 0.0000

11 Acquisiton Time L0424

12 Acquisiton Date: 20190226 10:04:33
13 Modifcation Date. 20190226 10:05:12
14 Spectrometer Frequency 125.74

15 Spectral Width 314342

16 LowestFrequency  -1807.5

17 Nuceus 15

18 Acquired Size 52788

18 Spectral Sz 65536

——
— 15610
— 14745

/

230 220 210 200 190 180

70

65

60

50

45

40

35

30

25

20

15

10




[image: image31.emf]N

N

O

S

Br

[image: image32.jpg]— EK6_11-Mar-2019_057

b nudng £2.'61

7

)

£ UeBoIpAH 06E'8

| uebonN 157}

[mv]

400]

3001
2001
100

of

obejon



_1695922262.cdx

_1696243509.cdx

_1696243569.cdx

_1696095342.cdx

_1695832581.cdx

