Table 1. Adsorption acceleration and velocity parameters for the first and second region and related  and  values obtained from analysis of some adsorption processes by the KASRA model

| Symbol |  | Adsorption process | First region |  |  |  | Second region |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  | Ref. |
| A | Adsorption of oxalic acid on animal charcoal at 308 K |  | 0 | 9.0×10−3 | 10 | 0.02 | –2.0×10−5 | 2.0×10−2 | 23 |
| B | Adsorption of natural dissolved organic matter (in terms of DOC) by multiwalled carbon nanotubes at 5 ˚C |  | 0 | 0.33 | 5.3 | 1.4 | –6.7×10−5 | 8.7×10−3 | 24 |
| C | Adsorption of natural dissolved organic matter (in terms of AOC) by multiwalled carbon nanotubes at 5 ˚C |  | –2.0×10−4 | 5.2×10−3 | 20.3 | 0.08 | –1.2×10−5 | 9.2×10−4 | 24 |
| D | Adsorption of direct yellow12 on coconut shell activated carbon |  | –0.02 | 1.46 | 10 | 14.9 | –1.4×10−4 | 1.49 | 25 |
| E | Adsorption of basic blue 3 onto sphagnum agellanicum peat |  | 0 | 9.75 | 1.2 | 11.7 | –3.6×10−2 | 0.54 | 26 |
| F | Adsorption of reactive red 239 from aqueous solution by chitosan 8B |  | –0.17 | 0.61 | 10 | 9.6 | –4.0×10−3 | 0.24 | 27 |
| G | Adsorption of methylene blue on activated carbon obtained from waste Elaeagnus stone |  | 0 | 13.90 | 10.3 | 143.4 | –3.8×10−2 | 2.88 | 28 |
| H | Adsorption of malachite green on activated carbon obtained from waste Elaeagnus stone |  | 0 | 20.90 | 9.6 | 200.7 | –5.6×10−2 | 4.75 | 28 |
| I | Adsorption of rhodamine B on activated carbon obtained from waste Elaeagnus stone |  | 0 | 14.27 | 10.3 | 147.0 | –2.4×10−2 | 2.30 | 28 |
| J | Adsorption of methyl orange on banana peel* |  | 0 | 0.16 | 5 | 0.8 | –4.0×10−3 | 0.27 | 29 |

Table 1 continued

| Symbol |  | Adsorption process | First region |  |  |  | Second region |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  | Ref. |
| K | Adsorption of methylene blue on orange peel* |  | 0 | 0.30 | 5 | 1.5 | –0.01 | 0.45 | 29 |
| L | Adsorption of methylene blue on poly(acrylic acid) (PAA)-based super-adsorbent nanocomposite hydrogel |  | 0 | 5.72 | 12.8 | 73.2 | –8.4×10−2 | 10.45 | 30 |
| M | Adsorption of remazol Y onto steam-activated carbons developed from date pits at pH=3 and 37 ˚C |  | 0 | 24.52 | 1.7 | 41.7 | –0.12 | 2.03 | 31 |
| N | Adsorption of methylene blue onto steam-activated carbons developed from date pits at pH=5 and 27 ˚C |  | 0 | 88.58 | 1.2 | 106.3 | –8.8×10−2 | 2.95 | 31 |
| O | Adsorption of acid red on corn stalks modified bycetylpyridinium bromide at 328 K |  | 0 | 2.03 | 3.5 | 7.1 | –4.0×10−3 | 0.26 | 32 |
| P | Adsorption of acid orange on corn stalks modified bycetylpyridinium bromide at 318 K |  | 0 | 2.28 | 5.6 | 10.5 | –2.0×10−3 | 0.15 | 32 |
| Q | Adsorption of malachite green on seeds of dates at 15 ˚C |  | –0.60 | 6.75 | 14.2 | 92.5 | –0.39 | 12.64 | 33 |
| R | Adsorption of methylene blue on nanocrystalline cellulose at 318 K and 80 rpm and 0.045 mM methylene blue |  | –4.4×10−2 | 0.21 | 10 | 2.8 | –8.7×10−4 | 0.08 | 19 |

Units of and  were in mg g-1 hour-2,  and  were in mg g-1 hour-1 and  and  were in hour and mg g-1 in example L and  and  were in μmol g-1 min-2,  and  were in μmol g-1 min-1 and  and  were in min and μmol g-1 in example F, respectively. In other cases,  and  were in mg g-1 min-2,  and  were in mg g-1 min-1 and  and  were in min and mg g-1, respectively. *In examples J and K, TD values were 2.5 and 2 min before starting adsorption process, respectively.

Table 2. Non-ideal adsorption acceleration and velocity parameters for the first and second curves and related  and  values obtained from analysis of some adsorption processes by the NIPPON equation

| Symbol |  | Adsorption process | First curve |  |  |  |  | Second curve |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  | Ref. |  |
| A | Adsorption of oxalic acid on animal charcoal at 308 K |  |  | –0.01 | 0.01 | – | – | – | – | 23 |  |
| B | Adsorption of natural dissolved organic matter (in terms of DOC) by multiwalled carbon nanotubes at 5 ˚C |  |  | 0 | 0.33 | 5.3 | 1.4 | –0.005 | 0.03 | 24 |  |
| C | Adsorption of natural dissolved organic matter (in terms of AOC) by multiwalled carbon nanotubes at 5˚C |  |  | 0.035 | –0.035 | – | – | – | – | 24 |  |
| D | Adsorption of direct yellow12 on coconut shell activated carbon |  |  | 0 | 1.49 | 20 | 30.2 | –0.46 | 5.02 | 25 |  |
| E | Adsorption of basic blue 3 onto sphagnum agellanicum peat |  |  | 0 | 9.75 | 1.2 | 11.7 | –0.59 | 1.29 | 26 |  |
| F | Adsorption of reactive red 239 from aqueous solution by chitosan 8B |  |  | –4.18 | 4.18 | – | – | – | – | 27 |  |
| G | Adsorption of methylene blue on activated carbon obtained from waste Elaeagnus stone |  |  | –17.88 | 17.88 | – | – | – | – | 28 |  |
| H | Adsorption of malachite green on activated carbon obtained from waste Elaeagnus stone |  |  | –19.07 | 19.07 | – | – | – | – | 28 |  |
| I | Adsorption of rhodamine B on activated carbon obtained from waste Elaeagnus stone |  |  | –17.54 | 17.54 | – | – | – | – | 28 |  |
| J | Adsorption of methyl orange on banana peel* |  | 0 |  | 0.16 | 5 | 0.8 | –0.10 | 0.61 | 29 |  |

Table 2 continued

| Symbol; Adsorption process; First curve; Second curve. Ref.. |
| --- |
| K | Adsorption of methylene blue on orange peel* | 0 | 0.30 | 5 | 1.5 | –0.15 | 0.88 | 29 |
| L | Adsorption of methylene blue on poly(acrylic acid) (PAA)-based super-adsorbent a nocomposite hydrogel | 0 | 5.72 | 12.8 | 73.2 | –1.51 | 20.79 | 30 |
| M | Adsorption of remazol Y onto steam-activated carbons developedfrom date pits at pH=3 and 37 ˚C | 0 | 24.52 | 1.7 | 41.7 | –1.47 | 3.96 | 31 |
| N | Adsorption of methylene blue onto steam-activated carbons developed from date pits at pH=5 and 27 ˚C | 0 | 88.58 | 1.2 | 106.3 | –5.15 | 11.32 | 31 |
| O | Adsorption of acid red on corn stalks modified by cetylpyridinium bromide at 328 K | 0 | 2.03 | 3.5 | 7.1 | –0.14 | 0.63 | 32 |
| P | Adsorption of acid orange on corn stalks modified by cetylpyridinium bromide at 318 K | 0 | 2.28 | 5.6 | 10.5 | –0.05 | 0.31 | 32 |
| Q | Adsorption of malachite green on seeds of dates at 15 ˚C | –56.61 | 56.61 | – | – | – | – | 33 |
| R | Adsorption of methylene blue on nanocrystalline cellulose at 318 K and 80 rpm and 0.045 mM methylene blue | –1.34 | 1.34 | – | – | – | – | 19 |

Units of  and  were in mg g-1 hour-2,  and  were in mg g-1 hour-1 and  and  were in hour and mg g-1 in example L and  and  were in μmol g-1 min-2,  and  were in μmol g-1 min-1 and  and  were in min and μmol g-1 in example F, respectively. In other cases,  and  were in mg g-1 min-2,  and  were in mg g-1 min-1 and  and  were in min and mg g-1, respectively. *In examples J and K, TD values were 2.5 and 2 min, and thus for first curve,  and  min were used in Eqs. (10) and (11), respectively. Subscripts fc, sc and tc are abbreviations for starting first curve and starting second curve, respectively.

Table 3. TRAKs for adsorption of MnO4- on Co-Al-LDH in 0.1 M NaCl and acidic             and alkaline solutions at 308–328 K

| Solvent | T |  | [MnO4-]0 | rpm |  | qTRAKC1-C2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  | (mM) |  | (min-min) | (mg g-1) | (min) | (mg g-1) |
| 0.1 M NaCl* |  | 318 | 0.5 | 100 | 300–360 | 141.4–141.7 | 1290 | 316.3 |
| pH=2.8** |  | 318 | 0.5 | 100 | 60–90 | 82.5–85.7 | 1290 | 278.3 |
| pH=12* |  | 318 | 0.5 | 100 | 180–420 | 178.3–185.4 | 660 | 273.6 |
| pH=14** |  | 318 | 0.5 | 100 | > 0.5–180 | 112.2–110.1 | 930 | 216.6 |

is the observed TRAKs between the first and second kinetic curves. *TRAK appeared at the

end of ME sites range. **TRAK was in the time range of ME sites.  is the time of reaching equilibrium.

Table 4. Experimental , , , ,  and  values and coefficients obtained from the KASRA equation and values of intraparticle diffusion equation for kinetics of MnO4- adsorption on Co-Al-LDH at different temperatures and in various shaking rates and initial MnO4- concentrations

| Solvent | T |  | [MnO4-]0 |  |  | rpm |  |  |  | KASRA region 1 (1st curve) |  |  |  |  |  | KASRA region 2 (1st curve) |  |  |  |  |  | KASRA region 2 (2nd curve) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  |  | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to: |  |  |  |  |  |  | ARIAN region I (ME Site) |  |  |  |  |  |  |  | ARIAN section IIA (ME Site) |  |  |  |  |  |  |  | ARIAN section IIB (MI Site) |  |  |  |  |  |
| Water | 318 |  |  | 0.25 | 100 |  | (1350,177.7) |  |  | –2.0×10-2 |  | 1.00 | 4.7 | (30,20.9) |  |  | –9.9×10-5 | 0.18 | 5.2 | – |  |  |  | – |  | – |  | – |
|  | 308 |  |  | 0.50 | 100 |  | (1470,160.0) |  |  | –1.3×10-3 |  | 0.39 | 4.1 | (300,59.7) |  |  | –1.9×10-4 | 0.13 | 3.8 | (780,100.3) |  |  |  | –8.5×10-5 |  | 0.18 |  | 5.8 |
|  | 318 |  |  | 0.50 | 100 |  | (1650,275.6) |  |  | –2.3×10-2 |  | 1.42 | 6.8 | (60,43.7) |  |  | –2.1×10-3 | 0.54 | 7.4 | (300,113.2) |  |  |  | –1.4×10-4 |  | 0.25 |  | 6.8 |
|  |  | 328 |  | 0.50 | 100 |  | (1110,266.7) |  |  | –4.2×10-2 |  | 1.58 | 6.8 | (30,27.3) |  |  | –3.6×10-3 | 0.95 | 12.3 | (240,148.0) |  |  |  | –2.3×10-4 |  | 0.31 |  | 7.6 |
|  |  | 318 |  | 0.70 | 100 |  | (1350,319.3) |  |  | –6.8×10-2 |  | 2.55 | 8.5 | (30,46.3) |  |  | –3.2×10-3 | 0.59 | 8.7 | (180,99.5) |  |  |  | –2.9×10-4 |  | 0.36 |  | 10.2 |
|  |  | 318A 0.50 |  |  | 70 |  | (1290,281.1) |  | –1.6×10-2 |  |  | 1.15 | 5.9 | (60,38.6) |  |  | –1.0×10-3 | 0.50 | 8.2 | (420,142.6) |  |  |  | –3.6×10-4 |  | 0.31 |  | 10.3 |
|  |  | 318B 0.50 |  |  | 40 |  | (1470,293.7) |  | –4.2×10-3 |  |  | 0.82 | 6.9 | (120,58.7) |  |  | –6.1×10-4 | 0.30 | 6.7 | (420,123.8) |  |  |  | –2.9×10-4 |  | 0.30 |  | 11.2 |
| 0.1M NaCl |  | 318 |  | 0.50 | 100 |  | (1290,316.3) |  |  | –0.46 |  | 4.76 | 10.2 | (10,25.0) |  |  | –1.7×10-3 | 0.65 | 6.7 | C(360,141.7) |  |  |  | –3.1×10-4 |  | 0.33 |  | 11.3 |
| pH=2.8 |  | 318 |  | 0.50 | 100 |  | (1290,278.3) –2.9×10-2 |  |  |  |  | 2.24 | 10.8 | D(90,85.7) |  |  | –2.0×10-4 | 0.29 | 7.3 | – |  |  |  | – |  | – |  | – |
| pH=3.8 |  | 318 |  | 0.50 | 100 |  | (780,293.3) |  |  | –6.8×10-2 |  | 4.03 | 18.3 | (60,120.4) |  |  | –9.3×10-4 | 0.55 | 11.2 | – |  |  |  | – |  | – |  | – |
| pH=12 |  | 318 |  | 0.50 | 100 |  | (660,273.6) |  |  | –0.19 | 5.53 |  | 14.1 | (30,82.6) |  |  | –8.2×10-3 | 1.21 | 11.6 | E(420,185.4) |  |  |  | –8.1×10-4 |  | 0.46 |  | 16.8 |
| pH=13 |  | 308 |  | 0.50 | 100 |  | (1110,289.4) |  |  | –6.3×10-3 |  | 1.14 | 9.1 | (180,107.2) |  |  | –4.8×10-4 | 0.42 | 11.6 | – |  |  |  | – |  | – |  | – |
| pH=13 |  | 318 |  | 0.50 | 100 |  | (1470,315.7) |  |  | –6.6×10-3 |  | 1.16 | 9.4 | (180,103.8) |  |  | –2.2×10-4 | 0.30 | 8.8 | – |  |  |  | – |  | – |  | – |
| pH=13 |  | 328 |  | 0.50 | 100 |  | (930,309.5) |  |  | –8.2×10-3 |  | 1.51 | 17.4 | (120,122.7) |  |  | –1.0×10-3 | 0.58 | 12.1 | – |  |  |  | – |  | – |  | – |
| pH=14 |  | 318 |  | 0.50 | 100 |  | (930,216.6) |  |  | Very fast (0.5 min < )F |  |  |  | (180,110.1) |  |  | –4.8×10-4 | 0.31 | 7.7 | – |  |  |  | – |  | – |  | – |

Units of , and  are in mg g-1 min-2 and those of ,  and  are in mg g-1 min-1, respectively. Units of ,  and   are in min and those of ,  and  are in mg g-1, respectively. In region 1,  and  are equal to zero. A and B refer to cases that there were TDs at 4 and 5 min before starting adsorption process, respectively. C, D, E and F refer to TRAKs in the range of 300–360, 60–90, 180–420 and >0.5–180 min, respectively.

Table 5. Coefficients of region 1 and region 2 (parts 2a and 2b) of the ISO equation for kinetics of MnO4- adsorption on different sites of Co-Al-LDH at 308–328 K

| Solvent | T | [MnO4-]0 |  |  | rpm kI1 |  |  | (tssr,qssr) |  |  | kI2a (tsp,qsp) kI2b ([MnO4-]t,max1,t1,qt,max1) kI2a (tsp,qsp) kI2b |  |  |  |  |  |  |  |  |  | ([MnO4-]e ,te,qe) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) (mM) |  |  |  |  | (min,mg g-1) (min,mg g-1) (mM,min,mg g-1) (min,mg g-1) (mM,min,mg g-1) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to: |  |  |  |  |  |  | ARIAN region I and section IIA (ME Site) |  |  |  |  |  |  |  |  |  |  | ARIAN section IIB (MI Site) |  |  |  |
| Water | 318 |  | 0.25 | 100 |  | 3562 |  | (30,20.9) | 130 |  |  | (360,76.7) |  | 2803 |  | (0.025,1350,177.7) | – |  | – | – | – |
|  | 308 |  | 0.50 | 100 |  | 645 |  | (300,59.7) | – |  |  | – |  | 1075 |  | (0.37,780,100.3) | 1022 (1290,151.1) |  |  | 3227 | (0.30,1470,160.0) |
|  | 318 |  | 0.50 | 100 |  | 1841 |  | (90,43.7) | – |  |  | – |  | 3745 |  | (0.36,300,113.2) | 1743 |  | (930,220.4) | 3155 | (0.15,1650,275.6) |
|  | 328 |  | 0.50 | 100 |  | 2699 |  | (90,27.3) | – |  |  | – |  | 6391 |  | (0.31,240,148.0) | 2188 |  | (540,212.2) | 7842 | (0.15,1110,275.6) |
|  | 318 |  | 0.70 | 100 |  | 3571 |  | (15,31.5) | – |  |  | – |  | 2805 |  | (0.5,180,99.5) | 1317 |  | (660,230.7) | 4052 | (0.31,1350,316.3) |
|  | 318A 0.50 |  |  | 70 |  | 1785 |  | (240,108.1) | – |  |  | – |  | 5082 |  | (0.32,420,142.6) | 2729 |  | (660,208.1) | 6042 | (0.14,1290,281.1) |
|  | 318B 0.50 |  |  | 40 |  | 1731 |  | (300,101.6) | – |  |  | – |  | 2164 |  | (0.34,420,123.8) | 2155 |  | (600,178.7) | 5727 | (0.13,1470,293.7) |
| 0.1M NaCl | 318 |  | 0.50 | 100 |  | 2467 |  | (180,106.9) | – |  |  | – |  | 9031 |  | C(0.32,300,141.4) | 3176 |  | (780,250.2) | 14292 | (0.10,1290,316.3) |
| pH=2.8 | 318 |  | 0.50 | 100 |  | 4708 |  | (30,56.7)D | 2072 |  |  |  | (660,223.4) | 7156 |  | (0.15,1290,278.3) | – |  | – | – | – |
| pH=3.8 | 318 |  | 0.50 | 100 |  | 6836 |  | (60,120.4) |  | 4557 |  |  | (360,252.2) | 9114 |  | (0.13,780,293.3) | – |  | – | – | – |
| pH=12 | 318 |  | 0.50 | 100 |  | 7866 |  | (60,112.9) – |  |  |  | – |  |  | 12461 | E(0.29,180,178.3) | 5550 |  | (540,229.0) | 31450 | (0.15,660,273.6) |
| pH=13 | 308 |  | 0.50 | 100 |  | 1607 |  | (180,107.2) |  | – |  | – |  | 3638 |  | (0.13,1110,289.4) | – |  | – | – | – |
| pH=13 | 318 |  | 0.50 | 100 |  | 2348 |  | (420,168.7) |  | – |  | – |  | 18820 |  | (0.04,1470,315.7) | – |  | – | – | – |
| pH=13 | 328 |  | 0.50 | 100 |  | 4859 |  | (480,263.8) |  |  | – | – |  | 18006 |  | (0.11,930,309.5) | – |  | – | – | – |
| pH=14 | 318 |  | 0.50 | 100 |  | – (0.36,0.5<,112.2)F 3358 (540,194.4) |  |  |  |  |  |  |  | 6427 |  | (0.23,930,216.6) | – |  | – | – | – |

[MnO4-]t,max1 , t1 and qt,max1 are MnO4- concentration, time and adsorption capacity at the end of the adsorption on ME site, respectively (corresponding to [MnO4-]e , te and qe on MI site). [MnO4-]e , te and qe are MnO4- concentration, time and adsorption capacity at the beginning of the plateau, respectively. Units of  ,  and  are in mg g-1 M-1 min-1. A and B refer to cases that there were TDs at 4 and 5 min before starting adsorption process, respectively. C, D, E and F refer to TRAKs in the range of 300–360, 60–90, 180–420 and >0.5–180 min, respectively.

| Solvent | T |  | [MnO4-]0 |  |  | rpm |  |  | NIPPON curve 1 |  |  |  |  |  | NIPPON curve 2 |  |  |  |  |  |  | NIPPON curve 3 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  |  | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Water | 318 |  |  | 0.25 | 100 |  | (1350,177.7) |  |  | –2.7×10-2 | 1.07 |  | (16,12.6) |  |  |  | –5.9×10-2 |  | 1.01 |  | (241,61.1) |  | –1.2×10-3 | 0.29 |
|  | 308 |  |  | 0.50 | 100 |  | (1470,160.0) |  |  | –4.0×10-3 | 0.49 |  | (90,28.3) |  |  |  | –4.0×10-3 |  | 0.36 |  | (780,100.3) |  | –1.6×10-4 | 0.12 |
|  | 318 |  |  | 0.50 | 100 |  | (1650,275.6) |  |  | –2.5×10-2 | 1.44 |  | (30,31.4) |  |  |  | –4.7×10-2 |  | 1.45 |  | (300,113.2) |  | –1.1×10-3 | 0.32 |
|  |  | 328 |  | 0.50 | 100 |  | (1110,266.7) |  |  | 0 | 1.09 |  | (5,5.5) |  |  |  | –0.38 |  | 2.29 |  | (30,27.3) |  | –7.6×10-2 | 2.35 |
|  |  | 318 |  | 0.70 | 100 |  | (1350,319.3) |  |  | –0.25 | 3.41 |  | (5,12.7) |  |  |  | –0.72 |  | 4.29 |  | (180,99.5) |  | –3.4×10-4 | 0.06 |
|  |  | 318A 0.50 |  |  | 70 |  | (1290,281.1) |  |  | –0.62 | 3.08 |  | (60,38.9) |  |  |  | –1.5×10-2 |  | 0.91 |  | (420,142.6) |  | –7.3×10-4 | 0.31 |
|  |  | 318B 0.50 |  |  | 40 |  | (1470,293.7) |  |  | –8.8×10-3 | 0.97B |  | (30,21.1) |  |  |  | –0.04 |  | 1.29 |  | (420,123.8) |  | –7.8×10-4 | 0.33 |
| 0.1M NaCl |  | 318 |  | 0.50 | 100 |  | (1290,316.3) |  |  | –13.89 | 13.89 |  | (60,58.6) |  |  |  | –1.4×10-2 |  | 0.88 |  | C(360,141.7) |  | –1.0×10-3 | 0.38 |
| pH=2.8 |  | 318 |  | 0.50 | 100 |  | (1290,278.3) |  |  | 0 | 1.08 |  | (2,2.2) |  |  |  | –2.92 |  | 8.77 |  | D(90,85.7) |  | –8.9×10-3 | 0.81 |
| pH=3.8 |  | 318 |  | 0.50 | 100 |  | (780,293.3) |  |  | –11.32 | 11.32 |  | (5,20.4) |  |  |  | –1.25 |  | 7.50 |  | (90,120.4) |  | –0.02 | 1.21 |
| pH=12 |  | 318 |  | 0.50 | 100 |  | (660,273.6) |  |  | –21.39 | 21.39 |  |  | (15,59.6) |  | –0.20 |  |  |  | 3.13 | E(420,185.4) |  | –1.1×10-3 | 0.46 |
| pH=13 |  | 308 |  | 0.50 | 100 |  | (1110,289.4) |  |  | 0 | 1.28 |  | (30,38.2) |  |  | –4.1×10-2 |  |  |  | 1.28 | (180,170.2) |  | –3.5×10-3 | 0.64 |
| pH=13 |  | 318 |  | 0.50 | 100 |  | (1470,315.7) |  |  | –4.35 | 4.35 |  | (10,10.6) |  |  | –0.28 |  |  |  | 3.11 | (180,103.8) |  | –3.3×10-3 | 0.59 |
| pH=13 |  | 328 |  | 0.50 | 100 |  | (930,309.5) |  |  | 0 | 0.89 |  | (30,26.8) |  |  | –0.10 |  |  |  | 2.99 | – |  | – | – |
| pH=14 |  | 318 |  | 0.50 | 100 |  | (930,216.6) |  |  | Very fastF |  |  | (180,110.1) |  |  | –2.2×10-3 |  |  |  | 0.41 | – |  | – | – |

Table 6. Non-ideal adsorption acceleration and velocity parameters for the first, second and third curves obtained from the NIPPON equation for kinetics of MnO4- adsorption on the surface of Co-Al-LDH at 308–328 K

A and B refer to cases that there are TDs at 4 and 5 min before starting adsorption process and thus for first curve 1,  and  min were used in Eqs. (10) and (11), respectively. C, D, E and F refer to TRAKs in the range of 300–360, 60–90, 180–420 and >0.5–180 min, respectively. Units of ,  and  are in mg g-1 min-2 and those of ,  and  are in mg g-1 min-1. Units of ,  and  are in min and those of ,  and  are in mg g-1. Subscripts fc, sc and tc are abbreviations for starting first curve, starting second curve and starting third curve, respectively.

Table 7. Coefficients of the Elovich equation for adsorption of MnO4- adsorption on the surface of ME sites of Co-Al-LDH in various shaking rates and initial MnO4- concentrations and media at 308–328 K

| Solvent | T | [MnO4-]0 | rpm |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | (K) | (mM) |  | (mg g-1 min-1) | (g mg-1) |  |
| Water | 318 | 0.25 | 100 | 2.96 | 0.037 | 0.80 |
|  | 308 | 0.50 | 100 | 1.01 | 0.037 | 0.95 |
|  | 318 | 0.50 | 100 | 4.01 | 0.037 | 0.94 |
|  | 328 | 0.50 | 100 | 4.73 | 0.027 | 0.92 |
|  | 318 | 0.70 | 100 | 8.22 | 0.046 | 0.96 |
|  | 318A | 0.50 | 70 | – | – | – |
|  | 318B | 0.50 | 40 | – | – | – |
| 0.1M NaCl | 318 | 0.50 | 100 | 7.92 | 0.037 | 0.89 |
| pH=2.8 | 318 | 0.50 | 100 | 7.91 | 0.022 | 0.92 |
| pH=3.8 | 318 | 0.50 | 100 | 13.56 | 0.019 | 0.96 |
| pH=12 | 318 | 0.50 | 100 | 15.83 | 0.023 | 0.93 |
| pH=13 | 308 | 0.50 | 100 | 2.81 | 0.014 | 0.94 |
| pH=13 | 318 | 0.50 | 100 | 4.30 | 0.018 | 0.88 |
| pH=13 | 328 | 0.50 | 100 | 3.45 | 0.011 | 0.99 |
| pH=14 | 318 | 0.50 | 100 | Very fast (0.5 min < ) |  |  |

A and B refer to cases that there were TDs at 4 and 5 min before starting adsorption process, respectively.

Table 8. Experimental , ,  and values and coefficients obtained from the KASRA equation and  values of intraparticle diffusion equation for kinetics of MnO4- adsorption on MoS2 at different temperatures and in various shaking rates and initial MnO4- concentrations and media

| Solvent | T [MnO4-]0 rpm |  |  |  |  |  |  | KASRA region 1 |  |  |  |  |  |  | KASRA region 2 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to: |  |  |  |  |  |  |  |  |  | ARIAN region I |  |  |  | ARIAN region II |  |  |  |  |  |  |
| Water | 318 |  | 0.25 | 100 |  | (90,149.6) |  |  | –0.04 |  | 3.57 | 21.0 | – |  |  | – |  | – |  | – |
|  | 308 |  | 0.50 | 100 |  | (180,164.2) |  |  | –0.06 |  | 2.14 | 7.0 | (30,39.1) |  |  | –2.0×10-2 |  | 2.41 |  | 22.7 |
|  | 318 |  | 0.50 | 100 |  | (120,273.2) |  |  | –0.11 |  | 4.67 | 22.5 | (30,91.9) |  |  | –1.2×10-2 |  | 2.51 |  | 30.7 |
|  |  | 328 | 0.50 | 100 |  | (90,313.4) |  |  | –0.54 |  | 11.0 | 21.9 | (20,119.9) |  |  | –2.2×10-2 |  | 3.56 |  | 38.9 |
|  |  | 318 | 0.75 | 100 |  | (120,335.6) |  |  | –0.23 |  | 8.34 | 33.9 | (30,145.1) |  |  | –1.2×10-2 |  | 2.72 |  | 34.3 |
|  |  | 318A | 0.50 | 70 |  | (180,125.5) |  |  | –0.05 |  | 1.90 | 8.70 | (20,15.0) |  |  | –1.0×10-2 |  | 1.65 |  | 15.6 |
|  |  | 318B | 0.50 | 40 |  | (120,90.1) |  |  | –0.006 |  | 1.24 | 12.3 | – |  |  | – |  | – |  | – |
| 0.1M NaCl |  | 318 | 0.50 | 100 |  | (120,196.9) |  |  | –0.07 |  | 2.52 | 9.80 | (30,44.1) |  |  | –0.03 |  | 3.25 |  | 34.3 |
| pH=1 |  | 318 | 0.50 | 100 |  | (120,272.0) |  |  | –0.72 |  | 13.2 | 27.8 | (20,119.6) |  |  | –1.4×10-2 |  | 2.31 |  | 23.4 |
| pH=2 |  | 318 | 0.50 | 100 |  | (60,258.3) |  |  | –0.11 |  | 7.53 | 41.8 | (20,128,9) |  |  | –2.6×10-2 |  | 3.87 |  | 39.8 |
| pH=11 |  | 318 | 0.50 | 100 |  | (60,76.0) |  |  | –0.016 |  | 1.57 | 10.4 | – |  |  | – |  | – |  | – |
| pH=12 |  | 318 | 0.50 | 100 |  | (20,241.5) |  |  | 0.00 |  | 18.0 | 62.2 | (7, 128.3) |  |  | –1.27 |  | 16.9 |  | 62.5 |

Units of  andare in mg g-1 min-2 and those of  and  are in mg g-1 min-1. Units of  and  are in min and those of  and  are in mg g-1. In region 1,  and  are equal to zero. A and B refer to cases that there are TDs at 7.5 and 10 min before starting adsorption process, respectively.

Table 9. Coefficients of region 1 and region 2 (parts 2a and 2b) of the ISO equation for kinetics of MnO4- adsorption on MoS2 at different temperatures and in various shaking rates and initial MnO4- concentrations and media

| Solvent | T | [MnO4-]0 |  | rpm kI1 |  |  | (tssr,qssr) |  |  | kI2a (tsp,qsp) kI2b ([MnO4-]e,te,qe) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) (mM) |  |  |  |  | (min,mg g-1) (min,mg g-1) (mM,min,mg g-1) |  |  |  |  |  |  |  |  |  |  |  |
| Corresponding to: |  |  |  |  | ARIAN region I |  |  |  |  | ARIAN region II |  |  |  |  |  |  |  |
| Water | 318 |  | 0.25 | 100 | 27718 |  |  | – |  | – |  | – |  |  | – | (0.11,90,149.6) |  |
|  | 308 |  | 0.50 | 100 | 2287 |  |  | (30,39.1) |  | – |  | – |  |  | 5363 | (0.34,180,164.2) |  |
|  | 318 |  | 0.50 | 100 | 7623 |  |  | (30,91.9) |  | – |  | – |  |  | 16517 | (0.22,120,273.2) |  |
|  | 328 |  | 0.50 | 100 | 9286 |  |  | (20,111.9) |  | – |  | – |  |  | 27857 | (0.20,90,313.4) |  |
|  | 318 |  | 0.75 | 100 | 8558 |  |  | (30,145.1) |  | – |  | – |  |  | 13226 | (0.43,120,335.6) |  |
|  | 318A |  | 0.50 | 70 | 1977 |  |  | (20,15.0) |  | – |  | – |  |  | 4284 | (0.38,180,125.5) |  |
|  | 318B |  | 0.50 | 40 | 1522 |  |  | – |  | – |  | – |  |  | – | (0.42,120,90.1) |  |
| 0.1M NaCl | 318 |  | 0.50 | 100 | 2832 |  |  | (30,44.1) |  | – |  | – |  |  | 13454 | (0.28,120,196.9) |  |
| pH=1 | 318 |  | 0.50 | 100 | 13499 |  |  | (20,119.6) |  | – |  | – |  |  | 14624 | (0.24,120,272.0) |  |
| pH=2 | 318 |  | 0.50 | 100 | 25348 |  |  | (20.0,128.9) |  | – |  | – |  |  | 35488 | (0.26,60,258.3) |  |
| pH=11 | 318 |  | 0.50 | 100 | 7993 |  |  | – |  | – |  | – |  |  | – | (0.43,60,76.0) |  |
| pH=12 | 318 |  | 0.50 | 100 | 88376 |  |  |  | (7,128.3) |  | – |  | – | 239706 |  |  | (0.20,20,241.5) |

A and B refer to cases that there are TDs at 7.5 and 10 min before starting adsorption process, respectively. [MnO4-]e ,  and  are MnO4- concentration, time and adsorption capacity at the beginning of the plateau respectively. Units of  ,  and  are in mg g-1 M-1 min-1.

Table 10. Non-ideal adsorption acceleration and velocity parameters for the first, second and third curves obtained from the NIPPON equation for kinetics of MnO4- adsorption on the surface of MoS2 at 308–328 K

| Solvent | T |  | [MnO4-]0 |  |  | rpm |  |  |  | NIPPON curve 1 |  |  |  | NIPPON curve 2 |  |  |  |  |  |  | NIPPON curve 3 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (K) |  |  | (mM) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Water | 318 |  |  | 0.25 | 100 |  | (90,149.6) |  | –17.02 |  | 17.02 |  | (10,40.5) |  |  | –0.46 |  | 5.01 |  | – |  | – | – |
|  | 308 |  |  | 0.50 | 100 |  | (180,164.2) |  | 0 |  | 3 |  | (5,15.0) |  |  | –1.24 |  | 7.4 |  | (30,91.9) |  | –0.13 | 3.99 |
|  | 318 |  |  | 0.50 | 100 |  | (120,273.2) |  | 0 |  | 2.05 |  | (10,20.5) |  |  | –0.15 |  | 1.61 |  | (30,39.1) |  | –0.10 | 2.99 |
|  |  | 328 |  | 0.50 | 100 |  | (90,313.4) |  | –36.1 |  | 36.1 |  | (20,111.9) |  |  | –0.30 |  | 6.27 |  | – |  | – | – |
|  |  | 318 |  | 0.75 | 100 |  | (120,335.6) |  | –6.64 |  | 6.64 |  | (5,33.2) |  |  | –2.10 |  | 12.57 |  | (45,191.0) |  | –0.07 | 3.18 |
|  |  | 318 |  | 0.50 | 70 |  | (180,125.5) |  | –0.21A |  | 1.76A |  | (20,15.0) |  |  | –0.12 |  | 2.56 |  | – |  | – | – |
|  |  | 318 |  | 0.50 | 40 |  | (120,90.1) |  | –0.17B |  | 1.90B |  | (30,22.3) |  |  | –0.05 |  | 1.61 |  | – |  | – | – |
| 0.1M NaCl |  | 318 |  | 0.50 | 100 |  | (120,196.9) |  | –2.23 |  | 2.23 |  | (10,22.3) |  |  | –0.17 |  | 1.92 |  | (30,44.1) |  | –0.12 | 3.85 |
| pH=1 |  | 318 |  | 0.50 | 100 |  | (120,272.0) |  | –39.6 |  | 39.6 |  | (20,119.6) |  |  | –0.19 |  | 3.97 |  | – |  | – | – |
| pH=2 |  | 318 |  | 0.50 | 100 |  | (60,258.3) |  | –7.17 |  | 7.17 |  | (5,35.9) |  |  | –2.07 |  | 12.40 |  | (20,138.9) |  | –0.28 | 5.85 |
| pH=11 |  | 318 |  | 0.50 | 100 |  | (60,76.0) |  | –2.76 |  | 2.76 |  | (10,27.6) |  | –0.24 |  |  |  | 2.62 | – |  | – | – |
| pH=12 |  | 318 |  | 0.50 | 100 |  | (20,241.5) |  | –36.71 |  | 36.71 |  | (3,50.9) |  | –7.46 |  |  |  | 29.85 | – |  | – | – |

A and B refer to cases that there are TDs at 7.5 and 10 min before starting adsorption process, respectively and thus for curve 1,  and  min were used in Eqs. (10) and (11), respectively. Units of ,  and  are in mg g-1 min-2 and those of ,  and  are in mg g-1 min-1. Units of ,  and  are in min and those of ,  and  are in mg g-1. Subscripts fc, sc and tc are abbreviations for starting first curve, starting second curve and starting third curve, respectively.

Table 11. Coefficients of the Elovich equation for adsorption of MnO4- adsorption on the surface of MoS2 in various shaking rates and initial MnO4- concentrations and media at 308–328 K

| Solvent | T | [MnO4-]0 | rpm |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | (K) | (mM) |  | (mg g-1 min-1) | (g mg-1) |  |
| Water | 318 | 0.25 | 100 | 13.2 | 0.022 | 0.96 |
|  | 308 | 0.50 | 100 | 13.3 | 0.013 | 0.92 |
|  | 318 | 0.50 | 100 | 5.51 | 0.017 | 0.93 |
|  | 328 | 0.50 | 100 | 18.9 | 0.001 | 0.95 |
|  | 318 | 0.75 | 100 | 20.8 | 0.011 | 0.96 |
|  | 318A | 0.50 | 70 | – | – | – |
|  | 318B | 0.50 | 40 | – | – | – |
| 0.1M NaCl | 318 | 0.50 | 100 | 6.70 | 0.013 | 0.88 |
| pH=1 | 318 | 0.50 | 100 | 24.7 | 0.015 | 0.97 |
| pH=2 | 318 | 0.50 | 100 | 21.9 | 0.011 | 0.97 |
| pH=11 | 318 | 0.50 | 100 | 4.70 | 0.037 | 0.96 |
| pH=12 | 318 | 0.50 | 100 | 54.4 | 0.009 | 0.99 |

A and B refer to cases that there are TDs at 7.5 and 10 min before starting adsorption process, respectively.