Dear Editor and Reviewers:

Many thanks for your expectation of the revised version of our manuscript (Article reference:  (7799-53895-1-RV). We hope that the revised manuscript is accepted for publication.

The following is the description of our revisions.

Reviewer A:

Comment:

- The researchers did not test the simple method to check the corrosion
inhibition behavior (weight loss method)

- The weight loss method was not used because we employed the electrochemical method which is more quantitative and allows access to reaction rates and values of physical parameters describing the state of the system (corrosion current, inhibition rate, double layer capacity, charge transfer resistance, etc.). We have also noticed that in the literature many authors have opted to use electrochemical methods1-2.

- Hamani, H., et al., Electrochemical and quantum chemical studies of some azomethine compounds as corrosion inhibitors for mild steel in 1 M hydrochloric acid. 2014. 88: p. 234-245.

- Alibakhshi, E., et al., Glycyrrhiza glabra leaves extract as a green corrosion inhibitor for mild steel in 1 M hydrochloric acid solution: experimental, molecular dynamics, Monte Carlo and quantum mechanics study. 2018. 255: p. 185-198.

Reviewer C:

Question 01

- Authors described two different reference electrodes. Which one is the
correct?

Answer

- In a Pyrex cell with a typical three-electrode configuration steel as the working electrode (ET), platinum as the auxiliary electrode and a saturated Hg/Hg2Cl2/KCl calomel electrode (ECS) as the reference electrode, the electrochemical experiments are carried out.

Question 02

- Conditions of impedance spectroscopy and potentiodynamic polarization
spectroscopy were not established.

- Electrochemical impedance spectroscopies (EIS) were performed in the frequency range of 10 kHz to 10 mHz with a sinusoidal voltage amplitude of 10 mV at open circuit potential (OCP). The potentiodynamic polarization test was performed in the potential range and at a slew rate of - 250 to + 250 mV relative to the OCP and at 1 mV/s, respectively. We first plotted the electrochemical impedance spectroscopy and potentiodynamic polarization spectroscopy curves.

Question 03

- How do the authors determine that the active area of the electrode decreases
as the inhibitor concentration and the inhibitory efficiency rise, and the
adsorbed film can exhibit ohmic behavior?

Answer

- Corrosion inhibitors operate by creating a barrier between the metal and the reagent. They adsorb to the metal surface in a form that depends on their nature by locking the active sites on the steel surface. The adsorbed film shows an ohmic behavior because it reacts as a barrier which leads to a decrease in the current intensity.