Supporting information:

Preparation of porous imidazole-based poly(ionic liquid) adsorbents and their toluene adsorption performance

Fangwen Luo 1, Xujiao Tian 1, Xian Dong 1, Longchao Liang 1 and Zhuo Chen 1,*

School of Chemistry and Material Science, Key Lab for Functional Material Chemistry, Guizhou Normal University, Guiyang 550025, PR China

* Corresponding author E-mail address: chenzhuo19@163.com

| Adsorbents | Breakthrough time/min | Equilibrium adsorption time/ min | Equilibrium adsorption capacity/mg⋅g-1 |
| --- | --- | --- | --- |
| PVIC-2 | 20 | 31 | 150 |
| PVIC-3 | 27 | 44 | 195 |
| PVIC-4 | 35 | 56 | 264 |
| PVIC-5 | 33 | 53 | 232 |

Table S1. Evaluation of toluene adsorption performance of PVICs

| Adsorbents | Pseudo first order model |  |  |  | Pseudo-second order model |  |  |  | Bangham |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | k1(min-1) | R2 | qe(mg/g) |  | k2(min-1) | R2 | qe(mg/g) |  | k(min-1) | z | R2 | qe(mg/g) |
| PVIC-2 | 0.089 | 0.971 | 155.6 |  | 8.8*10-4 | 0.957 | 174.3 |  | 2.96*10-4 | 2.869 | 0.999 | 150.9 |
| PVIC-3 | 0.062 | 0.985 | 208.2 |  | 3.3*10-4 | 0.979 | 247.9 |  | 8.22*10-5 | 3.028 | 0.999 | 195.4 |
| PVIC-4 | 0.032 | 0.991 | 324.2 |  | 5.9*10-5 | 0.988 | 450.2 |  | 1.03*10-4 | 2.706 | 0.999 | 265.9 |
| PVIC-5 | 0.052 | 0.993 | 248.6 |  | 2.1*10-4 | 0.991 | 301.4 |  | 7.24*10-5 | 2.915 | 0.999 | 231.6 |

Table S2. Dynamic fitting parameters of PVICs

| Adsorbents | ki |  |  | Ci |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | k1 | k2 | k3 | C1 | C2 | C3 |  |  |  |
| PVIC-0.4 | 26.49 | 41.04 | 3.27 | -0.037 | -62.43 | 132.26 | 0.999 | 0.986 | 0.791 |
| PVIC-0.6 | 31.44 | 35.28 | 4.11 | -0.025 | -16.06 | 168.26 | 0.999 | 0.934 | 0.926 |
| PVIC-0.8 | 35.72 | 51.19 | 9.04 | -0.019 | -89.11 | 197.51 | 0.999 | 0.979 | 0.885 |
| PVIC-1.0 | 34.68 | 44.63 | 5.27 | -0.019 | -55.74 | 193.95 | 0.999 | 0.992 | 0.944 |

Table S3. Fitting parameters of internal diffusion model for PVICs

| Isotherm models | Parameters | Adsorbents |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | PVIC-2 | PVIC-3 | PVIC-4 | PVIC-5 |
| Langmuir | qm(mg/g） | 152.08 | 198.37 | 268.34 | 235.13 |
|  | KL(L/mg) | 0.0035 | 0.0052 | 0.0038 | 0.0043 |
|  | RL | 0.07~0.52 | 0.05~0.42 | 0.07~0.50 | 0.06~0.47 |
|  | R2 | 0.989 | 0.996 | 0.997 | 0.996 |
| Freundlich | KF | 25.05 | 49.26 | 48.78 | 49.92 |
|  | 1/n | 0.224 | 0.174 | 0.213 | 0.194 |
|  | R2 | 0.978 | 0.989 | 0.987 | 0.986 |

Table S4. Isotherm model parameters for toluene on PVICs