## Table S1. Statistical evaluation of the correlation of kinetic parameters of the interaction of copper sulfides with 0.05M iron (III) chloride in 1M hydrochloric acid medium and reduced Gibbs energy of the oxidation reaction of copper sulfides ΔrG⁰/σ

| Parameters | lnk = a(–ΔrG⁰/σ) + b | lnW = a(–ΔrG⁰/σ) + b |
| --- | --- | --- |
| R | 0.941 | 0.993 |
| R² | 0.886 | 0.987 |
| t_sample | 6.22 | 19.41 |
| t_crit | 5.89 (0.1%) | 6.87 (0.05%) |
| a | 0.163 | 0.559 |
| Sₐ | 0.026 | 0.029 |
| b | 23.27 | 3.919 |
| Sᵦ | 0.769 | 1.037 |
| Average approximation error | 4.8% | 2.5% |

## Table S2. Statistical evaluation of the correlation of kinetic parameters of the interaction of copper sulfides with 0.01M sodium nitrite in 0.05M hydrochloric acid medium and reduced Gibbs energy of the oxidation reaction of copper sulfides ΔrG⁰/σ

| Parameters | lnk = a(–ΔrG⁰/σ) + b | lnW = a(–ΔrG⁰/σ) + b |
| --- | --- | --- |
| R | 0.945 | 0.948 |
| R² | 0.894 | 0.898 |
| t_sample | 5.020 | 5.140 |
| t_crit | 4.060 (0.5%) | 4.06 (0.5%) |
| a | 0.110 | 0.112 |
| Sₐ | 0.022 | 0.022 |
| b | –23.21 | –20.150 |
| Sᵦ | 1.115 | 1.112 |
| Average approximation error | 5.5% | 7.0% |

## Table S3. Statistical evaluation of the correlation of kinetic parameters of the interaction of copper sulfides with 0.05M iron (III) chloride in 1M hydrochloric acid medium and Gibbs average atomic energy of the formation of copper sulfides ΔfG⁰/n

| Parameters | lnk = a·ΔfG⁰/n + b | lnW = a·ΔfG⁰/n + b |
| --- | --- | --- |
| R | 0.981 | 0.993 |
| R² | 0.963 | 0.987 |
| t_sample | 11.36 | 19.41 |
| t_crit | 6.87 (0.05%) | 6.87 (0.05%) |
| a | 0.421 | 0.559 |
| Sₐ | 0.037 | 0.029 |
| b | –4.385 | 3.919 |
| Sᵦ | 1.334 | 1.037 |
| Average approximation error | 2.2% | 2.5% |

## Table S4. Statistical evaluation of the correlation of kinetic parameters of the interaction of copper sulfides with 0.01M sodium nitrite in 0.05M hydrochloric acid and Gibbs average atomic energy of the formation of copper sulfides ΔfG⁰/n

| Parameters | lnk = a·ΔfG⁰/n + b | lnW = a·ΔfG⁰/n + b |
| --- | --- | --- |
| R | 0.993 | 0.995 |
| R² | 0.986 | 0.990 |
| t_sample | 14.63 | 17.00 |
| t_crit | 12.92 (0.05%) | 12.92 (0.05%) |
| a | 0.404 | 0.412 |
| Sₐ | 0.028 | 0.024 |
| b | –4.189 | –0.740 |
| Sᵦ | 1.032 | 0.906 |
| Average approximation error | 2.2% | 2.3% |